Fabrication of Highly Porous MOF/Cellulose Beads for Sustained Degradation of Dye

Yuhang Wuab*, Yuwen Lic, Yanchun Zhenga, Juming Yaob, Junkuo Gaob*

aDepartment of Industrial Design, School of Art and Archaeology, Hangzhou City University, Hangzhou, Zhejiang, China

bSchool of Materials Science and Engineering, Zhejiang Sci-Tech University, Hangzhou Zhejiang, China

cState Key Laboratory of Silicon Materials, School of Materials Science and Engineering, Zhejiang University, Hangzhou, Zhejiang, China

Figure S1 XRD patterns of powdered MIL-100 and MIL-100/CMC-HD

Figure S2 TG plots of CMC, MIL-100, and MIL-100/CMC-HD

Table S1 Porosity and pore structure properties of MIL-100/CMC-FD and MIL-100/CMC-HD

| Samples | Porosity（%） | Total pore volume （mL g-1） | Total pore area （m2 g-1） | Average pore size （nm） |
| --- | --- | --- | --- | --- |
| MIL-100/CMC-FD | 64.4 | 1.8 | 8.2 | 896.5 |
| MIL-100/CMC-HD | 62.5 | 1.6 | 6.1 | 1061.0 |

Table S2 Ash content of different samples after pyrolysis

|  | MIL-100/CMC-HD |
| --- | --- |
| MIL-100 ash | 27% |
| CMC ash | 46% |
| MIL-100/CMC-HD ash | 42% |
| MIL-100 Loading content | 79% |

Equation S1 MIL-100 Loadingwt% = MIL-100/CMC-HD ash -CMC ashMIL-100 ash-CMC ash