Mesoporous Effects on SiC Fiber Matrix Combined with Active Metal Oxides  for Atmospheric Gas Sensing under High Temperature Conditions

Zambaga Otgonbayar 1, Young Jun Joo 3, Kwang Youn Cho 3, Sang Yul Park 4, Kwang Youl Park 4, Won-Chun Oh 1. 2

1 Department of Advanced Materials Science & Engineering, Hanseo University, Seosan-si, Chungnam, Korea, 356-706

2 Anhui International Joint Research Center for Nano Carbon‑Based Materials and Environmental Health, College of Materials Science and Engineering, Anhui University of Science & Technology, Huainan 232001, China

3 Korea Institutes of Ceramic Engineering and Technology, Soho-ro, Jinju-Si, Gyeongsangnam-do, South Korea

4 Daeho I&T, Changwon-si, Gyeongsangnam-do, 51338, Korea

Characterization

The crystallinity of the samples were analyzed by the XRD (SHIMADZU XRD-6000) equipped with a Cu Ka X-ray source (1.5406 Å). The surface state and element units of the samples were analyzed by the SEM-EDX (JSM-5600 JEOL, Akishima, Tokyo, Japan). The shape of the particle and dispersion were analyzed by the TEM (Hitachi H9500, Tokyo, Japan). The electrochemical properties of the samples were evaluated by the PL, EIS, Tafel and LSV measurements..

Electrode preparation.

The working electrode (WE) was prepared by following the Doctor Blade method. In detail, the prepared nanocomposite was mixed with binder material (ethyl cellulose) to make a fine slurry with pure ethanol dispersant. Ni-foil is used as a current collector and base for coating. The slurry was spread on the current collector to make a thin-film, and coated electrode was dried in an electric oven (100°C), then put into the furnace and kept under 400°C.

Scheme S1. The schematic illustration of the gas sensing mechanism.

Figure S1. XPS spectrum of the W4f of mWO3.

Table S1. The resistance (Ω) value of each electrode from CV graph without gas-purging conditions with Ni foil current collector.

| № | Working electrode | Current collector | Conditions | Current density (mA/cm2) | (k*Ohm*cm2) |
| --- | --- | --- | --- | --- | --- |
| 1 | mWO3 | Ni-foil | Without gas purged system (at room temp) | 4.65×10-3 | 451.613 |
| 2 | SCISOW101 |  |  | 4.68×10-3 | 448.718 |
| 3 | SCISOW103 |  |  | 1.19×10-6 | 1764706 |
| 4 | SCISOW105 |  |  | 1.01×10-5 | 207921 |

Table S2. The resistance (Ω) value of each electrode from CV graph under CO2 and O2 gas-purging conditions at normal room temperature (25°C).

| № | Working electrode | Current collector | Conditions | Current density (mA/cm2) | (k*Ohm*cm2) |
| --- | --- | --- | --- | --- | --- |
| 1 | mWO3 | Ni-foil | With CO2-gas purged system (at room temp) | 9.47×10-3 | 221.753 |
| 2 | SCISOW101 |  |  | 4.65×10-3 | 451.613 |
| 3 | SCISOW103 |  |  | 1.16×10-6 | 1810345 |
| 4 | SCISOW105 |  |  | 6.88×10-6 | 305233 |
| 5 | mWO3 | Ni-foil | With O2-gas purged system (at room temp) | 4.62×10-3 | 454.545 |
| 6 | SCISOW101 |  |  | 4.64×10-3 | 452.586 |
| 7 | SCISOW103 |  |  | 1.47×10-6 | 1428571 |
| 8 | SCISOW105 |  |  | 1.42×10-6 | 1478873 |

Table S3. The resistance (Ω) value of each electrode from CV graph electrode under different high temperatures with without gas purging.

| № | Working electrode | Temperature | Current collector | Conditions | Current density (mA/cm2) | (k*Ohm*cm2) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | mWO3 | 100 °C | Ni-foil | Without gas purged system | 4.70×10-3 | 446.809 |
| 2 | mWO3 | 200 °C |  |  | 4.69×10-3 | 447.761 |
| 3 | mWO3 | 300 °C |  |  | 4.69×10-3 | 447.761 |
| 4 | mWO3 | 400 °C |  |  | 4.67×10-3 | 449.679 |
| 5 | mWO3 | 500 °C |  |  | 4.67×0-3 | 449.679 |
| 6 | mWO3 | 600 °C |  |  | 4.66×10-3 | 450.644 |
| 7 | SCISOW101 | 100 °C | Ni-foil | Without gas purged system | 4.70×10-3 | 446.809 |
| 8 | SCISOW101 | 200 °C |  |  | 4.15×10-3 | 506.024 |
| 9 | SCISOW101 | 300 °C |  |  | 3.86×10-3 | 544.041 |
| 10 | SCISOW101 | 400 °C |  |  | 3.04×10-3 | 690.789 |
| 11 | SCISOW101 | 500 °C |  |  | 2.79×10-3 | 752.688 |
| 12 | SCISOW101 | 600 °C |  |  | 2.20×10-3 | 954.545 |
| 13 | SCISOW103 | 100 °C | Ni-foil | Without gas purged system | 2.49×10-7 | 8433735 |
| 14 | SCISOW103 | 200 °C |  |  | 1.79×10-7 | 1.2E+07 |
| 15 | SCISOW103 | 300 °C |  |  | 1.69×10-7 | 1.2E+07 |
| 16 | SCISOW103 | 400 °C |  |  | 1.15×10-7 | 1.8E+07 |
| 17 | SCISOW103 | 500 °C |  |  | 5.26×10-8 | 4E+07 |
| 18 | SCISOW103 | 600 °C |  |  | 4.48×10-8 | 4.7E+07 |
| 19 | SCISOW105 | 100 °C | Ni-foil | Without gas purged system | 9.3910-6 | 223642 |
| 20 | SCISOW105 | 200 °C |  |  | 9.27×10-6 | 226537 |
| 21 | SCISOW105 | 300 °C |  |  | 4.71×10-6 | 445860 |
| 22 | SCISOW105 | 400 °C |  |  | 4.54 ×10-6 | 462555 |
| 23 | SCISOW105 | 500 °C |  |  | 4.43×10-6 | 474041 |
| 24 | SCISOW105 | 600 °C |  |  | 3 3.62×10-6 | 580110 |

Table S4. The resistance (Ω) value of each electrode from CV graph electrode under different high temperatures with CO2 gas purging.

| № | Working electrode | Temperature | Current collector | Conditions | Current density (mA/cm2) | (k*Ohm*cm2) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | mWO3 | 100 °C | Ni-foil | With CO2 gas purged system | 4.65×10-3 | 451.613 |
| 2 | mWO3 | 200 °C |  |  | 4.64×10-3 | 452.586 |
| 3 | mWO3 | 300 °C |  |  | 4.65×10-3 | 453.564 |
| 4 | mWO3 | 400 °C |  |  | 4.62×10-3 | 454.545 |
| 5 | mWO3 | 500 °C |  |  | 4.38×0-3 | 479.452 |
| 6 | mWO3 | 600 °C |  |  | 4.29×10-3 | 489.51 |
| 7 | SCISOW101 | 100 °C | Ni-foil | With CO2 gas purged system | 4.67×10-3 | 449.679 |
| 8 | SCISOW101 | 200 °C |  |  | 4.51×10-3 | 465.632 |
| 9 | SCISOW101 | 300 °C |  |  | 3.82×10-3 | 549.738 |
| 10 | SCISOW101 | 400 °C |  |  | 3.63×10-3 | 578.512 |
| 11 | SCISOW101 | 500 °C |  |  | 2.62×10-3 | 801.527 |
| 12 | SCISOW101 | 600 °C |  |  | 1.98×10-3 | 1060.61 |
| 13 | SCISOW103 | 100 °C | Ni-foil | With CO2 gas purged system | 1.87×10-7 | 1.1E+07 |
| 14 | SCISOW103 | 200 °C |  |  | 1.63×10-7 | 1.3E+07 |
| 15 | SCISOW103 | 300 °C |  |  | 1.04×10-7 | 2E+07 |
| 16 | SCISOW103 | 400 °C |  |  | 8.33×10-8 | 2.5E+07 |
| 17 | SCISOW103 | 500 °C |  |  | 4.58×10-8 | 4.6E+07 |
| 18 | SCISOW103 | 600 °C |  |  | 2.29×10-8 | 9.2E+07 |
| 19 | SCISOW105 | 100 °C | Ni-foil | With CO2 gas purged system | 9.3710-6 | 224120 |
| 20 | SCISOW105 | 200 °C |  |  | 9.22×10-6 | 227766 |
| 21 | SCISOW105 | 300 °C |  |  | 4.65×10-6 | 451613 |
| 22 | SCISOW105 | 400 °C |  |  | 4.47×10-6 | 469799 |
| 23 | SCISOW105 | 500 °C |  |  | 4.19×10-6 | 501193 |
| 24 | SCISOW105 | 600 °C |  |  | 3. 3.53×10-6 | 594901 |

Table S5. The resistance (Ω) value of each electrode from CV graph electrode under different high temperatures with O2 gas purging.

| № | Working electrode | Temperature | Current collector | Conditions | Current density (mA/cm2) | (k*Ohm*cm2) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | mWO3 | 100 °C | Ni-foil | With O2 gas purged system | 4.61×10-3 | 455.531 |
| 2 | mWO3 | 200 °C |  |  | 4.60×10-3 | 456.522 |
| 3 | mWO3 | 300 °C |  |  | 4.58×10-3 | 458.515 |
| 4 | mWO3 | 400 °C |  |  | 4.55×10-3 | 461.538 |
| 5 | mWO3 | 500 °C |  |  | 4.34×0-3 | 483.871 |
| 6 | mWO3 | 600 °C |  |  | 4.21×10-3 | 498.812 |
| 7 | SCISOW101 | 100 °C | Ni-foil | With O2 gas purged system | 4.31×10-3 | 487.239 |
| 8 | SCISOW101 | 200 °C |  |  | 4.11×10-3 | 510.949 |
| 9 | SCISOW101 | 300 °C |  |  | 3.88×10-3 | 541.237 |
| 10 | SCISOW101 | 400 °C |  |  | 2.98×10-3 | 704.698 |
| 11 | SCISOW101 | 500 °C |  |  | 2.61×10-3 | 804.598 |
| 12 | SCISOW101 | 600 °C |  |  | 1.82×10-3 | 1153.85 |
| 13 | SCISOW103 | 100 °C | Ni-foil | With O2 gas purged system | 2.44×10-7 | 8606557 |
| 14 | SCISOW103 | 200 °C |  |  | 2.31×10-7 | 9090909 |
| 15 | SCISOW103 | 300 °C |  |  | 1.66×10-7 | 1.3E+07 |
| 16 | SCISOW103 | 400 °C |  |  | 8.81×10-8 | 2.4E+07 |
| 17 | SCISOW103 | 500 °C |  |  | 4.86×10-8 | 4.3E+07 |
| 18 | SCISOW103 | 600 °C |  |  | 3.59×10-8 | 5.8E+07 |
| 19 | SCISOW105 | 100 °C | Ni-foil | With O2 gas purged system | 9.33×10-6 | 224120 |
| 20 | SCISOW105 | 200 °C |  |  | 9.18×10-6 | 227766 |
| 21 | SCISOW105 | 300 °C |  |  | 4.59×10-6 | 451613 |
| 22 | SCISOW105 | 400 °C |  |  | 4.40×10-6 | 469799 |
| 23 | SCISOW105 | 500 °C |  |  | 4.05×10-6 | 501193 |
| 24 | SCISOW105 | 600 °C |  |  | 3.4 3.43×10-6 | 594901 |

Corresponding author

E-mail: wc_oh@hanseo.ac.kr

Tel: +82-41-660-1337, Fax: +82-41-688-3352