Electrofluids as liquid conductors with tunable gauge factors

Dominik Sebastian Schmidt1, Tobias Kraus1,2, Lola González-García1,3*

1INM – Leibniz Institute for New Materials, Campus D2 2, 66123 Saarbrücken, Germany
2Colloid and Interface Chemistry, Saarland University, Campus D2 2, 66123 Saarbrücken, Germany

3Department of Materials Science and Engineering, Saarland University, Campus D2 2, 66123 Saarbrücken, Germany

*E-mail: lola.gonzalez-garcia@leibniz-inm.de

Table of Content

| Supplementary Figure 1: | Raman spectrum of Carbon Black Powder |
| --- | --- |
| Supplementary Figure 2: | Fitting curves of the percolation threshold determination for the CB mixtures |
| Supplementary Figure 3: | Rheoelectrical graphs of 5 vol% CB in A) Hexadecane and B) Ethylene Glycol |
| Supplementary Figure 4: | Flow curves for 5 vol% CB in A) PDMS and B) Glycerol |
| Supplementary Figure 5: | Electromechanical tests with 0.9 vol% CB in glycerol |
| Supplementary Figure 6: | Testing protocol of uniaxial tensile tests |

Figure S1: Raman spectrum of Carbon Black powder.

Figure S2: Fitting curves of the percolation threshold determination for the CB mixtures in PDMS (A), in glycerol (B), in hexadecane (C), and in ethylene glycol (D).

Figure S3: Rheoelectrical measurements of 5 vol% CB in A) hexadecane and B) ethylene glycol.

Figure S4: Flow curves of 5 vol% CB in A) PDMS and B) glycerol.

Figure S5: Resistance variation during cyclical loading between 0% and 10% strain (1000 cycles). The inset shows the strain rate. The overall decreasing trend found for the smaller concentration of 0.9 vol% CB in glycerol indicates that the equilibrium for this system was not reached within the (pre)test time.

Figure S6: Image of the uniaxial tensile test set-up. The electrofluid was encapsulated in an EcoFlex® tube, clamped into the tensile machine, and electrically connected to the Keithley DAQ6510 Sourcemeter.

Videos of the demonstrators can be found as electronic supporting information.