Supporting Information (Tables)

Explaining the increase in “high-quality chert” in the Early Upper Paleolithic artifacts in southern Jordan: Quantitative examination of chert mechanical properties and fracture predictability

Eiki Suga 1, *, Kazuhiro Tsukada 2, Odai Tarawneh 3, Sate Massadeh 4, Seiji Kadowaki 2

1 Graduate School of Environmental Studies, Nagoya University, Furo-cho, Chikusa-ku, Nagoya 464-8601, Japan.

2 Nagoya University Museum, Nagoya University, Furo-cho, Chikusa-ku, Nagoya 464-8601, Japan.

3 Department of Antiquities, Jordan, Third Circle, Jabal Amman, Jordan

4 Ministry of Tourism and Antiquities, Jordan, Third Circle, Jabal Amman, Jordan

*Corresponding author

E-mail address: suga.eiki.z6@s.mail.nagoya-u.ac.jp (E. Suga)

ORCIO ID: 0000-0002-9672-1595

Table S1 Measurement values of rebound hardness. Some samples are not included in the list because they broke during the measurement and could not be measured 10 times.

| No. | Outcrops | Raw Material type | Mass (kg) | Measurement values |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | 1st | 2nd | 3rd | 4th | 5th | 6th | 7th | 8th | 9th | 10th |
| 1 | Abbasiya | Type M chert | 21.4 | 71 | 81 | 75 | 80 | 70 | 82 | 81 | 71 | 78 | 82 |
| 2 | Abbasiya | Type FH chert | 61.4 | 84 | 83 | 78 | 80 | 80 | 75 | 73 | 82 | 83 | 80 |
| 3 | Abbasiya | Type M chert | 20 | 75 | 78 | 72 | 79 | 80 | 81 | 76 | 80 | 77 | 78 |
| 4 | Abbasiya | Type FH chert | 20 | 85 | 82 | 83 | 80 | 79 | 78 | 74 | 78 | 77 | 80 |
| 5 | Abbasiya | Type M chert | 9.2 | 68 | 69 | 78 | 73 | 78 | 75 | 76 | 70 | 72 | 75 |
| 7 | Abbasiya | Type M chert | 24.4 | 84 | 84 | 82 | 81 | 81 | 75 | 81 | 82 | 82 | 82 |
| 8 | Abbasiya | Type FH chert | 23.4 | 80 | 80 | 81 | 81 | 79 | 81 | 74 | 80 | 81 | 79 |
| 9 | Abbasiya | Type M chert | 17.2 | 73 | 71 | 71 | 70 | 69 | 70 | 73 | 70 | 72 | 78 |
| 10 | Abbasiya | Type M chert | 24.4 | 72 | 82 | 75 | 78 | 81 | 79 | 74 | 74 | 77 | 83 |
| 11 | Abbasiya | Type FH chert | 24.6 | 85 | 85 | 76 | 75 | 72 | 80 | 78 | 75 | 76 | 81 |
| 13 | Abbasiya | Type FH chert | 13.6 | 72 | 80 | 73 | 73 | 79 | 75 | 71 | 77 | 74 | 73 |
| 14 | Abbasiya | Type FH chert | 12.2 | 79 | 73 | 72 | 69 | 75 | 69 | 76 | 77 | 76 | 79 |
| 15 | Abbasiya | Type FH chert | 31.8 | 86 | 85 | 84 | 77 | 77 | 82 | 83 | 77 | 80 | 82 |
| 16 | Abbasiya | Type M chert | 18.6 | 80 | 73 | 82 | 78 | 77 | 81 | 74 | 78 | 73 | 77 |
| 17 | Abbasiya | Type FH chert | 21.2 | 76 | 75 | 77 | 78 | 81 | 75 | 78 | 76 | 80 | 81 |
| 18 | Wadi Abu Sawwan | Type M chert | 18.2 | 70 | 75 | 76 | 70 | 79 | 81 | 75 | 76 | 73 | 81 |
| 19 | Wadi Abu Sawwan | Type M chert | 41.8 | 82 | 78 | 76 | 81 | 82 | 79 | 74 | 75 | 78 | 81 |
| 21 | Wadi Abu Sawwan | Type M chert | 42.6 | 86 | 84 | 83 | 77 | 78 | 76 | 80 | 80 | 79 | 80 |
| 22 | Wadi Abu Sawwan | Type M chert | 13.4 | 73 | 74 | 79 | 75 | 72 | 78 | 77 | 78 | 79 | 75 |
| 23 | Wadi Abu Sawwan | Type M chert | 36.2 | 78 | 79 | 82 | 83 | 75 | 78 | 80 | 79 | 74 | 77 |
| 26 | Humayma | Type FH chert | 35 | 86 | 84 | 79 | 81 | 77 | 77 | 76 | 80 | 77 | 80 |
| 29 | Ma'an Plateau | Type FH chert | 14.2 | 76 | 82 | 78 | 79 | 82 | 75 | 77 | 75 | 78 | 82 |
| 30 | Abbasiya | Type FH chert | 5.2 | 84 | 82 | 75 | 76 | 76 | 80 | 76 | 78 | 83 | 76 |
| 31 | Wadi Abu Sawwan | Type FH chert | 4.8 | 79 | 79 | 79 | 80 | 77 | 81 | 75 | 81 | 75 | 80 |
| 32 | Abbasiya | Type FH chert | 4.6 | 71 | 74 | 79 | 74 | 74 | 73 | 79 | 73 | 74 | 71 |
| 34 | Humayma | Type M chert | 5.6 | 78 | 77 | 77 | 75 | 71 | 77 | 73 | 74 | 75 | 75 |
| 35 | Ma'an Plateau | Type M chert | 4.8 | 73 | 72 | 75 | 71 | 73 | 71 | 72 | 75 | 71 | 72 |
| 40 | Hokkaido | Obsidian | 8.6 | 84 | 83 | 82 | 79 | 77 | 75 | 75 | 74 | 68 | 67 |
| 41 | Hokkaido | Obsidian | 18.3 | 82 | 78 | 78 | 77 | 77 | 76 | 76 | 74 | 71 | 71 |
| 42 | Hokkaido | Obsidian | 6.3 | 81 | 80 | 78 | 76 | 74 | 73 | 65 | 61 | 54 | 45 |
| 43 | Hokkaido | Obsidian | 12 | 84 | 83 | 82 | 81 | 80 | 79 | 71 | 69 | 69 | 61 |
| 44 | Hokkaido | Obsidian | 10.3 | 83 | 81 | 80 | 78 | 78 | 67 | 67 | 66 | 61 | 59 |
| 45 | Hokkaido | Obsidian | 5 | 79 | 79 | 79 | 78 | 77 | 77 | 74 | 73 | 73 | 70 |
| 46 | Hokkaido | Obsidian | 20 | 84 | 82 | 81 | 81 | 80 | 79 | 76 | 76 | 66 | 64 |
| 47 | Hokkaido | Obsidian | 18 | 87 | 86 | 85 | 85 | 84 | 83 | 82 | 81 | 78 | 66 |
| 48 | Hokkaido | Obsidian | 9 | 86 | 80 | 80 | 80 | 80 | 77 | 71 | 68 | 60 | 47 |
| 49 | Hokkaido | Andesite | 19.9 | 63 | 63 | 59 | 59 | 57 | 56 | 54 | 53 | 51 | 47 |
| 50 | Hokkaido | Andesite | 17 | 71 | 70 | 70 | 69 | 69 | 68 | 68 | 68 | 68 | 66 |
| 51 | Hokkaido | Andesite | 15.7 | 66 | 66 | 65 | 64 | 63 | 63 | 62 | 62 | 59 | 59 |
| 52 | Hokkaido | Andesite | 11.5 | 65 | 62 | 61 | 61 | 61 | 58 | 58 | 54 | 50 | 51 |
| 53 | Hokkaido | Andesite | 6 | 71 | 71 | 71 | 69 | 69 | 67 | 67 | 66 | 64 | 57 |
| 54 | Hokkaido | Andesite | 12.9 | 57 | 54 | 53 | 52 | 50 | 49 | 46 | 45 | 44 | 42 |
| 55 | Hokkaido | Andesite | 14.7 | 72 | 72 | 71 | 71 | 69 | 68 | 67 | 64 | 61 | 56 |

Table S2 Measurement values of Rockwell Hardness.

| No. | Raw Material Type | Outcrop | Measurement value |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | 1st | 2nd | 3rd | 4th | 5th | 6th | 7th | 8th | 9th | 10th |
| 1 | Type FH chert | Ma'an Plateau | 38.7 | 36.5 | 44.2 | 26.4 | 46.1 | 48.9 | 30.7 | 37.3 | 19.9 | -8.0 |
| 2 | Type FH chert | Ma'an Plateau | -11.0 | 33.3 | 43.1 | 14.8 | 39.7 | 5.9 | -3.2 | 44.7 | 53.2 | 1.5 |
| 3 | Type FH chert | Ma'an Plateau | 39.6 | 15.1 | 42.1 | 9.6 | -10.2 | 42.2 | 11.9 | 35.7 | 27.5 | 33.7 |
| 4 | Type FH chert | Ma'an Plateau | 23.7 | 16.6 | 45.9 | 31.7 | 17.7 | 7.2 | 18.1 | 16.2 | 30.8 | 20.0 |
| 5 | Type FH chert | Ma'an Plateau | 44.5 | 24.3 | 1.9 | 43.0 | 40.2 | 21.9 | 44.8 | 31.8 | 28.3 | 48.5 |
| 6 | Type FH chert | Humayma | 15.8 | 46.5 | 40.4 | 31.9 | 22.8 | 25.6 | 34.1 | -5.6 | 52.0 | 20.0 |
| 7 | Type FH chert | Humayma | 44.3 | 52.1 | 43.5 | 31.6 | 53.0 | 52.0 | 46.5 | 62.7 | 53.8 | -6.8 |
| 8 | Type FH chert | Abbasiya | 32.9 | 31.1 | -16.9 | -2.5 | 33.7 | 33.2 | -38.2 | 33.3 | -29.4 | 26.0 |
| 9 | Type FH chert | Abbasiya | 22.7 | 38.7 | 35.8 | 34.7 | 13.6 | 64.2 | 39.9 | 29.7 | 3.4 | 39.3 |
| 10 | Type FH chert | Abbasiya | 39.0 | -10.4 | 43.9 | 11.2 | 21.9 | 36.7 | 9.3 | 27.7 | 52.5 | -2.8 |
| 11 | Type M chert | Humayma | 57.5 | 29.1 | 46.0 | 57.8 | 62.4 | 50.2 | 29.2 | 51.7 | 42.8 | 45.4 |
| 12 | Type M chert | Humayma | 26.3 | 31.6 | 36.4 | 23.3 | 39.4 | 29.1 | 46.5 | 37.0 | 56.0 | 42.9 |
| 13 | Type M chert | Humayma | 1.6 | 41.0 | 25.4 | 26.2 | 33.0 | 23.4 | 34.5 | 11.6 | 47.6 | 15.7 |
| 14 | Type M chert | Humayma | 67.1 | -2.4 | 55.5 | 64.3 | 53.2 | 59.2 | 65.8 | 34.6 | 58.6 | 52.4 |
| 15 | Type M chert | Humayma | 59.2 | 12.6 | 22.4 | 33.8 | 51.8 | 57.3 | 43.1 | 51.7 | 63.1 | 53.2 |
| 16 | Type M chert | Humayma | 50.9 | 46.7 | 35.8 | 30.2 | 54.1 | 51.8 | 10.6 | 36.1 | 30.8 | 35.1 |
| 17 | Obsidian | Hokkaido | -45.3 | -10.4 | 34.0 | 2.8 | -7.8 | 31.6 | -2.4 | 36.9 | 23.4 | 1.9 |
| 18 | Obsidian | Hokkaido | 3.6 | -40.5 | 12.9 | -2.3 | 8.7 | 37.1 | 43.9 | -49.2 | 28.0 | 15.0 |
| 19 | Obsidian | Hokkaido | 25.8 | 4.8 | -1.0 | -7.8 | -10.7 | 28.7 | 18.8 | 22.4 | 0.0 | 34.0 |
| 20 | Glass block | ― | -42.6 | -16.1 | -11.6 | -25.6 | -51.6 | -24.7 | -37.6 | -10.9 | -51.3 | -18.8 |