Supplementary Information

A Wide Temperature 10 V Solid-state Electrolyte with a Critical Current Density of over 20 mA cm-2

Yiqi Wei1, Zhenglong Li2, Zichong Chen1, Panyu Gao3*, Mingxi Gao1, Chenhui Yan1, Zhijun Wu2, Qihang Ma1, Yinzhu Jiang1, Xuebin Yu3, Xin Zhang1, Yongfeng Liu1, Yaxiong Yang2*, Mingxia Gao1, Wenping Sun1, Jian Chen2*, Hongge Pan1,2*

1State Key Laboratory of Silicon Materials and School of Materials Science and Engineering, Zhejiang University, Hangzhou, 310027, China.

2Institute of Science and Technology for New Energy, Xi’an Technological University, Xi’an 710021, China

3 Department of Materials Science, Fudan University, Shanghai, 200433, China

*Corresponding authors: 21110300002@m.fudan.edu.cn; yangyaxiong@xatu.edu.cn; chenjian@xatu.edu.cn; honggepan@zju.edu.cn, hgpan@zju.edu.cn;

Supplementary Table 1. Summary of ex-situ XPS quantifications of HT150-0PMMA and HT150-5PMMA at the cut-off voltages of 2.8, 4.2 and 10 V during the 1st, 2nd and 3rd CV experiments.

| Specimen | Cycle Number /Voltage (V) | B1s (at %) |  |  |  |  | O1s (at %) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | B-O | Oxide BH4- | B-H | (OCH3)xBH4-x | O-B |  | O-Al | O-C=O | C-O-CH3 | Transition O | C=O(Li+•O=C) |
| HT150-0PMMA | 1/2.8 | 39.63 | 38.10 | 22.27 |  | 71.01 |  | 28.99 |  |  |  |  |
|  | 1/4.2 | 36.24 | 44.66 | 19.10 |  | 68.48 |  | 31.52 |  |  |  |  |
|  | 1/10 | 33.86 | 49.70 | 16.44 |  | 71.98 |  | 28.02 |  |  |  |  |
|  | 2/2.8 | 48.30 | 36.72 | 14.97 |  | 72.03 |  | 27.97 |  |  |  |  |
|  | 2/4.2 | 46.48 | 39.85 | 13.67 |  | 72.85 |  | 27.15 |  |  |  |  |
|  | 2/10 | 43.24 | 44.77 | 11.99 |  | 72.91 |  | 29.09 |  |  |  |  |
|  | 3/2.8 | 49.06 | 34.62 | 16.32 |  | 71.64 |  | 28.36 |  |  |  |  |
|  | 3/4.2 | 41.57 | 46.46 | 11.97 |  | 72.73 |  | 27.27 |  |  |  |  |
|  | 3/10 | 44.26 | 50.38 | 5.36 |  | 70.90 |  | 29.10 |  |  |  |  |
| HT150-5PMMA | 1/2.8 | 64.81 | 1.56 | 21.19 | 12.43 | 42.39 |  | 10.77 | 23.52 | 11.02 | 1.17 | 11.13 |
|  | 1/4.2 | 64.26 | 2.28 | 19.22 | 11.73 | 49.19 |  | 8.31 | 17.33 | 12.42 | 2.56 | 10.19 |
|  | 1/10 | 66.29 | 2.52 | 18.62 | 13.78 | 46.33 |  | 7.65 | 21.45 | 13.13 | 1.39 | 10.05 |
|  | 2/2.8 | 60.50 | 5.92 | 21.30 | 12.28 | 42.09 |  | 10.55 | 23.55 | 11.92 | 0.59 | 11.30 |
|  | 2/4.2 | 60.81 | 7.38 | 20.57 | 11.24 | 49.69 |  | 8.01 | 17.69 | 12.92 | 1.58 | 10.10 |
|  | 2/10 | 60.14 | 8.63 | 19.93 | 11.31 | 46.69 |  | 7.15 | 21.65 | 14.26 | 0.80 | 9.31 |
|  | 3/2.8 | 61.01 | 8.16 | 20.36 | 10.47 | 51.43 |  | 9.66 | 16.78 | 10.69 | 0.77 | 10.74 |
|  | 3/4.2 | 60.00 | 8.34 | 20.18 | 11.49 | 50.38 |  | 8.58 | 15.41 | 12.03 | 2.93 | 10.66 |
|  | 3/10 | 60.28 | 8.91 | 19.16 | 11.65 | 47.33 |  | 10.04 | 16.59 | 12.21 | 2.73 | 11.21 |

Supplementary Table 2. Summary of the electrical properties and electrochemical performances of the most-studied SEs.

| Typical SEs | Li-ion Conductivity (S cm-1) | Electronic Conductivity (S cm-1) | Voltage Windows (V) | CCD (mA cm-2) | Cycling performances | Capacity (mAh cm-2) | Temperature (℃) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| This Work | 5.1×10-4 | 3.5×10-10 | -0.2 ~ 10 | 21.6 | 10.8 mA cm-2 for 6000 h | 1.0 | 30 |
|  | 2.6×10-2 | 9.3×10-9 | -0.2 ~ 10 | 328.0 | 159.5 mA cm-2 for 6000 h | 1.0 | 130 |
| LiBH4-LZO1 | - | - | 1.7 ~ 2.5 | 13.0 | 3.0 mA cm-2 for 120 h | 0.4 | 120 |
| Li4(BH4)3I@SBA-152 | 8.6×10-4 | - | -0.2 ~5.0 | 2.6 | 0.5 mA cm-2 for 350 h | 0.1 | 55 |
| LiBH4-LiF3 | 1.0×10-3 | 3.7×10-8 | -0.3 ~ 3.0 | 6.6 | 5.0 mA cm-2 for 500 h | - | 125 |
| Li2B12H124 | 3.1×10-4 | 9.0×10-10 | -0.5 ~ 5.0 | 3.8 | - | 0.5 | 75 |
| (LiBH4)2AB5 | 4.9×10−3 | 1.1×10-6 | 0 ~ 2.0 | 3.0 | 0.2 mA cm-2 for 40 h | 0.2 | 50 |
| NZSP6 | - | - | - | 2.5 | 0.5 mA cm-2 for 500 h | 0.25 | 30 |
| LPSCl7 | - | - | - | 1.0 | 1.0 mA cm-2 for 500 h | 1.0 | 30 |
| LLZO1 | 1.0×10-3 | - | - | 2.4 | 1.0 mA cm-2 for 300 h | 0.5 | 30 |
| LPSCl8 | - | - | - | 10.0 | 0.25 mA cm-2 for 1800 h | 0.25 | 30 |
| LGPS9 | - | - | 0.1 ~ 2.5 | 11.0 | 0.5 mA cm-2 for 3800 h | 0.5 | 30 |
| YSZ@BASE10 | 2.7×10-3 | 6.0 10-12 | 3.0 ~ 4.5 | 7.0 | 0.5 mA cm-2 for 330 h | 3.5 | 80 |
| β″-alumina11 | 1.6×10-3 | 7.0 10-11 | - | 14.0 | - | 0.25 | 30 |

Supplementary Table 3. Summary of XPS quantifications of HT150-0PMMA and HTy-5PMMA (y = 100, 110, 120, 130, 140 and 150) SEs.

| Specimens | B1s (at %) |  |  | O1s (at %) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | B-O | B-H | (OCH3)xBH4-x | O-B | O-Al | O-C=O | C-O-CH3 | Transition O | C=O(Li+•O=C) |
| HT150-0PMMA | 46.27 | 53.73 | 0 | 68.30 | 15.00 | 6.67 | 9.07 | 0.86 | 0 |
| HT100-5PMMA | 46.95 | 53.05 | 2.05 | 63.25 | 8.00 | 17.00 | 9.05 | 0.65 | 0 |
| HT110-5PMMA | 47.55 | 52.45 | 3.06 | 60.77 | 7.88 | 16.90 | 9.95 | 0.22 | 1.22 |
| HT120-5PMMA | 48.85 | 51.15 | 6.96 | 57.20 | 7.55 | 16.50 | 9.05 | 0.52 | 2.22 |
| HT130-5PMMA | 48.44 | 43.63 | 7.93 | 52.52 | 7.90 | 16.69 | 8.66 | 0.34 | 5.96 |
| HT140-5PMMA | 58.90 | 41.10 | 10.09 | 51.27 | 7.79 | 15.98 | 8.26 | 0.55 | 6.06 |
| HT150-5PMMA | 49.15 | 39.40 | 11.45 | 48.23 | 7.31 | 15.04 | 10.24 | 0.44 | 7.29 |

Supplementary Fig. 1. Structural characterizations of ISMR-modified SEs. a, XRD curves for LiBH4, PMMA, HT150-0PMMA and HT150-5PMMA. SEM images of b, HT150-0PMMA and c, HT150-5PMMA. d, EDS of HT150-5PMMA secondary particle. Cryo-TEM images of e, HT150-0PMMA and f, HT150-5PMMA.

Supplementary Fig. 2. FTIR spectra of LiBH4, LiI, Al2O3, PMMA, HT150-0PMMA, 5PMMA and HT150-5PMMA.

Supplementary Fig. 3. Ex situ XPS analyses over the CV cycles for HT150-0PMMA and HT150-5PMMA. a, B1s and b, O1s XPS data for HT150-0PMMA with cutoff voltages of 2.8, 4.2 and 10.0 V at the 2nd cycle. c, B1s and d, O1s XPS spectra for HT150-0PMMA with cutoff voltages of 2.8, 4.2 and 10.0 V at the 3rd cycle. e, B1s and f, O1s XPS spectra for HT150-5PMMA with cutoff voltages of 2.8, 4.2 and 10.0 V at the 2nd cycle. g, B1s and h, O1s XPS spectra for HT150-5PMMA with cutoff voltages of 2.8, 4.2 and 10.0 V at the 3rd cycle.

Supplementary Fig. 4. Extended CV measurement from 8.0 to 15.0 V for HT150-5PMMA.

Supplementary Fig. 5. CV curves over wide operational temperature ranges. Temperature-dependent CV curves for HT150-0PMMA at a, -30 ℃, b, 0 ℃ and c, 80 ℃. CV curves for the HT150-5PMMA at d, -30 ℃, e, 0 ℃ and f, 80 ℃. CV curves for HT150-0PMMA at g, 110 ℃, h, 130 ℃ and i, 150 ℃. CV curves for HT150-5PMMA at j, 110 ℃, k, 130 ℃ and l, 150 ℃.

Supplementary Fig. 6. Extended Dendrite suppression with the ISMR-modified SEs. CCDs of a, HT150-1PMMA, b, HT150-3PMMA, c, HT150-7PMMA and d, HT150-10PMMA measured at 25 ℃. CCDs of e, HT150-0PMMA, f, HT150-1PMMA, g, HT150-3PMMA, h, HT150-5PMMA, i, HT150-7PMMA, j, HT150-10PMMA measured at 130 ℃. Li plating and stripping performances of HT150-0PMMA and HT150-5PMMA measured at 130 ℃ at k, 32.00 mA cm-2 and l, 164.00 mA cm-2.

Supplementary Fig. 7. Cycling performances of the ISMR-modified SEs over the wide operational temperature range. Li plating and stripping curves for HT150-0PMMA and HT150-5PMMA at a, 0.1 CCD and at b, 0.5 CCD at -30 ℃. Li plating and stripping curves for HT150-0PMMA and HT150-5PMMA at c, 0.1 CCD and at d, 0.5 CCD at 80 ℃. Li plating and stripping curves for HT150-0PMMA and HT150-5PMMA at e, 0.1 CCD and at f, 0.5 CCD at 110 ℃. Li plating and stripping curves of HT150-0PMMA and HT150-5PMMA at g, 0.1 CCD and at h, 0.5 CCD at 150 ℃.

Supplementary Fig. 8. Failure mechanisms of the ISMR-modified SEs a, Cross-sectional SEM images determined before cycling, b, after 500 h and c, after 800 h for HT150-0PMMA. d, Cross-sectional SEM images determined before cycling, e, after 500 h and f, after 5000 h for HT150-5PMMA. The blue circles represent the cracks and flaws in SEs and the yellow ones represent Li depositions.

Supplementary Fig. 9. AFM nanoindentations of pure PMMA and HT150-pure PMMA.

Supplementary Fig. 10. CCDs and voltage windows for other ISMR-modified hydride SEs. CCD for a, Li2B12H12, b, LiAlH4, c, LiNH2, d, HT150-Li2B12H12-5PMMA, e, HT150-LiAlH4-5PMMA and f, HT150-LiNH2-5PMMA. CV curves for g, Li2B12H12, h, LiAlH4, i, LiNH2, j, HT150-Li2B12H12-5PMMA, k, HT150-LiAlH4-5PMMA and l, HT150-LiNH2-5PMMA.

References

1	Takemoto, K. et al. Evaluation on hybrid-electrolyte structure using the liquid electrolyte interlayer containing LiBH4 at Li7La3Zr2O12 vertical bar Li interface at high operating temperature. J. Power Sources 478, doi:10.1016/j.jpowsour.2020.228751 (2020).

2	Lu, F. Q. et al. A High-Performance Li-B-H Electrolyte for All-Solid-State Li Batteries. Adv. Funct. Mater. 29, doi:10.1002/adfm.201809219 (2019).

3	Mo, F. et al. Inside or Outside: Origin of Lithium Dendrite Formation of All Solid‐State Electrolytes. Adv. Energy Mater. 9, doi:10.1002/aenm.201902123 (2019).

4	Shi, X. et al. In situ forming LiF nanodecorated electrolyte/electrode interfaces for stable all-solid-state batteries. Materials Today Nano 10, doi:10.1016/j.mtnano.2020.100079 (2020).

5	Liu, H. et al. Incorporation of Ammonia Borane Groups in the Lithium Borohydride Structure Enables Ultrafast Lithium Ion Conductivity at Room Temperature for Solid-State Batteries. Chem. Mater. 32, 671-678, doi:10.1021/acs.chemmater.9b03188 (2019).

6	Oh, J. A. S. et al. A Robust Solid-Solid Interface Using Sodium-Tin Alloy Modified Metallic Sodium Anode Paving Way for All-Solid-State Battery. Adv. Energy Mater. 11, doi:10.1002/aenm.202101228 (2021).

7	Hänsel, C., Singh, B., Kiwic, D., Canepa, P. & Kundu, D. Favorable Interfacial Chemomechanics Enables Stable Cycling of High-Li-Content Li–In/Sn Anodes in Sulfide Electrolyte-Based Solid-State Batteries. Chem. Mater. 33, 6029-6040, doi:10.1021/acs.chemmater.1c01431 (2021).

8	Ye, L. & Li, X. A dynamic stability design strategy for lithium metal solid state batteries. Nature 593, 218-222, doi:10.1038/s41586-021-03486-3 (2021).

9	Pan, H. et al. Carbon-free and binder-free Li-Al alloy anode enabling an all-solid-state Li-S battery with high energy and stability. Sci Adv 8, eabn4372, doi:10.1126/sciadv.abn4372 (2022).

10	Deng, T. et al. Interfacial-engineering-enabled practical low-temperature sodium metal battery. Nat Nanotechnol 17, 269-277, doi:10.1038/s41565-021-01036-6 (2022).

11	Bay, M. C. et al. Sodium Plating from Na‐β″‐Alumina Ceramics at Room Temperature, Paving the Way for Fast‐Charging All‐Solid‐State Batteries. Adv. Energy Mater. 10, doi:10.1002/aenm.201902899 (2019).