Polyhydrido Copper Nanocluster [Cu14H10(PPh3)8(SPhMe2)3]+ : Symmetry-Breaking by Thiolate Ligands to form Racemic Pairs of Chiral Clusters in Solid-State

Shuhuan Zeng1, Xin Ge1, Hongwen Deng2, Shuwei Hao1, Zhiye Zhang1, Boon K. Teo2*, Cunfa Sun1*

1College of Materials Science and Engineering, Huaqiao University, Xiamen 361021, China

2State Key Laboratory for Physical Chemistry of Solid Surfaces, Collaborative Innovation Center of Chemistry for Energy Materials,National & Local Joint Engineering Research Center of Preparation Technology of Nanomaterials, College of Chemistry andChemical Engineering, Xiamen University, Xiamen 361005, China

Experimental details

Reagents. Copper(II) acetate monohydrate [Cu(CH3COO)2·H2O, purity 99%], sodium borohydride (NaBH4, purity 98%), sodium borodeuteride (NaBD4, purity 99%), dichloromethane (CH2Cl2, A.R.), and methanol (CH3OH, A.R.) were purchased from Sinopharm Chemical Reagent Co. Ltd. (Shanghai, China). Tetraphenylphosphonium tetraphenylborate (TPPTPB, purity 99%), 2,4-dimethylbenzenethiol (HSPhMe2, purity 99%), were purchased from Alfa Aesar Chemical Reagent Co. Ltd. (Tianjin, China). The water used in all experiments was ultrapure. All reagents were used as received without further purification.

Synthetic process. In a typical synthesis, 100 mg of Cu(OAc)2•H2O and 32 mg TPPTPB were dissolved in a mixed solvent of 2 mL methanol and 4ml CH2Cl2, followed by the addition of 100 mg of PPh3 and 30 μL of HSPhMe2 under the vigorous stirring. After 20 min, 3 mL of an aqueous solution of NaBH4 (30 mg/mL) were added dropwise to the reaction mixture. After aged for 3 h at 25 °C, then the aqueous phase and precipitate were removed, while the organic phase was concentrated and washed with MeOH/H2O (4:1 by volume) several times, and then dissolved in CH2Cl2 for further analysis. By the diffusion with hexane at 4 °C for one week, bright-yellow single crystals suitable for X-ray diffraction study were obtained with ~12% yield based on copper. With the same procedures, instead of NaBH4, NaBD4 was used to synthesize the deuterium analog (1D).

Single Crystal Analysis: The diffraction data of all compounds were collected on an Agilent Technologies SuperNova system. X-ray single crystal diffractometer with Cu Kα radiation (λ = 1.54184 Å) at 100 K. The data were processed using CrysAlisPro.[1] All structures were solved and refined using Full-matrix least-squares based on F2 with program ShelXT and ShelXLwithin Olex2.[2-4]

Measurements of Optical Properties. Pure crystals were dissolved in Spectro Grade CH2Cl2 for spectrum measurements. UV/Vis absorption spectra were recorded on a Varian Carry 5000 spectrophotometer using a quartz cuvette of 1 mm path length. The signal of the blank solvent was subtracted. For each spectrum, eight scans at a scanning speed 100 nm/min with a data pitch of 0.1 nm were averaged. The spectra were recorded at room temperature.

Measurements of NMR. 2H-NMR spectrum was recorded on an AVANCE III 850 MHz spectrometer in dichloromethane. Chemical shifts are reported in ppm with the internal TMS signal at 0.0 ppm as a standard.

Figure S1  The cubic skeleton breaks into C3 symmetry, a) top view of the copper frame; b) side view of the copper cube and the thiolation. Color labels: brown = Cu, yellow = S.

Figure S2  Side view of the phosphorus frame. Color labels: brown = Cu, yellow = S, pink = P.

Figure S3  a): Chirality caused by the chiral orientation of the thiolate ligands in 2; b): The unit cell diagram of 2, the unit cell contains four pair of enantiomers (two different colors). All hydrogen and carbon atoms and solvents are omitted for clarity. Color labels: brown = Cu, yellow = S, pink = P.

Figure S4  Geometric change of the fcc unit gradually form inner octahedron to standard fcc cell. Skeleton of a): cluster 2, b): S. Q. Zang’s work, alkynyl copper cluster with quasi-fcc 14-Cu skeleton[5], c): S. Q. Zang’s dithiolated Cu14 cluster with regular fcc skeleton[6] d): [CuHPPh3]6 cluster[7]. All the H and part of ligands are omitted for clarity. Color labels: brown = Cu, yellow = S, pink = P, gray = C, teal = B, red = O.

Figure S5  The presence of intracluster weak interactions on the surface. a): cluster 2; b): cluster 1. c): space-filling model of cluster 1, viewed along the C3 axis. d): cubic 14-Cu in cluster 1.  In cluster 2, the hydrogen atoms of thiolate ligands bind with a phenyl group of the PPh3 ligand tightly via intracluster C−H…π interactions (2.72 Å), particularly with the protruded vertex. Furthermore, the phenyl groups of the PPh3 on the protruded vertex interact with nearby thiolates through C−H…π interactions (2.64 Å). While in cluster 1, the steric thiolate ligands also interact with copper atoms through intracluster C−H…π interactions (2.68 Å), but the thiolate further interact with the vertex copper atom via weak C−H…Cu interaction [8]. In cluster 1, the three tBuS are more packed, severe steric hindrance occurred with short C-H…H-C distances leaving no space for 8th PPh3 added (the distances between the ligands are 4.03 Å), which leads the vertex to be a bare copper atom other than Cu-PPh3 as in cluster 2. Thus, cluster 2 shows a protrude vertex, while cluster 1 possesses a standard fcc cell. Color labels: brown = Cu, yellow = S, pink = P, gray = C, light with gray = H.

Figure S6  ESI-MS: comparison of cluster 2 and 2D (left); full scale and analysis of 2D (right).

Figure S7  Shorter bonds in the skeleton, as obtained from experimental crystallographic data. Color labels: brown = Cu, yellow = S.

Figure S8  Four groups caused by the symmetry and thiolates’ coordination: a) the μ6- Ho; b) three facial μ3- Ha; c) three edged μ4- Hb sharing two Cu with thiolate; d) three edged μ4- Hc sharing one Cu with thiolate. Color labels: brown = Cu, yellow = S, white = H.

| Table S1. Cluster 2: Cu-Cu bonds and Cu···Cu distances |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Atom1- Atom1 | Range /Å | Average/Å | Atom1- Atom1 | Range /Å | Average/Å |
| Cua···Cue | 3.68 | 3.68 | Cuf···Cuf | 3.03 | 3.03 |
| Cub-Cue | 2.63-2.70 | 2.67 | Cuc-Cuf | 2.42-2.50 | 2.46 |
| Cue···Cue | 2.95 | 2.95 | Cud-Cuf | 2.56 | 2.56 |
| Cue-Cuc | 2.67 | 2.67 | Cua···Cub | 4.29 | 4.29 |
| Cue-Cuf | 2.49-2.56 | 2.52 | Cub···Cuc | 3.92-4.04 | 3.98 |
| Cuf-Cud | 2.97 | 2.97 | Cud-Cuc | 2.97 | 2.97 |

| Table S2. Cluster 2: Cu-H and Cu-S bonds |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Atom1- Atom2 | Distance（±0.01）/Å |  |  |  |  |  |  |  |  |  |  |  | Average（±0.01）/Å |
| Ha-Cu | 1.80 | 1.90 | 2.05 | 1.80 | 1.90 | 2.05 | 1.80 | 1.90 | 2.05 |  |  |  | 1.92 |
| Hb-Cu | 1.90 | 1.97 | 2.02 | 2.04 | 1.90 | 1.97 | 2.02 | 2.04 | 1.90 | 1.97 | 2.02 | 2.04 | 1.98 |
| Hc-Cu | 1.89 | 1.94 | 2.09 | 2.10 | 1.89 | 1.94 | 2.09 | 2.10 | 1.89 | 1.94 | 2.09 | 2.10 | 2.00 |
| Ho-Cu | 1.84 | 2.09 | 1.84 | 2.09 | 1.84 | 2.09 |  |  |  |  |  |  | 1.96 |
| S-Cua | 2.42 | 2.42 | 2.42 |  |  |  |  |  |  |  |  |  | 2.42 |
| S-Cub | 2.31 | 2.31 | 2.31 |  |  |  |  |  |  |  |  |  | 2.31 |
| S-Cue | 2.28 | 2.28 | 2.28 |  |  |  |  |  |  |  |  |  | 2.28 |

References

[1]	CrysAlisPro Version 1.171.35.19. Agilent Technologies Inc. Santa Clara C, USA. 2011.

[2]	Sheldrick GM. Shelxt - integrated space-group and crystal-structure determination. Acta Crystallogr Sect A: Found Adv, 2015, 71(Pt 1): 3-8

[3]	Dolomanov OV, Bourhis LJ, Gildea RJ, et al. Olex2: A complete structure solution, refinement and analysis program. J Appl Crystallogr, 2009, 42(2): 339-341

[4]	Sheldrick GM. A short history of shelx. Acta Crystallogr A, 2008, 64(Pt 1): 112-122

[5]	M.M. Zhang, X.Y. Dong, Z.Y. Wang, H.Y. Li, S.J. Li, X. Zhao, S.Q. Zang, Angew. Chem. Int. Ed., 2020, 59, 10052-10058.

[6]	Y.L. Li, J. Wang, P. Luo, X.H. Ma, X.Y. Dong, Z.Y. Wang, C.X. Du, S.Q. Zang, T.C.W. Mak, Adv. Sci., 2019, 6, 1900833-1900839.

[7]	R.C. Stevens, M.R. McLean, R. Bau, T.F. Koetzle, J. Am. Chem. Soc., 1989, 111, 3472–3473;

[8]	L. Wang, X. Yan, G. Tian, Z. Xie, S. Shi, Y. Zhang, S. Li, X. Sun, J. Sun, J. He and H. Shen, Dalton Trans, 2023, 52, 3371-3377.