Supplementary Information

to

Green Preparation of Flexible and Transparent SiO2-Fe2O3-PS film for Dye Adsorption and UV-Shielding Applications

Abhijit Nath*, Mrityunjoy Mahato*

Physics Division, Department of Basic Sciences and Social Sciences, School of Technology, North-Eastern Hill University, Shillong, Meghalaya, 793022, India

*To whom correspondence should be addressed: mrityunjoyphy@gmail.com, abhijitnsh46@gmail.com,

TableS1: Experimental XRD peak position, planes of SiO2, Fe2O3 and SiO2-Fe2O3 heterostructure.

| Sl No | XRD Peak Position |  |  | Planes (hkl) | Phase and Literature 2𝜽 value | Reference |
| --- | --- | --- | --- | --- | --- | --- |
|  | SiO2 Nanoparticle | Fe2O3 Nanoparticle | SiO2-Fe2O3 Heterostructure |  |  |  |
| 1 | - | 24.16 | 24.01 | [012] | ⍺-Fe2O3 (24.20) | Nath et al 2023 |
| 2 | 27.37 | - | 26.71 | [101] | SiO2 (27) | Barma 2020 |
| 3 | 31.42 | 33.16 | - | [220] | ⍺-Fe2O3 (33.22) | Nath et al 2023 |
| 4 | - | 35.64 | - | [104] | ⍺-Fe2O3 (35.62) | Nath et al 2023 |
| 5 | - | - | 37.90 | - | SiO2 (27) | Barma 2020 |
| 6 | - | 40.92 | 40.33 | [113] | ⍺-Fe2O3 (40.79) | Nath et al 2023 |
| 7 | 45.27 | - | 44.87 | [102] | SiO2 (45) | Barma 2020 |
| 8 | - | 49.52 | 47.29 | [024] | ⍺-Fe2O3 (49.45) | Nath et al 2023 |
| 9 | - | 54.08 | - | [116] | ⍺-Fe2O3 (54.25) | Nath et al 2023 |
| 10 | 56.80 | - | - | [202] | SiO2 (56) | Barma 2020 |
| 11 | - | 57.56 | 57.79 | [018] | ⍺-Fe2O3 (57.67) | Nath et al 2023 |
| 12 | - | 62.52 | 62.20 | [214] | ⍺-Fe2O3 (62.59) | Nath et al 2023 |
| 13 | - | 64.08 | - | [300] | ⍺-Fe2O3 (63.59) | Nath et al 2023 |
| 14 | 64.65 | - | 64.75 | [113] | SiO2 (65) | Barma 2020 |
| 15 | - | - | 69.01 | - | SiO2 (70) | Barma 2020 |
| 16 | - | 72.12 | - | [119] | ⍺-Fe2O3 (72.19) | Nath et al 2023 |
| 17 | 75.29 | 75.52 | 74.56 | [101] | ⍺-Fe2O3 (75.67) | Nath et al 2023 |
| 18 | 77.90 | - | 77.82 | - | SiO2 (76) | Barma 2020 |

Fig. S1 W-H plot for SiO2, Fe2O3 and SiO2-Fe2O3 heterostructures.