Supplementary Material

Biochar promotes methane production during anaerobic digestion of organic waste, a meta-analysis

Leilei Xiao1,2*, Eric Lichtfouse3,4*, P. Senthil Kumar5, Quan Wang1, Fanghua Liu1,2

Number of pages: 13

Number of Tables: 1

Table SI 1 Literature data and references of the effect of biochar addition on biomethane production during anaerobic disposal of solid waste and wastewater.

Table S1 Literature data and references of the effect of biochar addition on biomethane production during anaerobic disposal of solid waste and wastewater.

| Feedstock | Pyrolysis temperature (°C) | pH | Conductivity (mS/m) | Size (mm) | BET (m2/g) | Doze | Methanogens 3 | Methanogens 4 | Control group |  |  | Experimental group |  |  | Hedge's d | References |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  | Max rate or yield | SD | Number | Max rate or yield | SD | Number |  |  |
| Pine wood | 980 | NA1 | 2.2 ± 0.46 | 2.0-2.4 | 451 ± 11 | NU2 | NA | NA | 0.87 | 0.018 | 2 | 1.06 | 0.0792 | 2 | 1.89 | (Cheng et al., 2018) |
| Pine wood | 980 | NA | 2.2 ± 0.46 | 2.0-2.4 | 451 ± 11 | NU | NA | NA | 0.935 | 0.015 | 2 | 1.3 | 0.0532 | 2 | 5.33 | (Cheng et al., 2018) |
| Pine wood | 980 | NA | 2.2 ± 0.46 | 2.0-2.4 | 451 ± 11 | NU | NA | NA | 1.16 | 0.145 | 2 | 1.11 | 0.0166 | 2 | -0.277 | (Cheng et al., 2018) |
| Pine wood | 980 | NA | 2.2 ± 0.46 | 0.21-0.25 | 531 ± 31 | NU | NA | NA | 1.08 | 0.037 | 2 | 0.741 | 0.0748 | 2 | -3.28 | (Cheng et al., 2018) |
| Pine wood | 980 | NA | 2.2 ± 0.46 | 0.21-0.25 | 531 ± 31 | NU | NA | NA | 1.11 | 0.014 | 2 | 0.748 | 0.184 | 2 | -1.59 | (Cheng et al., 2018) |
| Pine wood | 980 | NA | 2.2 ± 0.46 | 0.21-0.25 | 531 ± 31 | NU | NA | NA | 1.08 | 0.014 | 2 | 0.413 | 0.0317 | 2 | -15.54 | (Cheng et al., 2018) |
| Fruitwoods | 800 | 8.63 ± 0.13 | NA | NA | NA | 2 | NA | NA | 2.81 | 0.624 | 3 | 2.25 | 0.32909 | 3 | -0.899 | (Luo et al., 2015) |
| Fruitwoods | 800 | 8.63 ± 0.13 | NA | NA | NA | 4 | NA | NA | 1.12 | 0.087 | 3 | 2.09 | 0.121244 | 3 | 7.37 | (Luo et al., 2015) |
| Fruitwoods | 800 | 8.63 ± 0.13 | NA | 0.5-1 | NA | 6 | Methanobacterium | Methanobacterium | 1.26 | 0.104 | 3 | 1.53 | 0.121244 | 3 | 1.91 | (Luo et al., 2015) |
| Fruitwoods | 800 | 8.63 ± 0.13 | NA | NA | NA | 8 | Methanobacterium | Methanobacterium | 0.97 | 0.104 | 3 | 1.02 | 0.103923 | 3 | 0.385 | (Luo et al., 2015) |
| Sawdust | 500 | 9.15 ± 0.12 | NA | 0.25-1 | 248 ± 34 | 10 | NA | NA | 1.349 | 0.095 | 2 | 1.351 | 0.0843 | 2 | 0.0127 | (Li et al., 2018) |
| Sawdust | 500 | 9.15 ± 0.12 | NA | 0.25-1 | 248 ± 34 | 10 | NA | NA | 2.606 | 0.058 | 2 | 2.619 | 0.0635 | 2 | 0.123 | (Li et al., 2018) |
| Sawdust | 500 | 9.15 ± 0.12 | NA | 0.25-1 | 248 ± 34 | 10 | NA | NA | 3.502 | 0.163 | 2 | 5.482 | 0.192 | 2 | 6.36 | (Li et al., 2018) |
| Sawdust | 500 | 9.15 ± 0.12 | NA | 0.25-1 | 248 ± 34 | 10 | NA | NA | 4.675 | 0.075 | 2 | 8.473 | 0.114 | 2 | 22.5 | (Li et al., 2018) |
| Sawdust | 500 | 9.15 ± 0.12 | NA | 0.25-1 | 248 ± 34 | 10 | Methanosaeta | Methanosaeta | 5.696 | 0.2 | 2 | 10.21 | 0.534 | 2 | 6.40 | (Li et al., 2018) |
| Hardwood | NA | 7.9 ± 0.3 | 14 ± 10 | NA | NA | 5 | NA | NA | 1.813 | 0.142 | 3 | 2.872 | 0.245 | 3 | 4.23 | (Paritosh and Vivekanand, 2019) |
| Hardwood | NA | 7.9 ± 0.3 | 14 ± 10 | NA | NA | 10 | NA | NA | 1.813 | 0.142 | 3 | 3.662 | 0.254 | 3 | 7.19 | (Paritosh and Vivekanand, 2019) |
| Hardwood | NA | 7.9 ± 0.3 | 14 ± 10 | NA | NA | 15 | NA | NA | 1.813 | 0.142 | 3 | 2.993 | 0.238 | 3 | 4.82 | (Paritosh and Vivekanand, 2019) |
| Hardwood | NA | 7.9 ± 0.3 | 14 ± 10 | NA | NA | 20 | NA | NA | 1.813 | 0.142 | 3 | 2.611 | 0.12 | 3 | 4.86 | (Paritosh and Vivekanand, 2019) |
| Hardwood | NA | 7.9 ± 0.3 | 14 ± 10 | NA | NA | 25 | NA | NA | 1.813 | 0.142 | 3 | 2.463 | 0.214 | 3 | 2.86 | (Paritosh and Vivekanand, 2019) |
| Hardwood | NA | 7.9 ± 0.3 | 14 ± 10 | NA | NA | 30 | NA | NA | 1.813 | 0.142 | 3 | 2.49 | 0.228 | 3 | 2.85 | (Paritosh and Vivekanand, 2019) |
| Rice straw | 600 | 10.40 ± 0.02 | 2.853 ± 0.086 | <2 | 38.8 ± 0.99 | 20 | Methanosarcina | Methanosarcina | 0.0257 | 0.031 | 3 | 0.347 | 0.217 | 3 | 1.66 | (Yuan et al., 2018) |
| Wood chips | 600 | 9.60 ± 0.03 | 0.225 ± 0.006 | <2 | 14.75 ± 0.95 | 20 | Methanosarcina | Methanosarcina | 0.0257 | 0.031 | 3 | 0.0019 | 0.0014 | 3 | -0.868 | (Yuan et al., 2018) |
| cow Manure biomasses | 600 | 10.24 ± 0.06 | 0.277 ± 0.007 | <2 | 16.91 ± 0.73 | 20 | Methanobacterium | Methanobacterium | 0.0257 | 0.031 | 3 | 0.825 | 0.238 | 3 | 3.77 | (Yuan et al., 2018) |
| Pine sawdust | 650 | 9.6 | NA | 0.0035–0.0259 | 130 | 8.3 | NA | NA | 113 | 8.66 | 3 | 156 | 12.12436 | 3 | 3.27 | (Sunyoto et al., 2016) |
| Pine sawdust | 650 | 9.6 | NA | 0.0035–0.0259 | 130 | 16.6 | NA | NA | 113 | 8.66 | 3 | 160 | 5.196152 | 3 | 5.27 | (Sunyoto et al., 2016) |
| Pine sawdust | 650 | 9.6 | NA | 0.0035–0.0259 | 130 | 25.1 | NA | NA | 113 | 8.66 | 3 | 145 | 5.196152 | 3 | 3.58 | (Sunyoto et al., 2016) |
| Pine sawdust | 650 | 9.6 | NA | 0.0035–0.0259 | 130 | 33.3 | NA | NA | 113 | 8.66 | 3 | 138 | 13.85641 | 3 | 1.73 | (Sunyoto et al., 2016) |
| Switchgrass | 500 | 7.3 ± 0.3 | 33.8 ± 1.2 | 0.669 ± 0.453 | 5.7 ± 2.0 | NA | NA | NA | 190.8 | 20.61 | 3 | 328.7 | 4.458 | 3 | 7.40 | (Shanmugam et al., 2018) |
| Ashe juniper | 400 | 7.0 ± 0.2 | 35 ± 14 | 1.068 ± 0.838 | 8.0 ± 3.0 | NA | NA | NA | 190.8 | 20.61 | 3 | 327.2 | 14.7 | 3 | 6.10 | (Shanmugam et al., 2018) |
| Fruitwoods | 800–900 | 8.63 ± 0.13 | NA | NA | NA | 4 | NA | NA | 490 | 14.5 | 3 | 480.5 | 5.6 | 3 | -0.691 | (Cai et al., 2016) |
| Fruitwoods | 800–900 | 8.63 ± 0.13 | NA | NA | NA | 10 | NA | NA | 490 | 14.5 | 3 | 493.1 | 4.8 | 3 | 0.230 | (Cai et al., 2016) |
| Fruitwoods | 800–900 | 8.63 ± 0.13 | NA | NA | NA | 20 | NA | NA | 490 | 14.5 | 3 | 507.5 | 4.6 | 3 | 1.30 | (Cai et al., 2016) |
| Fruitwoods | 800–900 | 8.63 ± 0.13 | NA | NA | NA | 2 | NA | NA | 440 | 39.1 | 3 | 460.3 | 3.5 | 3 | 0.586 | (Cai et al., 2016) |
| Fruitwoods | 800–900 | 8.63 ± 0.13 | NA | NA | NA | 5 | NA | NA | 440 | 39.1 | 3 | 530.5 | 4.2 | 3 | 2.60 | (Cai et al., 2016) |
| Fruitwoods | 800–900 | 8.63 ± 0.13 | NA | NA | NA | 10 | NA | NA | 440 | 39.1 | 3 | 476.6 | 4 | 3 | 1.05 | (Cai et al., 2016) |
| Fruitwoods | 800–900 | 8.63 ± 0.13 | NA | NA | NA | 1.6 | NA | NA | 340 | 31.7 | 3 | 490.2 | 7.1 | 3 | 5.23 | (Cai et al., 2016) |
| Fruitwoods | 800–900 | 8.63 ± 0.13 | NA | NA | NA | 4 | NA | NA | 340 | 31.7 | 3 | 478.1 | 3.7 | 3 | 4.90 | (Cai et al., 2016) |
| Fruitwoods | 800–900 | 8.63 ± 0.13 | NA | NA | NA | 8 | NA | NA | 340 | 31.7 | 3 | 471.9 | 3 | 3 | 4.69 | (Cai et al., 2016) |
| Sewage sludge | 350 | 6.4 ± 0.1 | 44.22 ± 0.02 | NA | NA | 0.5 | NA | NA | 156.5 | 3.226 | 3 | 187.9 | 4.839 | 3 | 6.11 | (Ambaye et al., 2020) |
| Sewage sludge | 350 | 6.4 ± 0.1 | 44.22 ± 0.02 | NA | NA | 1 | NA | NA | 156.5 | 3.226 | 3 | 208.9 | 4.032 | 3 | 11.5 | (Ambaye et al., 2020) |
| Sewage sludge | 350 | 6.4 ± 0.1 | 44.22 ± 0.02 | NA | NA | 1.5 | NA | NA | 156.5 | 3.226 | 3 | 190.3 | 5.645 | 3 | 5.88 | (Ambaye et al., 2020) |
| Sewage sludge | 350 | 6.4 ± 0.1 | 44.22 ± 0.02 | NA | NA | 2 | NA | NA | 156.5 | 3.226 | 3 | 182.3 | 4.839 | 3 | 5.02 | (Ambaye et al., 2020) |
| Sewage sludge | 550 | 9.5 ± 0.1 | 21.07 ± 0.02 | NA | NA | 0.5 | NA | NA | 156.5 | 4.839 | 3 | 166.9 | 2.42 | 3 | 2.17 | (Ambaye et al., 2020) |
| Sewage sludge | 550 | 9.5 ± 0.1 | 21.07 ± 0.02 | NA | NA | 1 | NA | NA | 156.5 | 4.839 | 3 | 188.7 | 3.225 | 3 | 6.26 | (Ambaye et al., 2020) |
| Sewage sludge | 550 | 9.5 ± 0.1 | 21.07 ± 0.02 | NA | NA | 1.5 | NA | NA | 156.5 | 4.839 | 3 | 208.9 | 4.032 | 3 | 9.41 | (Ambaye et al., 2020) |
| Sewage sludge | 550 | 9.5 ± 0.1 | 21.07 ± 0.02 | NA | NA | 2 | NA | NA | 156.5 | 4.839 | 3 | 196.8 | 4.032 | 3 | 7.25 | (Ambaye et al., 2020) |
| Sewage sludge | 350 | 6.4 ± 0.1 | 44.22 ± 0.02 | NA | NA | 0.5 | NA | NA | 156.5 | 6.14 | 3 | 233.3 | 4.386 | 3 | 11.5 | (Ambaye et al., 2020) |
| Sewage sludge | 350 | 6.4 ± 0.1 | 44.22 ± 0.02 | NA | NA | 1 | NA | NA | 156.5 | 6.14 | 3 | 227.2 | 4.386 | 3 | 10.6 | (Ambaye et al., 2020) |
| Sewage sludge | 350 | 6.4 ± 0.1 | 44.22 ± 0.02 | NA | NA | 1.5 | NA | NA | 156.5 | 6.14 | 3 | 214.9 | 3.509 | 3 | 9.34 | (Ambaye et al., 2020) |
| Sewage sludge | 350 | 6.4 ± 0.1 | 44.22 ± 0.02 | NA | NA | 2 | NA | NA | 156.5 | 6.14 | 3 | 207 | 4.384 | 3 | 7.57 | (Ambaye et al., 2020) |
| Sewage sludge | 550 | 9.5 ± 0.1 | 21.07 ± 0.02 | NA | NA | 0.5 | NA | NA | 146.5 | 4.386 | 3 | 166.7 | 4.386 | 3 | 3.68 | (Ambaye et al., 2020) |
| Sewage sludge | 550 | 9.5 ± 0.1 | 21.07 ± 0.02 | NA | NA | 1 | NA | NA | 146.5 | 4.386 | 3 | 194.7 | 3.509 | 3 | 9.71 | (Ambaye et al., 2020) |
| Sewage sludge | 550 | 9.5 ± 0.1 | 21.07 ± 0.02 | NA | NA | 1.5 | NA | NA | 146.5 | 4.386 | 3 | 211.4 | 4.385 | 3 | 11.8 | (Ambaye et al., 2020) |
| Sewage sludge | 550 | 9.5 ± 0.1 | 21.07 ± 0.02 | NA | NA | 2 | NA | NA | 146.5 | 4.386 | 3 | 185.1 | 5.263 | 3 | 6.37 | (Ambaye et al., 2020) |
| Sewage sludge | 350 | 6.4 ± 0.1 | 44.22 ± 0.02 | NA | NA | 0.5 | NA | NA | 162.2 | 4.196 | 3 | 274.5 | 3.148 | 3 | 24.2 | (Ambaye et al., 2020) |
| Sewage sludge | 350 | 6.4 ± 0.1 | 44.22 ± 0.02 | NA | NA | 1 | NA | NA | 162.2 | 4.196 | 3 | 227.3 | 4.196 | 3 | 12.4 | (Ambaye et al., 2020) |
| Sewage sludge | 350 | 6.4 ± 0.1 | 44.22 ± 0.02 | NA | NA | 1.5 | NA | NA | 162.2 | 4.196 | 3 | 210.49 | 3.146 | 3 | 10.4 | (Ambaye et al., 2020) |
| Sewage sludge | 350 | 6.4 ± 0.1 | 44.22 ± 0.02 | NA | NA | 2 | NA | NA | 162.2 | 4.196 | 3 | 202.1 | 3.147 | 3 | 8.61 | (Ambaye et al., 2020) |
| Sewage sludge | 550 | 9.5 ± 0.1 | 21.07 ± 0.02 | NA | NA | 0.5 | NA | NA | 155.9 | 3.147 | 3 | 172.7 | 3.147 | 3 | 4.27 | (Ambaye et al., 2020) |
| Sewage sludge | 550 | 9.5 ± 0.1 | 21.07 ± 0.02 | NA | NA | 1 | NA | NA | 155.9 | 3.147 | 3 | 222 | 5.245 | 3 | 12.2 | (Ambaye et al., 2020) |
| Sewage sludge | 550 | 9.5 ± 0.1 | 21.07 ± 0.02 | NA | NA | 1.5 | NA | NA | 155.9 | 3.147 | 3 | 204.2 | 2.098 | 3 | 14.4 | (Ambaye et al., 2020) |
| Sewage sludge | 550 | 9.5 ± 0.1 | 21.07 ± 0.02 | NA | NA | 2 | NA | NA | 155.9 | 3.147 | 3 | 189.5 | 2.098 | 3 | 10.1 | 9 |
| NA | NA | NA | NA | NA | NA | 20 | Methanosarcina | Methanosarcina | 0.0054 | 2E-04 | 3 | 0.0068 | 0.00024 | 3 | 5.60 | (Huang et al., 2020) |
| Vineyard prunings | NA | 1.59 ± 0.60 | NA | NA | NA | 10 | Methanosaeta | Methanobacterium | 10.89 | 0.21 | 3 | 14.27 | 0.28 | 3 | 10.9 | (Martinez et al., 2018) |
| Vineyard prunings | NA | 1.59 ± 0.60 | NA | NA | NA | 30 | Methanosaeta | Methanofollis | 10.89 | 0.21 | 3 | 14.15 | 0.28 | 3 | 10.5 | (Martinez et al., 2018) |
| Vineyard prunings | NA | 1.59 ± 0.60 | NA | NA | NA | 10 | Methanosaeta | Methanosphaerula | 18.73 | 0.37 | 3 | 23.13 | 0.46 | 3 | 8.43 | (Martinez et al., 2018) |
| Vineyard prunings | NA | 1.59 ± 0.60 | NA | NA | NA | 30 | Methanosaeta | Mathanolinea | 18.73 | 0.37 | 3 | 33.39 | 0.66 | 3 | 21.9 | (Martinez et al., 2018) |
| Vineyard prunings | NA | 1.59 ± 0.60 | NA | NA | NA | 10 | NA | NA | 14.35 | 0.28 | 3 | 66.34 | 1.15 | 3 | 49.7 | (Martinez et al., 2018) |
| Vineyard prunings | NA | 1.59 ± 0.60 | NA | NA | NA | 30 | NA | NA | 14.35 | 0.28 | 3 | 75.53 | 3.2 | 3 | 21.5 | (Martinez et al., 2018) |
| Wood pellet | NA | 9.4 ± 0.2 | NA | NA | NA | NA | Methanosaetaceae | NA | 1.4 | 0.1 | 2 | 1.6 | 0.04 | 2 | 1.50 | (Indren et al., 2020) |
| Wheat straw | NA | 10.2 ± 0.03 | NA | NA | NA | NA | Methanosaetaceae | NA | 1.4 | 0.1 | 2 | 1.2 | 0.1 | 2 | -1.14 | (Indren et al., 2020) |
| Sheep manure | NA | 11 ± 0.1 | NA | NA | NA | NA | Methanosaetaceae | NA | 1.4 | 0.1 | 2 | 1.2 | 0.1 | 2 | -1.14 | (Indren et al., 2020) |
| Dry dairy manure | 350 | NA | NA | 0.42–0.6 | 6.3 | 1 | NA | NA | 20.19 | 0.96 | 2 | 21.4 | 1.09 | 2 | 0.673 | (Jang et al., 2018) |
| Dry dairy manure | 350 | NA | NA | 0.42–0.6 | 6.3 | 10 | NA | NA | 20.19 | 0.96 | 2 | 24.32 | 1.12 | 2 | 2.26 | (Jang et al., 2018) |
| Dry dairy manure | 350 | NA | NA | 0.42–0.6 | 6.3 | 1 | NA | NA | 28.23 | 0.64 | 2 | 29.85 | 0.62 | 2 | 1.47 | (Jang et al., 2018) |
| Dry dairy manure | 350 | NA | NA | 0.42–0.6 | 6.3 | 10 | NA | NA | 28.23 | 0.64 | 2 | 37.35 | 0.67 | 2 | 7.96 | (Jang et al., 2018) |
| Dry dairy manure | 350 | NA | NA | 0.42–0.6 | 6.3 | 1 | NA | NA | 25.58 | 0.87 | 2 | 31.07 | 1.01 | 2 | 3.33 | (Jang et al., 2018) |
| Dry dairy manure | 350 | NA | NA | 0.42–0.6 | 6.3 | 10 | NA | NA | 25.58 | 0.87 | 2 | 38.49 | 1.44 | 2 | 6.20 | (Jang et al., 2018) |
| Corn stover | 500 | NA | NA | 841 to <74 | NA | NA | NA | NA | 620 | 10.39 | 3 | 611 | 46.76537 | 3 | -0.152 | (Achi et al., 2020) |
| Corn stover | 500 | NA | NA | 841 to <74 | NA | NA | NA | NA | 620 | 10.39 | 3 | 611 | 27.71281 | 3 | -0.246 | (Achi et al., 2020) |
| Douglas fir wood | 400 | 5.62 ± 0.01 | 46.8±1.9 | NA | 16.99 ± 0.58 | 10 | Methanothermobacter | Methanosaeta | 19.3 | 1.4 | 2 | 31 | 1.9 | 2 | 4.01 | (Wang et al., 2020b) |
| Douglas fir wood | 500 | 5.77 ± 0.00 | 49.9±1.2 | NA | 13.17 ± 4.05 | 10 | Methanothermobacter | Methanosarcina | 19.3 | 1.4 | 2 | 38 | 2.2 | 2 | 5.80 | (Wang et al., 2020b) |
| Douglas fir wood | 600 | 6.08 ± 0.04 | 51.2±5.7 | NA | 18.36 ± 2.61 | 10 | Methanothermobacter | Methanosarcina | 19.3 | 1.4 | 2 | 33.5 | 1.6 | 2 | 5.40 | (Wang et al., 2020b) |
| Douglas fir wood | 730 | 6.13 ± 0.08 | 63.6±3.4 | NA | 18.39 ± 0.29 | 10 | Methanothermobacter | Methanosarcina | 19.3 | 1.4 | 2 | 25.6 | 1.8 | 2 | 2.23 | (Wang et al., 2020b) |
| Douglas fir wood | 400 | 5.62 ± 0.01 | 46.8±1.9 | NA | 16.99 ± 0.58 | 10 | Methanothermobacter | Methanothermobacter | 3.9 | 1.8 | 2 | 7.4 | 0.5 | 2 | 1.51 | (Wang et al., 2020b) |
| Douglas fir wood | 500 | 5.77 ± 0.00 | 49.9±1.2 | NA | 13.17 ± 4.05 | 10 | Methanothermobacter | Methanobacterium | 3.9 | 1.8 | 2 | 6.7 | 0.2 | 2 | 1.25 | (Wang et al., 2020b) |
| Douglas fir wood | 600 | 6.08 ± 0.04 | 51.2±5.7 | NA | 18.36 ± 2.61 | 10 | Methanothermobacter | Methanobacterium | 3.9 | 1.8 | 2 | 6.8 | 1 | 2 | 1.14 | (Wang et al., 2020b) |
| Douglas fir wood | 730 | 6.13 ± 0.08 | 63.6±3.4 | NA | 18.39 ± 0.29 | 10 | Methanothermobacter | Methanothermobacter | 3.9 | 1.8 | 2 | 4 | 0.7 | 2 | 0.0418 | (Wang et al., 2020b) |
| Douglas fir wood | 400 | 5.62 ± 0.01 | 46.8±1.9 | NA | 16.99 ± 0.58 | 10 | Methanobrevibacter | Methanobrevibacter | 30.7 | 1.4 | 2 | 35.8 | 1.9 | 2 | 1.75 | (Wang et al., 2020b) |
| Douglas fir wood | 500 | 5.77 ± 0.00 | 49.9±1.2 | NA | 13.17 ± 4.05 | 10 | Methanothermobacter | Methanomassiliicoccus | 30.7 | 1.4 | 2 | 35.5 | 2.2 | 2 | 1.49 | (Wang et al., 2020b) |
| Douglas fir wood | 600 | 6.08 ± 0.04 | 51.2±5.7 | NA | 18.36 ± 2.61 | 10 | Methanothermobacter | Methanomassiliicoccus | 30.7 | 1.4 | 2 | 36.2 | 2.2 | 2 | 1.70 | (Wang et al., 2020b) |
| Douglas fir wood | 730 | 6.13 ± 0.08 | 63.6±3.4 | NA | 18.39 ± 0.29 | 10 | Methanothermobacter | Methanomassiliicoccus | 30.7 | 1.4 | 2 | 33.8 | 2.1 | 2 | 0.992 | (Wang et al., 2020b) |
| Douglas fir wood | 400 | 5.62 ± 0.01 | 46.8±1.9 | NA | 16.99 ± 0.58 | 10 | Methanothermobacter | Methanothermobacter | 17.6 | 1.6 | 2 | 25 | 2.8 | 2 | 4.44 | (Wang et al., 2020b) |
| Douglas fir wood | 500 | 5.77 ± 0.00 | 49.9±1.2 | NA | 13.17 ± 4.05 | 10 | Methanothermobacter | Methanothermobacter | 17.6 | 1.6 | 2 | 24.6 | 1 | 2 | 2.0487 | (Wang et al., 2020b) |
| Douglas fir wood | 600 | 6.08 ± 0.04 | 51.2±5.7 | NA | 18.36 ± 2.61 | 10 | Methanothermobacter | Methanothermobacter | 17.6 | 1.6 | 2 | 24.2 | 1.7 | 2 | 1.28 | (Wang et al., 2020b) |
| Douglas fir wood | 730 | 6.13 ± 0.08 | 63.6±3.4 | NA | 18.39 ± 0.29 | 10 | Methanothermobacter | Methanothermobacter | 17.6 | 1.6 | 2 | 22.6 | 1.9 | 2 | 0.723 | (Wang et al., 2020b) |
| Sewage sludge | 300 | 6.78 | 64.1 | NA | 21.3196 | 10 | Methanosaeta | NA | 111.4 | 0.87 | 3 | 132.1 | 4.775 | 3 | 4.83 | (Wu et al., 2019) |
| Sewage sludge | 500 | 7.5 | 27.4 | NA | 39.7573 | 10 | Methanosaeta | NA | 111.4 | 0.874 | 3 | 123.4 | 2.581 | 3 | 4.98 | (Wu et al., 2019) |
| Sewage sludge | 700 | 7.92 | 24.85 | NA | 31.7746 | 10 | Methanosaeta | NA | 111.4 | 0.874 | 3 | 114.7 | 0.735 | 3 | 3.27 | (Wu et al., 2019) |
| Cow manure | 500 | 8.5 | NA | 0.5–1.0 | 112.6 | 2 | Methanospirillum | Methanospirillum | 220.1 | 7.7 | 2 | 263.6 | 8.9 | 2 | 2.99 | (Sun et al., 2019) |
| Cow manure | 500 | 8.5 | NA | 0.5–1.0 | 112.6 | 6 | Methanospirillum | Methanospirillum | 220.1 | 7.7 | 2 | 341.5 | 3.6 | 2 | 11.5 | (Sun et al., 2019) |
| Cow manure | 500 | 8.5 | NA | 0.5–1.0 | 112.6 | 10 | Methanospirillum | Methanospirillum | 220.1 | 7.7 | 2 | 401.8 | 7.7 | 2 | 13.5 | (Sun et al., 2019) |
| Cow manure | 500 | 8.5 | NA | 0.5–1.0 | 112.6 | 14 | Methanospirillum | Methanospirillum | 220.1 | 7.7 | 2 | 358.1 | 4.2 | 2 | 12.7 | (Sun et al., 2019) |
| Cow manure | 500 | 8.5 | NA | 0.5–1.0 | 112.6 | 2 | Methanosaeta | Methanosaeta | 310.4 | 9.2 | 2 | 350 | 3.9 | 2 | 3.20 | (Sun et al., 2019) |
| Cow manure | 500 | 8.5 | NA | 0.5–1.0 | 112.6 | 6 | Methanosaeta | Methanosaeta | 310.4 | 9.2 | 2 | 391.8 | 5.5 | 2 | 6.14 | (Sun et al., 2019) |
| Cow manure | 500 | 8.5 | NA | 0.5–1.0 | 112.6 | 10 | Methanosaeta | Methanosaeta | 310.4 | 9.2 | 2 | 456.8 | 7.7 | 2 | 9.86 | (Sun et al., 2019) |
| Cow manure | 500 | 8.5 | NA | 0.5–1.0 | 112.6 | 14 | Methanosaeta | Methanosaeta | 310.4 | 9.2 | 2 | 416.9 | 8.9 | 2 | 6.72 | (Sun et al., 2019) |
| Corn straw | 400 | 8.2 | NA | NA | 29.8 | 8 | NA | NA | 117.2 | 8.244 | 3 | 184.2 | 9.178 | 3 | 6.14 | (Zhang et al., 2019) |
| Corn straw | 500 | 8.3 | NA | NA | 32.8 | 8 | NA | NA | 117.2 | 8.244 | 3 | 196.1 | 6.859 | 3 | 8.32 | (Zhang et al., 2019) |
| Corn straw | 600 | 8.3 | NA | NA | 56.6 | 8 | NA | NA | 117.2 | 8.244 | 3 | 218.4 | 9.352 | 3 | 9.18 | (Zhang et al., 2019) |
| Sewage sludge | 400 | 9.3 | NA | NA | 16.1 | 8 | NA | NA | 117.2 | 8.244 | 3 | 155.9 | 8.986 | 3 | 3.59 | (Zhang et al., 2019) |
| Sewage sludge | 500 | 9.5 | NA | NA | 18.9 | 8 | NA | NA | 117.2 | 8.244 | 3 | 207.6 | 8.092 | 3 | 8.85 | (Zhang et al., 2019) |
| Sewage sludge | 600 | 9.7 | NA | NA | 26.3 | 8 | NA | NA | 117.2 | 8.244 | 3 | 165.8 | 7.662 | 3 | 4.89 | (Zhang et al., 2019) |
| Coconut shell | 400 | 8.7 | NA | NA | 2.32 | 8 | NA | NA | 117.2 | 8.244 | 3 | 143.8 | 8.923 | 3 | 2.48 | (Zhang et al., 2019) |
| Coconut shell | 500 | 9.5 | NA | NA | 1.92 | 8 | NA | NA | 117.2 | 8.244 | 3 | 125.4 | 9.005 | 3 | 0.760 | (Zhang et al., 2019) |
| Coconut shell | 600 | 11.1 | NA | NA | 12.7 | 8 | NA | NA | 117.2 | 8.244 | 3 | 173.7 | 5.964 | 3 | 6.28 | (Zhang et al., 2019) |
| Corn straw | 600 | 8.3 | NA | NA | 56.6 | 6.2 | NA | NA | 126.9 | 1.997 | 3 | 149 | 3.472 | 3 | 6.24 | (Zhang et al., 2019) |
| Corn straw | 600 | 8.3 | NA | NA | 56.6 | 15.9 | NA | NA | 126.9 | 1.997 | 3 | 185.3 | 5.015 | 3 | 12.2 | (Zhang et al., 2019) |
| Corn straw | 600 | 8.3 | NA | NA | 56.6 | 26.1 | NA | NA | 126.9 | 1.997 | 3 | 199.2 | 5.016 | 3 | 15.2 | (Zhang et al., 2019) |
| Corn straw | 600 | 8.3 | NA | NA | 56.6 | 34.2 | NA | NA | 126.9 | 1.997 | 3 | 137.5 | 3.858 | 3 | 2.76 | (Zhang et al., 2019) |
| Sewage sludge | 600 | 9.7 | NA | NA | 26.3 | 6.2 | NA | NA | 126.9 | 1.997 | 3 | 140.2 | 4.659 | 3 | 2.97 | (Zhang et al., 2019) |
| Sewage sludge | 600 | 9.7 | NA | NA | 26.3 | 15.9 | NA | NA | 126.9 | 1.997 | 3 | 155.5 | 1.997 | 3 | 11.5 | (Zhang et al., 2019) |
| Sewage sludge | 600 | 9.7 | NA | NA | 26.3 | 26.1 | NA | NA | 126.9 | 1.997 | 3 | 168.5 | 3.661 | 3 | 11.3 | (Zhang et al., 2019) |
| Sewage sludge | 600 | 9.7 | NA | NA | 26.3 | 34.2 | NA | NA | 126.9 | 1.997 | 3 | 124.9 | 2.663 | 3 | -0.680 | (Zhang et al., 2019) |
| Coconut shell | 600 | 11.1 | NA | NA | 12.7 | 6.2 | NA | NA | 126.9 | 1.997 | 3 | 142.7 | 3.802 | 3 | 4.16 | (Zhang et al., 2019) |
| Coconut shell | 600 | 11.1 | NA | NA | 12.7 | 15.9 | NA | NA | 126.9 | 1.997 | 3 | 154.1 | 2.662 | 3 | 9.25 | (Zhang et al., 2019) |
| Coconut shell | 600 | 11.1 | NA | NA | 12.7 | 26.1 | NA | NA | 126.9 | 1.997 | 3 | 169.7 | 2.661 | 3 | 14.6 | (Zhang et al., 2019) |
| Coconut shell | 600 | 11.1 | NA | NA | 12.7 | 34.2 | NA | NA | 126.9 | 1.997 | 3 | 184.9 | 3.042 | 3 | 18.0 | (Zhang et al., 2019) |
| Bamboo biochar | NA | 8.42 ± 0.02 | 0.024 ± 0.002 | 2-3 | 54.5 | NA | NA | NA | 9.01 | 0.96 | 3 | 4.11 | 0.678 | 3 | -4.72 | (Mao et al., 2018) |
| Pine | 800 | NA | NA | 0.5–1 | 5.21 | NA | Methanothermobacter | Methanothermobacter | 9.11 | 0.53 | 3 | 7.06 | 0.66 | 3 | -2.74 | (Lu et al., 2019) |
| Pine | 800 | NA | NA | < 0.00 5 | 210.78 | NA | Methanolinea | Methanolinea | 9.11 | 0.53 | 3 | 9.55 | 0.53 | 3 | 0.664 | (Lu et al., 2019) |
| Pine | 800 | NA | NA | 0.5–1 | 5.21 | NA | Methanomicrobia | Methanomicrobia | 9.08 | 0.69 | 3 | 10.56 | 0.53 | 3 | 1.92 | (Lu et al., 2019) |
| Pine | 800 | NA | NA | < 0.00 5 | 210.78 | NA | Methanomicrobia | Methanomicrobia | 9.08 | 0.69 | 3 | 9.44 | 0.75 | 3 | 0.400 | (Lu et al., 2019) |
| Sawdust | 300 | 7.3 ± 0.1 | NA | 0.25–1 | 53.2 ± 2.8 | 15 | NA | NA | 115.9 | 2.362 | 3 | 159.7 | 2.362 | 3 | 14.8 | (Wang et al., 2020a) |
| Sawdust | 500 | 9.2 ± 0.1 | NA | 0.25–1 | 248.6 ± 3.5 | 15 | NA | NA | 115.9 | 2.362 | 3 | 168.7 | 5.196 | 3 | 10.5 | (Wang et al., 2020a) |
| Sawdust | 700 | 10.0 ± 0.2 | NA | 0.25–1 | 511.3 ± 3.8 | 15 | NA | NA | 115.9 | 2.362 | 3 | 150.7 | 1.89 | 3 | 13.0 | (Wang et al., 2020a) |
| Straw | 350–550 | NA | 143 | NA | NA | 1 | Methanosaetaceae | Methanobacteriaceae | 0.756 | 0.092 | 3 | 0.811 | 0.094 | 3 | 0.0744 | (Xiao et al., 2019) |
| Sludge | 500 | 8.01 ± 0.05 | 46.6 ± 2.8 | NA | NA | NA | Methanothermobacter | NA | 20.14 | 1.49 | 3 | 30.06 | 2.87 | 3 | 3.47 | (Yin et al., 2019) |
| Sawdust | 500 | 9.2 | NA | 0.25-1 | 248.6 | 2 | NA | NA | 6.7 | 0.1 | 2 | 8.7 | 0.2 | 2 | 7.23 | (Wang et al., 2018) |
| Sawdust | 500 | 9.2 | NA | 0.25-1 | 248.6 | 6 | NA | NA | 6.7 | 0.1 | 2 | 9.4 | 0.2 | 2 | 9.76 | (Wang et al., 2018) |
| Sawdust | 500 | 9.2 | NA | 0.25-1 | 248.6 | 10 | NA | NA | 6.7 | 0.1 | 2 | 8.2 | 0.2 | 2 | 5.42 | (Wang et al., 2018) |
| Sawdust | 500 | 9.2 | NA | 0.25-1 | 248.6 | 15 | Methanosaeta | Methanosaeta | 6.7 | 0.1 | 2 | 7.8 | 0.2 | 2 | 3.98 | (Wang et al., 2018) |
| Red spruce woodchips | NA | 8.4 | NA | NA | 327 | NA | NA | NA | 486.9 | 13.12 | 3 | 640.6 | 16.88 | 3 | 8.13 | (Mainardis et al., 2019) |
| Red spruce woodchips | NA | 8.4 | NA | NA | 327 | NA | NA | NA | 291 | 7.693 | 3 | 402.6 | 8.974 | 3 | 10.7 | (Mainardis et al., 2019) |
| Pine biochar | NA | NA | NA | NA | 310.19 | NU | NA | NA | 72.45 | 1.11 | 3 | 82.9 | 0.28 | 3 | 10.3 | (Mainardis et al., 2019) |
| Pine biochar | NA | NA | NA | NA | 310.19 | NU | NA | NA | 72.45 | 1.11 | 3 | 71.35 | 1.19 | 3 | -0.765 | (Shen et al., 2016) |
| White oak biochar | NA | NA | NA | NA | 296.81 | NU | NA | NA | 72.45 | 1.11 | 3 | 83.22 | 0.28 | 3 | 10.6 | (Shen et al., 2016) |
| White oak biochar | NA | NA | NA | NA | 296.81 | NU | NA | NA | 72.45 | 1.11 | 3 | 79.41 | 1.27 | 3 | 4.67 | (Shen et al., 2016) |
| Pine biochar | NA | NA | NA | NA | 310.19 | NU | NA | NA | 101.8 | 6.46 | 3 | 107.1 | 3.35 | 3 | 0.824 | (Shen et al., 2016) |
| Pine biochar | NA | NA | NA | NA | 310.19 | NU | NA | NA | 101.8 | 6.46 | 3 | 103.9 | 2.81 | 3 | 0.337 | (Shen et al., 2016) |
| White oak biochar | NA | NA | NA | NA | 296.81 | NU | NA | NA | 101.8 | 6.46 | 3 | 106.1 | 3.59 | 3 | 0.658 | (Shen et al., 2016) |
| White oak biochar | NA | NA | NA | NA | 296.81 | NU | NA | NA | 101.8 | 6.46 | 3 | 101.5 | 3.04 | 3 | -0.0475 | (Shen et al., 2016) |
| Wheat bran pellets | 800 | NA | 49900 | 1.7–2 | 55 ± 1 | 25 | Methanosarcina | Methanosarcina | 14.154 | 4.001 | 2 | 58.308 | 2.308 | 2 | 4.17 | (Viggi et al., 2017) |
| Coppiced woodlands | 500 | NA | 1600 | 1.7–2 | 61 ± 1 | 25 | Methanosarcina | Methanosarcina | 14.154 | 4.001 | 2 | 66.923 | 2.461 | 2 | 4.28 | (Viggi et al., 2017) |
| Orchard pruning | 500 | NA | 500 | 1.7–2 | 13.7 ± 0.5 | 25 | Methanosarcina | Methanosarcina | 14.154 | 4.001 | 2 | 72.154 | 1.539 | 2 | 4.12 | (Viggi et al., 2017) |

Notes: 1, NA, not available; 2, Not used; 3, The predominant methanogens; 4, Methanogens with the highest increase in abundance. These paired measurements of control and biochar-amended treatments was in duplicate with a gray background.

References

Achi C, Hassanein A, Lansing S (2020) Enhanced Biogas Production of Cassava Wastewater Using Zeolite and Biochar Additives and Manure Co-Digestion. Energies 13:491.

Ambaye T, Rene E, Dupont C, Wongrod S, van Hullebusch E (2020) Anaerobic Digestion of Fruit Waste   Mixed With Sewage Sludge Digestate Biochar: Influence on Biomethane Production. Front Energy R   es 8:

Cai J, He P, Wang Y, Shao L, Lu F (2016) Effects and optimization of the use of biochar in anaerobic digestion of food wastes. Waste Manage Res 34:409-416.

Cheng Q, de los Reyes F, Call D (2018) Amending anaerobic bioreactors with pyrogenic carbonaceous materials: the influence of material properties on methane generation. Environ Sci-Wat Res 4:1794-1806.

Huang J, Ma K, Xia X, Gao K, Lu Y (2020) Biochar and magnetite promote methanogenesis during anaerobic decomposition of rice straw. Soil Biol Biochem 143, 107740.

Indren M, Birzer C, Kidd S, Hall T, Medwell P (2020) Effects of biochar parent material and microbial pre-loading in biochar-amended high-solids anaerobic digestion. Bioresour. Technol 298, 122457.

Jang H, Choi Y, Kan E (2018) Effects of dairy manure-derived biochar on psychrophilic, mesophilic and   thermophilic anaerobic digestions of dairy manure. Bioresour. Technol 250:927-931.

Li Q, Xu M, Wang G, Chen R, Qiao W, Wang X. (2018) Biochar assisted thermophilic co-digestion of food waste and waste activated sludge under high feedstock to seed sludge ratio in batch experiment. Bioresour. Technol 249:1009-1016.

Lu F, Liu Y, Shao L, He, P (2019) Powdered biochar doubled microbial growth in anaerobic digestion  of oil. Appl Energ 247:605-614.

Luo C, Lu F, Shao L, He P (2015) Application of eco-compatible biochar in anaerobic digestion to relieve acid stress and promote the selective colonization of functional microbes (vol 68, pg 710, 2014). Water Res 70:496-496.

Mainardis M, Flaibani S, Mazzolini F, Peressotti A, Goi D (2019) Techno-economic analysis of anaerobic digestion implementation in small Italian breweries and evaluation of biochar and granular activated carbon addition effect on methane yield. J Environ Chem Eng 7, 103184.

Mao H, Lv Z, Sun H, Li R, Zhai B, Wang Z, Awasthi M, Wang Q, Zhou L (2018) Improvement of biochar and bacterial powder addition on gaseous emission and bacterial community in pig manure compost. Bioresour. Technol 258:195-202.

Martinez E, Rosas J, Sotres A, Moran A, Cara J, Sanchez M, Gomez X (2018) Codigestion of sludge and citrus peel wastes: Evaluating the effect of biochar addition on microbial communities. Biochem Eng J 137: 314-325.

Paritosh K, Vivekanand V (2019) Biochar enabled syntrophic action: Solid state anaerobic digestion of agricultural stubble for enhanced methane production. Bioresour. Technol 289, 121712.

Shanmugam S, Adhikari S, Nam H, Sajib S (2018) Effect of bio-char on methane generation from glucose and aqueous phase of algae liquefaction using mixed anaerobic cultures. Biomass Bioenerg 108:479-486.

Shen Y, Linville J, Ignacio-de Leon P, Schoene R, Urgun-Demirtas M (2016) Towards a sustainable paradigm of waste-to-energy process: Enhanced anaerobic digestion of sludge with woody biochar. J Clean Prod 135:1054-1064.

Sun C, Liu F, Song Z, Wang J, Li Y, Pan Y, Sheng T, Li L (2019) Feasibility of dry anaerobic digestion of beer lees for methane production and biochar enhanced performance at mesophilic and thermophilic temperature. Bioresour. Technol 276:65-73.

Sunyoto N, Zhu M, Zhang Z, Zhang D (2016) Effect of biochar addition on hydrogen and methane production in two-phase anaerobic digestion of aqueous carbohydrates food waste. Bioresour. Technol 219:29-36.

Viggi C, Simonetti S, Palma E, Pagliaccia P, Braguglia C, Fazi S, Baronti S, Navarra M, Pettiti I, Koch C, Harnisch F,  Aulenta F (2017) Enhancing methane production from food waste fermentate using biochar: the added value of electrochemical testing in pre-selecting the most effective type of biochar. Biotechnol Biofuels 10, 303.

Wang G, Li Q, Gao X, Wang X (2018) Synergetic promotion of syntrophic methane production from anaerobic digestion of complex organic wastes by biochar: Performance and associated mechanisms. Bioresour. Technol 250:812-820.

Wang G, Li Q, Li Y, Xing Y, Yao G, Liu Y, Chen R, Wang X (2020a) Redox-active biochar facilitates potential electron tranfer between syntrophic partners to enhance anaerobic digestion under high organic loading rate. Bioresour. Technol 298, 122524.

Wang P, Peng H, Adhikari S, Higgins B, Roy P, Dai W, Shi X (2020b) Enhancement of biogas production from wastewater sludge via anaerobic digestion assisted with biochar amendment. Bioresour. Technol 309, 123368.

Wu B, Yang Q, Yao F, Chen S, He L, Hou K, Pi Z, Yin H, Fu J, Wang D, Li X (2019) Evaluating the effect of biochar on mesophilic anaerobic digestion of waste activated sludge and microbial diversity. Bioresour. Technol 294, 122235.

Xiao L, Sun R, Zhang P, Zheng S, Tan Y, Li J, Zhang Y, Liu, F (2019) Simultaneous intensification of direct acetate cleavage and CO2 reduction to generate methane by bioaugmentation and increased electron transfer. Chem Eng J 378, 122229.

Yin C, Shen Y, Yuan R, Zhu N, Yuan H, Lou Z (2019) Sludge-based biochar-assisted thermophilic anaerobic digestion of waste-activated sludge in microbial electrolysis cell for methane production. Bioresour. Technol 284:315-324.

Yuan H, Ding L, Zama E, Liu P, Hozzein W, Zhu Y (2018) Biochar Modulates Methanogenesis through Electron Syntrophy of Microorganisms with Ethanol as a Substrate. Environ Sci Technol 52:12198-12207.

Zhang M, Li J, Wang Y, Yang C (2019) Impacts of different biochar types on the anaerobic digestion of sewage sludge. Rsc Adv 9(72): 42375-42386.