Electronic Supplementary Information (ESI)

# Supramolecular architecture of a novel non-centrosymmetric heteromolybdate hybrid for nonlinear optical applications: structure, characterization, stability study and DFT calculations

Malek Djeribi1, Ichraf Nagazi 1*, Necmi Dege 2, Noureddine Issaoui3, Amor Haddad 4

1 Laboratory of Physico-chemistry of Materials LR01ES19, University of Monastir, Faculty of Sciences of Monastir, 5019 Monastir, Tunisia.

2 Faculty of Arts and Sciences, Department of Physics, Ondokuz Mayıs University, 55139 Samsun, Turkey.

3Laboratory of Quantum and Statistical Physics (LR18ES18), University of Monastir, Faculty of Sciences of Monastir, 5019 Monastir, Tunisia.

4Higher Institute of Applied Sciences and Technology of Mahdia, University of Monastir, Mahdia, Tunisia.

*Corresponding author: ichrafnagazi@gmail.com

Table Captions:

Table S1 Reduced atomic coordinates and equivalent isotropic thermal displacement parameters of compound (I)

Table S2 Bond valence sums (Σs) for compound (I)

Table S3 Experimental conditions of solutions

Table S4 Electrochemical response of compound (I) at different electrolytic solutions

Table S5 Calculated electric dipole moment μ (D) the average polarizability αtot (× 10-24 esu) and the first hyperpolarizability βtot (× 10-33 esu) for compound (I)

Table S6 Topological parameters of compound (I) calculated at DFT/B3LYP/ LANL2DZ

Table S1 Reduced atomic coordinates and equivalent isotropic thermal displacement parameters of compound (I)

|  | x | y | z | Uiso*/Ueq | Occ. (<1) |
| --- | --- | --- | --- | --- | --- |
| Mo1 | 0.47758 (4) | 0.48305 (3) | 0.41043 (2) | 0.02508 (10) |  |
| Mo2 | 0.33267 (4) | 0.32946 (3) | 0.51068 (2) | 0.02454 (10) |  |
| Mo3 | 0.66208 (5) | 0.65148 (3) | 0.50824 (2) | 0.02643 (10) |  |
| Mo4 | 0.36300 (5) | 0.41608 (3) | 0.65801 (2) | 0.03003 (11) |  |
| Mo5 | 0.54111 (6) | 0.62499 (3) | 0.65313 (2) | 0.03638 (13) |  |
| Se1 | 0.32646 (5) | 0.59937 (3) | 0.53707 (2) | 0.02537 (11) |  |
| Se2 | 0.62951 (5) | 0.40407 (4) | 0.55885 (2) | 0.02754 (11) |  |
| O1 | 0.3397 (4) | 0.3954 (3) | 0.43227 (16) | 0.0285 (8) |  |
| O2 | 0.3828 (4) | 0.3132 (2) | 0.59880 (18) | 0.0315 (8) |  |
| O3 | 0.4791 (4) | 0.6164 (3) | 0.55808 (16) | 0.0278 (8) |  |
| O4 | 0.6034 (4) | 0.7666 (3) | 0.49306 (19) | 0.0340 (9) |  |
| O5 | 0.5115 (3) | 0.4101 (3) | 0.50521 (16) | 0.0265 (7) |  |
| O6 | 0.3866 (4) | 0.5568 (3) | 0.67100 (18) | 0.0345 (9) |  |
| O7 | 0.5934 (4) | 0.5801 (3) | 0.43870 (17) | 0.0315 (8) |  |
| O8 | 0.6793 (5) | 0.6607 (3) | 0.60008 (17) | 0.0396 (10) |  |
| O9 | 0.3419 (4) | 0.5894 (3) | 0.46077 (16) | 0.0290 (8) |  |
| O10 | 0.5753 (4) | 0.3992 (3) | 0.37749 (19) | 0.0377 (9) |  |
| O11 | 0.8122 (4) | 0.6670 (3) | 0.4864 (2) | 0.0403 (10) |  |
| O12 | 0.1761 (4) | 0.3127 (3) | 0.5140 (2) | 0.0364 (9) |  |
| O13 | 0.4144 (4) | 0.5386 (3) | 0.3463 (2) | 0.0365 (9) |  |
| O14 | 0.3000 (4) | 0.4781 (3) | 0.56032 (17) | 0.0286 (8) |  |
| O15 | 0.7223 (4) | 0.4938 (3) | 0.5336 (2) | 0.0340 (9) |  |
| O16 | 0.2091 (5) | 0.4083 (3) | 0.6765 (2) | 0.0450 (11) |  |
| O17 | 0.5632 (4) | 0.4570 (3) | 0.62362 (18) | 0.0325 (9) |  |
| O18 | 0.3884 (4) | 0.2132 (3) | 0.49123 (19) | 0.0338 (8) |  |
| O19 | 0.4345 (5) | 0.3670 (3) | 0.7222 (2) | 0.0473 (12) |  |
| O20 | 0.6306 (5) | 0.5943 (4) | 0.7162 (2) | 0.0532 (13) |  |
| O21 | 0.4821 (6) | 0.7402 (3) | 0.6706 (2) | 0.0559 (15) |  |
| N1 | 0.4791 (5) | 0.0845 (3) | 0.5785 (2) | 0.0339 (10) |  |
| H1 | 0.464 (7) | 0.129 (4) | 0.551 (2) | 0.041* |  |
| N2 | 0.5124 (5) | −0.0513 (3) | 0.6545 (2) | 0.0322 (10) |  |
| H2 | 0.504 (7) | −0.097 (4) | 0.682 (2) | 0.039* |  |
| N3 | 0.8836 (7) | 0.6682 (5) | 0.6721 (3) | 0.0583 (17) |  |
| H3 | 0.828 (6) | 0.645 (5) | 0.647 (3) | 0.050* |  |
| N4 | 1.0825 (7) | 0.7164 (7) | 0.7230 (3) | 0.071 (2) |  |
| H4 | 1.152 (5) | 0.736 (7) | 0.738 (4) | 0.085* |  |
| C1 | 0.3767 (6) | −0.0277 (5) | 0.6521 (3) | 0.0393 (13) |  |
| H1A | 0.347653 | −0.007942 | 0.693162 | 0.047* |  |
| H1B | 0.330273 | −0.086160 | 0.639108 | 0.047* |  |
| C2 | 0.3570 (6) | 0.0568 (5) | 0.6058 (3) | 0.0451 (15) |  |
| H2A | 0.300515 | 0.035690 | 0.573109 | 0.054* |  |
| H2B | 0.320777 | 0.113938 | 0.626874 | 0.054* |  |
| C3 | 0.5862 (7) | 0.0370 (5) | 0.6741 (3) | 0.0408 (14) |  |
| H3A | 0.673757 | 0.019886 | 0.675531 | 0.049* |  |
| H3B | 0.560754 | 0.058051 | 0.715494 | 0.049* |  |
| C4 | 0.5652 (6) | 0.1213 (4) | 0.6276 (3) | 0.0357 (13) |  |
| H4A | 0.529347 | 0.178585 | 0.648585 | 0.043* |  |
| H4B | 0.643569 | 0.141255 | 0.609076 | 0.043* |  |
| C5 | 0.5546 (6) | −0.0867 (4) | 0.5920 (3) | 0.0412 (14) |  |
| H5A | 0.507719 | −0.145378 | 0.579811 | 0.049* |  |
| H5B | 0.641967 | −0.104406 | 0.593592 | 0.049* |  |
| C6 | 0.5344 (7) | −0.0039 (4) | 0.5452 (3) | 0.0409 (14) |  |
| H6A | 0.612959 | 0.014619 | 0.526220 | 0.049* |  |
| H6B | 0.478683 | −0.026295 | 0.512482 | 0.049* |  |
| C7 | 0.8586 (8) | 0.7486 (5) | 0.7175 (4) | 0.0562 (19) |  |
| H7A | 0.795179 | 0.727674 | 0.746890 | 0.067* |  |
| H7B | 0.829464 | 0.807837 | 0.696027 | 0.067* |  |
| C8 | 0.9783 (8) | 0.7706 (8) | 0.7514 (4) | 0.068 (2) |  |
| H8A | 0.994789 | 0.841709 | 0.749998 | 0.082* |  |
| H8B | 0.970223 | 0.751180 | 0.794851 | 0.082* |  |
| C9 | 0.9340 (17) | 0.5814 (7) | 0.7070 (7) | 0.125 (7) |  |
| H9B | 0.939785 | 0.524005 | 0.679580 | 0.150* |  |
| H9A | 0.879071 | 0.564673 | 0.741330 | 0.150* |  |
| C10 | 1.0612 (16) | 0.6081 (10) | 0.7316 (6) | 0.128 (7) |  |
| H10A | 1.066652 | 0.591367 | 0.775611 | 0.154* |  |
| H10B | 1.124313 | 0.570520 | 0.709443 | 0.154* |  |
| C11 | 0.9725 (10) | 0.7021 (8) | 0.6238 (4) | 0.071 (3) |  |
| H11A | 0.936112 | 0.755956 | 0.599654 | 0.086* |  |
| H11B | 0.991675 | 0.647619 | 0.595618 | 0.086* |  |
| C12 | 1.0905 (8) | 0.7381 (8) | 0.6556 (4) | 0.070 (3) |  |
| H12A | 1.162132 | 0.704544 | 0.637844 | 0.083* |  |
| H12B | 1.100402 | 0.809312 | 0.649222 | 0.083* |  |
| OW1 | 0.9814 (10) | 0.4027 (9) | 0.6098 (4) | 0.132 (4) |  |
| HW1A | 0.958 (14) | 0.358 (10) | 0.584 (7) | 0.198* |  |
| HW1B | 1.057 (6) | 0.393 (13) | 0.621 (8) | 0.198* |  |
| OW3 | 0.3024 (14) | 0.7223 (16) | 0.7634 (8) | 0.073 (5) | 0.4 |
| HW3A | 0.364 (13) | 0.729 (11) | 0.738 (8) | 0.050* | 0.4 |
| HW3B | 0.276 (16) | 0.662 (6) | 0.762 (9) | 0.050* | 0.4 |
| OW4 | 0.835 (3) | 0.279 (2) | 0.6469 (11) | 0.062 (7) | 0.2 |
| HW4A | 0.81 (4) | 0.25 (3) | 0.615 (13) | 0.093* | 0.2 |
| HW4B | 0.89 (4) | 0.24 (3) | 0.667 (18) | 0.093* | 0.2 |
| OW2A | 0.6927 (16) | 0.3161 (16) | 0.7298 (10) | 0.124 (6) | 0.6 |
| HWA1 | 0.65 (3) | 0.285 (19) | 0.756 (13) | 0.186* | 0.6 |
| HWA2 | 0.75 (2) | 0.278 (18) | 0.713 (13) | 0.186* | 0.6 |
| OW2B | 0.7782 (18) | 0.3918 (15) | 0.6982 (8) | 0.086 (5) | 0.4 |
| HWB1 | 0.745 (4) | 0.356 (3) | 0.6702 (15) | 0.129* | 0.4 |
| HWB2 | 0.83 (2) | 0.435 (17) | 0.683 (4) | 0.129* | 0.4 |

Table S2 Bond valence sums (Σs) for compound (I)

| Atomes | Mo1 | Mo2 | Mo3 | Mo4 | Mo5 | Se1 | Se2 | calSi |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| O1 | 0.892 | 1.021 |  |  |  |  |  | 1.913 |
| O2 |  | 0.831 |  | 1.061 |  |  |  | 1.892 |
| O3 |  |  | 0.358 |  | 0.525 | 1.283 |  | 2.166 |
| O4 |  |  | 1.757 |  |  |  |  | 1.757 |
| O5 | 0.362 | 0.442 |  |  |  |  | 1.299 | 2.103 |
| O6 |  |  |  | 0.956 | 0.929 |  |  | 1.885 |
| O7 | 1.019 |  | 0.969 |  |  |  |  | 1.988 |
| O8 |  |  | 0.821 |  | 0.938 |  |  | 1.759 |
| O9 | 0.339 |  |  |  |  | 1.553 |  | 1.892 |
| O10 | 1.782 |  |  |  |  |  |  | 1.782 |
| O11 |  |  | 1.779 |  |  |  |  | 1.779 |
| O12 |  | 1.747 |  |  |  |  |  | 1.747 |
| O13 | 1.727 |  |  |  |  |  |  | 1.724 |
| O14 |  | 0.359 |  | 0.301 |  | 1.268 |  | 1.928 |
| O15 |  |  | 0.368 |  |  |  | 1.530 | 1.898 |
| O16 |  |  |  | 1.728 |  |  |  | 1.728 |
| O17 |  |  |  | 0.309 | 0.301 |  | 1.301 | 1.911 |
| O18 |  | 1.654 |  |  |  |  |  | 1.654 |
| O19 |  |  |  | 1.717 |  |  |  | 1.717 |
| O20 |  |  |  |  | 1.709 |  |  | 1.709 |
| O21 |  |  |  |  | 1.696 |  |  | 1.696 |
| calSi | 6.120 | 6.054 | 6.052 | 6.072 | 6.098 | 4.104 | 4.130 |
| thSi | +6 | +6 | +6 | +6 | +6 | +4 | +4 |

Table S3 Experimental conditions of solutions

|  | S 1 | S 2 : buffer solution | S 3 |
| --- | --- | --- | --- |
| Solution | H2O | (0.5 M Na2SO4 + H2SO4) | 1M H2SO4 |
| pH | 5 | 3 | 1 |
| Concentration | 8.10-6 mol. L-1 | 8.10-6 mol. L-1 | 8.10-6 mol. L-1 |

Table S4 Electrochemical response of compound (I) at different electrolytic solutions

| pH | Electrolytic solution | Epa(V) | Epc(V) | E0' = (Epa + Epc)/2 |
| --- | --- | --- | --- | --- |
| 1 | 1M H2SO4 | 1.045 | 0.5 | 0.772 |
| 3 | (0.5 M Na2SO4 + H2SO4) | 0.844 | 0.180 | 0.512 |
| 5 | (1 M CH3COONa + CH3COOH) | 0.729 | 0.067 | 0.400 |

Table S5 Calculated electric dipole moment μ (D) the average polarizability αtot (× 10-24 esu) and the first hyperpolarizability βtot (× 10-33 esu) for compound (I)

| Parameter | Values | Parameter | Values |
| --- | --- | --- | --- |
| μx | -11.8310 | βxxx | 4146.3948187 |
| μy | 60.2234 | βxxy | 2964.0079563 |
| μz | -16.6708 | βxyy | 4420.7534101 |
| μ (D) | 63.599659 | βyyy | 7283.9614109 |
| αxx | 796.5338965 | βxxz | 3001.3949545 |
| αxy | 561.2252311 | βxyz | 589.0028212 |
| αyy | 1334.5262672 | βyyz | -525.8699205 |
| αxz | 114.0051112 | βxzz | 302.3817065 |
| αyz | 148.1365346 | βyzz | -854.0567445 |
| αzz | 515.1105757 | βzzz | -844.8745558 |
| αtot (esu) | 1.30720×10-22 | βtot (esu) | 1.125011 10-28 |

However, α and β values of the Gaussian output are in atomic units (a.u.), so they have been converted into electronic units (esu) ) (α; 1 a.u. = 0.1482×10−24 esu, β; 1 a.u. = 8.6393×10−33 esu).

Table S6 Topological parameters of compound (I) calculated at DFT/B3LYP/ LANL2DZ.

| BCP | ρ(r) (a.u) | Δ2ρ(r) (a.u) | G(r) (a.u) | H(r) (a.u) | V (r) (a.u) | ¦EO...H¦ (kcal/mol) |
| --- | --- | --- | --- | --- | --- | --- |
| 88 | 0.05376 | 0.25142 | 0.06412 | -0.0012769 | -0.065397 |  |
| 89 | 0.055040 | 0.27019 | 0.068627 | -0.0010926 | -0.069719 |  |
| 90 | 0.054692 | 0.27644 | 0.070101 | -0.0010038 | -0.07110 |  |
| 91 | 0.056922 | 0.25989 | 0.066759 | -0.0018015 | -0.068561 |  |
| 92 | 0.079707 | 0.37502 | 0.10143 | -0.77204 | -0.10915 |  |
| 93 | 0.01021 | 0.03851 | 0.008562 | 0.001065 | -0.007497 |  |
| 94 | 0.049204 | 0.22563 | 0.057038 | -0.0006392 | -0.057678 |  |
| 95 | 0.05744 | 0.27482 | 0.070624 | -0.0019324 | -0.072556 |  |
| 96 | 0.067379 | 0.33023 | 0.08648 | -0.0039529 | -0.090439 |  |
| 97 | 0.003831 | 0.01564 | 0.003831 | 0.0009543 | -0.002003 |  |
| 98 | 0.04863 | 0.22465 | 0.056942 | -0.0007878 | -0.05772 |  |
| 99 | 0.03147 | 0.1302 | 0.03116 | 0.001394 | -0.02977 | 9.332 |
| 100 | 0.050019 | 0.23595 | 0.059807 | -0.0008302 | -0.06063 |  |
| 101 | 0.007793 | 0.03324 | 0.006467 | 0.001845 | -0.004622 | 1.449 |
| 102 | 0.03115 | 0.1271 | 0.03041 | 0.001369 | -0.0290 | 9.091 |
| 103 | 0.005074 | 0.02080 | 0.003946 | 0.001254 | -0.002692 | 0.844 |
| 104 | 0.006298 | 0.02588 | 0.005005 | 0.001466 | -0.003538 | 1.109 |
| 105 | 0.003112 | 0.01170 | 0.002334 | 0.005905 | -0.001744 |  |
| 106 | 0.01080 | 0.03970 | 0.008713 | 0.001211 | -0.007502 | 2.352 |
| 107 | 0.007433 | 0.03146 | 0.006127 | 0.001737 | -0.004389 | 1.376 |
| 108 | 0.006904 | 0.02928 | 0.005852 | 0.001467 | -0.004385 | 1.375 |
| 109 | 0.002292 | 0.07470 | 0.001320 | 0.0005467 | -0.0007740 | 0.243 |
| 110 | 0.007095 | 0.02599 | 0.005175 | 0.001318 | -0.003857 |  |
| 111 | 0.009688 | 0.04229 | 0.008546 | 0.002027 | -0.006518 |  |
| 112 | 0.01376 | 0.06682 | 0.01399 | 0.002710 | -0.01128 |  |
| 113 | 0.01331 | 0.06250 | 0.01290 | 0.002725 | -0.01017 | 3.188 |
| 115 | 0.004555 | 0.01902 | 0.003437 | 0.001319 | -0.002118 |  |
| 117 | 0.01712 | 0.02242 | 0.002242 | -0.001994 | -0.009595 |  |

1 a.u. of energy = 2625 kJ/mol