Synthesis, characterization and application of double network hydrogels with superior ultraviolet resistance and antioxidant properties constructed from oligomeric proanthocyanidins and poly(vinyl alcohol)/sodium alginate

Jie Songa,b&Shuyu Zhanga,b ,Liuping Dua,b, Chong Gaob, Longyue Xieb, Yu Shic, Ling Su*d, Yanli Maa,b Shixue Ren*a,b

&These authors contributed equally to this work and should be considered co-first authors.

aKey Laboratory of Bio-based Material Science & Technology(Northeast Forestry University) Ministry of Education, Harbin 150040, China

bCollege of Material Science and Engineering

Northeast Forestry University,Harbin, P.R.China 150040

cCollege of engineering and technology

Northeast Forestry University,Harbin, P.R.China 150040

dYantai Vocational College, Yantai City, P.R.China 264670

- Mail

Jie Song: sj18846799984@163.com

Shuyu Zhang: zhangshuyusy@163.com

Liuping Du: dlp188461719512022@163.com

Chong Gao: g1635758204s@163.com

Longyue Xie: xlyxvn@163.com

Yu Shi: tubage_0744_sy@126.com

Ling Su: sulingling2007@163.com

Yanli Ma: myl219@126.com

Shixue Ren: renshixue@nefu.edu.cn

*Correspondence: renshixue@nefu.edu.cn (shixue, Ren)

Table S1

Table 1: Tensile properties of different OPCs-PVA/SA hydrogels

| Concentration of OPCs (%) | 0 | 0.5 | 1 | 3 | 5 | 10 |
| --- | --- | --- | --- | --- | --- | --- |
| Tensile strength (MPa) | 0.011 | 0.040 | 0.019 | 0.018 | 0.020 | 0.024 |
| Elongation at break (%) | 117.95 | 131.67 | 138.46 | 151.26 | 139.51 | 166.83 |

Table S2

Table 2: Compressive strength of different OPCs-PVA/SA hydrogel specimens

| Concentration of OPCs (%) | 0 | 0.5 | 1 | 3 | 5 | 10 |
| --- | --- | --- | --- | --- | --- | --- |
| Compressive strength (MPa) | 0.215 | 0.943 | 0.558 | 1.356 | 1.346 | 1.353 |