ZIF-67 derived 2D porous carbon nanosheets decorated with Co nanoflakes as bifunctional electrocatalysts toward effective overall water splitting

Ru Liu1, Haixia Zhang1*, Yanhui Song1, Peizhi Liu1, Bingshe Xu1,2, Jianguo Liang3*, Junjie Guo1*

1 Key Laboratory of Interface Science and Engineering in Advanced Materials Ministry of Education, College of Materials Science and Engineering, Taiyuan University of Technology, Taiyuan 030024, Shanxi, China.

2 Materials Institute of Atomic and Molecular Science, Shaanxi University of Science & Technology, Xi'An 710021, Shaanxi, China.

3 College of Mechanical and Vehicle Engineering, Taiyuan University of Technology, Taiyuan 030024, Shanxi, China.

*Corresponding Authors E-mails: zhanghaixia@tyut.edu.cn (H.X. Zhang)

liangjianguo20@tyut.edu.cn (G.J. Liang)

guojunjie@tyut.edu.cn (J.J. Guo)

Fig. S1 (a) XRD patterns and (b) XPS survey spectra of Co(OH)2/CC and ZIF-67/CC; High-resolution spectra (c) Co(OH)2/CC and (d) ZIF-67/CC

Fig. S2 CV curves of OER within a non-faradaic reaction region of 1.09～1.19 V versus RHE at different scan rates for (a) Co(OH)2/CC; (b) ZIF-67/CC; (c) Co@NC/CC-400; (d) Co@NC/CC-500; (e) Co@NC/CC-600 and (f) RuO2

Fig. S3 CV curves of HER within a non-faradaic reaction region of 0.14～0.24 V versus RHE at different scan rates for (a) Co(OH)2/CC; (b) ZIF-67/CC; (c) Co@NC/CC-400; (d) Co@NC/CC-500; (e) Co@NC/CC-600 and (f) Pt/C

Table 1 Summary of non-precious metal carbon-based electrocatalysts for OER

| Material | Electrolyte | η10 (mV) | Tafel slop (mV dec-1) | Stability (h) | Ref. |
| --- | --- | --- | --- | --- | --- |
| Co@CoNx/NCT | 1.0 M KOH | 290 | 60 | 2000 cycles | [1] |
| CoCuNCNT@PC-700-2 | 1.0 M KOH | 340 | 109 | 24 | [2] |
| Co–N/PC@CNT | 1.0 M KOH | 430 | 89 | 1000 cycles | [3] |
| Fe-Co-CN/rGO | 1.0 M KOH | 308 | 38 | 45 | [4] |
| Co-NC/CNT | 1.0 M KOH | 284 | 78 | 8.4 | [5] |
| Co/Mn-ZIF@Fe-Co-Mn | 1.0 M KOH | 270 | 78 | 10 | [6] |
| Co-N-PHCNTs | 1.0 M KOH | 390 | 63.8 | 2000 cycles | [7] |
| NiCoPO/NC | 1.0 M KOH | 300 | 94 | 10 | [8] |
| Co/ CNT/MCP | 1.0 M KOH | 270 | 79 | 1000 cycles | [9] |
| CoFe-PBA NS@NF-24 | 1.0 M KOH | 256 | 54 | 24 | [10] |
| CoS2 NS/CC | 1.0 M KOH | 220 | 92 | 17 | [11] |
| Co@NC/CC-500 | 1.0 M KOH | 183 | 78 | 48 | This work |

Table 2 Summary of non-precious metal carbon-based electrocatalysts for HER

| Material | Electrolyte | η10 (mV) | Tafel slop (mV dec-1) | Stability (h) | Ref. |
| --- | --- | --- | --- | --- | --- |
| Co@NC/NF | 1.0 M KOH | 240 | 126.8 | 45 | [12] |
| Mo/Co@N–C | 1.0 M KOH | 157 | 148 | 10 | [13] |
| Au/CoP@NC-3 | 1.0 M KOH | 141 | 73 | 24 | [14] |
| Co@NC | 1.0 M KOH | 95 | 76 | 24 | [15] |
| Co-NCNT/CC | 1.0 M KOH | 230 | 97 | 40 | [16] |
| CoSP/NC | 1.0 M KOH | 150 | 64 | 10 | [17] |
| CoP@ NC/CF | 1.0 M KOH | 151.3 | 64.8 | 25 | [18] |
| Co–Zn/PNC/NF | 1.0 M KOH | 180 | 100 | 10 | [19] |
| Co-NC-ZR-2 | 1.0 M KOH | 163 | 65 | 1000 cycles | [20] |
| Co@NCNTs-800 | 1.0 M KOH | 240 | 95.9 | 10 | [21] |
| Co/NCNT/NG | 1.0 M KOH | 123 | 67 | 12 | [22] |
| Co@NC/CC-500 | 1.0 M KOH | 95 | 77 | 48 | This work |

Table 3 Summary of non-precious metal carbon-based electrocatalysts for overall water splitting

| Material | Electrolyte | j (mA cm-2) | Cell voltage (V) | Stability (h) | Ref. |
| --- | --- | --- | --- | --- | --- |
| Co-Zn/PNC | 1.0 M KOH | 10 | 1.63 | 10 | [23] |
| CoOx/CoNy@CNz | 1.0 M KOH | 10 | 1.57 | 40 | [24] |
| FeNiCo@NC/NF | 1.0 M KOH | 10 | 1.61 | 24 | [25] |
| Co-Mo2C-CNx-2 | 1.0 M KOH | 10 | 1.68 | 10 | [26] |
| CoP-InNC@CNT | 1.0 M KOH | 10 | 1.58 | 15 | [27] |
| S-CoW@(S,N)-C | 1.0 M KOH | 10 | 1.65 | 12 | [28] |
| Co/b-Mo2C@N-CNTs | 1.0 M KOH | 10 | 1.64 | 24 | [29] |
| CoFe–PBAs | 1.0 M KOH | 10 | 1.545 | 24 | [30] |
| PNC/Co | 1.0 M KOH | 10 | 1.64 | 24 | [31] |
| NiCoP/NC PHCs | 1.0 M KOH | 10 | 1.55 | 10 | [32] |
| CoP/NCNHP | 1.0 M KOH | 10 | 1.64 | 36 | [33] |
| ZnCoS-CNT/NP | 1.0 M KOH | 10 | 1.59 | 40 | [34] |
| Co@NC/CC-500 | 1.0 M KOH | 10 | 1.52 | 48 | This work |

References

1. 	Xie Z, Wang Y (2019) Facile synthesis of MOF-Derived Co@CoNx/bamboo-like carbon tubes for efficient electrocatalytic water oxidation. Electrochim Acta 296:372–378. https://doi.org/10.1016/j.electacta.2018.11.071

2. 	Liu G, Wang B, Ding P, et al (2020) In-situ synthesis strategy for CoM (M = Fe, Ni, Cu) bimetallic nanoparticles decorated N-doped 1D carbon nanotubes/3D porous carbon for electrocatalytic oxygen evolution reaction. J Alloys Compd 815. https://doi.org/10.1016/j.jallcom.2019.152470

3. 	Ban J, Xu G, Zhang L, et al (2018) Efficient Co-N/PC@CNT bifunctional electrocatalytic materials for oxygen reduction and oxygen evolution reactions based on metal-organic frameworks. Nanoscale 10:9077–9086. https://doi.org/10.1039/c8nr01457d

4. 	Fang W, Wang J, Hu Y, et al (2021) Metal-organic framework derived Fe-Co-CN/reduced graphene oxide for efficient HER and OER. Electrochim Acta 365. https://doi.org/10.1016/j.electacta.2020.137384

5. 	Yang F, Zhao P, Hua X, et al (2016) A cobalt-based hybrid electrocatalyst derived from a carbon nanotube inserted metal-organic framework for efficient water-splitting. J Mater Chem A 4:16057–16063. https://doi.org/10.1039/c6ta05829a

6. 	Zhang Q, Wang H, Han W, et al (2022) Core—shell Prussian blue analogues derived from metal-organic frameworks as efficient electrocatalysts for oxygen evolution reaction. Nano Res. https://doi.org/10.1007/s12274-022-4832-2

7. 	Guan Y, Li Y, Luo S, et al (2019) Rational design of positive-hexagon-shaped two-dimensional ZIF-derived materials as improved bifunctional oxygen electrocatalysts for use as long-lasting rechargeable Zn–Air batteries. Appl Catal B 256. https://doi.org/10.1016/j.apcatb.2019.117871

8. 	Wang C, Chen W, Yuan D, et al (2020) Tailoring the nanostructure and electronic configuration of metal phosphides for efficient electrocatalytic oxygen evolution reactions. Nano Energy 69. https://doi.org/10.1016/j.nanoen.2020.104453

9. 	Zhou X, Liu X, Zhang J, et al (2020) Highly-dispersed cobalt clusters decorated onto nitrogen-doped carbon nanotubes as multifunctional electrocatalysts for OER, HER and ORR. Carbon 166:284–290. https://doi.org/10.1016/j.carbon.2020.05.037

10. 	Chen Z, Fei B, Hou M, et al (2020) Ultrathin Prussian blue analogue nanosheet arrays with open bimetal centers for efficient overall water splitting. Nano Energy 68. https://doi.org/10.1016/j.nanoen.2019.104371

11. 	Yao N, Tan T, Yang F, et al (2018) Well-aligned metal-organic framework array-derived CoS2 nanosheets toward robust electrochemical water splitting. Mater Chem Front 2:1732–1738. https://doi.org/10.1039/c8qm00259b

12. 	Aijaz A, Masa J, Rösler C, et al (2017) Metal–Organic Framework Derived Carbon Nanotube Grafted Cobalt/Carbon Polyhedra Grown on Nickel Foam: An Efficient 3D Electrode for Full Water Splitting. ChemElectroChem 4:188–193. https://doi.org/10.1002/celc.201600452

13. 	Wu C, Liu D, Li H, Li J (2018) Molybdenum Carbide-Decorated Metallic Cobalt@Nitrogen-Doped Carbon Polyhedrons for Enhanced Electrocatalytic Hydrogen Evolution. Small 14. https://doi.org/10.1002/smll.201704227

14. 	Wang X, Fei Y, Li W, et al (2020) Gold-Incorporated Cobalt Phosphide Nanoparticles on Nitrogen-Doped Carbon for Enhanced Hydrogen Evolution Electrocatalysis. ACS Appl Mater Interfaces 12:16548–16556. https://doi.org/10.1021/acsami.0c02076

15. 	Mo Q, Chen N, Deng M, et al (2017) Metallic Cobalt@Nitrogen-Doped Carbon Nanocomposites: Carbon-Shell Regulation toward Efficient Bi-Functional Electrocatalysis. ACS Appl Mater Interfaces 9:37721–37730. https://doi.org/10.1021/acsami.7b10853

16. 	Xing Z, Liu Q, Xing W, et al (2015) Interconnected Co-entrapped, N-doped carbon nanotube film as active hydrogen evolution cathode over the whole PH range. ChemSusChem 8:1850–1855. https://doi.org/10.1002/cssc.201500138

17. 	Zhao L, Yang A, Wang A, et al (2020) Metallic Co, CoS, and P co-doped N enriched carbon derived from ZIF-67 as an efficient catalyst for hydrogen evolution reaction. Int J Hydrogen Energy 45:30367–30374. https://doi.org/10.1016/j.ijhydene.2020.08.003

18. 	Wang Y, Li S, Chen Y, et al (2020) 3D hierarchical MOF-derived CoP@N-doped carbon composite foam for efficient hydrogen evolution reaction. Appl Surf Sci 505. https://doi.org/10.1016/j.apsusc.2019.144503

19. 	Peng W, Zheng G, Wang Y, et al (2019) Zn doped ZIF67-derived porous carbon framework as efficient bifunctional electrocatalyst for water splitting. Int J Hydrogen Energy 44:19782–19791. https://doi.org/10.1016/j.ijhydene.2019.05.101

20. 	Sang X, Chen J, Jing M, et al (2019) Sustainable synthesis of nitrogen-doped porous carbon with improved electrocatalytic performance for hydrogen evolution. New Journal of Chemistry 43:3078–3083. https://doi.org/10.1039/c8nj05819a

21. 	Li J Sen, Du B, Lu ZH, et al (2017) In situ -generated Co@nitrogen-doped carbon nanotubes derived from MOFs for efficient hydrogen evolution under both alkaline and acidic conditions. New Journal of Chemistry 41:10966–10971. https://doi.org/10.1039/c7nj02334k

22. 	Yang L, Lv Y, Cao D (2018) Co,N-codoped nanotube/graphene 1D/2D heterostructure for efficient oxygen reduction and hydrogen evolution reactions. J Mater Chem A 6:3926–3932. https://doi.org/10.1039/c7ta11140a

23. 	Peng W, Zheng G, Wang Y, et al (2019) Zn doped ZIF67-derived porous carbon framework as efficient bifunctional electrocatalyst for water splitting. Int J Hydrogen Energy 44:19782–19791. https://doi.org/10.1016/j.ijhydene.2019.05.101

24. 	Liu J, Wang C, Sun H, et al (2020) CoOx/CoNy nanoparticles encapsulated carbon-nitride nanosheets as an efficiently trifunctional electrocatalyst for overall water splitting and Zn-air battery. Appl Catal B 279. https://doi.org/10.1016/j.apcatb.2020.119407

25. 	Ren S, Duan X, Ge F, et al (2020) Trimetal-based N-doped carbon nanotubes arrays on Ni foams as self-supported electrodes for hydrogen/oxygen evolution reactions and water splitting. J Power Sources 480. https://doi.org/10.1016/j.jpowsour.2020.228866

26. 	Zhang P, Liu Y, Liang T, et al (2021) Nitrogen-doped carbon wrapped Co-Mo2C dual Mott–Schottky nanosheets with large porosity for efficient water electrolysis. Appl Catal B 284. https://doi.org/10.1016/j.apcatb.2020.119738

27. 	Chai L, Hu Z, Wang X, et al (2020) Stringing Bimetallic Metal–Organic Framework-Derived Cobalt Phosphide Composite for High-Efficiency Overall Water Splitting. Advanced Science 7. https://doi.org/10.1002/advs.201903195

28. 	Weng B, Grice CR, Meng W, et al (2018) Metal-Organic Framework-Derived CoWP@C Composite Nanowire Electrocatalyst for Efficient Water Splitting. ACS Energy Lett 3:1434–1442. https://doi.org/10.1021/acsenergylett.8b00584

29. 	Ouyang T, Ye Y, Wu C, et al (2019) Heterostructures Composed of N‐Doped Carbon Nanotubes Encapsulating Cobalt and β‐Mo2C Nanoparticles as Bifunctional Electrodes for Water Splitting. Angewandte Chemie 131:4977–4982. https://doi.org/10.1002/ange.201814262

30. 	Chen Z, Fei B, Hou M, et al (2020) Ultrathin Prussian blue analogue nanosheet arrays with open bimetal centers for efficient overall water splitting. Nano Energy 68. https://doi.org/10.1016/j.nanoen.2019.104371

31. 	Li X, Niu Z, Jiang J, Ai L (2016) Cobalt nanoparticles embedded in porous N-rich carbon as an efficient bifunctional electrocatalyst for water splitting. J Mater Chem A 4:3204–3209. https://doi.org/10.1039/c6ta00223d

32. 	Zhang X, Huang L, Wang Q, Dong S (2017) Transformation of homobimetallic MOFs into nickel-cobalt phosphide/nitrogen-doped carbon polyhedral nanocages for efficient oxygen evolution electrocatalysis. J Mater Chem A 5:18839–18844. https://doi.org/10.1039/c7ta06272a

33. 	Pan Y, Sun K, Liu S, et al (2018) Core-Shell ZIF-8@ZIF-67-Derived CoP Nanoparticle-Embedded N-Doped Carbon Nanotube Hollow Polyhedron for Efficient Overall Water Splitting. J Am Chem Soc 140:2610–2618. https://doi.org/10.1021/jacs.7b12420

34. 	Yu Z, Bai Y, Zhang S, et al (2018) Metal-organic framework-derived Zn0.975Co0.025S/CoS2 embedded in N, S-codoped carbon nanotube/nanopolyhedra as an efficient electrocatalyst for overall water splitting. J Mater Chem A 6:10441–10446. https://doi.org/10.1039/c8ta01370e