Chloramphenicol and Methylene Blue Adsorption by Modestly Treated Paper Sewage Sludge Based Activated Carbon

Azrina Aziza, Huzairy Hassanb* and Mohd Azmier Ahmad a*

aSchool of Chemical Engineering, Universiti Sains Malaysia, Engineering Campus, 14300 Nibong Tebal, Pulau Pinang, Malaysia;

bFaculty of Chemical Engineering & Technology, Universiti Malaysia Perlis, 02600 Arau, Perlis, Malaysia.

*Corresponding authors: huzairyhassan@unimap.edu.my; chazmier@usm.my

Supplementary Data

Table S1. ANOVA for CAP drug removal by PMSSAC.

| Source | Sum of Squares | Degree of freedom (df) | Mean Square | F-value | Prob > F |
| --- | --- | --- | --- | --- | --- |
| Model | 1448.06 | 5 | 289.61 | 21.47 | 0.0004 |
| X1 | 384.64 | 1 | 384.64 | 28.52 | 0.0011 |
| X2 | 52.33 | 1 | 52.33 | 3.88 | 0.0895 |
| X1 X2 | 11.02 | 1 | 11.02 | 0.8173 | 0.396 |
| X12 | 853.75 | 1 | 853.75 | 63.3 | < 0.0001 |
| X22 | 0.0028 | 1 | 0.0028 | 0.0002 | 0.9889 |

Table S2. ANOVA for MB dye removal by PMSSAC.

| Source | Sum of Squares | Degree of freedom (df) | Mean Square | F-value | Prob > F |
| --- | --- | --- | --- | --- | --- |
| Model | 393.03 | 5 | 78.61 | 62.49 | < 0.0001 |
| X1 | 51.04 | 1 | 51.04 | 40.58 | 0.0004 |
| X2 | 97.69 | 1 | 97.69 | 77.66 | < 0.0001 |
| X1 X2 | 12.18 | 1 | 12.18 | 9.68 | 0.017 |
| X12 | 205.3 | 1 | 205.3 | 163.21 | < 0.0001 |
| X22 | 0.4492 | 1 | 0.4492 | 0.3571 | 0.569 |

Table S3. Isotherms for adsorption of CAP and MB by optimized PMSSAC at 30°C.

| Isotherms | Parameters | CAP | MB |
| --- | --- | --- | --- |
| Langmuir | q𝑚 | 17.0835 | 20.7130 |
|  | 𝐾L (L/mg) | 0.0171 | 0.0035 |
|  | R2 | 0.9973 | 0.7853 |
| Freundlich | KF(mg/g) (L/mg)1/n | 1.8995 | 2.1089 |
|  | nF | 0.9226 | 0.6797 |
|  | R2 | 0.9988 | 0.9893 |
| Temkin | BT(L/mg) | 3.8448 | 2.8600 |
|  | AT (L/mg) | 0.1609 | 0.0892 |
|  | R2 | 0.9924 | 0.9491 |

Table S4. Kinetics parameters for CAP-PMSSAC system at 30°C.

| Initial concentration | qe, exp (mg/g) | Pseudo-first order |  |  | Pseudo-second order |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | qe, calc. (mg/g) | k1 (min-1) | R2 | qe, calc. (mg/g) | k2 (min-1) | R2 |
| 50 | 3.4740 | 0.8735 | 0.7089 | 0.9871 | 3.4675 | 2.5451 | 0.9992 |
| 100 | 6.6250 | 4.1581 | 1.3585 | 0.9330 | 7.3766 | 0.4000 | 0.9972 |
| 150 | 8.6860 | 4.1430 | 1.2130 | 0.9961 | 9.1394 | 0.5360 | 0.9992 |
| 200 | 10.4740 | 5.4059 | 1.3498 | 0.9605 | 11.2067 | 0.3935 | 0.9994 |
| 250 | 11.7410 | 6.2514 | 1.4528 | 0.9838 | 12.6173 | 0.3529 | 0.9994 |
| 300 | 12.8800 | 5.3095 | 1.2831 | 0.9484 | 13.5274 | 0.4259 | 0.9997 |

Table S5. Kinetics parameters for MB-PMSSAC system at 30°C.

| Initial concentration (mg/L) | qe, exp (mg/g) | Pseudo-first order |  |  | Pseudo-second order |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | qe, calc. (mg/g) | k1(min-1) | R2 | qe, calc. (mg/g) | k2(min-1) | R2 |
| 50 | 4.0410 | 0.8012 | 0.7889 | 0.8833 | 4.0534 | 2.9946 | 1.0000 |
| 100 | 4.7959 | 3.3682 | 1.0378 | 0.9944 | 5.2820 | 0.4400 | 0.9958 |
| 150 | 5.9581 | 4.1733 | 0.9830 | 0.9860 | 6.7014 | 0.2998 | 0.9980 |
| 200 | 6.7550 | 4.4236 | 0.8859 | 0.9767 | 7.4784 | 0.2776 | 0.9983 |
| 250 | 7.9440 | 6.8433 | 0.9485 | 0.9550 | -5.4137 | 0.0507 | 0.1023 |
| 300 | 8.7700 | 13.4743 | 1.2806 | 0.9752 | -13.7165 | 0.0121 | 0.1632 |