Materials sustainability of thermoelectric generators for waste heat utilization

Supplementary Section

The recent developments in thermoelectric materials with high figure-of-merit zT has prompted an analysis of the potential of this technology for waste heat harvesting. To aid this analysis requires an extensive search of materials that exhibit high zT and hence the search was undertaken, the results of which are given in Tables S1, S2 and S3.1 The materials have been categorised into low temperature < 373 K, medium temperature 373 K < T < 573 K and high temperature > 573 K in accordance with categorisation of waste heat. From among these alloys, two pairs from each of the category were selected for an in depth analysis of materials requirement and sustainability.

Table S1: List of alloys/compounds that exhibit high zT at low temperatures, < 373 K.

| Type | Alloy/Compound | (zT)max | Tmax, K |
| --- | --- | --- | --- |
| p-type | (AgCu)0.995Te0.9Se0.1 | 1.10 | 350 |
|  | (Bi0.26Sb0.74)2Te3+3%Te ingot | 1.12 | 298 |
|  | BiSbTe | 1.20 | 300 |
|  | Bi0.4Sb1.6Te | 0.90 | 300 |
|  | (Bi0.2Sb0.8)2Te3 with 0.12 wt% multiwall carbon nanotubes | 1.47 | 348 |
|  | Bi0.5Sb1.5Te3 | 1.90 | 320 |
|  | Bi0.52Sb1.48Te3 | 1.56 | 300 |
|  | Bi0.5Sb1.5Te3 | 1.40 | 300 |
|  | BiSbTe+0.75 wt% ZnAlO | 1.33 | 370 |
|  | Bi0.5Sb1.5Te3 | 1.20 | 363 |
|  | Bi0.5Sb1.5Te3 | 1.20 | 320 |
|  | Bi0.5Sb1.5Te3 | 1.42 | 348 |
|  | Bi0.5Sb1.5Te3+20 wt% Te | 1.24 | 350 |
|  | Bi0.4Sb1.6Te3+0.2 at% Te | 1.38 | 323 |
|  | Mn doped Bi2Te3 | 1.47 | 310 |
|  | Bi0.4Sb1.6Te3 doped with 0.5 at% In | 1.20 | 320 |
|  | Bi0.48Sb1.52Te3 +WSe2 | 1.27 | 360 |
|  | Bi0.5Sb1.5Te3 | 1.60 | 323 |
|  | Bi0.5Sb1.5Te3 | 1.00 | 300 |
|  | Bi0.48Sb1.52Te3 | 1.10 | 350 |
|  | Polycrystalline Bi0.5Sb1.5Te3 | 1.71 | 323 |
| n-type | Ternary (BiSb)2Te3 Bulk nanostructured | 1.28 | 303 |
|  | Ag0.011Bi2Te2.7Se0.3 | 1.10 | 350 |
|  | Bi2Te2.7Se0.3 | 0.76 | Room Temperature |
|  | Bi2Te2.7Se0.3 | 0.94 | 300 |
|  | Mg3.2Bi1.498Sb0.5Te0.002 | 0.75 | Room Temperature |
|  | Mg3.2Bi1.498Sb0.5Te0.002 | 0.90 | 350 |
|  | Bi2Te2.7Se0.3 with0.8 atom % excess Bi | 0.88 | 348 |
|  | Bi2Te2.79Se0.21 | 1.20 | 357 |
|  | Bi2Te2.85Se0.15+0.08 wt% I | 1.07 | 360 |
|  | Bi2Se3 | 0.96 | 370 |
|  | Ag2S0.4Se0.6 | 1.08 | 350 |
|  | Ag2Se1.01 | 1.00 | 320 |

Table S2: List of alloys/compounds that exhibit high zT at medium temperatures, 373 K < T < 573 K.

| Type | Alloys/Compounds | (zT)max | Tmax, K |
| --- | --- | --- | --- |
| p-type | Cu2Se | 0.72 | 380 |
|  | BixSb2-xTe3 | 1.40 | 373 |
|  | Bi0.3Sb1.7Te3+0.4 vol% SiC | 1.33 | 373 |
|  | Bi0.3Sb1.7Te3 | 1.30 | 380 |
|  | Bi0.5Sb1.5Te3 + Graphene | 1.05 | 425 |
|  | Bi0.4Sb1.6Te3+ 5wt% Cu7Te4 | 1.14 | 444 |
|  | Bi0.5Sb1.5Te3 +1 vol% Cu3SbSe4 | 1.60 | 476 |
|  | Bi0.4Sb1.6Te3 + Cu2Se nanocomposite | 1.60 | 488 |
|  | Cu1.97Ag0.03Se | 1.00 | 400 |
|  | Iodine‐doped Cu2Se | 2.30 | 400 |
|  | MgAgSb | 1.00 | 423 |
|  | Mg0.97Zn0.03Ag0.9Sb0.95 | 1.40 | 423 |
|  | MgAg0.965Ni0.005Sb0.99 | 1.40 | 450 |
|  | Mg0.995Yb0.005Ag0.97Sb0.99 | 1.40 | 550 |
|  | AgSb0.94Cd0.06Te2 | 2.60 | 573 |
|  | MgAg0.97Sb0.99 | 1.30 | 533 |
| n-type | Bi2Te3 | 1.19 | 420 |
|  | Bi2Te2.7Se0.3 | 1.04 | 399 |
|  | Cu0.01Bi2Te2.7Se0.3 | 1.06 | 398 |
|  | Bi2Te2.3Se0.7 | 1.20 | 445 |
|  | Bi2Te2.2Se0.8 | 1.11 | 475 |
|  | Bi2Te2.4Se0.6 | 1.22 | 477 |
|  | Bi1.95Sb0.05Te2.3Se0.7 | 1.30 | 450 |
|  | Bi2Te2.7Se0.3+16 wt% Te | 1.10 | 400 |
|  | Bi1.8Sb0.2Te2.7Se0.3 + 15 wt% Te | 1.40 | 425 |
|  | Lu doped LuxBi2-xTe2.7Se0.3 | 1.37 | 373 |
|  | Mg3.3Bi1.498Sb0.5Te0.002 | 0.90 | 423 |
|  | Mg3.3Bi1.298Sb0.7Te0.002 | 1.20 | 548 |
|  | Mg3.2Bi1.29Sb0.7Te0.01 | 1.24 | 573 |
|  | Mg3.2Bi1.4 Sb0.59Se0.01 | 1.24 | 498 |
|  | Ag2Se with 0.5 wt% carbon nanotubes | 0.97 | 375 |
|  | Ag2Se | 0.90 | 390 |
|  | Ag2Se | 1.21 | 389 |
|  | Ag2Sb0.01Te0.99 | 1.40 | 410 |
|  | Ba8Ga15.8Cu0.033Sn30.17 | 1.45 | 500 |

Table S3: List alloys/compounds that exhibit high zT at high temperatures > 573 K.

| Type | Alloys/Compounds | (zT)max | Tmax, K |
| --- | --- | --- | --- |
| p-type | Pb0.98Na0.02Te- 8%SrTe | 2.50 | 923 |
|  | PbTe0.8Se0.2 with 8% MgTe | 2.20 | 820 |
|  | Pb0.935Na0.025Cd0.04Se0.5S0.25Te0.25 | 2.00 | 900 |
|  | Pb0.98Na0.02Se-2%HgSe | 1.70 | 970 |
|  | Pb0.975Na0.025S-3%CdS | 1.30 | 923 |
|  | (GeTe)0.95(Sb2Te3)0.05 | 2.70 | 720 |
|  | Na0.03Eu0.03Sn0.02Pb0.92Te | 2.57 | 850 |
|  | Ge0.87Pb0.13Te | 2.27 | 723 |
|  | Ge0.87Pb0.13Te-5%Bi2Te3 | 2.10 | 690 |
|  | AgCuTe0.90Se0.10 | 1.60 | 670 |
|  | Sn0.91Mn0.14Te(Cu2Te)0.05 | 1.60 | 920 |
|  | CuInTe1.99Sb0.01+1.0 wt% ZnO | 1.61 | 823 |
|  | Cu0.7Ag0.3Ga0.4In0.6Te2 | 1.64 | 873 |
|  | Cu2S0.52Te0.48 | 2.10 | 1000 |
|  | DD0.7Fe3CoSb12 | 1.30 | 800 |
|  | (Nb0.6Ta0.4)0.8Ti0.2FeSb | 1.60 | 1200 |
|  | Zn3.8In0.2Sb3 | 1.80 | 698 |
|  | Bi0.94Pb0.06Cu0.99Fe0.01SeO | 1.50 | 873 |
|  | Cu1.97S | 1.70 | 1000 |
|  | Polycrystalline SnSe | 3.10 | 783 |
|  | SnSe Single Crystal | 2.60 | 923 |
|  | Cu2Se with 0.75 wt % carbon nano tubes | 2.40 | 1000 |
|  | Mn30.4Re6Si63.6 | 1.15 | 873 |
|  | Mn1.06Te-2% SnTe | 1.40 | 873 |
|  | Yb14Mn0.2Al0.2Sb11 | 1.30 | 1223 |
|  | SiGe-YSi2 nanocomposite | 1.81 | 1100 |
| n-type | Bi doped PbTe/Ag2Te (15%) | 2.05 | 800 |
|  | PbTe0.998I0.002–3%Sb | 1.80 | 773 |
|  | PbTe-4%InS | 1.83 | 773 |
|  | PbSe0.998Br0.002-2%Cu2Se | 1.80 | 723 |
|  | PbS-4.4%Ag | 1.70 | 850 |
|  | Pr2.74Te4 | 1.70 | 1200 |
|  | Ba0.08La0.05Yb0.04Co4Sb12 | 1.70 | 850 |
|  | (Sm,Mm)0.15Co4Sb12 | 2.10 | 850 |
|  | Ti0.5Zr0.25Hf0.25NiSn + 1 wt% DA | 1.50 | 825 |
|  | Ti0.5Zr0.25Hf0.25NiSn0.998Sb0.002 | 1.50 | 700 |
|  | Mg3.2Sb1.5Bi0.49Te0.01Cu0.01 | 1.90 | 773 |
|  | Bromine doped SnSe | 2.80 | 773 |
|  | Bi and Cr co doped Mg2Si0.3Sn0.7 | 1.70 | 673 |
|  | La3-x-yYbyTe4 | 1.20 | 1273 |
|  | SiGe | 1.84 | 1073 |

The number of pn-junctions required to convert the maximum exergy available in the 3 temperature regions has been determined using Eq. (6) given in the main text. This number of junctions has then been converted into alloys and elements required using the procedure given below. The calculations shown below are an example for one particular case and is applicable to all the different cases studied.

Low temperature exergy conversion:

The cold side temperature Tc of the thermoelectric device in all the cases is considered to be 300 K and hence the temperature difference T that drives the conversion is 73 K with a Carnot efficiency factor of 0.196. The maximum exergy available therefore is 8.4718 PWh which translates to 0.9671 TW of power PmaxN every year. Assuming the contact resistance to be zero, the device resistance RTED for an aspect ratio l/A of 0.5 cm-1 has been determined using Equation (5) of main text by considering an average value of 2.336 and 0.951 m cm-1 as resistivities for p-type and n-type alloys respectively. This has been found to be 1.6435 m. The average Seebeck coefficient is 0.2396 and 0.1424 mVK-1 for the p-type and n-type respectively and the corresponding device Seebeck coefficient is 0.382 mVK-1. These parameters have been used in Equation (6) of the main text to determine Nmin and it is found to be 81.757x1011. Considering 1 cm2 to be the cross sectional area of the leg results in the leg volume to be 0.5 cm3 for an aspect ratio of 0.5 cm-1. The density of Bi2Te3 is 7.7 gcm-3 and hence each leg will weigh 3.85 g. The total amount of Bi2Te3 required to make 81.757x1011 legs will be 31.4765 Mt. Therefore, the amount of elemental Bi and Te required will be 16.4307 and 15.0457 Mt corresponding to 52.195 wt.% and 47.8 wt.% in Bi2Te3 respectively.

Table S4: The minimum number of junctions required Nmin and amount of alloys and elements required to convert the exergy into electrical power is given. These are determined as per the procedure mentioned above.

| For low temperatures < 373 K |  |  |  |
| --- | --- | --- | --- |
|  | l/A=0.5 cm-1 | l/A=1.0 cm-1 | l/A=1.5 cm-1 |
| Nmin | 81.757×1011 | 163.515×1011 | 245.248×1011 |
| Bi2Te3 (Mt) | 31.4765 | 125.9066 | 283.2614 |
| Bi (Mt) | 16.4307 | 65.7232 | 147.8625 |
| Te (Mt) | 15.0457 | 60.1833 | 135.3990 |
| (Bi0.5Sb1.5)Te3 (Mt) | 28.1244 | 112.4983 | 253.0956 |
| Bi (Mt) | 4.3874 | 17.5497 | 39.4830 |
| Sb (Mt) | 7.6667 | 30.6670 | 68.9940 |
| Te (Mt) | 16.0703 | 64.2815 | 144.6190 |
| (BiSb)2Te3 (Mt) | 28.0018 | 112.0078 | 251.9923 |
| Bi (Mt) | 8.2018 | 32.8071 | 73.8086 |
| Sb (Mt) | 4.7771 | 19.1085 | 42.9899 |
| Te (Mt) | 15.0230 | 60.0922 | 135.1939 |
| Bi2(Te2.79Se0.21) (Mt) | 31.4765 | 125.9066 | 283.2614 |
| Bi | 16.6416 | 66.5668 | 149.7603 |
| Te | 14.1738 | 56.6957 | 127.5526 |
| Se | 0.6610 | 2.6440 | 5.9485 |
| For medium temperatures, 373 K < T < 573 K. |  |  |  |
|  | l/A=0.5 cm-1 | l/A=1.0 cm-1 | l/A=1.5 cm-1 |
| Nmin | 8.8010×1011 | 17.6020×1011 | 26.4030×1011 |
| Cu2Se (Mt) | 3.0099 | 12.0398 | 27.0895 |
| Cu (Mt) | 1.8565 | 7.4261 | 16.7088 |
| Se (Mt) | 1.1534 | 4.6136 | 10.3807 |
| (AgSb0.94Cd0.06)Te2 (Mt) | 3.0892 | 12.3566 | 27.8024 |
| Ag (Mt) | 0.688 | 2.7518 | 6.1916 |
| Sb (Mt) | 0.730 | 2.9199 | 6.5697 |
| Cd (Mt) | 0.0429 | 0.1717 | 0.3864 |
| Te (Mt) | 1.6283 | 6.5132 | 14.6546 |
| (Bi1.8Sb0.2)(Te2.7Se0.3 ) (Mt) | 3.3884 | 13.5535 | 30.4955 |
| Bi (Mt) | 1.6579 | 6.6318 | 14.9214 |
| Sb (Mt) | 0.1073 | 0.4294 | 0.9661 |
| Te (Mt) | 1.5187 | 6.0747 | 13.6681 |
| Se (Mt) | 0.1044 | 0.4177 | 0.9399 |
| For High temperatures, > 573 K |  |  |  |
|  | l/A=0.5 cm-1 | l/A=1.0 cm-1 | l/A=1.5 cm-1 |
| Nmax | 8.2197×1011 | 16.4394×1011 | 24.6591×1011 |
| PbTe (Mt) | 3.3536 | 13.4146 | 30.1827 |
| Pb (Mt) | 2.0756 | 8.3023 | 18.6801 |
| Te (Mt) | 1.2781 | 5.1123 | 11.5026 |
| (Ge0.87Pb0.13)Te (Mt) | 2.6315 | 10.5262 | 23.6838 |
| Ge (Mt) | 0.7637 | 3.0547 | 6.8731 |
| Pb (Mt) | 0.3255 | 1.3021 | 2.9297 |
| SnSe (Mt) | 2.5399 | 10.1596 | 22.8589 |
| Sn (Mt) | 1.5252 | 6.1009 | 13.7268 |
| Se (Mt) | 1.0147 | 4.0588 | 9.1322 |
| Co4Sb12 (Mt) | 3.0577 | 12.2309 | 27.5196 |
| Co (Mt) | 0.4364 | 1.7454 | 3.9271 |
| Sb (Mt) | 2.6214 | 10.4856 | 23.5925 |

The embodied energy EE and CO2 emissions for most of the groups 14-16 elements are not available and these are typically secondary products of extraction of primary metals such as Cu and Pb. Hence, to determine the EE and emissions due to extraction of the elements required for thermoelectric conversion, typical values of Cu and Pb: 80 GJt-1 and 25 GJt-1 and 5.5 tt-1 and 2.5 tt-1 respectively have been used.2,3 Te, Se and Sn are assumed to have EE and emissions similar to Cu while Bi and Sb are assumed to be similar to Pb.

The Herfindahl-Hirschman Index HHI has been determined using the relation;

HHI=i=1NSi2		(S1)

where Si is the percentage share of world production of i and N is the total number of producers in the world.4,5 The world production statistics of different elements have been obtained from USGS data base.6

References:

- Anilkumar Bohra and Satish Vitta, ‘Review of status of thermoelectric modules for different temperatures’, to be published.

- T.G. Gutowski, S. Sahni, J.M. Allwood, M.F. Ashby and E. Wornell, ‘The energy required to produce materials: constraints on energy-intensity improvement, parameters of demand’, Phil Trans Royal Soc A371: 20120003 (2013).

- J. Rankin, ‘Energy use in metal production’, High Temperature Processing Symposium 2012, Swinburne University of Technology.

- Herfindahl, O. C. Concentration in the US Steel Industry. Ph.D. Thesis, Columbia University, New York, 1950.

- Hirschman, A. O. National power and the structure of foreign trade; California University Press: Berkeley, CA, 1980.

- U.S. Geological Survey, Mineral Commodity Summaries.