Supporting Information

Kinetic studies of the removal of methylene blue from aqueous solution by biochar derived from jackfruit peel

Loc Ton-That1,2, Thi-Ngoc-Linh Huynh3, Bich-Ngoc Duong4, Duy-Khoi Nguyen1,2, Ngoc-An Nguyen4, Van-Hien Pham5, Thien-Hoang Ho6, Van-Phuc Dinh4*

1Institute of Fundamental and Applied Sciences, Duy Tan University, Ho Chi Minh City 700000, Viet Nam

2Faculty of Natural Sciences, Duy Tan University, Da Nang City 550000, Viet Nam

3Can Tho Department of Science and Technology, Can Tho City, 900000, Viet Nam

4Institute of Applied Technology and Sustainable Development, Nguyen Tat Thanh University, Ho Chi Minh City, Vietnam

5Institute of Applied Materials Science, VAST, TL29, Thanh Loc Ward, Dist. 12, Ho Chi Minh City 700000, Vietnam.

6Dong Nai University, 09 Le Quy Don Street, Tan hiep Ward,  Bien Hoa City, Ddong Nai province, 76100, Vietnam.

Corresponding author: dvphuc@ntt.edu.vn

### Section 1: Kinetic and isotherm of adsorption models

### In this study, the non-linear equivalence of all the kinetic models were visualized by origin software to describe the experiment data, including the pseudo-first-order (PFO), pseudo-second-order (PSO), Intra-particle Diffusion, and the Elovich model, the details are expressed in equation (1.1)-(1.4), respectively.

  - Pseudo-first-order equation (PFO)

The pseudo-first-order equation (Simonin, 2016) is generally determined as

Qt=Qe1-e-k1t 							     (1.1)

where Qt (mg. g-1) is the adsorbed amount of methylene blue under equilibrium by mass unit of biochar at anytime t (min); Qe (mg. g-1) is the amount of methylene blue adsorbed at equilibrium,  k1 (min-1) denotes rate constants of the PFO model.

  - Pseudo-second-order equation (PSO)

The amount of adsorbed of material surface and at the equilibrium state have a profound influence on the rate of PSO reaction. The pseudo-second-order equation (Ho and McKay, 1999; Liu et al., 2021) is calculated in form (1.2)

Qt= Qe2k2t1+Qek2t							     (1.2)

where k2 (g. mg-1. min-1) represents rate constants of the PSO model.

    - Elovich equation (ELO)

Elovich model assumes that if the adsorption sites in rise extraordinarily within the adsorption process, chemical mechanism primarily happens in the kinetic adsorption. The heterogeneous surfaces of solid material were assumed in the Elovich equation. It is believed that adsorption sites of adsorbent witness an exponential surge over the period of adsorption of contaminants following the Elovich model (Aysu and Küçük, 2014).

The Elovich model is expressed in the following equation  (1.3).

Qt=1βln(1+αβt)						      	(1.3)

where Qt is the MB adsorption capacity at any time t (mg.g-1); α (mg.g-1. min-1) is the initial adsorption rate constant và β (mg.g-1) is desorption constant.

    - Intra-particle Diffusion equation (IPD)

The adsorption procedure of contaminants in solution based on porous solids comprises four periods following orders: (1) interaction of solute and particle boundary layer; (2) interaction of solute and adsorbent surface; (3) interaction of solute and adsorbent sites (diffusion into pores); (4) interactions of the solute molecules and the adsorbent surface active sites (adsorption, complexation, and precipitation) (Benjelloun et al., 2021). The intra-particulate diffusion (Chang et al., 2021) is equated in the following form (1.4)

Qt=kidt+∁						            (1.4)

where: kid (mg.g-1. min-0,5) and C (mg.g-1. min-1) are intra diffusion constant and  rate constant, respectively; The constant of C indicates the boundary layer thickness of adsorbent.

### Section 2: Characterization of materials

### Table S1: Textural parameters of jackfruit peel biochar (AHLP)

|  | Unit | AHLP |
| --- | --- | --- |
| BET surface area | m2/g | 12.67 |
| Total pore volume | cm3/g | 0.025 |
| Pore size | nm | 8.046 |

Fig. S1 Plot of pHPZC of biochar derived jackfruit peel

REFERENCES

Aysu, T. and Küçük, M.M.  2014.  Removal of crystal violet and methylene blue from aqueous solutions by activated carbon prepared from Ferula orientalis. International Journal of Environmental Science and Technology 12(7), 2273-2284.

Benjelloun, M., Miyah, Y., Akdemir Evrendilek, G., Zerrouq, F. and Lairini, S.  2021.  Recent Advances in Adsorption Kinetic Models: Their Application to Dye Types. Arabian Journal of Chemistry 14(4).

Chang, B.P., Gupta, A. and Mekonnen, T.H.  2021.  Flame synthesis of carbon nanoparticles from corn oil as a highly effective cationic dye adsorbent. Chemosphere 282, 131062.

Ho, Y.S. and McKay, G.  1999.  Pseudo-second order model for sorption processes. Process Biochemistry 34(5), 451-465.

Liu, X.-J., Li, M.-F. and Singh, S.K.  2021.  Manganese-modified lignin biochar as adsorbent for removal of methylene blue. Journal of Materials Research and Technology 12, 1434-1445.

Simonin, J.-P.  2016.  On the comparison of pseudo-first order and pseudo-second order rate laws in the modeling of adsorption kinetics. Chemical Engineering Journal 300, 254-263.