SUPPLEMENTARY MATERIAL

Extraction of new exopolysaccharide from K. oxytoca J7 and its possible application in biosorption of Ni2+ions from contaminated water

Verica Ljubic1, Jovana Perendija1, Slobodan Cvetkovic1, Jelena Rogan2, Katarina Trivunac2,Marijana Stojanovic3,and Mina Popovic1*

1 University of Belgrade, Institute of Chemistry, Technology and Metallurgy, National Institute of Republic of Serbia, Njegoseva 12, 11000 Belgrade, Serbia, corresponding author*

2Faculty of Technology and Metallurgy, University of Belgrade, Karnegijeva 4, Belgrade, Serbia

3 University of Belgrade, Institute for Biological Research “Siniša Stanković”, National Institute of Republic of Serbia, Bulevar despota Stefana 142, 11060 Belgrade, Serbia

2.3.6 Determination of point zero charge

The method proposed by Mustafa et al.[1], 2002 was used to determine the point zero charges (PZC) of EPS extracted from K. oxytoca J7. Briefly, the PZC of the EPS was determined in 0.1 M NaNO3 (Sigma Aldrich) solution at room temperature. 40 mL of 0.1 M NaNO3 (Sigma Aldrich) solutions were taken in different titration flasks. The pHs of the solutions were adjusted to 2, 4, 6, 8, and 10 using HNO3 (Sigma Aldrich) and NaOH solutions (Sigma Aldrich). InoLab 730 pH meter (WTW GmbH) was used to record the initial pH of the EPS solution, with an accuracy of ± 0.01 pH units. About 0.2g of EPS sample was added to each flask and was shaken for 24 h on a shaker bath. The final pH of the solution was recorded; the difference between initial and final pH values (∆ pH) was plotted against initial pH values. PZC value was identified at the pH when ∆ pH was zero, i.e., initial pH equals the final pH.

3.1.5 TGA/DTG

Fig S1. Thermogravimetric analysis of EPS from K. oxytoca J7

3.3.1 Isotherm study

Fig. S2. Isotherm study, Langmuir a), and Freundlich b) isotherms for adsorption of Ni2+ ions on EPS isolated from K. oxytoca J7, equilibrium experiments were performed for different Ni2+ ions concentrations (0-35 mg L–1) at 25 ˚C, for 60 min at pH 5.5

3.3.2 Thermodynamic study

Fig. S3. Thermodynamic study of the adsorption for Ni2+ ions on EPS isolated from K. oxytoca J7, equilibrium experiments were performed for Ni2+ ions concentrations 10 mg L–1 at different temperatures (298.15, 318.15 and 338.15 K) for 60 min at pH 5.5

References:

1. 	Mustafa S, Dilara B, Nargis K, et al (2002) Surface properties of the mixed oxides of iron and silica. Colloids Surfaces A Physicochem Eng Asp 205:273–282. https://doi.org/10.1016/S0927-7757(02)00025-0