Supplementary Information

Multi-layered CuO/SiO2 core-shell structure improves electrocatalytic CO2-to-n-propanol conversion

Sha Wang,[a] Jianling Zhang,*[a], [b] Yingzhe Zhao,[a], [b] Jiajun Zhong,[c] Zhongjun Chen,[c] Yisen Yang,[a], [b] Buxing Han,[a], [b] Yongxin Cheng,[d] Meiling Li,[a], [b] Qian Li[d]

[a] Dr. S. Wang, Prof. J. Zhang, Y. Zhao, Y. Yang, Prof. B. Han, M. Li

Beijing National Laboratory for Molecular Sciences, CAS Key Laboratory of Colloid, Interface and Chemical Thermodynamics, CAS Research/Education

Center for Excellence in Molecular Sciences, Institute of Chemistry, Chinese Academy of Sciences

Beijing 100190, P. R. China

E-mail: zhangjl@iccas.ac.cn

[b] Prof. J. Zhang, Y. Zhao, Y. Yang, Prof. B. Han, M. Li

School of Chemical Sciences

University of Chinese Academy of Sciences

Beijing 100049, P. R. China

[c] J. Zhong, Dr. Z. Chen

Beijing Synchrotron Radiation Facility (BSRF), Institute of High Energy Physics, Chinese Academy of Sciences

Beijing 100049, P. R. China

[d] Dr. Y. Cheng, Dr. Q. Li

Center for Physicochemical Analysis and Measurement, Institute of Chemistry, Chinese Academy of Sciences

Beijing 100190, P. R. China

Results

Figure S1. FT-IR spectra of CuO/SiO2-3 and pure SiO2.

The adsorption peak at 1078 cm-1 corresponds to the asymmetrical stretching vibration of Si-O-Si, which confirms the existence of SiO2 in CuO/SiO2-3. It is red-shifted compared with that of pure SiO2 (1097 cm-1), implying there is a strong interaction between CuO and SiO2.

Figure S2. An enlarged view of the selected section in Figure 2c.

Figure S3. An enlarged view of the selected section in Figure 2f.

Figure S4. A typical 1H NMR spectrum of liquid products over CuO/SiO2-3 at -2.38 V after ECO2RR in flow cell.

Figure S5. Total current density at various potentials on CuO/SiO2-3.

Figure S6. Comparison of electrochemical performances of jC2+ alcohols vs. FEC2+ alcohols during ECO2RR on Cu-based electrocatalysts in flow cell.

Figure S7. EDX element line scan of (a) CuO/SiO2-2 and (b) CuO/SiO2-4.

Figure S8. FE values of various products at -2.38 V over CuO/SiO2-n (n=1, 2 and 4).

Figure S9. EDX element line scan of CuO-3.

Figure S10. FE values of various products at -2.38 V over CuO-3.

Figure S11. n-PrOH FE and partial current density on CuO-3 at various potentials.

Figure S12. In situ Raman spectroscopy at various potentials over CuO/SiO2-1.

Figure S13. In situ Raman spectroscopy at various potentials over CuO/SiO2-4.

Table S1 Comparison of electrochemical performances for CO2 reduction to n-PrOH on Cu-based electrocatalysts in flow cell and H-type cell. The given potential is iR-corrected one for the sake of comparison.

| catalyst | FEn-PrOH (%) | jn-PrOH (mA cm-2) | E (V vs. RHE) | cell | Ref. |
| --- | --- | --- | --- | --- | --- |
| Activated Cu mesh | 13.1 | ＜2 | -0.9 | H cell | ACS Catal. 2017, 7, 7946 |
| Pd9Cu91 catalyst | 13.7 | 1.15 | -0.65 | H cell | Green Chem. 2020, 22, 6497 |
| Cu-NC20 | ∼10.6 | 1.50 | -0.95 | H cell | - Phys. Chem. Lett. 2016, 7, 20 |
| Cu-on-Cu3N | 6 | 1.3 | -0.95 | H cell | Nat. Commun. 2018, 9, 3828 |
| Cu2O nanostructure | 12.6 | 0.65 | -0.3 | H cell | ACS Appl. Mater. Interfaces 2021, 13, 39165 |
| Hex-2Cu-O | 18.3 ~8 | 2.2 ~21.0 | -1.2 -0.66 | H cell flow-cell | Nat. Commun. 2022, 13, 5122 |
| CuSx with double-sulfur vacancy | 15.4 ~3.8 | 3.1 9.9 | -1.05 -0.85 | H cell flow-cell | Nat. Commun. 2021, 12, 1580 |
| modified Cu2S | 8.0 7.0 | 2.5 27.9 | -0.95 -0.92 | H cell flow-cell | Nat. Catal. 2018, 1, 421 |
| NGQ/Cu-nr | ~7 | ~20.0 | -0.9 | flow-cell | Angew. Chem. Int. Ed. 2020, 59, 1 |
| CuO/SiO2-3 | 13.3 | 94.0 | -0.81 | flow-cell | This work |

Table S2 Comparison of electrochemical performances for CO2 reduction to C2+ alcohols on Cu-based electrocatalysts in flow cell.

| catalyst | FEC2+ alcohols (%) | jC2+ alcohols (mA cm-2) | E (V vs. RHE) | Ref. |
| --- | --- | --- | --- | --- |
| NGQ/Cu-nr | 52.4 | 147.8 | -0.9 | Angew. Chem. Int. Ed. 2020, 59, 16459 |
| FeTPP[Cl]/Cu | 41 | 124 | -0.82 | Nat. Catal. 2020, 3, 75 |
| Ce(OH)x/Cu | 42.6 | 128 | -0.7 | Nat. Commun. 2019, 10, 5814 |
| Defect-Site-Rich Cu Surface | 67 | 100 | -0.95 | Joule 2021, 5, 429 |
| Cu2S-Cu-vacancy | 31.6 | 126 | -0.85 | Nat. Catal. 2018, 1, 421 |
| Cu-DAT | 30.8 | 81.2 | -0.69 | ACS Catal. 2017, 7, 3313 |
| CuOx@C | 49 | 176 | -1.0 | Angew. Chem. Int. Ed. 2022, 61, e2022096 |
| Cu(B) | 27 | 70 | -1.1 | Nat. Chem. 2018, 10, 974 |
| CuO/SiO2-3 | 45.7 | 322.8 | -0.81 | This work |