The effects of the geometry parameters and oxidation on the localized surface plasmon resonance properties of copper nanoparticle thin film via calculation

Zhonghua Liu1#, Bing Xu1#,Yuqing Chen2, Mengting Si3, Xiangqian Chu1, Yingcui Fang1*, Mengtao Sun2*

1Department of Vacuum Science and Technology, Hefei University of Technology, Hefei 230009, China

2School of Mathematics and Physics, University of Science and Technology Beijing, Beijing 100083, China.

3 School of Physics, Peking University, Beijing 100083, China.

*Corresponding author: ycfang@hfut.edu.cn, mengtaosun@ustb.edu.cn (M. T. Sun)

1. Table S1 The evolution of resonance wavelength with the diameters of the nanoparticles (D) and the interparticle distance (L/D).

| D (nm) | L/D | Resonance Wavelength(nm) |  |  |
| --- | --- | --- | --- | --- |
|  |  | n=1 | n=1.5 | n=2 |
| 5 | 2 | 540 | 580 | 610 |
|  | 1.5 | 540 | 580 | 620 |
|  | 1.1 | 560 | 600 | 640 |
|  | 1.01 | 570 | 630 | 720 |
| 10 | 2 | 540 | 580 | 610 |
|  | 1.5 | 540 | 580 | 620 |
|  | 1.1 | 560 | 600 | 650 |
|  | 1.01 | 570 | 630 | 730 |
| 15 | 2 | 540 | 580 | 610 |
|  | 1.5 | 540 | 580 | 620 |
|  | 1.1 | 560 | 600 | 650 |
|  | 1.01 | 570 | 630 | 730 |
| 50 | 2 | 550 | 590 | 640 |
|  | 1.5 | 540 | 600 | 650 |
|  | 1.1 | 560 | 620 | 740 |
|  | 1.01 | 580 | 660 | >800 |

2. The schematic diagram shown how to determine the average nanoparticle size D, the average thickness t, and the average distance L between two nanoparticles of Figure 4c.

L

The mean t is 4.682 nm

The mean D is 35.864 nm

The mean L is 66.348 nm

3. Table S2. The redshift amount of the LSPR with n and t/R, when L/D decreased from 2 to 1.01.

| n | Redshift(nm) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | t/R=0.1 | 0.2 | 0.3 | 0.4 | 0.5 | 0.6 |
| 1 | 15 | 10 | 5 | 10 | 5 | 5 |
| 1.5 | 30 | 15 | 15 | 10 | 5 | 5 |
| 2 | 45 | 25 | 15 | 15 | 10 | 0 |