Supporting information

Synthesis and application of novel benzophenone photoinitiators

Chao Feng1 QinLin Wang1 Feng Liu1,* BianXiang Zhang1,*

School of Chemistry and Chemical Engineering, Shanxi University, Taiyuan 030006, China

Catalogue

Supporting information	1

Catalogue	2

Instruments and Reagents	3

Experimental Method	3

Preparation of Cured Film	3

Synthetic Data and UV Spectra	4

Physical and Chemical Data	8

Spectrogram	14

Properties of Cured Film	41

# Instruments and Reagents

1H NMR and 13C NMR were measured in CDCl3 (internal standard TMS) using a Bruker AVANCE III 600 MHz spectrometer. High - resolution mass spectra were tested on a Thermo Scientific Q Exactive mass spectrometer. Melting point tester (XT - 5 type). The ultraviolet - visible absorption spectrum was measured in CH2Cl2 (1x10-5 M) using a Hitachi UH - 5300 ultraviolet spectrophotometer (Hitachi High - Tech Group). The photocuring test of the film was carried out on a UV curing machine (ZB - T150 - UV1000). Film hardness was tested using a portable pencil scratch hardness tester (QHQ - A).

All reagents used were commercially available AR unless otherwise specified. 1, 6 - Hexanediol diacrylate (HDDA) and polyurethane acrylic resin (UV - 2100) were provided by Jiangsu Sanmu Group. 1 - Hydroxycyclohexyl phenyl ketone (Irgacure 184) and benzophenone (BP) were provided by Beijing Yingli Fine Chemical Technology Development Co., Ltd.

# Experimental Method

The substitution reaction of benzophenone and acid chloride or sulfonyl chloride is carried out under milder conditions. Add triethylamine (1.0 mmol) after dissolving in THF, pass through N2, ice - water bath until the system temperature is 0 °C, add acid chlorides 2a - 2f (1.2 mmol) or sulfonyl chlorides 4a - 4b (1.2 mmol), react for 1 h the temperature was raised to room temperature for reaction, and the reaction was stopped after 2 h. The target products 3 and 5 were obtained after extraction, solvent removal, and column chromatography separation.

# Preparation of Cured Film

The product 3 (0.3 g) obtained from the above reaction was dissolved in the monomer (HDDA, 0.45 g) as a photoinitiator, and polyurethane acrylic resin (UV - 2100, 0.50 g) was added to make a transparent coating solution, and stirred evenly until transparent, remove the air bubbles, if there are still air bubbles, use an ultrasonic machine to remove them. After the air bubbles completely disappeared, apply it on a clean glass plate with an applicator, the thickness of the coating is 75 m, irradiate and cure under a medium - pressure mercury lamp with a power of 1000 w, record the curing time.

Gel content was determined by solvent extraction. The cured film was baked at 60 °C for 3 hours and weighed as M1. After soaking in absolute ethanol solution for 24 hours, the filtered solid matter was dried and weighed as M2. The gel content was calculated according to the following formula.

Gel content=M2/M1×100%

# Synthetic Data and UV Spectra

Table 1 Reaction of benzophenone and acid chloride

| Entry | Compound 1 | Acyl chloride 2 | Product 3 (Yield%) | max (nm) | (L mol-1 cm-1) |
| --- | --- | --- | --- | --- | --- |
| 1 |  |  |  | 282 | 3.02×104 |
| 2 | 1a |  |  | 283 | 3.34×104 |
| 3 | 1a |  |  | 285 | 2.73×104 |
| 4 | 1a |  |  | 278 | 4.77×104 |
| 5 | 1a |  |  | 282 | 2.48×104 |
| 6 | 1a |  |  | 283 | 5.83×104 |
| 7 |  | 2f |  | 284 | 6.04×104 |
| 8 |  | 2f |  | 310 | 3.00×104 |
| 9 |  | 2f |  | 264 | 8.16×104 |
|  |  |  |  | 262 | 8.07×104 |

Table 2 Reaction of Benzophenone 1 with Sulfonyl Chloride 4

| Entry | Compound 1 | Acyl chloride 4 | Product 5 (Yield%) | max (nm) | (L mol-1 cm-1) |
| --- | --- | --- | --- | --- | --- |
| 1 | 1a | 4a |  | 277 | 4.15×104 |
| 2 | 1b | 4a |  | 277 | 5.30×104 |
| 3 | 1c | 4a |  | 311 | 2.46×104 |
| 4 | 1d | 4a |  | 262 | 7.94×104 |
| 5 | 1a | 4b |  | 276 | 3.69×104 |
| 6 | 1b | 4b |  | 283 | 5.06×104 |
| 7 | 1c | 4b |  | 311 | 2.70×104 |
| 8 | 1d | 4b |  | 261 | 8.38×104 |

Ts: 4-Methylbenzenesulfonyl

Table 3 Absorption wavelength and molar absorption coefficient of BP and product 3

| Entry |  | λ(nm) |  | ε(L(mol-1cm-1)) |  |  | Entry | λ(nm) | ε(L(mol-1cm-1)) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| BP |  | 249 |  | 3.27×104 |  |  | 3e | 241 | 4.78×104 |
|  |  | 280 |  | 1.24×104 |  |  |  | 282 | 2.48×104 |
| 3a |  | 247 |  | 5.97×104 |  |  | 3f | 230 252 | 7.33×104 6.61×104 |
|  |  | 282 |  | 3.02×104 |  |  |  | 283 | 5.83×104 |
| 3b |  | 241 |  | 5.12×104 |  |  | 3g | 230 256 | 7.29×104 4.25×104 |
|  |  | 283 |  | 3.34×104 |  |  |  | 276 | 3.69×104 |
| 3c |  | 256 |  | 5.35×104 |  |  | 3h | 234 256 | 6.64×104 4.78×104 |
|  |  | 285 |  | 2.73×104 |  |  |  | 277 | 4.15×104 |
| 3d | 252 |  | 5.52×104 |  |
|  | 278 |  | 4.77×104 |  |
| Figure 2 UV absorption spectrum of product 5 and BP |  |  |  |  |  |  |  |  |  |  |

Table 4 Absorption wavelength and molar absorption coefficient of BP and product 5

| Entry | λ(nm) | ε(L(mol-1cm-1)) |  | Entry | λ(nm) | ε(L(mol-1cm-1)) |
| --- | --- | --- | --- | --- | --- | --- |
| BP | 249 | 3.27×104 |  | 5e | 227 | 3.56×104 |
|  | 280 | 1.24×104 |  |  | 264 | 8.16×104 |
| 3i | 229 251 284 | 7.41×104 6.89×104 6.04×104 |  | 5f | 227 262 | 3.20×104 8.07×104 |
| 3j | 234 256 277 | 8.42×104 5.98×104 5.30×104 |  | 5g | 228 262 | 6.30×104 7.94×104 |
| 5a | 230 256 283 | 7.99×104 6.03×104 5.06×104 |  | 5h | 227 261 | 5.31×104 8.38×104 |
| 5b | 229 251 310 | 6.09×104 8.06×104 3.00×104 |  |  |  |  |
| 5c | 231 | 8.61×104 |
|  | 250 | 7.40×104 |
|  | 311 | 2.46×104 |
| 5d | 229 | 6.59×104 |
|  | 249 | 7.96×104 |
|  | 311 | 2.70×104 |

# Physical and Chemical Data

3a，white solid，m. p.：59-61 ℃，yield：93 %。1H NMR (600 MHz, CDCl3) δ 7.75 (dd, J = 13.0, 7.9 Hz, 4H), 7.60 (d, J = 8.5 Hz, 1H), 7.46 (t, J = 7.4 Hz, 1H), 7.38 (t, J = 7.6 Hz, 2H), 7.17 (d, J = 8.0 Hz, 2H), 6.91 (dd, J = 11.4, 2.8 Hz, 2H), 6.09 (ddd, J = 15.9, 10.5, 5.3 Hz, 1H), 5.45 (dd, J = 26.5, 13.0 Hz, 1H), 5.41 – 5.30 (dd, J = 16.6 Hz, 8.1 Hz, 1H), 4.64 (d, J = 5.2 Hz, 2H), 2.45 – 2.35 (s, 3H). 13C NMR (151 MHz, CDCl3) δ 194.25, 164.67, 161.95, 150.95, 144.33, 138.51, 132.52, 132.39, 132.34, 130.10, 129.61, 129.03, 128.21, 126.14, 124.30, 118.35, 112.16, 109.69, 69.23, 21.72. HRMS (ESI) cacld for C24H20O4 (M+H)+ 373.1434, found 373.1428.

3b，white solid，m. p.：64-66 ℃，yield：83 %。1H NMR (600 MHz, CDCl3) δ 7.74 (d, J = 7.9 Hz, 2H), 7.63 (d, J = 8.6 Hz, 1H), 7.52 (dd, J = 14.0, 7.0 Hz, 3H), 7.42 (t, J = 7.5 Hz, 2H), 6.94 (dt, J = 15.3, 7.7 Hz, 1H), 6.88 (s, 1H), 6.09 (ddd, J = 16.5, 10.4, 5.2 Hz, 1H), 5.46 (dd, J = 19.6 Hz, 8.8 Hz, 1H), 5.36 (dd, J = 15.6 Hz, 8.2 Hz, 1H), 4.66 (d, J = 4.4 Hz, 2H). 13C NMR (151 MHz, CDCl3) δ 193.88, 162.19, 162.06, 151.76, 151.74, 150.51, 144.35, 138.40, 133.11, 132.62, 132.15, 129.58, 128.35, 124.92, 123.59, 118.52, 114.78, 112.44, 109.68, 69.33. HRMS (ESI) cacld for C23H15F3O4 (M+H)+ 413.0995, found 413.0990.

3c，colorless liquid，yield：90 %。1H NMR (600 MHz, CDCl3) δ 7.78 – 7.71 (m, 2H), 7.58 (dd, J = 14.3, 4.5 Hz, 2H), 7.50 – 7.45 (m, 1H), 7.43 – 7.36 (m, 2H), 7.00 (dd, J = 15.1, 2.9 Hz, 1H), 6.94 – 6.88 (m, 2H), 6.46 (dd, J = 3.4, 1.6 Hz, 1H), 6.08 (ddd, J = 15.8, 10.5, 5.3 Hz, 1H), 5.47 (dd, J = 17.3 Hz, 8.1 Hz, 1H), 5.36 (dd, J = 10.5 Hz, 7.1 Hz, 1H), 4.67 – 4.59 (m, 2H). 13C NMR (151 MHz, CDCl3) δ 194.14, 161.97, 159.94, 150.41, 138.43, 134.77, 133.64, 132.61, 132.41, 132.28, 132.14, 129.60, 128.24, 127.76, 124.18, 118.40, 112.40, 109.62, 69.26. HRMS (ESI) cacld for C21H16O5 (M+H)+ 349.1071, found 349.1067.

3d，light brown liquid，yield：87 %。1H NMR (600 MHz, CDCl3) δ 7.75 (t, J = 10.5 Hz, 2H), 7.68 – 7.64 (m, 1H), 7.59 (t, J = 8.1 Hz, 1H), 7.58 (s, 1H), 7.46 (t, J = 7.4 Hz, 1H), 7.37 (dd, J = 16.7, 9.2 Hz, 2H), 7.07 – 7.03 (m, 1H), 6.92 (dd, J = 10.8, 2.1 Hz, 2H), 6.09 (ddd, J = 22.4, 10.5, 5.3 Hz, 1H), 5.47 (dd, J = 17.3, 1.2 Hz, 1H), 5.35 (dd, J = 10.3 Hz, 1H), 4.66 (m, 2H). 13C NMR (151 MHz, CDCl3) δ 194.04, 162.01, 156.21, 150.12, 147.21, 143.39, 138.42, 132.71, 132.40, 132.25, 129.61, 128.20, 124.08, 119.55, 118.44, 112.35, 112.03, 109.67, 69.27. HRMS (ESI) cacld for C21H16O4S (M+H)+ 365.0842, found 365.0837.

3e，brown liquid，yield79 %。1H NMR (600 MHz, CDCl3) δ 7.81 – 7.73 (m, 2H), 7.62 – 7.56 (m, 1H), 7.47 (dd, J = 11.9, 5.5 Hz, 3H), 7.33 – 7.25 (m, 5H), 7.22 (d, J = 28.7 Hz, 5H), 6.81 (dt, J = 25.4, 7.6 Hz, 2H), 6.11 – 6.00 (m, 1H), 5.43 (dd, J = 15.5 Hz, 8.1 Hz, 1H), 5.32 (dd, J = 15.2, 8.6 Hz, 1H), 4.63 – 4.56 (m, 2H). 13C NMR (151 MHz, CDCl3) δ 194.22, 161.83, 152.20, 151.02, 138.46, 132.53, 132.44, 132.35, 129.82, 128.92, 128.27, 124.27, 118.25, 111.85, 109.45, 69.17. HRMS (ESI) cacld for C29H23NO4 (M+H)+ 450.1700, found 450.1701.

3f，light yellow oily liquid，yield: 49 %。1H NMR (600 MHz, CDCl3) δ 7.82 – 7.64 (m, 2H), 7.62 – 7.36 (m, 4H), 6.99 – 6.48 (m, 2H), 6.11 – 5.97 (m, 1H), 5.57 – 5.32 (m, 2H), 4.62 (t, J = 5.1 Hz, 2H), 1.87 – 1.66 (m, 3H), 1.34 (d, J = 76.2 Hz, 2H). 13C NMR (151 MHz, CDCl3) δ 18.21, 23.75, 30.43, 69.24, 80.94, 103.98, 109.41, 111.93, 118.55, 124.39, 128.41, 129.98, 132.23, 135.07, 137.86, 150.11, 161.71, 165.26, 170.34, 193.53. HRMS (ESI) cacld for C20H18O4 (M+H)+ 323.1278, found 323.1281.

3g, light yellow oily liquid，yield: 56 %。1H NMR (600 MHz, CDCl3) δ 7.81 – 7.72 (m, 2H), 7.61 – 7.41 (m, 5H), 6.90 – 6.65 (m, 3H), 5.55 (s, 1H), 3.89 (d, J = 4.8 Hz, 3H), 1.41 (s, 1H), 1.27 (s, 2H). 13C NMR (151 MHz, CDCl3) δ 18.02, 23.77, 25.32, 30.44, 55.82, 108.74, 111.45, 123.91, 128.22, 129.51, 132.42, 134.96, 138.56, 151.05, 163.05, 165.28, 170.39, 194.36. HRMS (ESI) cacld for C18H16O4 (M+H)+ 297.1121, found 297.1124.

3h, light yellow oily liquid，yield: 41 %。1H NMR (600 MHz, CDCl3) δ 7.86 – 7.79 (m, 2H), 7.42 (dt, J = 10.5, 5.2 Hz, 1H), 7.20 (d, J = 8.7 Hz, 1H), 7.16 – 7.10 (m, 1H), 6.57 (ddd, J = 8.5, 2.4, 1.2 Hz, 1H), 6.53 (t, J = 2.9 Hz, 1H), 3.89 (s, 3H), 3.73 (d, J = 5.5 Hz, 3H), 2.09 (s, 2H), 1.80 – 1.69 (m, 3H). 13C NMR (151 MHz, CDCl3) δ 18.38, 24.67, 25.51, 30.68, 55.58, 81.13, 98.79, 104.06, 104.58, 120.96, 121.26, 127.80, 131.29, 132.20, 135.61, 136.29, 136.75, 154.14, 159.56, 163.44, 165.38, 194.41. HRMS (ESI) cacld for C19H18O5 (M+H)+ 327.1227, found 327.1230.

3i, white flaky solid，m. p.147-148℃, yield: 62 %。1H NMR (600 MHz, CDCl3) δ 7.89 – 7.84 (m, 2H), 7.80 – 7.75 (m, 2H), 7.53 – 7.45 (m, 2H), 7.30 – 7.27 (m, 2H), 6.41 (t, J = 1.1 Hz, 1H), 5.83 (q, J = 1.5 Hz, 1H), 2.10 (t, J = 1.3 Hz, 3H). 13C NMR (151 MHz, CDCl3) δ 18.37, 121.76, 127.94, 128.72, 131.39, 131.58, 134.66, 135.51, 135.80, 138.97, 154.38, 165.99, 194.33. HRMS (ESI) cacld for C17H13ClO3 (M+H)+ 301.0626, found 301.0629.

3j, white lumpy solid，m. p.80-82℃, yield: 23 %。1H NMR (600 MHz, CDCl3) δ 7.85 (d, J = 8.7 Hz, 2H), 7.76 (d, J = 8.5 Hz, 2H), 7.48 (d, J = 8.6 Hz, 2H), 7.22 (d, J = 7.4 Hz, 2H), 2.52 – 2.44 (m, 1H), 1.75 (d, J = 10.7 Hz, 6H).13C NMR (151 MHz, CDCl3) δ 18.22, 24.70, 25.46, 30.75, 81.14, 104.15, 121.44, 128.74, 131.38, 131.59, 135.16, 135.70, 136.51, 139.12, 153.84, 170.99, 194.18. HRMS (ESI) cacld for C17H15ClO3 (M+H)+ 303.0782, found 303.0597.

5a, yellow-white solid, yield: 46 %, m. p.81-83 ℃。1H NMR (600 MHz, CDCl3) δ 7.66 – 7.33 (m, 8H), 7.15 (d, J = 7.9 Hz, 2H), 7.00 – 6.82 (m, 2H), 6.05 (ddt, J = 16.4, 10.7, 5.2 Hz, 1H), 5.40 (dd, J = 56.0, 13.9 Hz, 2H), 4.59 (d, J = 5.3 Hz, 2H), 2.35 (s, 3H). 13C NMR (151 MHz, CDCl3) δ 21.70, 69.31, 110.09, 113.50, 118.61, 125.48, 128.02, 128.50, 129.67, 130.01, 131.81, 132.06, 132.24, 132.85, 137.26, 145.49, 147.95, 161.53, 192.87. HRMS (ESI) cacld for C23H20O5S (M+H)+ 409.1104, found 409.1109.

5b, Pale yellow lumpy solid, yield: 62 %, m. p.76-78 ℃。1H NMR (600 MHz, CDCl3) δ 7.68 – 7.35 (m, 8H), 7.15 (d, J = 7.9 Hz, 2H), 6.99 – 6.81 (m, 2H), 3.87 (s, 3H), 2.35 (s, 3H). 13C NMR (151 MHz, CDCl3) δ 21.66, 55.81, 109.47, 112.70, 125.38, 128.09, 128.49, 129.66, 130.06, 131.72, 132.36, 132.83, 137.33, 145.45, 148.04, 162.58, 192.83. HRMS (ESI) cacld for C21H18O5S (M+H)+ 383.0948, found 383.0949.

5c, light yellow oily liquid，yield: 94 %。1H NMR (600 MHz, CDCl3) δ 7.81 – 7.65 (m, 4H), 7.42 (d, J = 8.5 Hz, 1H), 7.33 (d, J = 8.1 Hz, 2H), 7.08 – 6.97 (m, 2H), 6.59 – 6.49 (m, 2H), 3.89 (s, 3H), 3.69 (s, 3H), 2.47 (s, 3H). 13C NMR (151 MHz, CDCl3) δ 21.76, 55.48, 55.56, 98.77, 104.78, 120.86, 121.95, 128.61, 129.87, 131.23, 132.14, 132.40, 137.65, 145.67, 152.35, 159.64, 163.75, 194.13. HRMS (ESI) cacld for C22H20O6S (M+H)+ 413.1053, found 413.1057.

5d, white snowflake solid, yield: 95 %, m. p.121-123 ℃。1H NMR (600 MHz, CDCl3) δ 7.78 – 7.71 (m, 6H), 7.52 – 7.46 (m, 2H), 7.36 (d, J = 8.1 Hz, 2H), 7.17 – 7.11 (m, 2H), 2.48 (s, 3H). 13C NMR (151 MHz, CDCl3) δ 21.79, 122.39, 128.53, 128.81, 129.98, 131.34, 131.68, 132.13, 135.35, 135.86, 139.33, 145.85, 152.67, 194.10. HRMS (ESI) cacld for C20H15ClO4S (M+H)+ 387.0452, found 387.0455.

5e, yellow-white solid, yield: 53 %, m. p.144-145 ℃。1H NMR (600 MHz, CDCl3) δ 7.70 – 7.54 (m, 5H), 7.45 – 7.37 (m, 3H), 7.08 – 6.91 (m, 4H), 6.06 (ddt, J = 17.4, 10.5, 5.3 Hz, 1H), 5.61 – 5.24 (m, 2H), 4.62 (dt, J = 5.4, 1.6 Hz, 2H). 13C NMR (151 MHz, CDCl3) δ 69.37, 110.18, 113.63, 116.40, 116.52, 118.64, 125.30, 128.22, 130.00, 130.80, 130.83, 131.38, 131.44, 132.03, 132.29, 133.03, 137.24, 147.90, 161.67, 165.48, 167.17, 192.73, 215.04. HRMS (ESI) cacld for C22H17FO5S (M+H)+ 413.0853, found 413.0859.

5f, Pale yellow flaky solid, yield: 89 %, m. p.108-110℃, 1H NMR (600 MHz, CDCl3) δ 7.71 – 7.50 (m, 5H), 7.47 – 7.38 (m, 3H), 7.05 (t, J = 8.5 Hz, 2H), 6.98 – 6.87 (m, 2H), 3.90 (s, 3H). 13C NMR (151 MHz, CDCl3) δ 55.88, 109.50, 112.89, 116.37, 116.52, 125.22, 128.20, 129.97, 130.88, 131.38, 131.44, 132.32, 133.01, 137.26, 147.75, 162.69, 165.21, 166.92, 192.65. HRMS (ESI) cacld for C20H15FO5S (M+H)+ 387.0697, found 387.0699.

5g, light yellow oily liquid，yield: 95 %。1H NMR (600 MHz, CDCl3) δ 7.94 – 7.80 (m, 2H), 7.76 – 7.69 (m, 2H), 7.42 (d, J = 8.5 Hz, 1H), 7.23 (t, J = 8.4 Hz, 2H), 7.09 – 7.02 (m, 2H), 6.60 – 6.47 (m, 2H), 3.89 (s, 3H), 3.69 (s, 3H). 13C NMR (151 MHz, CDCl3) δ 55.53, 55.59, 98.81, 104.89, 116.64, 116.79, 120.76, 121.86, 131.32, 132.44, 137.92, 152.07, 159.65, 163.82, 165.27, 166.98, 194.18. HRMS (ESI) cacld for C21H17FO6S (M+H)+ 417.0803, found 417.0808.

5h, white snowflake solid. yield: 93 %, m. p.180-181 ℃。1H NMR (600 MHz, CDCl3) δ 7.97 – 7.87 (m, 2H), 7.81 – 7.71 (m, 4H), 7.52 – 7.45 (m, 2H), 7.28 – 7.24 (m, 2H), 7.19 – 7.13 (m, 2H). 13C NMR (151 MHz, CDCl3) δ 116.77, 116.91, 122.37, 128.85, 131.37, 131.44, 131.73, 135.18, 136.10, 139.38, 152.36, 165.36, 167.07, 193.96. HRMS (ESI) cacld for C19H12ClFO4S (M+H)+ 391.0202, found 391.0205.

# Spectrogram

| Sample No. | Formula (M) | Ion Formula | Measured m/z | Calc m/z |
| --- | --- | --- | --- | --- |
| 3a | C24H20O4 | C24H21O4 | 373.1428 | 373.1434 |

| Sample No. | Formula (M) | Ion Formula | Measured m/z | Calc m/z |
| --- | --- | --- | --- | --- |
| 3b | C23H15F3O4 | C23H16F3O4 | 413.0990 | 413.0995 |

| Sample No. | Formula (M) | Ion Formula | Measured m/z | Calc m/z |
| --- | --- | --- | --- | --- |
| 3c | C21H16O5 | C21H17O5 | 349.1067 | 349.1071 |

| Sample No. | Formula (M) | Ion Formula | Measured m/z | Calc m/z |
| --- | --- | --- | --- | --- |
| 3d | C21H16O4S | C21H17O4S | 365.0837 | 365.0842 |

| Sample No. | Formula (M) | Ion Formula | Measured m/z | Calc m/z |
| --- | --- | --- | --- | --- |
| 3e | C29H23NO4 | C29H24NO4 | 450.1701 | 450.1700 |

| Sample No. | Formula (M) | Ion Formula | Measured m/z | Calc m/z |
| --- | --- | --- | --- | --- |
| 3f | C20H18O4 | C20H19O4 | 323.1281 | 323.1278 |

| Sample No. | Formula (M) | Ion Formula | Measured m/z | Calc m/z |
| --- | --- | --- | --- | --- |
| 3g | C18H16O4 | C18H16O4 | 297.1124 | 297.1121 |

| Sample No. | Formula (M) | Ion Formula | Measured m/z | Calc m/z |
| --- | --- | --- | --- | --- |
| 3h | C19H18O5 | C19H19O5 | 327.1230 | 327.1227 |

| Sample No. | Formula (M) | Ion Formula | Measured m/z | Calc m/z |
| --- | --- | --- | --- | --- |
| 3i | C17H13ClO3 | C17H14ClO3 | 301.0629 | 301.0626 |

| Sample No. | Formula (M) | Ion Formula | Measured m/z | Calc m/z |
| --- | --- | --- | --- | --- |
| 3j | C17H15ClO3 | C17H16ClO3 | 303.0597 | 303.0782 |

| Sample No. | Formula (M) | Ion Formula | Measured m/z | Calc m/z |
| --- | --- | --- | --- | --- |
| 5a | C23H20O5S | C23H21O5S | 409.1109 | 409.1104 |

| Sample No. | Formula (M) | Ion Formula | Measured m/z | Calc m/z |
| --- | --- | --- | --- | --- |
| 5b | C21H18O5S | C21H19O5S | 383.0949 | 383.0948 |

| Sample No. | Formula (M) | Ion Formula | Measured m/z | Calc m/z |
| --- | --- | --- | --- | --- |
| 5c | C22H20O6S | C22H21O6S | 413.1057 | 413.1053 |

| Sample No. | Formula (M) | Ion Formula | Measured m/z | Calc m/z |
| --- | --- | --- | --- | --- |
| 5d | C20H15ClO4S | C20H16ClO4S | 387.0455 | 387.0452 |

| Sample No. | Formula (M) | Ion Formula | Measured m/z | Calc m/z |
| --- | --- | --- | --- | --- |
| 5e | C22H17FO5S | C22H18FO5S | 413.0859 | 413.0853 |

| Sample No. | Formula (M) | Ion Formula | Measured m/z | Calc m/z |
| --- | --- | --- | --- | --- |
| 5f | C20H15FO5S | C20H16FO5S | 387.0699 | 387.0697 |

| Sample No. | Formula (M) | Ion Formula | Measured m/z | Calc m/z |
| --- | --- | --- | --- | --- |
| 5g | C21H17FO6S | C21H17FO6S | 417.0808 | 417.0803 |

| Sample No. | Formula (M) | Ion Formula | Measured m/z | Calc m/z |
| --- | --- | --- | --- | --- |
| 5h | C19H12ClFO4S | C19H13ClFO4S | 391.0205 | 391.0202 |

# Properties of Cured Film

Table 5 UV-curing performance of compounds 3, BP, and Irgacure 184

| Entry | photoinitiators | Gloss | Curing timea (s) | Adhesionb | Pencil hardnessc | Gel content (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 3a | Smooth and transparent | 10 | 1 | 4H | 94.3 |
| 2 | 3b | Smooth and transparent | 10 | 0 | 5H | 95.4 |
| 3 | 3c | Smooth and transparent | 40 | 1 | 4H | 98.1 |
| 4 | 3d | Smooth and transparent | 40 | 1 | 3H | 95.2 |
| 5 | 3e | Smooth and transparent | 20 | 2 | 3H | 94.8 |
| 6 | 3f | Frosted and transparent | 36 | 1 | 3H | 93.2 |
| 7 | 3g | Smooth and transparent | 33 | 1 | 3H | 96.7 |
| 8 | 3h | Frosted and transparent | 12 | 1 | 2H | 96.1 |
| 9 | 3i | Frosted and transparent | 50 | 3 | 4H | 96.3 |
| 10 | 3j | Frosted and transparent | 12 | 0 | 4H | 96.2 |
| / | BP | Smooth and transparent | 20 | 1 | 3H | 94.3 |
| / | 184 | Smooth and transparent | 20 | 2 | 4H | 96.2 |

Table 5 UV-curing performance of compounds 5, BP, and Irgacure 184

| Entry | photoinitiators | Gloss | Curing timea (s) | Adhesionb | Pencil hardnessc | Gel content (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 5a | Smooth and transparent | 16 | 1 | 4H | 97.0 |
| 2 | 5b | Frosted and transparent | 18 | 1 | 3H | 96.9 |
| 3 | 5c | Smooth and transparent | 15 | 0 | 3H | 94.5 |
| 4 | 5d | Frosted and transparent | 10 | 0 | 5H | 96.6 |
| 5 | 5e | Smooth and transparent | 10 | 0 | 5H | 96.7 |
| 6 | 5f | Smooth and transparent | 15 | 0 | 4H | 96.8 |
| 7 | 5g | Smooth and transparent | 12 | 0 | 4H | 96.4 |
| 8 | 5h | Frosted and transparent | 12 | 0 | 5H | 96.9 |
| / | BP | Smooth and transparent | 20 | 1 | 3H | 94.3 |
| / | 184 | Smooth and transparent | 20 | 2 | 4H | 96.2 |