Supplementary Information

Probabilistic Computing with NbOx Mott Memristor-based Self-oscillatory pbit

Hakseung Rhee, Gwangmin Kim, Hanchan Song, Woojoon Park, Do Hoon Kim, Jae Hyun In, and Kyung Min Kim*

Department of Materials Science and Engineering, Korea Advanced Institute of Science and Technology (KAIST), Daejeon, 34141, Republic of Korea

*Correspondence and requests for materials should be addressed to K.M.K. (Email: km.kim@kaist.ac.kr)

Figure S1. Oscillation dataset of NbOx oscillator. Five tests were performed for each external voltage (Vext) condition. For each test, the current oscillations were measured under 30 μs width of a single Vext pulse. The data collection process for Vext cases involved collecting data once for all Vext cases initially and then repeating the process four more times for each Vext case individually.

| Parameter | Value | Units |
| --- | --- | --- |
| d | 15.0E-9 | m |
| A | 12.56E-16 | m2 |
| q | 1.60E-19 | C |
| kB | 8.617E-5 | eV/K |
| σ0 | 8.40E+4 | S/m |
| Ea | 0.255 | eV |
| Cth | 5.0E-17 | Ws/K |
| Rth.I | 1.70E+6 | K/W |
| Rth.M | 2.20E+6 | K/W |
| p | 100 | - |
| Tamb | 300 | K |
| Tmott | 1070 | K |

Table S1. Parameters used in NbOx mott memristor-based numerical oscillator model.

Supplementary Note 1. Simulational derivation of Tmott as a threshold for the occurrence of oscillations

Figure S2a shows the equilibrium I-V curve (black) obtained from the numerical model by Equation 1-4, where dT/dt = 0 and dv/dt = 0. The blue dashed line shows the load line by RL = 1.2 kΩ at Vext = 1.40 V. Figure S2b enlarges the T-V curve near the mott transition region. At the given load line, the operating point (blue dot) is at the positive differential resistance region above the NDR-2 region, so the self-oscillator is not oscillating but stays at the on-state.

At the equilibrium state, the perturbation may change the operating point to the metastable space.1,2 Once it happens, the time-dependent temperature gradient (dT/dt) and voltage gradient (dv/dt) at the point act as a restoring force that drives it to an equilibrium point. Figure S2c and S2d show the calculated dv/dt and dT/dt vectors on the T-V space, respectively. The black lines are equilibrium lines giving dv/dt = 0 and dT/dt = 0, which are equal to the load line and equilibrium T-V curve. In Figure S2d, the dT/dt was abruptly changed at the mott transition temperature (Tmott) due to the drastic change of Rth between the metallic phase (Rth,M) and the insulating phase (Rth,I). By using the two gradient vectors, the trajectory from the metastable state to the equilibrium state over time can be estimated. Figure S2e shows the schematics of two perturbation results in a completely different trajectory; one is a larger voltage perturbation case (black arrow), and the other is a smaller voltage perturbation case (red arrow). The t0,(v0, T0) is the equilibrium point which is defined by the intersection of dv/dt = 0 and dT/dt = 0 at a given Vext. When external voltage perturbation (vpert, blue vector) is engaged to t0, it tends to go to t0,(v0+vpert, T0). However, due to the restore forces (yellow vector), the metastable state after dt can be defined by t1v1, T1=t1v0+vpert+dvdtt0,dt, T0+dTdtt0,dt (black vector). As such, the sum of perturbation and restore forces gives the metastable points trajectory toward the equilibrium point over time. This results in a spiral tn(vn, Tn) trajectory at the T-V space. Here, when the perturbation was small, the metastable state temperature was kept higher than the Tmott and it eventually converged to the initial equilibrium state (red trajectory). Whereas, when the perturbation was large, the metastable temperature dropped below the Tmott, so the temperature gradient drastically increased negatively due to the metallic-to-insulator transition. This resulted in a cooling down of the NbOx device to the off-state (black trajectory). Then, due to the positive voltage gradient at the off-state, the v increased until it exceeded the Vth, and the device returned to the on-state, generating an oscillation peak. Then, it converged to the initial equilibrium state. As a result, perturbation-induced oscillation could be possible when the perturbation was sufficient. In addition to voltage perturbation, temperature perturbation can be considered similarly.

Figure S2f-h show the perturbation-induced oscillation generation by intentionally applying a perturbing pulse in the numerical simulation model. Before that, we investigated the boundary condition of Vext between the periodic oscillation and no oscillation as shown in Figure S2f. The model confirmed that the Vext under 1.33 V generated the periodic oscillation, and over 1.40 V showed no oscillation at the on-state. Next, we set the device to the on-state (Vext = 1.40 V) and then inserted the following three perturbing pulses: 1.30 V for 5 ns (P1, red), 1.33 V for 5 ns (P2, green), and 1.30 V for 1 ns (P3, blue) as shown in the top panel of Figure S2g. The lower panel shows the output currents for three perturbating cases. Despite all voltage conditions corresponding to the oscillation condition, only P1 generated an oscillation. Figure S2h shows the tn(vn, Tn) trajectory of the three cases. The perturbation by P1 was sufficiently large to cause the temperature to go down below the Tmott. Whereas the perturbation by P2 and P3 was weak, making the non-equilibrium state converge to the equilibrium point via a small spiral trajectory. Thus, these simulation results show that Tmott corresponds to the threshold for the occurrence of oscillation generation for the metastable state of the NbOx oscillator.

Figure S2. Detailed discussion on the noise-driven oscillation in NbOx oscillator model. a Simulational I-V curve by the current sweep (black) and temperature sweep (red), and load line (blue dotted) at Vext = 1.40 V, RL = 1.2 kΩ. (i) The inset is the corresponding T-V curve. b The magnified T-V curve around the NDR-2 and the load line. c, d dv/dt and dT/dt vector maps around the NDR-2. e The pseudo-equilibrium state trajectories (black and red vectors) in the T-V space by the negative voltage perturbation (blue vector) from the equilibrium state. The purple and yellow vectors represent the dv/dt and dT/dt, respectively. f The simulated output currents at Vext = 1.30 V, 1.33 V, and 1.40 V from the numerical model. g The input voltages and corresponding output currents at various perturbating conditions (P1-P3). h The pseudo-equilibrium state trajectories near NDR-2 for P1-P3.

Supplementary Note 2. Deriving a general solution of the simultaneous equations of the Ornstein-Uhlenbeck process of the NbOx oscillator

The two stochastic differential equations (SDE) of the Ornstein-Uhlenbeck (OU) process are given as Equations 5 and 6 in main text:

Equation 5: dTt=1RthCthRthivt+Tamb-Ttdt+σTdW(t)                                 (S1)

Equation 6: dvt=1RLCmvext-RLi-vtdt+σvdW(t)                                                 (S2)

, which consists of the drift term and diffusion term.

From the simulation result of Section 2.2 in the main text, we conclude that oscillation generates due to the drastic acceleration at Tmott. Thus the temperature threshold (Tmott) is assumed as a boundary condition for oscillation generation. By solving the simultaneous equations of Equations S1 and S2, we derived the temperature variation due to collective interference by temperature and voltage noises.

First, we derived the general solution of Equation S2, the stochastic process of voltage, as follows.

dvt+1RLCmvtdt=1RLCmvext-RLidt+σvdW(t)                                                               (S3)

By multiplying etRLCm to both sides,

etRLCmdvt+etRLCm1RLCmvtdt=etRLCm1RLCmvext-RLidt+etRLCmσvdW(t)              (S4)

Equation S4 is equal to Equation S5 as below:

ddt(etRLCmvt)=etRLCm1RLCmvext-RLi+etRLCmσvdW(t)dt                                                 (S5)

By integrating both sides with respect to time from 0 to t'

d(etRLCmvt)=etRLCm1RLCmvext-RLidt+etRLCmσvdW(t)                                                 (S6)

0t'(etRLCmvt)=0t'etRLCm1RLCmvext-RLidt+etRLCmσvdW(t)                                       (S7)

et'RLCmvT-v0=vext-RLiet'RLCm-1+σv0t'etRLCmdW(t)                                  (S8)

vt'=v0e-t'RLCm+vext-RLi1-e-t'RLCm+σv0t'e-t'-tRLCmdW(t)                         (S9)

From Equation S9, we can calculate probability distribution. Because Wiener process is the definite integral of a white noise Gaussian process, it is characterized by having zero mean, unit variance3,4. Then the mean and variance of Equation S9 are calculated as below:

Evt=v0e-t'RLCm+vext-RLi1-e-t'RLCm                                                        (S10)

σ2vt=E[vt-Evt2]=RLCmσv22(1-e2t'RLCm)                                                   (S11)

and the long-term mean and variance of voltage distribution are

limt'→∞Evt=vext-RLi                                                                                                   (S12)

limt'→∞σ2[v(t)]=RLCmσv22                                                                                                        (S13)

Next, we calculate the temperature distribution induced by collective interference of temperature and voltage by putting the result of voltage variation into the voltage term in the OU process equation of temperature.

dTt=1RthCthRthivt+dTdvv∆v+Tamb-Ttdt+σTdW(t)                            (S14)

Thereafter, we assigned the voltage variation term (∆v) as ∆v=ϵ∙σvt=ϵ∙σvRLCm2 , where ϵ has a standard normal distribution N(0, 1). As a consequence, the temperature variation induced by voltage noise in infinitesimal time interval dt is described as below equation.

1RthCthdTdvv∆vdt=1RthCthdTdvvσvRLCm2ϵ∙dt                                                              (S15)

In addition, Wiener process is defined as Markov process with zero mean and variance of ∆t, thus a change during a small period of time dt, dW(t), is equal to ϵdt. Then, Equation S15 can be modified as below:

1RthCthdTdvvσvRLCm2ϵ∙dt∙dt=1RthCthdTdvvσvRLCm2dt∙dW(t)                       (S16)

As a result, the temperature variation induced by voltage noise can be included in the noise term, and the stochastic differential equation of temperature considering collective noises of temperature and voltage is described in the following equation.

dTt=1RthCthRthivt+Tamb-Ttdt+σT+1RthCthdTdvvσvRLCm∆t2dW(t)      (S17)

In the same way of calculating the mean (Equation S12) and variance (Equation S13) from Equation S2, the long-term mean and variance of Equation S17 can be calculated as below:

limt'→∞ETt=Rthivt+Tamb                                                                                                          (S18)

limt'→∞σTt=RthCth2σT+1RthCth∙dTdvv∙σvRLCm∆t2                                                           (S19)

which are Equation 7 and 8 in main text. The correspondence between this derived general solution and the numerical model (p-osc model) is illustrated in Figure S3.

Figure S3. a T-V plot of pseudo-equilibrium states of numerical oscillator model at Vext = 1.47 V, RL = 1.2 kΩ (blue dot is an equilibrium point). b Temperature histogram (red) from T-V plot and normal distribution (blue) from compact stochastic oscillator model (Equation 7 and 8) under the same condition.

Figure S4. a Probabilistic oscillation result of the numerical oscillator model with the OU process in the same case of Fig. 3 in main text as increasing the Vext from 1.25 V to 1.49 V with a 0.02 V interval. b Oscillation probability distribution calculated from the above oscillation results.

Figure S5. Autocorrelation function of all Vext conditions of experimental NbOx oscillator.

References

1.	Khovanov, I. A., Polovinkin, A. V., Luchinsky, D. G. & McClintock, P. V. E. Noise-induced escape in an excitable system. Phys. Rev. E - Stat. Nonlinear, Soft Matter Phys. 87, 1–11 (2013).

2.	Yamakou, M. E., Tran, T. D., Duc, L. H. & Jost, J. The stochastic Fitzhugh–Nagumo neuron model in the excitable regime embeds a leaky integrate-and-fire model. J. Math. Biol. 79, 509–532 (2019).

3.	Hull, J. C. Options, Futures, and Other Derivatives: Solutions Manual. Asset Pricing vol. 59 (2002).

4.	Huang, S. T. & Cambanis, S. Stochastic and Multiple Wiener Integrals for Gaussian Processes. Ann. Probab. 6, 585–614 (1978).