Supplementary Materials

Novel alginate-based binders for silicon-graphite anodes

in lithium-ion batteries: Effect of binder chemistry on the electrochemical performance

Alper Güneren*, Ahmed A. Nada, Alena Opálková Šišková, Katarína Mosnáčková, Angela Kleinová, Jaroslav Mosnáček, Zoltán Lenčéš

Fig. S1. Sp2 XPS spectrum of milled Si/Gr active material.

Fig. S2. Schematic illustration of the silicon surface interaction units for hydrogen bonding with binders and structural changes of the anode during lithiation/de-lithiation due to silicon expansion/contraction.

Fig. S3. Differential capacity plots of the anodes containing (a) CMC/SBR, (b) d-Alg, and (c) s-Alg binders during the first 5 cycles at 0.1 C-rate.

Fig. S4. Differential capacity plots of the anodes containing (a) CMC/SBR, (b) d-Alg, and (c) s-Alg binders during formation cycle and SEI formation peaks.

Table S1. Redox voltage values of the Si/Gr anodes at 0.2 C-rate at 30. cycle obtained from dQ/dV analysis.

| Binder | ###### Lithiation (V) |  |  |  | ###### Delithiation (V) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | ###### a-Li2Si | ###### a-Li2Si | ###### LiC12 | ###### a-Li3.5Si/LiC6 | ###### LiC6 | ###### LiC12 | ###### a-Li2Si | ###### a-Si |
| s-Alg pH3 | 0.30 | 0.24 | 0.2 | 0.1 | 0.09 | 0.14 | 0.23 | 0.44 |
| s-Alg pH7 | 0.30 | 0.24 | 0.2 | 0.1 | 0.09 | 0.14 | 0.23 | 0.44 |
| s-AlgpH12 | 0.30 | 0.24 | 0.2 | 0.1 | 0.09 | 0.14 | 0.23 | 0.44 |
| CMC/SBR | 0.28 | - | 0.19 | 0.09 | 0.11 | 0.15 | 0.24 | - |

| (a) | (b) |
| --- | --- |
| (c) | (d) |

Fig. S5. Differential capacity plots of the anodes containing (a) CMC/SBR, (b) s-Alg pH3,  (c) s-Alg, (c) s-Alg pH12 binder at 1st ,5th and 100th cycle.