Supporting information for:

Preparation of PDMS Composite Gel Matrix through Oxygen Tolerance Nitroxide Mediated Polymerization

Xiaoguang Qiao,a,b§* Xin Dong, b§Ge shi,b Yanjie He,b Xinchang Pang b*

aCollege of Materials Engineering, Henan International Joint Laboratory of Rare Earth Composite Materials, Henan Engineering Technology Research Center for  Fiber Preparation and Modification，Henan University of Engineering, Zhengzhou, P. R. China, 451191

bHenan Joint International Research Laboratory of Living Polymerizations and Functional Nanomaterials, Henan Key Laboratory of Advanced Nylon Materials and Application, School of Materials Science and Engineering, Zhengzhou University, Zhengzhou 450001, China

E-mail: joexiaoguang@hotmail.com

Pangxinchang1980@163.com

Figure S1.  Synthesis route for Alkoxyamine Dispolreg 007.

Figure S2.  1H NMR of the final  product

Figure S3. 1NMR analysis of the KH571, PDMS and MA-PDMS.

Figure S4. UV spectra of gel before and after chains extention with TPEE.

Characterization of crosslinking networks

To characterize the crosslinking degree of the synthetic gel, excess tetrahydrofuran (THF) was poured into the glass bottles of the gel sample and treated by ultrasonic to remove the unreacted PDMS and monomers. After removing the solution, the sample was dried in a vacuum oven and weighed for calculation.

Where W refers to the total weight before the crosslinked polymerization begins, and Wd refers to the weight of the dried gel.

To characterize swelling ratio of PDMS gel, excess tetrahydrofuran (THF) was poured into the glass bottles of the gel sample to remove unreacted monomer. After dried in a vacuum oven, the gel was immerged in solvents (toluene for tBA based PDMS and benzotrifluoride for FMA based PDMS) and kept for 24h before weighting for calculation.

Where Wd refers to the weight of the dried gel, and Ws refers to the weight of the swelling gel.