Table 1 The parameters for the milling experiment 
	[bookmark: _GoBack]Fiber direction
	Spindle speed n(rpm)
	Feed speed F(mm/min)
	Depth of axial cutting ap(mm)
	Before the angle l(°)

	0
	5000
	500
	2
	20

	45
	3000
	400
	1.5
	10

	90
	4000
	300
	3
	15

	135
	2000
	200
	2.5
	0

	multi-directional laminates 1
	2000
	200
	1.5
	10

	multi-directional laminates 2
	3000
	300
	2
	15

	multi-directional laminates 3
	4000
	400
	2.5
	10

	multi-directional laminates 4
	5000
	500
	3
	15



