Table 1 The parameters for the milling experiment

| Fiber direction | Spindle speed n(rpm) | Feed speed F(mm/min) | Depth of axial cutting ap(mm) | Before the angle l(°) |
| --- | --- | --- | --- | --- |
| 0 | 5000 | 500 | 2 | 20 |
| 45 | 3000 | 400 | 1.5 | 10 |
| 90 | 4000 | 300 | 3 | 15 |
| 135 | 2000 | 200 | 2.5 | 0 |
| multi-directional laminates 1 | 2000 | 200 | 1.5 | 10 |
| multi-directional laminates 2 | 3000 | 300 | 2 | 15 |
| multi-directional laminates 3 | 4000 | 400 | 2.5 | 10 |
| multi-directional laminates 4 | 5000 | 500 | 3 | 15 |