soil moisture content

| soil type | Serial numbers | Wet soil quality（g） | Dry soil quality（g） | Water mass (g) | Water content（%） | Mean value（%） |
| --- | --- | --- | --- | --- | --- | --- |
| Gneiss mountain soil | 1 | 303.99 | 289.29 | 14.7 | 5.08 | 7.35 |
|  | 2 | 326.34 | 305.96 | 20.38 | 6.66 |  |
|  | 3 | 328.4 | 306.71 | 21.69 | 7.07 |  |
|  | 4 | 342.23 | 315.94 | 26.29 | 8.32 |  |
|  | 5 | 355.8 | 328.47 | 27.33 | 8.32 |  |
|  | 6 | 350.2 | 322.38 | 27.82 | 8.63 |  |

soil particle degree

| Soil type | <2（g） | 2-3mm（g） | 3-6mm（g） | Sun（g） | <2 proportion（%） | 2-3mm proportion（%） | 3-6mm proportion（%） | Total proportion（%） |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Gneiss mountain soil | 208.31 | 21.85 | 28.43 | 258.59 | 80.56 | 8.45 | 10.99 | 100.00 |
|  | 202.15 | 26.94 | 26.82 | 255.91 | 78.99 | 10.53 | 10.48 | 100.00 |
|  | 212.25 | 46.7 | 23.13 | 282.08 | 75.24 | 16.56 | 8.20 | 100.00 |
|  | 231.99 | 46.25 | 28.14 | 306.38 | 75.72 | 15.10 | 9.18 | 100.00 |
|  | 228.83 | 46.79 | 39.27 | 314.89 | 72.67 | 14.86 | 12.47 | 100.00 |
|  | 229.49 | 41.78 | 32.54 | 303.81 | 75.54 | 13.75 | 10.71 | 100.00 |
|  | Average particle proportion |  |  |  | 76.45 | 13.21 | 10.34 | 100.00 |

Soil density data table

| soil type | Serial numbers | Cutting ring（g） | Cutting ring+soil（g） | Soil weight(g) | Density (g/cm) | Average |
| --- | --- | --- | --- | --- | --- | --- |
| Gneiss mountain soil | 1 | 171.79 | 490.9 | 319.11 | 1.60 | 1.695 |
|  | 2 | 165.29 | 491.16 | 325.87 | 1.63 |  |
|  | 3 | 170.83 | 505.63 | 334.8 | 1.67 |  |
|  | 4 | 169.01 | 514.17 | 345.16 | 1.73 |  |
|  | 5 | 178.79 | 536.39 | 357.6 | 1.79 |  |
|  | 6 | 171.54 | 523.88 | 352.34 | 1.76 |  |

Direct shear test data table

| soil type | Vertical pressure（kPa） | 50 | 100 | 150 | 200 |
| --- | --- | --- | --- | --- | --- |
| Gneiss mountain soil | 抗剪强度（kPa） | 33.8 | 69.9 | 102.4 | 129.7 |
|  |  | 35.6 | 73.4 | 106.7 | 133.7 |
|  |  | 34.7 | 71.7 | 104.6 | 131.7 |

Soil firmness measurement

| soil type | Serial numbers | Soil compaction（MPa） | Average（MPa） |
| --- | --- | --- | --- |
| Gneiss mountain soil | 1 | 2.59 | 2.43 |
|  | 2 | 2.34 |  |
|  | 3 | 2.18 |  |
|  | 4 | 2.48 |  |
|  | 5 | 2.56 |  |

Measurement method of repose angle

| soil type | repose angle（°） | Average repose angle（°） |
| --- | --- | --- |
| Gneiss mountain soil | 41.51 | 43.26 |
|  | 43.78 |  |
|  | 44.55 |  |
|  | 43.21 |  |
|  | 43.26 |  |

Determination of static friction coefficient

| soil type | Static friction coefficient | The range of static friction coefficient |
| --- | --- | --- |
| Gneiss mountain soil | 0.36 | 0.36~0.51 |
|  | 0.40 |  |
|  | 0.51 |  |
|  | 0.38 |  |
|  | 0.48 |  |

Rolling friction coefficient measurement

| soil type | Rolling friction coefficient | The range of rolling friction coefficient |
| --- | --- | --- |
| Gneiss mountain soil | 0.09 | 0.08~0.16 |
|  | 0.16 |  |
|  | 0.13 |  |
|  | 0.15 |  |
|  | 0.12 |  |
|  | 0.08 |  |

Coefficient of restitution measurement

| soil type | Coefficient of restitution measurement | The range of coefficient of restitution measurement |
| --- | --- | --- |
| Gneiss mountain soil | 0.36 | 0.36~0.51 |
|  | 0.40 |  |
|  | 0.51 |  |
|  | 0.38 |  |
|  | 0.40 |  |
|  | 0.48 |  |
|  | 0.39 |  |
|  | 0.43 |  |
|  | 0.49 |  |
|  | 0.48 |  |

Sliding friction angle measurement

| soil type | Sliding friction angle（°） | Average sliding friction angle（°） |
| --- | --- | --- |
| Gneiss mountain soil | 18.68 | 18.82 |
|  | 18.65 |  |
|  | 18.45 |  |
|  | 18.68 |  |
|  | 18.71 |  |
|  | 18.6 |  |
|  | 18.67 |  |
|  | 19.21 |  |
|  | 19.34 |  |
|  | 19.23 |  |

Table 3. List of Plackett-Burman test parameters

| Symbol | parameter | low level | high level |
| --- | --- | --- | --- |
| X1 | JKR surface energy/J | 4.5 | 13.5 |
| X2 | Coefficient of static friction | 0.2 | 1.16 |
| X3 | Coefficient of rolling friction | 0.1 | 0.2 |
| X4 | Coefficient of restitution | 0.15 | 0.75 |
| X5 | Shear modulus/MPa | 1 | 100 |

Table 4. Factor level table

| Serial number | JKR surface energy /J |  | Coefficient of static friction |  | Coefficient of rolling friction |  | Coefficient of restitution | Shear modulus /MPa | Repose angle /° |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 |  | 13.5 |  | 1.16 |  | 0.2 | 0.15 | 100 | 69.11 |
| 2 |  | 4.5 |  | 1.16 |  | 0.1 | 0.75 | 100 | 31.35 |
| 3 |  | 4.5 |  | 1.16 |  | 0.2 | 0.15 | 1 | 52.82 |
| 4 |  | 13.5 |  | 0.2 |  | 0.2 | 0.75 | 1 | 69.62 |
| 5 |  | 4.5 |  | 0.2 |  | 0.2 | 0.75 | 100 | 56.66 |
| 6 |  | 13.5 |  | 0.2 |  | 0.2 | 0.15 | 100 | 79.5 |
| 7 |  | 4.5 |  | 0.2 |  | 0.1 | 0.15 | 100 | 53.1 |
| 8 |  | 4.5 |  | 0.2 |  | 0.1 | 0.15 | 1 | 65.81 |
| 9 |  | 13.5 |  | 1.16 |  | 0.1 | 0.15 | 1 | 53.8 |
| 10 |  | 13.5 |  | 0.2 |  | 0.1 | 0.75 | 1 | 63.64 |
| 11 |  | 4.5 |  | 1.16 |  | 0.2 | 0.75 | 1 | 39.01 |
| 12 |  | 13.5 |  | 1.16 |  | 0.1 | 0.75 | 100 | 35.52 |

Table 5. Significance analysis of Plackett-Burman test parameters

| Factors | Sum of Squares | F-value | P-value | saliency list |
| --- | --- | --- | --- | --- |
| X1- JKR surface energy | 437.30 | 19.01 | 0.0048** | 3 |
| X2- Coefficient of static friction | 949.10 | 41.27 | 0.0007** | 1 |
| X3- Coefficient of rolling friction | 336.02 | 14.61 | 0.0087** | 4 |
| X4- Coefficient of restitution | 511.43 | 22.24 | 0.0033** | 2 |
| X5- Shear modulus | 31.56 | 1.37 | 0.2858 | 5 |

Note :** extremely significant ( P < 0.01 ), * significant ( P < 0.05 ).

Table 6. The steepest climbing test design and results

| Serial number | JKR surface energy /J | Coefficient of static friction | Coefficient of rolling friction | Coefficient of restitution | Repose angle /° | Relative error /% |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 4.50 | 0.20 | 0.10 | 0.15 | 34.38 | 20.53 |
| 2 | 6.75 | 0.44 | 0.13 | 0.30 | 46.67 | 7.88 |
| 3 | 9.00 | 0.68 | 0.15 | 0.45 | 49.59 | 14.63 |
| 4 | 11.25 | 0.92 | 0.18 | 0.60 | 53.15 | 22.86 |
| 5 | 13.50 | 1.16 | 0.20 | 0.75 | 53.94 | 24.69 |

Table 7. Box-Behnken experimental design and results

|  |  | Factors |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Serial number | A: JKR surface energy /J |  | B: Coefficient of static friction | C: Coefficient of rolling friction |  | D: Coefficient of restitution |  | Repose angle/° |
| 1 |  | 4.50 | 0.20 |  | 0.11 | 0.23 | 40.36 |  |
| 2 |  | 6.75 | 0.20 |  | 0.11 | 0.23 | 42.03 |  |
| 3 |  | 4.50 | 0.44 |  | 0.11 | 0.23 | 36.66 |  |
| 4 |  | 6.75 | 0.44 |  | 0.11 | 0.23 | 38.52 |  |
| 5 |  | 5.63 | 0.32 |  | 0.10 | 0.15 | 25.38 |  |
| 6 |  | 5.63 | 0.32 |  | 0.13 | 0.15 | 23.61 |  |
| 7 |  | 5.63 | 0.32 |  | 0.10 | 0.30 | 43.06 |  |
| 8 |  | 5.63 | 0.32 |  | 0.13 | 0.30 | 38.05 |  |
| 9 |  | 4.50 | 0.32 |  | 0.11 | 0.15 | 27.99 |  |
| 10 |  | 6.75 | 0.32 |  | 0.11 | 0.15 | 15.49 |  |
| 11 |  | 4.50 | 0.32 |  | 0.11 | 0.30 | 40.31 |  |
| 12 |  | 6.75 | 0.32 |  | 0.11 | 0.30 | 41.87 |  |
| 13 |  | 5.63 | 0.20 |  | 0.10 | 0.23 | 41.52 |  |
| 14 |  | 5.63 | 0.44 |  | 0.10 | 0.23 | 36.93 |  |
| 15 |  | 5.63 | 0.20 |  | 0.13 | 0.23 | 39.47 |  |
| 16 |  | 5.625 | 0.44 |  | 0.125 | 0.23 | 38.29 |  |
| 17 |  | 4.50 | 0.32 |  | 0.10 | 0.23 | 39.95 |  |
| 18 |  | 6.75 | 0.32 |  | 0.10 | 0.23 | 42.22 |  |
| 19 |  | 4.50 | 0.32 |  | 0.13 | 0.23 | 39.01 |  |
| 20 |  | 6.75 | 0.32 |  | 0.13 | 0.23 | 35.98 |  |
| 21 |  | 5.63 | 0.20 |  | 0.11 | 0.15 | 24.11 |  |
| 22 |  | 5.63 | 0.44 |  | 0.11 | 0.15 | 18.06 |  |
| 23 |  | 5.63 | 0.20 |  | 0.11 | 0.30 | 43.71 |  |
| 24 |  | 5.63 | 0.44 |  | 0.11 | 0.30 | 41.08 |  |
| 25 |  | 5.63 | 0.32 |  | 0.11 | 0.23 | 40.89 |  |
| 26 |  | 5.63 | 0.32 |  | 0.11 | 0.23 | 42.69 |  |
| 27 |  | 5.63 | 0.32 |  | 0.11 | 0.23 | 40.72 |  |
| 28 |  | 5.63 | 0.32 |  | 0.11 | 0.23 | 41.68 |  |
| 29 |  | 5.63 | 0.32 |  | 0.11 | 0.23 | 42.51 |  |

Table 8. Soil sliding friction angle simulation factor coding table

| Coding | Factors |  |  |
| --- | --- | --- | --- |
|  | Soil-65Mn static friction coefficient E | Soil-65Mn rolling friction coefficient F | Restitution coefficient of soil-65Mn collision G |
| -1 | 0.36 | 0.08 | 0.11 |
| 0 | 0.44 | 0.12 | 0.42 |
| 1 | 0.51 | 0.16 | 0.73 |

Table 9. Soil sliding friction angle simulation test design and results

| Serial number | Factors |  |  |  |
| --- | --- | --- | --- | --- |
|  | Soil-65Mn static friction coefficient E | Soil-65Mn rolling friction coefficient F | Restitution coefficient of soil-65Mn collision G | Sliding friction angle /° |
| 1 | 0.36 | 0.08 | 0.42 | 15.76 |
| 2 | 0.51 | 0.08 | 0.42 | 19.48 |
| 3 | 0.36 | 0.16 | 0.42 | 15.6 |
| 4 | 0.51 | 0.16 | 0.42 | 18.41 |
| 5 | 0.36 | 0.12 | 0.11 | 13.44 |
| 6 | 0.51 | 0.12 | 0.11 | 17.42 |
| 7 | 0.36 | 0.12 | 0.73 | 13.87 |
| 8 | 0.51 | 0.12 | 0.73 | 17.21 |
| 9 | 0.44 | 0.08 | 0.11 | 17.2 |
| 10 | 0.44 | 0.16 | 0.11 | 14.4 |
| 11 | 0.44 | 0.08 | 0.73 | 17.56 |
| 12 | 0.44 | 0.16 | 0.73 | 17.01 |
| 13 | 0.44 | 0.12 | 0.42 | 19.21 |
| 14 | 0.44 | 0.12 | 0.42 | 18.35 |
| 15 | 0.44 | 0.12 | 0.42 | 18.39 |
| 16 | 0.44 | 0.12 | 0.42 | 18.31 |
| 17 | 0.44 | 0.12 | 0.42 | 19.45 |

Table 10. Regression model analysis of variance table

| Sources | Sum of squares | Degree of Freedom | Mean Square | F-Value | P-value |
| --- | --- | --- | --- | --- | --- |
| Models | 1729.63 | 22 | 78.62 | 87.50 | <0.0001 |
| A-JKR surface energy/J | 29.92 | 1 | 29.92 | 33.30 | 0.0012** |
| B-Coefficient of static friction | 18.84 | 1 | 18.84 | 20.96 | 0.0038** |
| C- Coefficient of rolling friction | 11.49 | 1 | 11.49 | 12.79 | 0.0117* |
| D- Coefficient of restitution | 257.92 | 1 | 257.92 | 287.07 | <0.0001** |
| AB | 0.0090 | 1 | 0.0090 | 0.0100 | 0.9234 |
| AC | 7.02 | 1 | 7.02 | 7.82 | 0.0313* |
| AD | 49.42 | 1 | 49.42 | 55.01 | 0.0003** |
| BC | 2.91 | 1 | 2.91 | 3.24 | 0.1222 |
| BD | 2.92 | 1 | 2.92 | 3.25 | 0.1213 |
| CD | 2.62 | 1 | 2.62 | 2.92 | 0.1383 |
| A² | 12.16 | 1 | 12.16 | 13.54 | 0.0103* |
| B² | 11.40 | 1 | 11.40 | 12.69 | 0.0119* |
| C² | 6.29 | 1 | 6.29 | 7.00 | 0.0383* |
| D² | 477.31 | 1 | 477.31 | 531.25 | <0.0001** |
| A²B | 0.2701 | 1 | 0.2701 | 0.3006 | 0.6033 |
| A²C | 0.0200 | 1 | 0.0200 | 0.0223 | 0.8863 |
| A²D | 5.41 | 1 | 5.41 | 6.02 | 0.0495* |
| AB² | 26.17 | 1 | 26.17 | 29.13 | 0.0017** |
| AC² | 12.95 | 1 | 12.95 | 14.42 | 0.0090** |
| B²C | 4.64 | 1 | 4.64 | 5.16 | 0.0635 |
| B²D | 13.78 | 1 | 13.78 | 15.34 | 0.0078** |
| BC² | 1.06 | 1 | 1.06 | 1.18 | 0.3194 |
| Residual | 5.39 | 6 | 0.8985 |  |  |
| Lack of Fit | 2.14 | 2 | 1.07 | 1.31 | 0.3642 |
| Pure Error | 3.25 | 4 | 0.8133 |  |  |
| Cor Total | 1735.02 | 28 |  |  |  |
|  | R2=0.9969，R2adj＝0.9855，C.V.＝2.59% |  |  |  |  |

Note : ** extremely significant ( P < 0.01 ), * significant ( P < 0.05 ).

Table 11. Analysis of variance

| Sources | Sum of squares | Degree of Freedom | Mean Square | F-Value | P-value |
| --- | --- | --- | --- | --- | --- |
| Model | 56.27 | 12 | 4.69 | 15.83 | 0.0083 |
| E | 12.32 | 1 | 12.32 | 41.61 | 0.0030** |
| F | 2.81 | 1 | 2.81 | 9.47 | 0.0370* |
| G | 2.21 | 1 | 2.21 | 7.45 | 0.0525 |
| EF | 0.21 | 1 | 0.21 | 0.70 | 0.4501 |
| EG | 0.03 | 1 | 0.03 | 0.10 | 0.7703 |
| FG | 1.27 | 1 | 1.27 | 4.27 | 0.1075 |
| E² | 6.91 | 1 | 6.91 | 23.33 | 0.0085** |
| F² | 0.09 | 1 | 0.09 | 0.31 | 0.6054 |
| G² | 17.71 | 1 | 17.71 | 59.81 | 0.0015** |
| E²F | 0.56 | 1 | 0.56 | 1.90 | 0.2404 |
| E²G | 0.75 | 1 | 0.75 | 2.53 | 0.1866 |
| EF² | 0.03 | 1 | 0.03 | 0.10 | 0.7661 |
| 纯误差 | 1.18 | 4 | 0.30 |  |  |
| 总和 | 57.45 | 16 |  |  |  |
| R2=0.9794，R2adj＝0.9175，C.V.＝3.18% |  |  |  |  |  |

Table 12. Rotary tillage blade contact accumulated energy data table

| Times（s） |  | normal cumulative contact energy /J | tangential cumulative contact energy /J |
| --- | --- | --- | --- |
| 0.10 | 3.935936 |  | 17.36322 |
| 0.20 | 4.207992 |  | 19.00928 |
| 0.30 | 8.119406 |  | 34.57458 |
| 0.40 | 8.428594 |  | 36.22847 |
| 0.50 | 12.21475 |  | 52.98029 |
| 0.60 | 12.54301 |  | 54.59764 |

Table 13 The disturbance area of rotary tillage blade to soil

| Parameter | Actual value /cm2 | Simulative value /cm2 | Error /% |
| --- | --- | --- | --- |
| Longitudinal soil disturbance area | 157.31 | 163.43 | 3.89 |
| Overlooking soil disturbance area | 423.38 | 435.15 | 2.78 |

Normal cumulative contact energy data table of different speed method

| Time | Normal cumulative contact energy |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 300 rpm | 280 rpm | 260 rpm | 240 rpm | 220 rpm | 200 rpm | 180 rpm | 160 rpm |
| 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |
| 0.01001 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |
| 0.02003 | 0.05413 | 0.04732 | 0.04097 | 0.03382 | 0.02925 | 0 | 0 | 0 |
| 0.03004 | 0.17749 | 0.11621 | 0.08838 | 0.06298 | 0.03716 | 0 | 0.02539 | 0.0179 |
| 0.04001 | 0.50639 | 0.35728 | 0.22192 | 0.15005 | 0.09377 | 0.03018 | 0.04279 | 0.02244 |
| 0.05003 | 0.86492 | 0.75288 | 0.52279 | 0.39591 | 0.27178 | 0.07073 | 0.08261 | 0.0478 |
| 0.06004 | 1.21247 | 1.05543 | 0.79532 | 0.627 | 0.42395 | 0.15266 | 0.24776 | 0.09405 |
| 0.07001 | 1.59905 | 1.37607 | 1.0487 | 0.85114 | 0.65916 | 0.29695 | 0.34071 | 0.25996 |
| 0.08002 | 1.92292 | 1.73234 | 1.35476 | 1.08197 | 0.82668 | 0.45857 | 0.46401 | 0.34038 |
| 0.09004 | 2.23613 | 2.06559 | 1.61257 | 1.29686 | 1.02408 | 0.6281 | 0.60366 | 0.45576 |
| 0.10001 | 2.37597 | 2.29783 | 1.90186 | 1.52023 | 1.23783 | 0.80093 | 0.70884 | 0.55492 |
| 0.11002 | 2.4481 | 2.38866 | 2.00984 | 1.73402 | 1.38387 | 0.94063 | 0.83284 | 0.66181 |
| 0.12004 | 2.45661 | 2.41747 | 2.07835 | 1.82487 | 1.55186 | 1.11824 | 0.98184 | 0.77396 |
| 0.13001 | 2.46764 | 2.42422 | 2.08818 | 1.85096 | 1.63381 | 1.30867 | 1.11971 | 0.89487 |
| 0.14002 | 2.4694 | 2.4292 | 2.09027 | 1.85888 | 1.65821 | 1.4014 | 1.21869 | 1.0335 |
| 0.15003 | 2.46941 | 2.43074 | 2.093 | 1.86232 | 1.66464 | 1.4814 | 1.27428 | 1.10987 |
| 0.16 | 2.46941 | 2.43074 | 2.09301 | 1.86346 | 1.6667 | 1.51819 | 1.32286 | 1.17372 |
| 0.17002 | 2.46941 | 2.43074 | 2.09301 | 1.86978 | 1.66935 | 1.53569 | 1.35921 | 1.221 |
| 0.18003 | 2.46941 | 2.43074 | 2.09301 | 1.86978 | 1.67172 | 1.54221 | 1.37356 | 1.25963 |
| 0.19 | 2.46941 | 2.43074 | 2.09301 | 1.86978 | 1.67662 | 1.5445 | 1.38186 | 1.29478 |
| 0.20001 | 2.46941 | 2.43074 | 2.09301 | 1.86978 | 1.67664 | 1.54693 | 1.3838 | 1.31028 |
| 0.21003 | 2.46941 | 2.43074 | 2.09301 | 1.86978 | 1.67664 | 1.54974 | 1.38399 | 1.31936 |
| 0.22004 | 2.46941 | 2.43074 | 2.09301 | 1.86978 | 1.67669 | 1.55204 | 1.38471 | 1.32125 |
| 0.23001 | 2.48069 | 2.43074 | 2.09301 | 1.86978 | 1.67669 | 1.55204 | 1.38558 | 1.32197 |
| 0.24003 | 2.73705 | 2.43074 | 2.09301 | 1.86978 | 1.67669 | 1.55204 | 1.3856 | 1.32278 |
| 0.25004 | 2.81934 | 2.50345 | 2.09301 | 1.86978 | 1.67669 | 1.55204 | 1.38564 | 1.32316 |
| 0.26001 | 3.16718 | 2.61024 | 2.09301 | 1.86978 | 1.67669 | 1.55204 | 1.38564 | 1.32316 |
| 0.27002 | 3.5849 | 2.71304 | 2.15622 | 1.86978 | 1.67669 | 1.55204 | 1.38564 | 1.32316 |
| 0.28004 | 3.93635 | 3.01938 | 2.25163 | 1.87131 | 1.67669 | 1.55204 | 1.38564 | 1.32316 |
| 0.29001 | 4.17057 | 3.34251 | 2.37486 | 1.92782 | 1.67669 | 1.55204 | 1.38564 | 1.32316 |
| 0.30002 | 4.34276 | 3.60227 | 2.69837 | 2.02248 | 1.67669 | 1.55204 | 1.38564 | 1.32316 |
| 0.31004 | 4.37828 | 3.81519 | 2.99115 | 2.12543 | 1.67962 | 1.55204 | 1.38564 | 1.32316 |
| 0.32 | 4.38964 | 3.93385 | 3.2632 | 2.28535 | 1.72643 | 1.55204 | 1.38564 | 1.32316 |
| 0.33002 | 4.39665 | 3.99334 | 3.46562 | 2.52535 | 1.85513 | 1.55204 | 1.38564 | 1.32316 |
| 0.34003 | 4.39688 | 4.00347 | 3.59551 | 2.77852 | 2.03008 | 1.55204 | 1.38564 | 1.32316 |
| 0.35 | 4.39688 | 4.00454 | 3.65439 | 2.96646 | 2.1965 | 1.55438 | 1.38564 | 1.32316 |
| 0.36002 | 4.39688 | 4.00606 | 3.67175 | 3.10896 | 2.38655 | 1.58636 | 1.38564 | 1.32316 |
| 0.37003 | 4.39688 | 4.007 | 3.67622 | 3.22871 | 2.56744 | 1.64036 | 1.38564 | 1.32316 |
| 0.38 | 4.39688 | 4.007 | 3.67959 | 3.30059 | 2.74831 | 1.97115 | 1.38762 | 1.32316 |
| 0.39002 | 4.39688 | 4.007 | 3.6832 | 3.3198 | 2.88639 | 2.11482 | 1.41465 | 1.32316 |
| 0.40003 | 4.39688 | 4.007 | 3.6832 | 3.32282 | 2.98167 | 2.27509 | 1.48908 | 1.32316 |
| 0.41004 | 4.39688 | 4.007 | 3.6832 | 3.32628 | 3.055 | 2.43117 | 1.56261 | 1.32316 |
| 0.42001 | 4.39688 | 4.007 | 3.6832 | 3.32654 | 3.08552 | 2.58279 | 1.67432 | 1.32316 |
| 0.43003 | 4.39688 | 4.007 | 3.6832 | 3.32654 | 3.09199 | 2.69622 | 1.82309 | 1.33955 |
| 0.44004 | 4.88202 | 4.007 | 3.6832 | 3.32654 | 3.09446 | 2.81087 | 1.94631 | 1.36217 |
| 0.45001 | 5.07367 | 4.007 | 3.6832 | 3.32654 | 3.09768 | 2.90364 | 2.08285 | 1.41221 |
| 0.46002 | 5.45358 | 4.01405 | 3.6832 | 3.32654 | 3.09818 | 2.96245 | 2.18984 | 1.47948 |
| 0.47004 | 5.76463 | 4.14668 | 3.6832 | 3.32654 | 3.09824 | 2.98886 | 2.29546 | 1.59433 |
| 0.48001 | 6.08605 | 4.32493 | 3.6832 | 3.32654 | 3.09824 | 2.9982 | 2.37489 | 1.70849 |
| 0.49002 | 6.36611 | 4.54732 | 3.6832 | 3.32654 | 3.09824 | 2.99993 | 2.43475 | 1.81234 |
| 0.50004 | 6.47303 | 4.88161 | 3.6832 | 3.32654 | 3.09824 | 3.00203 | 2.47288 | 1.92177 |
| 0.51001 | 6.51572 | 5.19764 | 3.82988 | 3.32654 | 3.09824 | 3.00263 | 2.49552 | 2.01257 |
| 0.52002 | 6.52035 | 5.42689 | 3.94595 | 3.32654 | 3.09824 | 3.00268 | 2.50349 | 2.11333 |
| 0.53003 | 6.53376 | 5.59173 | 4.20471 | 3.32654 | 3.09824 | 3.00268 | 2.5056 | 2.19813 |
| 0.54 | 6.53817 | 5.69343 | 4.52139 | 3.32654 | 3.09824 | 3.00268 | 2.50599 | 2.26162 |
| 0.55002 | 6.53819 | 5.71977 | 4.77781 | 3.42335 | 3.09824 | 3.00268 | 2.509 | 2.32249 |
| 0.56003 | 6.53819 | 5.72071 | 4.95185 | 3.53244 | 3.09824 | 3.00268 | 2.50938 | 2.35631 |
| 0.57 | 6.53819 | 5.72283 | 5.11728 | 3.73461 | 3.09824 | 3.00268 | 2.50956 | 2.38808 |
| 0.58001 | 6.53819 | 5.7261 | 5.18222 | 3.97943 | 3.09824 | 3.00268 | 2.50956 | 2.40196 |
| 0.59003 | 6.53819 | 5.7261 | 5.21043 | 4.20222 | 3.09916 | 3.00268 | 2.50956 | 2.40638 |
| 0.60004 | 6.53819 | 5.7261 | 5.21376 | 4.40899 | 3.16616 | 3.00268 | 2.50956 | 2.40693 |
| 0.61001 | 6.53819 | 5.7261 | 5.21994 | 4.5607 | 3.23896 | 3.00268 | 2.50956 | 2.40854 |
| 0.62003 | 6.53819 | 5.7261 | 5.22089 | 4.67612 | 3.42701 | 3.00268 | 2.50956 | 2.4093 |
| 0.63004 | 6.54267 | 5.7261 | 5.22089 | 4.74379 | 3.61719 | 3.00268 | 2.50956 | 2.40932 |
| 0.64001 | 6.6659 | 5.7261 | 5.22089 | 4.76321 | 3.80258 | 3.00268 | 2.50956 | 2.40932 |
| 0.65002 | 6.8067 | 5.7261 | 5.22089 | 4.76536 | 3.99143 | 3.00268 | 2.50956 | 2.40932 |
| 0.66004 | 7.08002 | 5.7261 | 5.22089 | 4.7662 | 4.12399 | 3.02704 | 2.50956 | 2.40932 |
| 0.67001 | 7.4523 | 5.7261 | 5.22089 | 4.77096 | 4.22326 | 3.0875 | 2.50956 | 2.40932 |
| 0.68002 | 7.78385 | 5.73703 | 5.22089 | 4.77096 | 4.28902 | 3.16533 | 2.50956 | 2.40932 |
| 0.69004 | 8.04302 | 5.86095 | 5.22089 | 4.77096 | 4.32758 | 3.28942 | 2.50956 | 2.40932 |
| 0.70001 | 8.16549 | 6.0373 | 5.22089 | 4.77096 | 4.33784 | 3.45543 | 2.50956 | 2.40932 |
| 0.71002 | 8.22144 | 6.32896 | 5.22089 | 4.77096 | 4.34401 | 3.61512 | 2.50956 | 2.40932 |
| 0.72003 | 8.23782 | 6.66752 | 5.22089 | 4.77096 | 4.34522 | 3.75848 | 2.51986 | 2.40932 |
| 0.73 | 8.24401 | 6.96898 | 5.22973 | 4.77096 | 4.34526 | 3.91399 | 2.57136 | 2.40932 |
| 0.74002 | 8.24401 | 7.17712 | 5.32535 | 4.77096 | 4.34527 | 4.01681 | 2.6332 | 2.40932 |
| 0.75003 | 8.24424 | 7.29864 | 5.4734 | 4.77096 | 4.34527 | 4.1059 | 2.75673 | 2.40932 |
| 0.76 | 8.24424 | 7.35049 | 5.70066 | 4.77096 | 4.34527 | 4.16847 | 2.87759 | 2.40932 |
| 0.77002 | 8.24424 | 7.36073 | 5.98237 | 4.77096 | 4.34527 | 4.19454 | 3.05516 | 2.40932 |
| 0.78003 | 8.24424 | 7.36547 | 6.20719 | 4.77096 | 4.34527 | 4.20879 | 3.19647 | 2.40932 |
| 0.79004 | 8.24424 | 7.36558 | 6.42004 | 4.78312 | 4.34527 | 4.21173 | 3.3133 | 2.40932 |
| 0.80001 | 8.24424 | 7.36558 | 6.57953 | 4.86823 | 4.34527 | 4.21352 | 3.42584 | 2.4107 |
| 0.81003 | 8.24424 | 7.36558 | 6.63974 | 4.97373 | 4.34527 | 4.21435 | 3.51955 | 2.42451 |
| 0.82004 | 8.24424 | 7.36558 | 6.67277 | 5.16598 | 4.34527 | 4.21477 | 3.5877 | 2.45945 |
| 0.83001 | 8.24788 | 7.36558 | 6.67991 | 5.39427 | 4.34527 | 4.21477 | 3.63163 | 2.51238 |
| 0.84003 | 8.50629 | 7.36558 | 6.69233 | 5.62243 | 4.34527 | 4.21477 | 3.65165 | 2.5912 |
| 0.85004 | 8.65245 | 7.36558 | 6.69355 | 5.83195 | 4.34527 | 4.21477 | 3.66699 | 2.70703 |
| 0.86001 | 8.92019 | 7.36558 | 6.69355 | 6.00031 | 4.35401 | 4.21477 | 3.67196 | 2.80429 |
| 0.87002 | 9.31097 | 7.36558 | 6.69503 | 6.088 | 4.414 | 4.21477 | 3.67237 | 2.92526 |
| 0.88004 | 9.6857 | 7.36558 | 6.69503 | 6.21603 | 4.50914 | 4.21477 | 3.67559 | 3.01872 |
| 0.89001 | 9.94664 | 7.36558 | 6.69503 | 6.26501 | 4.65909 | 4.21477 | 3.6767 | 3.10028 |
| 0.90002 | 10.68492 | 7.49842 | 6.69503 | 6.26988 | 4.88096 | 4.21477 | 3.67688 | 3.19268 |
| 0.91003 | 10.70755 | 7.65079 | 6.69503 | 6.27667 | 5.08073 | 4.21477 | 3.67688 | 3.27278 |
| 0.92 | 10.71536 | 7.90815 | 6.69503 | 6.28067 | 5.27383 | 4.21477 | 3.67688 | 3.82003 |
| 0.93002 | 10.72459 | 8.29821 | 6.69503 | 6.28071 | 5.43243 | 4.21477 | 3.67688 | 3.9184 |
| 0.94003 | 10.72498 | 8.62665 | 6.69503 | 6.28071 | 5.59138 | 4.21477 | 3.67688 | 3.94281 |
| 0.95 | 10.72498 | 8.93281 | 6.69503 | 6.28071 | 5.67371 | 4.21648 | 3.67688 | 3.95504 |
| 0.96001 | 10.72498 | 9.12983 | 6.70439 | 6.28071 | 5.72687 | 4.25795 | 3.67688 | 3.9606 |
| 0.97003 | 10.72498 | 9.18762 | 6.81167 | 6.28071 | 5.73956 | 4.32338 | 3.67688 | 3.96244 |
| 0.98004 | 10.72498 | 9.24332 | 6.92078 | 6.28071 | 5.74196 | 4.40195 | 3.67688 | 3.96328 |
| 0.99001 | 10.72498 | 9.24552 | 7.23123 | 6.28071 | 5.74871 | 4.54963 | 3.67688 | 3.9645 |
| 1.00003 | 10.72498 | 9.25315 | 7.55126 | 6.28071 | 5.74974 | 4.79857 | 3.67688 | 3.96479 |
| 1.01004 | 10.72498 | 9.26633 | 7.85575 | 6.28071 | 5.75149 | 4.97048 | 3.67688 | 3.96595 |
| 1.02001 | 10.72498 | 9.26643 | 8.05894 | 6.28071 | 5.75162 | 5.13684 | 3.67688 | 3.9667 |
| 1.03002 | 10.72895 | 9.26643 | 8.2079 | 6.28071 | 5.7517 | 5.28747 | 3.67688 | 3.9667 |
| 1.04004 | 10.92963 | 9.26643 | 8.28551 | 6.28184 | 5.7517 | 5.40125 | 3.67688 | 3.9667 |
| 1.05001 | 11.12617 | 9.26643 | 8.30874 | 6.34822 | 5.7517 | 5.46561 | 3.68852 | 3.9667 |
| 1.06002 | 11.38746 | 9.26643 | 8.31217 | 6.43352 | 5.7517 | 5.58793 | 3.72378 | 3.9667 |
| 1.07004 | 11.70411 | 9.26643 | 8.31353 | 6.68892 | 5.7517 | 5.60414 | 3.76778 | 3.9667 |
| 1.08001 | 12.02603 | 9.26643 | 8.31549 | 6.95469 | 5.7517 | 5.61008 | 3.87591 | 3.9667 |
| 1.09002 | 12.29701 | 9.26643 | 8.31549 | 7.17113 | 5.7517 | 5.61179 | 4.0164 | 3.9667 |
| 1.10003 | 12.46956 | 9.26643 | 8.31549 | 7.3503 | 5.7517 | 5.61443 | 4.15367 | 3.9667 |
| 1.11 | 12.62494 | 9.34127 | 8.31549 | 7.53661 | 5.7517 | 5.61652 | 4.28267 | 3.9667 |
| 1.12002 | 12.63601 | 9.48465 | 8.31549 | 7.64853 | 5.7517 | 5.6169 | 4.41587 | 3.9667 |
| 1.13003 | 12.63818 | 9.65042 | 8.31549 | 7.70165 | 5.7517 | 5.6169 | 4.50145 | 3.9667 |
| 1.14 | 12.63997 | 9.94681 | 8.31549 | 7.72596 | 5.76753 | 5.6169 | 4.6133 | 3.9667 |
| 1.15002 | 12.63998 | 10.29037 | 8.31549 | 7.72896 | 5.84164 | 5.6169 | 4.68882 | 3.9667 |
| 1.16003 | 12.63998 | 10.75296 | 8.31549 | 7.73431 | 5.9422 | 5.6169 | 4.74293 | 3.9667 |
| 1.17004 | 12.63998 | 10.91916 | 8.31549 | 7.73688 | 6.14337 | 5.6169 | 4.78321 | 3.9667 |
| 1.18001 | 12.63998 | 11.02087 | 8.31549 | 7.73688 | 6.34485 | 5.6169 | 4.8042 | 3.97052 |
| 1.19003 | 12.63998 | 11.04497 | 8.32507 | 7.73688 | 6.56163 | 5.6169 | 4.81399 | 3.99325 |
| 1.20004 | 12.63998 | 11.05254 | 8.44085 | 7.73688 | 6.74421 | 5.6169 | 4.81568 | 4.04154 |
| 1.21001 | 12.63998 | 11.0561 | 8.57178 | 7.73688 | 6.87299 | 5.6169 | 4.81742 | 4.09595 |
| 1.22003 | 12.63998 | 11.05615 | 8.77488 | 7.73688 | 6.93858 | 5.6169 | 4.81919 | 4.1908 |
| 1.23004 | 12.63998 | 11.05709 | 9.08395 | 7.73688 | 6.99164 | 5.6169 | 4.81996 | 4.30559 |
| 1.24001 | 12.76647 | 11.05709 | 9.36834 | 7.73688 | 7.01918 | 5.6169 | 4.81996 | 4.40314 |
| 1.25002 | 12.91134 | 11.05709 | 9.56413 | 7.73688 | 7.02764 | 5.6169 | 4.81996 | 4.53362 |
| 1.26004 | 13.1718 | 11.05709 | 9.73082 | 7.73715 | 7.02932 | 5.65211 | 4.81996 | 4.62667 |
| 1.27001 | 13.64127 | 11.05709 | 9.814 | 7.73715 | 7.0339 | 5.74522 | 4.81996 | 4.71613 |
| 1.28002 | 13.91382 | 11.05709 | 9.84743 | 7.89906 | 7.03491 | 6.01675 | 4.81996 | 4.79397 |
| 1.29003 | 14.17201 | 11.05709 | 9.85323 | 7.90671 | 7.03495 | 6.15487 | 4.81996 | 4.8581 |
| 1.3 | 14.2997 | 11.05709 | 9.85795 | 7.95519 | 7.03497 | 6.39163 | 4.81996 | 4.90292 |
| 1.31002 | 14.35051 | 11.05709 | 9.85978 | 8.10333 | 7.03497 | 6.55284 | 4.81996 | 4.94828 |
| 1.32003 | 14.36223 | 11.05709 | 9.86073 | 8.34008 | 7.03497 | 6.68072 | 4.81996 | 4.97909 |
| 1.33 | 14.3678 | 11.17774 | 9.86073 | 8.58145 | 7.03497 | 6.80654 | 4.81996 | 4.9919 |
| 1.34002 | 14.37045 | 11.32642 | 9.86073 | 8.80896 | 7.03497 | 6.82905 | 4.81996 | 4.99498 |
| 1.35003 | 14.3775 | 11.55342 | 9.86073 | 9.00474 | 7.03497 | 6.82905 | 4.81996 | 4.99606 |
| 1.36004 | 14.38593 | 11.87291 | 9.86073 | 9.15541 | 7.03497 | 6.82905 | 4.81996 | 4.99795 |
| 1.37001 | 14.38593 | 12.27104 | 9.86073 | 9.26881 | 7.03497 | 6.82905 | 4.81996 | 4.99885 |
| 1.38003 | 14.38593 | 12.56701 | 9.86073 | 9.33881 | 7.03497 | 6.82905 | 4.81996 | 4.99897 |
| 1.39004 | 14.38593 | 12.69601 | 9.86073 | 9.36707 | 7.03497 | 6.82905 | 4.84612 | 4.99897 |
| 1.40001 | 14.38593 | 12.77592 | 9.86073 | 9.37035 | 7.03497 | 6.82905 | 4.90521 | 4.99897 |
| 1.41003 | 14.38593 | 12.7823 | 9.86092 | 9.37444 | 7.04063 | 6.82905 | 4.98691 | 4.99897 |
| 1.42004 | 14.38593 | 12.79129 | 9.86092 | 9.37674 | 7.11044 | 6.82905 | 5.12726 | 4.99897 |
| 1.43001 | 14.38622 | 12.79331 | 9.96488 | 9.37682 | 7.21159 | 6.82905 | 5.25982 | 4.99897 |
| 1.44002 | 14.48855 | 12.79331 | 10.07472 | 9.37683 | 7.39729 | 6.82905 | 5.42691 | 4.99897 |
| 1.45004 | 14.68581 | 12.79331 | 10.28302 | 9.37683 | 7.75941 | 6.82905 | 5.59684 | 4.99897 |
| 1.46001 | 15.02341 | 12.79331 | 10.68251 | 9.37683 | 7.9772 | 6.82905 | 5.70919 | 4.99897 |
| 1.47002 | 15.50564 | 12.79331 | 10.91169 | 9.37683 | 8.11918 | 6.82905 | 5.80693 | 4.99897 |
| 1.48003 | 15.83773 | 12.79331 | 11.08974 | 9.37683 | 8.25005 | 6.82905 | 5.89336 | 4.99897 |
| 1.49 | 16.07874 | 12.79331 | 11.2622 | 9.37683 | 8.34927 | 6.82905 | 5.94921 | 4.99897 |
| 1.50002 | 16.20663 | 12.79331 | 11.34927 | 9.37683 | 8.42372 | 6.82905 | 5.99142 | 4.99897 |
| 1.51003 | 16.23944 | 12.79331 | 11.37885 | 9.37683 | 8.45413 | 6.84439 | 6.02102 | 4.99897 |
| 1.52 | 16.25772 | 12.79331 | 11.38297 | 9.37683 | 8.46688 | 6.8866 | 6.02753 | 4.99897 |
| 1.53002 | 16.26169 | 12.7951 | 11.3927 | 9.37683 | 8.46874 | 7.00306 | 6.03119 | 4.99897 |
| 1.54003 | 16.27272 | 12.84016 | 11.39477 | 9.39619 | 8.47157 | 7.09905 | 6.03324 | 4.99897 |
| 1.55 | 16.27272 | 13.01987 | 11.39503 | 9.53172 | 8.47159 | 7.11905 | 6.03696 | 5.00229 |
| 1.56001 | 16.27272 | 13.19531 | 11.39503 | 9.64159 | 8.47159 | 7.15642 | 6.0373 | 5.02714 |
| 1.57003 | 16.27272 | 13.69883 | 11.39503 | 9.80105 | 8.47159 | 7.21905 | 6.03743 | 5.05954 |
| 1.58004 | 16.27272 | 13.93296 | 11.39503 | 10.11585 | 8.47159 | 7.30339 | 6.03743 | 5.1246 |
| 1.59001 | 16.27272 | 14.19359 | 11.39503 | 10.36369 | 8.47159 | 7.47118 | 6.03743 | 5.20784 |
| 1.60003 | 16.27272 | 14.38605 | 11.39503 | 10.56393 | 8.47159 | 7.62596 | 6.03743 | 5.32137 |
| 1.61004 | 16.27272 | 14.4922 | 11.39503 | 10.70051 | 8.47159 | 7.77975 | 6.03743 | 5.44814 |
| 1.62001 | 16.27272 | 14.53753 | 11.39503 | 10.79898 | 8.47159 | 7.93203 | 6.03743 | 5.54062 |
| 1.63002 | 16.27272 | 14.54264 | 11.39503 | 10.84802 | 8.47159 | 8.06294 | 6.03743 | 5.64331 |
| 1.64004 | 16.40872 | 14.5432 | 11.39543 | 10.87512 | 8.47159 | 8.159 | 6.03743 | 5.72107 |
| 1.65001 | 16.53405 | 14.54362 | 11.39558 | 10.87683 | 8.47159 | 8.26922 | 6.03743 | 5.79861 |
| 1.66002 | 16.84957 | 14.54362 | 11.472 | 10.87914 | 8.47159 | 8.31865 | 6.03743 | 5.8828 |
| 1.67004 | 17.26334 | 14.54362 | 11.60143 | 10.88598 | 8.47159 | 8.34194 | 6.03743 | 5.94164 |
| 1.68 | 17.58215 | 14.54362 | 11.77196 | 10.88624 | 8.48119 | 8.35269 | 6.03743 | 5.98865 |
| 1.69002 | 17.83168 | 14.54362 | 12.05757 | 10.88624 | 8.55769 | 8.35426 | 6.03743 | 6.02433 |
| 1.70003 | 17.96213 | 14.54362 | 12.32718 | 10.88624 | 8.6411 | 8.35474 | 6.03743 | 6.04051 |
| 1.71 | 18.00695 | 14.54362 | 12.54075 | 10.88624 | 8.80046 | 8.35576 | 6.03743 | 6.04847 |
| 1.72002 | 18.03129 | 14.54362 | 12.6708 | 10.88624 | 9.01143 | 8.35576 | 6.04854 | 6.05038 |
| 1.73003 | 18.03249 | 14.54362 | 12.81672 | 10.88624 | 9.23345 | 8.35576 | 6.09778 | 6.05087 |
| 1.74 | 18.03365 | 14.54362 | 12.85615 | 10.88624 | 9.3837 | 8.35576 | 6.16427 | 6.05211 |
| 1.75001 | 18.03369 | 14.56458 | 12.86179 | 10.88624 | 9.52922 | 8.35576 | 6.2803 | 6.05304 |

Different rotational speed tangential cumulative contact energy data table

| Time | Tangential cumulative contact energy |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 300 rpm | 280 rpm | 260 rpm | 240 rpm | 220 rpm | 200 rpm | 180 rpm | 160 rpm |
| 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |
| 0.01001 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 |
| 0.02003 | 0.02299 | 0.02047 | 0.01813 | 0.01606 | 0.01287 | 0 | 0 | 0 |
| 0.03004 | 0.25611 | 0.15458 | 0.08831 | 0.04319 | 0.01625 | 0 | 0.01357 | 0.00978 |
| 0.04001 | 1.49859 | 0.91224 | 0.5792 | 0.2911 | 0.1646 | 0.01403 | 0.027 | 0.01287 |
| 0.05003 | 2.84499 | 2.2302 | 1.82453 | 1.34991 | 0.91692 | 0.09181 | 0.19399 | 0.07157 |
| 0.06004 | 4.72247 | 3.66584 | 3.20295 | 2.41819 | 1.68086 | 0.41597 | 0.76459 | 0.31559 |
| 0.07001 | 6.137 | 4.88713 | 4.42521 | 3.25637 | 2.77714 | 1.04589 | 1.13968 | 1.56727 |
| 0.08002 | 7.34045 | 5.99722 | 5.74636 | 4.27446 | 3.44215 | 1.62033 | 1.68509 | 2.14398 |
| 0.09004 | 8.15648 | 7.25315 | 6.84111 | 5.14286 | 4.25049 | 2.54069 | 2.28824 | 2.77297 |
| 0.10001 | 8.51913 | 8.24687 | 7.46442 | 5.98373 | 5.19751 | 3.12732 | 2.79082 | 3.33413 |
| 0.11002 | 8.7827 | 8.69857 | 7.80284 | 6.42463 | 5.84252 | 3.83743 | 3.6629 | 3.91328 |
| 0.12004 | 8.83493 | 8.82814 | 8.09088 | 6.70095 | 6.2711 | 4.54746 | 4.41552 | 4.35836 |
| 0.13001 | 8.84939 | 8.86539 | 8.25281 | 6.7943 | 6.55813 | 5.053 | 4.78846 | 4.90013 |
| 0.14002 | 8.85347 | 8.87229 | 8.27963 | 6.85141 | 6.67441 | 5.56515 | 5.13434 | 5.26067 |
| 0.15003 | 8.85358 | 8.87615 | 8.28374 | 6.85972 | 6.74886 | 5.98121 | 5.44987 | 5.67478 |
| 0.16 | 8.85358 | 8.87615 | 8.28403 | 6.8654 | 6.76839 | 6.26287 | 5.65542 | 6.05662 |
| 0.17002 | 8.85358 | 8.87615 | 8.28403 | 6.87295 | 6.78279 | 6.43117 | 5.79372 | 6.23969 |
| 0.18003 | 8.85358 | 8.87615 | 8.28403 | 6.87295 | 6.79003 | 6.49963 | 5.89841 | 6.49367 |
| 0.19 | 8.85358 | 8.87615 | 8.28403 | 6.87295 | 6.79408 | 6.51575 | 5.95968 | 6.61734 |
| 0.20001 | 8.85358 | 8.87615 | 8.28403 | 6.87295 | 6.79428 | 6.5174 | 5.96936 | 6.80466 |
| 0.21003 | 8.85358 | 8.87615 | 8.28403 | 6.87295 | 6.79428 | 6.52102 | 5.97001 | 6.87859 |
| 0.22004 | 8.85358 | 8.87615 | 8.28403 | 6.87295 | 6.7944 | 6.52252 | 5.97116 | 6.89503 |
| 0.23001 | 8.87176 | 8.87615 | 8.28403 | 6.87295 | 6.7944 | 6.52253 | 5.97524 | 6.89724 |
| 0.24003 | 9.16326 | 8.87615 | 8.28403 | 6.87295 | 6.7944 | 6.52254 | 5.97554 | 6.89896 |
| 0.25004 | 9.48416 | 8.96656 | 8.28403 | 6.87295 | 6.7944 | 6.52254 | 5.97594 | 6.90114 |
| 0.26001 | 10.22019 | 9.30646 | 8.28403 | 6.87295 | 6.7944 | 6.52254 | 5.97594 | 6.90127 |
| 0.27002 | 11.69562 | 9.6038 | 8.41096 | 6.87295 | 6.7944 | 6.52254 | 5.97594 | 6.90132 |
| 0.28004 | 13.08571 | 10.46992 | 8.64083 | 6.8732 | 6.7944 | 6.52254 | 5.97594 | 6.90132 |
| 0.29001 | 13.98275 | 11.57004 | 9.06176 | 6.9741 | 6.7944 | 6.52254 | 5.97594 | 6.90132 |
| 0.30002 | 14.58092 | 12.47324 | 9.96179 | 7.47489 | 6.7944 | 6.52254 | 5.97594 | 6.90132 |
| 0.31004 | 14.77015 | 13.27859 | 10.89537 | 7.89356 | 6.79912 | 6.52254 | 5.97594 | 6.90132 |
| 0.32 | 14.7862 | 13.74563 | 11.96149 | 8.68504 | 6.91146 | 6.52254 | 5.97594 | 6.90132 |
| 0.33002 | 14.79653 | 14.02011 | 12.74039 | 9.65275 | 7.27552 | 6.52254 | 5.97594 | 6.90132 |
| 0.34003 | 14.79725 | 14.09178 | 13.32552 | 10.85854 | 7.72636 | 6.52254 | 5.97594 | 6.90132 |
| 0.35 | 14.79725 | 14.09599 | 13.52743 | 11.51897 | 8.49346 | 6.52801 | 5.97594 | 6.90132 |
| 0.36002 | 14.79725 | 14.10106 | 13.66073 | 12.02183 | 9.65392 | 6.60087 | 5.97594 | 6.90132 |
| 0.37003 | 14.79725 | 14.10367 | 13.69481 | 12.47365 | 10.38677 | 6.82365 | 5.97594 | 6.90132 |
| 0.38 | 14.79725 | 14.1037 | 13.70246 | 12.89985 | 11.31931 | 7.49301 | 5.98595 | 6.90132 |
| 0.39002 | 14.79725 | 14.1037 | 13.7063 | 12.96259 | 11.93915 | 7.99995 | 6.04657 | 6.90132 |
| 0.40003 | 14.79725 | 14.1037 | 13.7063 | 12.97621 | 12.34843 | 8.9222 | 6.4203 | 6.90132 |
| 0.41004 | 14.79725 | 14.1037 | 13.7063 | 12.98007 | 12.66093 | 9.65763 | 6.79452 | 6.90132 |
| 0.42001 | 14.79725 | 14.1037 | 13.7063 | 12.98308 | 12.8258 | 10.25643 | 7.33448 | 6.90132 |
| 0.43003 | 14.79725 | 14.1037 | 13.7063 | 12.98308 | 12.90008 | 10.80177 | 8.27263 | 6.91903 |
| 0.44004 | 15.55162 | 14.1037 | 13.7063 | 12.98308 | 12.91198 | 11.4021 | 9.02803 | 6.97078 |
| 0.45001 | 15.86671 | 14.1037 | 13.7063 | 12.98308 | 12.91662 | 11.74746 | 9.5446 | 7.16693 |
| 0.46002 | 16.9666 | 14.11514 | 13.7063 | 12.98308 | 12.91869 | 12.06047 | 10.17736 | 7.45799 |
| 0.47004 | 18.25383 | 14.38936 | 13.7063 | 12.98308 | 12.91914 | 12.14454 | 10.62094 | 7.93126 |
| 0.48001 | 19.60875 | 14.79318 | 13.7063 | 12.98308 | 12.91914 | 12.22012 | 10.96405 | 8.5138 |
| 0.49002 | 20.71295 | 15.59246 | 13.7063 | 12.98308 | 12.91914 | 12.23511 | 11.26598 | 9.16948 |
| 0.50004 | 21.18634 | 16.83752 | 13.7063 | 12.98308 | 12.91914 | 12.23721 | 11.53044 | 9.69761 |
| 0.51001 | 21.42932 | 18.59462 | 13.96878 | 12.98308 | 12.91914 | 12.23951 | 11.72792 | 10.03639 |
| 0.52002 | 21.44673 | 19.52922 | 14.37233 | 12.98308 | 12.91914 | 12.23992 | 11.75844 | 10.47617 |
| 0.53003 | 21.45909 | 20.10715 | 15.18587 | 12.98308 | 12.91914 | 12.23992 | 11.77057 | 10.85104 |
| 0.54 | 21.46507 | 20.48908 | 16.49245 | 12.98308 | 12.91914 | 12.23992 | 11.77213 | 11.14149 |
| 0.55002 | 21.46519 | 20.60554 | 17.53469 | 13.17909 | 12.91914 | 12.23992 | 11.77517 | 11.56854 |
| 0.56003 | 21.46519 | 20.61276 | 18.30426 | 13.61603 | 12.91914 | 12.23992 | 11.77659 | 11.81791 |
| 0.57 | 21.46519 | 20.61881 | 19.07538 | 14.41812 | 12.91914 | 12.23992 | 11.77739 | 12.02362 |
| 0.58001 | 21.46519 | 20.62555 | 19.3689 | 15.54564 | 12.91914 | 12.23992 | 11.77739 | 12.159 |
| 0.59003 | 21.46519 | 20.62555 | 19.54881 | 16.57668 | 12.92485 | 12.23992 | 11.77739 | 12.23204 |
| 0.60004 | 21.46519 | 20.62555 | 19.57871 | 17.59948 | 13.14812 | 12.23992 | 11.77739 | 12.23707 |
| 0.61001 | 21.46519 | 20.62555 | 19.58641 | 18.27975 | 13.45621 | 12.23992 | 11.77739 | 12.23893 |
| 0.62003 | 21.46519 | 20.62555 | 19.58989 | 18.84 | 14.21723 | 12.23992 | 11.77739 | 12.24038 |
| 0.63004 | 21.47049 | 20.62555 | 19.58989 | 19.16617 | 15.35267 | 12.23992 | 11.77739 | 12.24044 |
| 0.64001 | 21.64879 | 20.62555 | 19.58989 | 19.28099 | 16.34993 | 12.23992 | 11.77739 | 12.24044 |
| 0.65002 | 22.02261 | 20.62555 | 19.58989 | 19.28798 | 17.35247 | 12.23992 | 11.77739 | 12.24044 |
| 0.66004 | 22.83189 | 20.62555 | 19.58989 | 19.29006 | 17.86711 | 12.28376 | 11.77739 | 12.24044 |
| 0.67001 | 24.49177 | 20.62555 | 19.58989 | 19.29618 | 18.27617 | 12.43923 | 11.77739 | 12.24044 |
| 0.68002 | 25.90776 | 20.65028 | 19.58989 | 19.29619 | 18.62426 | 12.67365 | 11.77739 | 12.24044 |
| 0.69004 | 26.8835 | 20.98768 | 19.58989 | 19.29619 | 18.80937 | 13.41222 | 11.77739 | 12.24044 |
| 0.70001 | 27.39007 | 21.58713 | 19.58989 | 19.29619 | 18.88183 | 14.17935 | 11.77739 | 12.24044 |
| 0.71002 | 27.61125 | 22.61382 | 19.58989 | 19.29619 | 18.89986 | 15.01625 | 11.77739 | 12.24044 |
| 0.72003 | 27.63955 | 24.10297 | 19.58989 | 19.29619 | 18.90399 | 15.64132 | 11.79447 | 12.24044 |
| 0.73 | 27.65023 | 25.11297 | 19.5989 | 19.29619 | 18.90459 | 16.13532 | 11.91018 | 12.24044 |
| 0.74002 | 27.65023 | 25.81572 | 19.79625 | 19.29619 | 18.90464 | 16.64991 | 12.12309 | 12.24044 |
| 0.75003 | 27.65179 | 26.23253 | 20.17569 | 19.29619 | 18.90464 | 17.09977 | 12.70051 | 12.24044 |
| 0.76 | 27.65179 | 26.43968 | 21.04173 | 19.29619 | 18.90464 | 17.47349 | 13.42226 | 12.24044 |
| 0.77002 | 27.65179 | 26.47641 | 22.36953 | 19.29619 | 18.90464 | 17.56987 | 14.23354 | 12.24044 |
| 0.78003 | 27.65179 | 26.48671 | 23.3818 | 19.29619 | 18.90464 | 17.6304 | 14.85605 | 12.24044 |
| 0.79004 | 27.65179 | 26.48915 | 24.23709 | 19.33928 | 18.90464 | 17.66398 | 15.30856 | 12.24044 |
| 0.80001 | 27.65179 | 26.48915 | 24.90178 | 19.53963 | 18.90464 | 17.66778 | 15.89165 | 12.24237 |
| 0.81003 | 27.65179 | 26.48915 | 25.20529 | 19.89843 | 18.90464 | 17.66965 | 16.23085 | 12.31122 |
| 0.82004 | 27.65179 | 26.48915 | 25.42046 | 20.54337 | 18.90464 | 17.67108 | 16.50718 | 12.45372 |
| 0.83001 | 27.6545 | 26.48915 | 25.45876 | 21.51191 | 18.90464 | 17.67108 | 16.69303 | 12.65437 |
| 0.84003 | 27.99309 | 26.48915 | 25.46979 | 22.41149 | 18.90464 | 17.67108 | 16.7935 | 12.94317 |
| 0.85004 | 28.44774 | 26.48915 | 25.4729 | 23.15537 | 18.90464 | 17.67108 | 16.86243 | 13.46812 |
| 0.86001 | 29.39221 | 26.48915 | 25.4729 | 23.7049 | 18.92357 | 17.67108 | 16.88219 | 14.04408 |
| 0.87002 | 30.863 | 26.48915 | 25.47534 | 24.17307 | 19.0592 | 17.67108 | 16.88678 | 14.63935 |
| 0.88004 | 31.98717 | 26.48915 | 25.47534 | 24.90061 | 19.3229 | 17.67108 | 16.89111 | 15.07105 |
| 0.89001 | 32.78374 | 26.48915 | 25.47534 | 25.62634 | 19.99552 | 17.67108 | 16.89249 | 15.53364 |
| 0.90002 | 33.88035 | 26.64056 | 25.47534 | 25.66835 | 21.09055 | 17.67108 | 16.89357 | 15.9898 |
| 0.91003 | 33.95854 | 27.09064 | 25.47534 | 25.67861 | 21.84836 | 17.67108 | 16.89357 | 16.32724 |
| 0.92 | 33.98032 | 28.04876 | 25.47534 | 25.68292 | 22.50112 | 17.67108 | 16.89357 | 17.93189 |
| 0.93002 | 33.99207 | 29.63959 | 25.47534 | 25.68404 | 23.11351 | 17.67108 | 16.89357 | 18.21346 |
| 0.94003 | 33.9936 | 30.85654 | 25.47534 | 25.68404 | 23.7066 | 17.67108 | 16.89357 | 18.33064 |
| 0.95 | 33.99372 | 32.44588 | 25.47534 | 25.68404 | 24.22934 | 17.67597 | 16.89357 | 18.4048 |
| 0.96001 | 33.99375 | 33.20586 | 25.49327 | 25.68404 | 24.40035 | 17.77273 | 16.89357 | 18.45761 |
| 0.97003 | 33.99375 | 33.44297 | 25.74456 | 25.68404 | 24.49984 | 18.02418 | 16.89357 | 18.47682 |
| 0.98004 | 33.99375 | 33.53984 | 26.10617 | 25.68404 | 24.51364 | 18.2998 | 16.89357 | 18.48056 |
| 0.99001 | 33.99375 | 33.54501 | 26.85605 | 25.68404 | 24.52105 | 18.87942 | 16.89357 | 18.48224 |
| 1.00003 | 33.99375 | 33.5511 | 28.20716 | 25.68404 | 24.52285 | 19.66204 | 16.89357 | 18.48321 |
| 1.01004 | 33.99375 | 33.55702 | 29.51717 | 25.68404 | 24.52518 | 20.45086 | 16.89357 | 18.48543 |
| 1.02001 | 33.99375 | 33.55727 | 30.28084 | 25.68404 | 24.52596 | 21.30959 | 16.89357 | 18.48646 |
| 1.03002 | 34.00273 | 33.55732 | 30.76956 | 25.68404 | 24.52673 | 22.00069 | 16.89357 | 18.48646 |
| 1.04004 | 34.26165 | 33.55732 | 31.07591 | 25.69166 | 24.52673 | 22.59517 | 16.89357 | 18.48646 |
| 1.05001 | 34.87863 | 33.55732 | 31.25735 | 25.83582 | 24.52673 | 23.00973 | 16.93044 | 18.48646 |
| 1.06002 | 35.98507 | 33.55732 | 31.26976 | 26.09171 | 24.52673 | 23.27278 | 17.04893 | 18.48646 |
| 1.07004 | 37.14937 | 33.55732 | 31.27668 | 26.95519 | 24.52673 | 23.33906 | 17.25477 | 18.48646 |
| 1.08001 | 38.38986 | 33.55732 | 31.27995 | 28.08282 | 24.52673 | 23.37027 | 17.70621 | 18.48646 |
| 1.09002 | 39.19658 | 33.55732 | 31.27995 | 29.0603 | 24.52673 | 23.37963 | 18.39757 | 18.48646 |
| 1.10003 | 39.77879 | 33.55732 | 31.27995 | 29.86058 | 24.52673 | 23.38309 | 19.08717 | 18.48646 |
| 1.11 | 40.02203 | 33.62098 | 31.27995 | 30.4745 | 24.52673 | 23.38701 | 19.90097 | 18.48646 |
| 1.12002 | 40.05707 | 33.98491 | 31.27995 | 30.90425 | 24.52673 | 23.38872 | 20.50874 | 18.48646 |
| 1.13003 | 40.06086 | 34.59246 | 31.27995 | 31.1432 | 24.52673 | 23.38872 | 20.97161 | 18.48646 |
| 1.14 | 40.06464 | 35.55948 | 31.27995 | 31.29603 | 24.56471 | 23.38872 | 21.48732 | 18.48646 |
| 1.15002 | 40.06484 | 36.77646 | 31.27995 | 31.31653 | 24.77595 | 23.38872 | 21.8556 | 18.48646 |
| 1.16003 | 40.06494 | 38.04133 | 31.27995 | 31.3212 | 25.1306 | 23.38872 | 22.17257 | 18.48646 |
| 1.17004 | 40.06495 | 38.75532 | 31.27995 | 31.32754 | 25.97394 | 23.38872 | 22.36329 | 18.48646 |
| 1.18001 | 40.06495 | 39.31319 | 31.27995 | 31.32754 | 26.78035 | 23.38872 | 22.50413 | 18.49314 |
| 1.19003 | 40.06495 | 39.48106 | 31.31785 | 31.32754 | 27.8639 | 23.38872 | 22.56577 | 18.53551 |
| 1.20004 | 40.06495 | 39.50111 | 31.59438 | 31.32754 | 28.8069 | 23.38872 | 22.57588 | 18.6396 |
| 1.21001 | 40.06495 | 39.51173 | 32.07653 | 31.32754 | 29.41129 | 23.38872 | 22.57857 | 18.87584 |
| 1.22003 | 40.06495 | 39.51208 | 32.78257 | 31.32754 | 29.79806 | 23.38872 | 22.58191 | 19.3394 |
| 1.23004 | 40.06495 | 39.5139 | 33.95655 | 31.32754 | 29.93034 | 23.38872 | 22.58316 | 19.84672 |
| 1.24001 | 40.26402 | 39.5139 | 35.21767 | 31.32754 | 30.03382 | 23.38872 | 22.58316 | 20.55082 |
| 1.25002 | 40.74655 | 39.5139 | 35.95034 | 31.32754 | 30.09035 | 23.38872 | 22.58316 | 21.09674 |
| 1.26004 | 41.69153 | 39.5139 | 36.38442 | 31.32759 | 30.09346 | 23.4789 | 22.58316 | 21.75875 |
| 1.27001 | 42.8655 | 39.5139 | 36.84696 | 31.32759 | 30.09895 | 23.7215 | 22.58316 | 22.22514 |
| 1.28002 | 43.9369 | 39.5139 | 36.98103 | 31.47832 | 30.10034 | 24.43316 | 22.58316 | 22.66323 |
| 1.29003 | 44.78113 | 39.5139 | 37.00358 | 31.54182 | 30.10093 | 25.27793 | 22.58316 | 22.97047 |
| 1.3 | 45.2794 | 39.5139 | 37.0144 | 31.75188 | 30.10122 | 26.11813 | 22.58316 | 23.19392 |
| 1.31002 | 45.52899 | 39.5139 | 37.01622 | 32.17623 | 30.10122 | 26.69624 | 22.58316 | 23.42493 |
| 1.32003 | 45.56413 | 39.5139 | 37.01982 | 33.12392 | 30.10122 | 27.36885 | 22.58316 | 23.56063 |
| 1.33 | 45.57291 | 39.70638 | 37.01982 | 34.04632 | 30.10122 | 28.02562 | 22.58316 | 23.64588 |
| 1.34002 | 45.5797 | 40.07227 | 37.01982 | 35.02508 | 30.10122 | 28.58916 | 22.58316 | 23.65863 |
| 1.35003 | 45.5871 | 40.82606 | 37.01982 | 35.73477 | 30.10122 | 28.9354 | 22.58316 | 23.66919 |
| 1.36004 | 45.59218 | 42.11663 | 37.01982 | 36.32781 | 30.10122 | 29.13827 | 22.58316 | 23.67027 |
| 1.37001 | 45.59218 | 43.60453 | 37.01982 | 36.88219 | 30.10122 | 29.30725 | 22.58316 | 23.6726 |
| 1.38003 | 45.59218 | 44.84639 | 37.01982 | 37.17148 | 30.10122 | 29.39913 | 22.58316 | 23.67309 |
| 1.39004 | 45.59218 | 45.43414 | 37.01982 | 37.24122 | 30.10122 | 29.40558 | 22.63429 | 23.67309 |
| 1.40001 | 45.59218 | 45.68693 | 37.01982 | 37.2618 | 30.10122 | 29.4084 | 22.79417 | 23.67309 |
| 1.41003 | 45.59218 | 45.73466 | 37.02013 | 37.26821 | 30.1162 | 29.41607 | 23.09561 | 23.67309 |
| 1.42004 | 45.59218 | 45.74291 | 37.02013 | 37.27345 | 30.31453 | 29.41659 | 23.72994 | 23.67309 |
| 1.43001 | 45.59312 | 45.74725 | 37.25395 | 37.27384 | 30.66334 | 29.41752 | 24.35413 | 23.67309 |
| 1.44002 | 45.80334 | 45.74731 | 37.58383 | 37.27414 | 31.47763 | 29.41752 | 25.04907 | 23.67309 |
| 1.45004 | 46.27102 | 45.74731 | 38.2548 | 37.27414 | 32.86504 | 29.41752 | 25.66401 | 23.67309 |
| 1.46001 | 47.04855 | 45.74731 | 39.37358 | 37.27414 | 33.78219 | 29.41752 | 26.14593 | 23.67309 |
| 1.47002 | 48.48894 | 45.74731 | 40.25913 | 37.27414 | 34.49393 | 29.41752 | 26.59296 | 23.67309 |
| 1.48003 | 49.79484 | 45.74731 | 41.09066 | 37.27414 | 35.04234 | 29.41752 | 26.99669 | 23.67309 |
| 1.49 | 50.56787 | 45.74731 | 41.72884 | 37.27414 | 35.55434 | 29.41752 | 27.28793 | 23.67309 |
| 1.50002 | 51.08503 | 45.74731 | 42.02397 | 37.27414 | 35.78166 | 29.41752 | 27.51145 | 23.67309 |
| 1.51003 | 51.24996 | 45.74731 | 42.20993 | 37.27414 | 35.91453 | 29.41752 | 27.65503 | 23.67309 |
| 1.52 | 51.30826 | 45.74731 | 42.2488 | 37.27414 | 35.96881 | 29.41752 | 27.74108 | 23.67309 |
| 1.53002 | 51.31338 | 45.74862 | 42.26705 | 37.27414 | 35.98296 | 29.41752 | 27.77063 | 23.67309 |
| 1.54003 | 51.32205 | 45.82108 | 42.27147 | 37.30821 | 35.98735 | 29.41752 | 27.7758 | 23.67309 |
| 1.55 | 51.32205 | 46.36564 | 42.27171 | 37.61088 | 35.9874 | 29.41752 | 27.7792 | 23.68119 |
| 1.56001 | 51.32205 | 47.12381 | 42.27172 | 38.00233 | 35.9874 | 29.4679 | 27.78068 | 23.72322 |
| 1.57003 | 51.32205 | 48.38247 | 42.27172 | 38.75377 | 35.9874 | 29.63614 | 27.78138 | 23.80389 |
| 1.58004 | 51.32205 | 49.59513 | 42.27172 | 39.99422 | 35.9874 | 29.85078 | 27.78138 | 24.03397 |
| 1.59001 | 51.32205 | 50.42786 | 42.27172 | 41.10616 | 35.9874 | 30.38576 | 27.78138 | 24.4078 |
| 1.60003 | 51.32205 | 51.1432 | 42.27172 | 41.87898 | 35.9874 | 31.26284 | 27.78138 | 24.86205 |
| 1.61004 | 51.32205 | 51.62018 | 42.27172 | 42.40808 | 35.9874 | 31.93392 | 27.78138 | 25.61744 |
| 1.62001 | 51.32205 | 51.78256 | 42.27172 | 42.87572 | 35.9874 | 32.55594 | 27.78138 | 26.07442 |
| 1.63002 | 51.32205 | 51.82425 | 42.27172 | 43.08596 | 35.9874 | 33.09531 | 27.78138 | 26.69882 |
| 1.64004 | 51.55592 | 51.82628 | 42.27178 | 43.19267 | 35.9874 | 33.54089 | 27.78138 | 27.1153 |
| 1.65001 | 51.91159 | 51.82771 | 42.27189 | 43.20849 | 35.9874 | 33.89681 | 27.78138 | 27.45302 |
| 1.66002 | 52.95829 | 51.82771 | 42.45282 | 43.21498 | 35.9874 | 34.12207 | 27.78138 | 27.81162 |
| 1.67004 | 54.50091 | 51.82771 | 42.79355 | 43.22039 | 35.9874 | 34.23054 | 27.78138 | 28.31659 |
| 1.68 | 55.65083 | 51.82771 | 43.46153 | 43.2218 | 36.02985 | 34.32434 | 27.78138 | 28.57244 |
| 1.69002 | 56.81098 | 51.82771 | 44.71232 | 43.22182 | 36.20015 | 34.335 | 27.78138 | 28.78181 |
| 1.70003 | 57.29766 | 51.82771 | 45.85414 | 43.22183 | 36.53498 | 34.33926 | 27.78138 | 28.8977 |
| 1.71 | 57.46007 | 51.82771 | 46.94025 | 43.22183 | 37.23419 | 34.34217 | 27.78138 | 28.94562 |
| 1.72002 | 57.53677 | 51.82771 | 47.61927 | 43.22183 | 38.14989 | 34.34219 | 27.79687 | 28.95786 |
| 1.73003 | 57.54356 | 51.82771 | 48.06775 | 43.22183 | 38.98048 | 34.34219 | 27.9402 | 28.95987 |
| 1.74 | 57.54621 | 51.82771 | 48.23296 | 43.22183 | 39.66749 | 34.34219 | 28.16755 | 28.96167 |
| 1.75001 | 57.54641 | 51.8619 | 48.26769 | 43.22183 | 40.38277 | 34.34219 | 28.64603 | 28.96361 |

Normal cumulative contact energy data table of different tillage depth method

| Time | Normal cumulative contact energy |  |  |
| --- | --- | --- | --- |
|  | 14cm | 12cm | 10cm |
| 0 | 0 | 0 | 0 |
| 0.01001 | 0.01502 | 0 | 0 |
| 0.0109 | 0.01504 | 0 | 0 |
| 0.02003 | 0.02137 | 0.03018 | 0 |
| 0.03004 | 0.04943 | 0.07073 | 0.02791 |
| 0.04001 | 0.09775 | 0.15266 | 0.07236 |
| 0.05003 | 0.21351 | 0.29695 | 0.43158 |
| 0.06004 | 0.37951 | 0.45857 | 0.54627 |
| 0.07001 | 0.53859 | 0.6281 | 0.69375 |
| 0.08002 | 0.72152 | 0.80093 | 0.82203 |
| 0.09004 | 0.91377 | 0.94063 | 0.96758 |
| 0.10001 | 1.09094 | 1.11824 | 1.18909 |
| 0.11002 | 1.31524 | 1.30867 | 1.29747 |
| 0.12004 | 1.48838 | 1.4014 | 1.46692 |
| 0.13001 | 1.61422 | 1.4814 | 1.52623 |
| 0.14002 | 1.69732 | 1.51819 | 1.56115 |
| 0.15003 | 1.76006 | 1.53569 | 1.57545 |
| 0.16 | 1.78846 | 1.54221 | 1.57785 |
| 0.17002 | 1.80102 | 1.5445 | 1.57835 |
| 0.18003 | 1.80405 | 1.54693 | 1.57841 |
| 0.19 | 1.80512 | 1.54974 | 1.57885 |
| 0.20001 | 1.80602 | 1.55204 | 1.57885 |
| 0.21003 | 1.80797 | 1.55204 | 1.57885 |
| 0.22004 | 1.80801 | 1.55204 | 1.57885 |
| 0.23001 | 1.80801 | 1.55204 | 1.57885 |
| 0.24003 | 1.80801 | 1.55204 | 1.57885 |
| 0.25004 | 1.80801 | 1.55204 | 1.57885 |
| 0.26001 | 1.80801 | 1.55204 | 1.57885 |
| 0.27002 | 1.80801 | 1.55204 | 1.57885 |
| 0.28004 | 1.80801 | 1.55204 | 1.57885 |
| 0.29001 | 1.80801 | 1.55204 | 1.57885 |
| 0.30002 | 1.80801 | 1.55204 | 1.57885 |
| 0.31004 | 1.80801 | 1.55204 | 1.57885 |
| 0.32 | 1.80801 | 1.55204 | 1.57885 |
| 0.33002 | 1.80955 | 1.55204 | 1.57885 |
| 0.34003 | 1.82534 | 1.55438 | 1.57885 |
| 0.35 | 1.89395 | 1.58636 | 1.64826 |
| 0.36002 | 1.99152 | 1.64036 | 1.89637 |
| 0.37003 | 2.19806 | 1.97115 | 2.05854 |
| 0.38 | 2.37773 | 2.11482 | 2.24887 |
| 0.39002 | 2.58021 | 2.27509 | 2.37173 |
| 0.40003 | 2.76884 | 2.43117 | 2.51694 |
| 0.41004 | 2.93444 | 2.58279 | 2.61238 |
| 0.42001 | 3.1018 | 2.69622 | 2.69788 |
| 0.43003 | 3.20979 | 2.81087 | 2.78505 |
| 0.44004 | 3.30401 | 2.83196 | 2.81798 |
| 0.45001 | 3.3772 | 2.90364 | 2.8355 |
| 0.46002 | 3.41627 | 2.96245 | 2.83841 |
| 0.47004 | 3.4327 | 2.98886 | 2.84284 |
| 0.48001 | 3.43646 | 2.9982 | 2.84558 |
| 0.49002 | 3.4376 | 2.99993 | 2.84576 |
| 0.50004 | 3.43799 | 3.00203 | 2.84576 |
| 0.51001 | 3.43945 | 3.00263 | 2.84577 |
| 0.52002 | 3.4397 | 3.00268 | 2.84577 |
| 0.53003 | 3.4397 | 3.00268 | 2.84577 |
| 0.54 | 3.4397 | 3.00268 | 2.84577 |
| 0.55002 | 3.4397 | 3.00268 | 2.84577 |
| 0.56003 | 3.4397 | 3.00268 | 2.84577 |
| 0.57 | 3.4397 | 3.00268 | 2.84577 |
| 0.58001 | 3.4397 | 3.00268 | 2.84577 |
| 0.59003 | 3.4397 | 3.00268 | 2.84577 |
| 0.60004 | 3.4397 | 3.00268 | 2.84577 |
| 0.60181 | 3.4397 | 3.00268 | 2.84577 |
| 0.61001 | 3.4397 | 3.00268 | 2.84577 |
| 0.62003 | 3.4397 | 3.00268 | 2.84577 |
| 0.63004 | 3.4397 | 3.00268 | 2.84577 |
| 0.64001 | 3.44441 | 3.00268 | 2.87479 |
| 0.65002 | 3.49473 | 3.02704 | 2.92261 |
| 0.66004 | 3.56989 | 3.0875 | 3.04819 |
| 0.67001 | 3.67187 | 3.16533 | 3.20288 |
| 0.68002 | 3.81889 | 3.28942 | 3.36552 |
| 0.69004 | 4.04819 | 3.45543 | 3.5041 |
| 0.70001 | 4.20652 | 3.61512 | 3.60853 |
| 0.71002 | 4.36061 | 3.75848 | 3.70442 |
| 0.72003 | 4.5157 | 3.91399 | 3.76978 |
| 0.73 | 4.63748 | 4.01681 | 3.80756 |
| 0.74002 | 4.77116 | 4.1059 | 3.83021 |
| 0.75003 | 4.83094 | 4.16847 | 3.83228 |
| 0.76 | 4.87537 | 4.19454 | 3.83398 |
| 0.77002 | 4.88815 | 4.20879 | 3.83673 |
| 0.78003 | 4.89229 | 4.21173 | 3.83673 |
| 0.79004 | 4.8928 | 4.21352 | 3.83694 |
| 0.80001 | 4.89632 | 4.21435 | 3.83694 |
| 0.81003 | 4.89769 | 4.21477 | 3.83694 |
| 0.82004 | 4.89774 | 4.21477 | 3.83694 |
| 0.83001 | 4.89774 | 4.21477 | 3.83694 |
| 0.84003 | 4.89774 | 4.21477 | 3.83694 |
| 0.85004 | 4.89774 | 4.21477 | 3.83694 |
| 0.86001 | 4.89774 | 4.21477 | 3.83694 |
| 0.87002 | 4.89774 | 4.21477 | 3.83694 |
| 0.88004 | 4.89774 | 4.21477 | 3.83694 |
| 0.89001 | 4.89774 | 4.21477 | 3.83694 |
| 0.90002 | 4.89774 | 4.21477 | 3.83694 |
| 0.91003 | 4.89774 | 4.21477 | 3.83694 |
| 0.92 | 4.89774 | 4.21477 | 3.83694 |
| 0.93002 | 4.8982 | 4.21477 | 3.84202 |
| 0.94003 | 4.91301 | 4.21648 | 3.88196 |
| 0.95 | 4.96172 | 4.25795 | 3.94981 |
| 0.96001 | 5.02022 | 4.32338 | 4.08548 |
| 0.97003 | 5.13171 | 4.40195 | 4.23534 |
| 0.98004 | 5.31453 | 4.54963 | 4.36437 |
| 0.99001 | 5.52037 | 4.79857 | 4.54128 |
| 1.00003 | 5.71458 | 4.97048 | 4.64348 |
| 1.01004 | 5.88887 | 5.13684 | 4.72518 |
| 1.02001 | 6.01712 | 5.28747 | 4.79048 |
| 1.03002 | 6.13882 | 5.40125 | 4.82413 |
| 1.04004 | 6.25828 | 5.46561 | 4.83953 |
| 1.05001 | 6.31839 | 5.58793 | 4.84546 |
| 1.06002 | 6.36877 | 5.60414 | 4.84687 |
| 1.07004 | 6.39273 | 5.61008 | 4.84707 |
| 1.08001 | 6.39922 | 5.61179 | 4.84754 |
| 1.09002 | 6.40072 | 5.61443 | 4.84754 |
| 1.10003 | 6.40349 | 5.61652 | 4.84754 |
| 1.11 | 6.40452 | 5.6169 | 4.84754 |
| 1.12002 | 6.40513 | 5.6169 | 4.84754 |
| 1.13003 | 6.40513 | 5.6169 | 4.84754 |
| 1.14 | 6.40513 | 5.6169 | 4.84754 |
| 1.15002 | 6.40513 | 5.6169 | 4.84754 |
| 1.16003 | 6.40513 | 5.6169 | 4.84754 |
| 1.17004 | 6.40513 | 5.6169 | 4.84754 |
| 1.18001 | 6.40513 | 5.6169 | 4.84754 |
| 1.19003 | 6.40513 | 5.6169 | 4.84754 |
| 1.20004 | 6.40513 | 5.6169 | 4.84754 |
| 1.21001 | 6.40513 | 5.6169 | 4.84754 |
| 1.22003 | 6.40513 | 5.6169 | 4.84754 |
| 1.23004 | 6.40586 | 5.6169 | 4.84754 |
| 1.24001 | 6.4139 | 5.6169 | 4.89032 |
| 1.25002 | 6.47006 | 5.65211 | 5.20262 |
| 1.26004 | 6.55108 | 5.74522 | 5.35736 |
| 1.27001 | 6.68529 | 6.01675 | 5.49738 |
| 1.28002 | 6.84096 | 6.15487 | 5.66169 |
| 1.29003 | 7.05437 | 6.39163 | 5.805 |
| 1.3 | 7.23588 | 6.55284 | 5.92685 |
| 1.31002 | 7.39974 | 6.68072 | 6.01906 |
| 1.32003 | 7.54384 | 6.80654 | 6.08729 |
| 1.33 | 7.72453 | 6.93598 | 6.13804 |
| 1.34002 | 7.8828 | 7.02025 | 6.16396 |
| 1.35003 | 7.93494 | 7.07439 | 6.16871 |
| 1.36004 | 7.97522 | 7.1166 | 6.16911 |
| 1.37001 | 7.98419 | 7.12306 | 6.16997 |
| 1.38003 | 7.98781 | 7.12473 | 6.17021 |
| 1.39004 | 7.98906 | 7.12551 | 6.17024 |
| 1.40001 | 7.98923 | 7.1283 | 6.17024 |
| 1.41003 | 7.98941 | 7.12879 | 6.17024 |
| 1.42004 | 7.98942 | 7.12905 | 6.17024 |
| 1.43001 | 7.98942 | 7.12905 | 6.17024 |
| 1.44002 | 7.98942 | 7.12905 | 6.17024 |
| 1.45004 | 7.98942 | 7.12905 | 6.17024 |
| 1.46001 | 7.98942 | 7.12905 | 6.17024 |
| 1.47002 | 7.98942 | 7.12905 | 6.17024 |
| 1.48003 | 7.98942 | 7.12905 | 6.17024 |
| 1.49 | 7.98942 | 7.12905 | 6.17024 |
| 1.50002 | 7.98942 | 7.12905 | 6.17024 |
| 1.51003 | 7.98942 | 7.12905 | 6.17024 |
| 1.52 | 7.98942 | 7.12905 | 6.17024 |
| 1.53002 | 7.98942 | 7.12905 | 6.17101 |
| 1.54003 | 7.99367 | 7.12905 | 6.21229 |
| 1.55 | 8.04616 | 7.15642 | 6.27117 |
| 1.56001 | 8.13829 | 7.21905 | 6.37831 |
| 1.57003 | 8.23436 | 7.30339 | 6.52851 |
| 1.58004 | 8.37013 | 7.47118 | 6.67137 |
| 1.59001 | 8.55245 | 7.62596 | 6.82693 |
| 1.60003 | 8.73904 | 7.77975 | 6.94738 |
| 1.61004 | 8.92789 | 7.93203 | 7.02995 |
| 1.62001 | 9.08973 | 8.06294 | 7.09955 |
| 1.63002 | 9.22264 | 8.159 | 7.12972 |
| 1.64004 | 9.29756 | 8.26922 | 7.14509 |
| 1.65001 | 9.36046 | 8.31865 | 7.15158 |
| 1.66002 | 9.40393 | 8.34194 | 7.15252 |
| 1.67004 | 9.42586 | 8.35269 | 7.1554 |
| 1.68 | 9.42922 | 8.35426 | 7.15563 |
| 1.69002 | 9.43048 | 8.35474 | 7.15568 |
| 1.70003 | 9.43214 | 8.35576 | 7.15568 |
| 1.71 | 9.43344 | 8.35576 | 7.15568 |
| 1.72002 | 9.43537 | 8.35576 | 7.15568 |
| 1.73003 | 9.43537 | 8.35576 | 7.15568 |
| 1.74 | 9.43537 | 8.35576 | 7.15568 |
| 1.75001 | 9.43537 | 8.35576 | 7.15568 |

Data table of tangential cumulative contact energy

in different tillage depths

| Time | Tangential cumulative contact energy |  |  |
| --- | --- | --- | --- |
|  | 14cm | 12cm | 10cm |
| 0 | 0 | 0 | 0 |
| 0.01001 | 0.0092 | 0 | 0 |
| 0.0109 | 0.00925 | 0 | 0 |
| 0.02003 | 0.0107 | 0.01403 | 0 |
| 0.03004 | 0.06676 | 0.09181 | 0.02232 |
| 0.04001 | 0.34451 | 0.41597 | 0.12649 |
| 0.05003 | 0.79812 | 1.04589 | 0.90257 |
| 0.06004 | 1.82008 | 1.62033 | 1.41477 |
| 0.07001 | 2.64679 | 2.54069 | 2.22523 |
| 0.08002 | 3.4719 | 3.12732 | 2.83932 |
| 0.09004 | 4.38179 | 3.83743 | 3.49215 |
| 0.10001 | 5.28041 | 4.54746 | 4.6945 |
| 0.11002 | 6.19991 | 5.053 | 5.11575 |
| 0.12004 | 6.83735 | 5.56515 | 5.39925 |
| 0.13001 | 7.52045 | 5.98121 | 5.61394 |
| 0.14002 | 7.86625 | 6.26287 | 5.85303 |
| 0.15003 | 8.11915 | 6.43117 | 5.92421 |
| 0.16 | 8.31698 | 6.49963 | 5.95183 |
| 0.17002 | 8.41636 | 6.51575 | 5.95373 |
| 0.18003 | 8.45705 | 6.5174 | 5.95432 |
| 0.19 | 8.45988 | 6.52102 | 5.95562 |
| 0.20001 | 8.46147 | 6.52252 | 5.95562 |
| 0.21003 | 8.46371 | 6.52252 | 5.95562 |
| 0.22004 | 8.46417 | 6.52253 | 5.95562 |
| 0.23001 | 8.46417 | 6.52254 | 5.95562 |
| 0.24003 | 8.46417 | 6.52254 | 5.95562 |
| 0.25004 | 8.46417 | 6.52254 | 5.95562 |
| 0.26001 | 8.46417 | 6.52254 | 5.95562 |
| 0.27002 | 8.46417 | 6.52254 | 5.95562 |
| 0.28004 | 8.46417 | 6.52254 | 5.95562 |
| 0.29001 | 8.46417 | 6.52254 | 5.95562 |
| 0.30002 | 8.46417 | 6.52254 | 5.95562 |
| 0.31004 | 8.46417 | 6.52254 | 5.95562 |
| 0.32 | 8.46417 | 6.52254 | 5.95562 |
| 0.33002 | 8.46571 | 6.52254 | 5.95562 |
| 0.34003 | 8.52449 | 6.52801 | 5.95562 |
| 0.35 | 8.74488 | 6.60087 | 6.19643 |
| 0.36002 | 9.0876 | 6.82365 | 6.73662 |
| 0.37003 | 9.70519 | 7.49301 | 7.1001 |
| 0.38 | 10.36441 | 7.99995 | 7.94366 |
| 0.39002 | 11.33254 | 8.9222 | 8.60604 |
| 0.40003 | 12.11238 | 9.65763 | 9.07901 |
| 0.41004 | 13.00741 | 10.25643 | 9.52153 |
| 0.42001 | 13.7127 | 10.80177 | 9.85765 |
| 0.43003 | 14.22726 | 11.4021 | 10.14112 |
| 0.44004 | 14.5912 | 11.45389 | 10.27923 |
| 0.45001 | 14.92508 | 11.74746 | 10.3907 |
| 0.46002 | 15.21792 | 12.06047 | 10.43083 |
| 0.47004 | 15.35352 | 12.14454 | 10.43974 |
| 0.48001 | 15.37032 | 12.22012 | 10.44765 |
| 0.49002 | 15.37647 | 12.23511 | 10.44919 |
| 0.50004 | 15.37814 | 12.23721 | 10.44921 |
| 0.51001 | 15.38139 | 12.23951 | 10.44934 |
| 0.52002 | 15.38244 | 12.23992 | 10.44934 |
| 0.53003 | 15.38258 | 12.23992 | 10.44934 |
| 0.54 | 15.38258 | 12.23992 | 10.44934 |
| 0.55002 | 15.38258 | 12.23992 | 10.44934 |
| 0.56003 | 15.38258 | 12.23992 | 10.44934 |
| 0.57 | 15.38258 | 12.23992 | 10.44934 |
| 0.58001 | 15.38258 | 12.23992 | 10.44934 |
| 0.59003 | 15.38258 | 12.23992 | 10.44934 |
| 0.60004 | 15.38258 | 12.23992 | 10.44934 |
| 0.60181 | 15.38258 | 12.23992 | 10.44934 |
| 0.61001 | 15.38258 | 12.23992 | 10.44934 |
| 0.62003 | 15.38258 | 12.23992 | 10.44934 |
| 0.63004 | 15.38258 | 12.23992 | 10.44934 |
| 0.64001 | 15.39843 | 12.23992 | 10.4958 |
| 0.65002 | 15.54889 | 12.28376 | 10.60625 |
| 0.66004 | 15.77776 | 12.43923 | 10.88576 |
| 0.67001 | 16.27696 | 12.67365 | 11.37608 |
| 0.68002 | 17.01343 | 13.41222 | 12.29092 |
| 0.69004 | 18.17388 | 14.17935 | 12.8433 |
| 0.70001 | 19.14048 | 15.01625 | 13.22056 |
| 0.71002 | 20.04682 | 15.64132 | 13.70348 |
| 0.72003 | 20.69166 | 16.13532 | 13.95397 |
| 0.73 | 21.09638 | 16.64991 | 14.16338 |
| 0.74002 | 21.73989 | 17.09977 | 14.27372 |
| 0.75003 | 22.05999 | 17.47349 | 14.31839 |
| 0.76 | 22.22626 | 17.56987 | 14.32656 |
| 0.77002 | 22.35449 | 17.6304 | 14.32981 |
| 0.78003 | 22.36847 | 17.66398 | 14.32981 |
| 0.79004 | 22.37142 | 17.66778 | 14.33136 |
| 0.80001 | 22.37609 | 17.66965 | 14.33136 |
| 0.81003 | 22.38131 | 17.67108 | 14.33136 |
| 0.82004 | 22.3815 | 17.67108 | 14.33136 |
| 0.83001 | 22.3815 | 17.67108 | 14.33136 |
| 0.84003 | 22.3815 | 17.67108 | 14.33136 |
| 0.85004 | 22.3815 | 17.67108 | 14.33136 |
| 0.86001 | 22.3815 | 17.67108 | 14.33136 |
| 0.87002 | 22.3815 | 17.67108 | 14.33136 |
| 0.88004 | 22.3815 | 17.67108 | 14.33136 |
| 0.89001 | 22.3815 | 17.67108 | 14.33136 |
| 0.90002 | 22.3815 | 17.67108 | 14.33136 |
| 0.91003 | 22.3815 | 17.67108 | 14.33136 |
| 0.92 | 22.3815 | 17.67108 | 14.33136 |
| 0.93002 | 22.38239 | 17.67108 | 14.34061 |
| 0.94003 | 22.43641 | 17.67597 | 14.48121 |
| 0.95 | 22.5788 | 17.77273 | 14.74081 |
| 0.96001 | 22.78364 | 18.02418 | 15.27019 |
| 0.97003 | 23.24241 | 18.2998 | 15.88986 |
| 0.98004 | 24.15663 | 18.87942 | 16.59771 |
| 0.99001 | 25.1955 | 19.66204 | 17.32935 |
| 1.00003 | 26.12091 | 20.45086 | 17.66209 |
| 1.01004 | 26.82399 | 21.30959 | 17.97331 |
| 1.02001 | 27.37105 | 22.00069 | 18.25235 |
| 1.03002 | 27.93303 | 22.59517 | 18.41725 |
| 1.04004 | 28.49515 | 23.00973 | 18.48755 |
| 1.05001 | 28.88775 | 23.27278 | 18.52669 |
| 1.06002 | 29.11582 | 23.33906 | 18.53614 |
| 1.07004 | 29.25757 | 23.37027 | 18.53684 |
| 1.08001 | 29.30819 | 23.37963 | 18.53759 |
| 1.09002 | 29.31616 | 23.38309 | 18.53764 |
| 1.10003 | 29.32105 | 23.38701 | 18.53764 |
| 1.11 | 29.32361 | 23.38872 | 18.53764 |
| 1.12002 | 29.32502 | 23.38872 | 18.53764 |
| 1.13003 | 29.32502 | 23.38872 | 18.53764 |
| 1.14 | 29.32502 | 23.38872 | 18.53764 |
| 1.15002 | 29.32502 | 23.38872 | 18.53764 |
| 1.16003 | 29.32502 | 23.38872 | 18.53764 |
| 1.17004 | 29.32502 | 23.38872 | 18.53764 |
| 1.18001 | 29.32502 | 23.38872 | 18.53764 |
| 1.19003 | 29.32502 | 23.38872 | 18.53764 |
| 1.20004 | 29.32502 | 23.38872 | 18.53764 |
| 1.21001 | 29.32502 | 23.38872 | 18.53764 |
| 1.22003 | 29.32502 | 23.38872 | 18.53764 |
| 1.23004 | 29.32764 | 23.38872 | 18.53764 |
| 1.24001 | 29.34435 | 23.38872 | 18.66083 |
| 1.25002 | 29.44056 | 23.4789 | 19.27254 |
| 1.26004 | 29.74828 | 23.7215 | 19.87669 |
| 1.27001 | 30.15733 | 24.43316 | 20.60686 |
| 1.28002 | 30.94678 | 25.27793 | 21.23665 |
| 1.29003 | 32.11471 | 26.11813 | 21.9152 |
| 1.3 | 33.18386 | 26.69624 | 22.37438 |
| 1.31002 | 34.0532 | 27.36885 | 22.80635 |
| 1.32003 | 34.73961 | 28.02562 | 23.05376 |
| 1.33 | 35.18727 | 28.58916 | 23.28961 |
| 1.34002 | 35.64357 | 28.9354 | 23.45066 |
| 1.35003 | 36.09583 | 29.13827 | 23.50332 |
| 1.36004 | 36.39409 | 29.30725 | 23.5078 |
| 1.37001 | 36.49709 | 29.39913 | 23.50978 |
| 1.38003 | 36.51662 | 29.40558 | 23.51072 |
| 1.39004 | 36.52255 | 29.4084 | 23.51106 |
| 1.40001 | 36.52331 | 29.41607 | 23.51106 |
| 1.41003 | 36.52353 | 29.41659 | 23.51106 |
| 1.42004 | 36.52357 | 29.41752 | 23.51106 |
| 1.43001 | 36.52357 | 29.41752 | 23.51106 |
| 1.44002 | 36.52357 | 29.41752 | 23.51106 |
| 1.45004 | 36.52357 | 29.41752 | 23.51106 |
| 1.46001 | 36.52357 | 29.41752 | 23.51106 |
| 1.47002 | 36.52357 | 29.41752 | 23.51106 |
| 1.48003 | 36.52357 | 29.41752 | 23.51106 |
| 1.49 | 36.52357 | 29.41752 | 23.51106 |
| 1.50002 | 36.52357 | 29.41752 | 23.51106 |
| 1.51003 | 36.52357 | 29.41752 | 23.51106 |
| 1.52 | 36.52357 | 29.41752 | 23.51106 |
| 1.53002 | 36.52357 | 29.41752 | 23.51518 |
| 1.54003 | 36.53217 | 29.41752 | 23.60644 |
| 1.55 | 36.67189 | 29.4679 | 23.7598 |
| 1.56001 | 36.98851 | 29.63614 | 24.27405 |
| 1.57003 | 37.41356 | 29.85078 | 24.97297 |
| 1.58004 | 38.21691 | 30.38576 | 25.46401 |
| 1.59001 | 39.21866 | 31.26284 | 26.1543 |
| 1.60003 | 40.0483 | 31.93392 | 26.62226 |
| 1.61004 | 40.9733 | 32.55594 | 27.04323 |
| 1.62001 | 41.64885 | 33.09531 | 27.32666 |
| 1.63002 | 42.19271 | 33.54089 | 27.48554 |
| 1.64004 | 42.53289 | 33.89681 | 27.58816 |
| 1.65001 | 42.86113 | 34.12207 | 27.61005 |
| 1.66002 | 42.99062 | 34.23054 | 27.61403 |
| 1.67004 | 43.06862 | 34.32434 | 27.61837 |
| 1.68 | 43.10919 | 34.335 | 27.62012 |
| 1.69002 | 43.11696 | 34.33926 | 27.62042 |
| 1.70003 | 43.12013 | 34.34217 | 27.62042 |
| 1.71 | 43.12434 | 34.34219 | 27.62042 |
| 1.72002 | 43.12544 | 34.34219 | 27.62042 |
| 1.73003 | 43.12544 | 34.34219 | 27.62042 |
| 1.74 | 43.12544 | 34.34219 | 27.62042 |
| 1.75001 | 43.12544 | 34.34219 | 27.62042 |

Normal cumulative contact energy data table of different forward speed

| Time | Normal cumulative contact energy |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 3.01m/s | 1.89m/s | 1.54m/s | 1.29m/s | 0.8m/s |
| 0 | 0 | 0 | 0 | 0 | 0 |
| 0.01001 | 0 | 0 | 0 | 0 | 0 |
| 0.02003 | 0 | 0 | 0 | 0 | 0 |
| 0.03004 | 0.0036 | 0.02208 | 0.02634 | 0.02247 | 0.03018 |
| 0.04001 | 0.04544 | 0.05777 | 0.06296 | 0.06129 | 0.07073 |
| 0.05003 | 0.15801 | 0.15685 | 0.17034 | 0.23144 | 0.15266 |
| 0.06004 | 0.4867 | 0.33618 | 0.31157 | 0.36079 | 0.29695 |
| 0.07001 | 0.95451 | 0.54366 | 0.4883 | 0.5387 | 0.45857 |
| 0.08002 | 1.51205 | 0.92293 | 0.71382 | 0.73765 | 0.6281 |
| 0.09004 | 1.9015 | 1.27412 | 1.06305 | 0.99599 | 0.80093 |
| 0.10001 | 2.35301 | 1.50471 | 1.39864 | 1.22585 | 0.94063 |
| 0.11002 | 2.85341 | 1.80085 | 1.60109 | 1.49847 | 1.11824 |
| 0.12004 | 3.26565 | 2.03171 | 1.81624 | 1.67824 | 1.30867 |
| 0.13001 | 3.68211 | 2.22925 | 1.97142 | 1.83258 | 1.4014 |
| 0.14002 | 3.94282 | 2.38272 | 2.09207 | 1.96284 | 1.4814 |
| 0.15003 | 4.19611 | 2.50916 | 2.20725 | 2.05547 | 1.51819 |
| 0.16 | 4.33262 | 2.57796 | 2.26355 | 2.09213 | 1.53569 |
| 0.17002 | 4.42173 | 2.61876 | 2.28271 | 2.10302 | 1.54221 |
| 0.18003 | 4.43926 | 2.6234 | 2.2864 | 2.10542 | 1.5445 |
| 0.19 | 4.44067 | 2.62457 | 2.28772 | 2.10664 | 1.54693 |
| 0.20001 | 4.44067 | 2.62479 | 2.28841 | 2.10828 | 1.54974 |
| 0.21003 | 4.4409 | 2.62765 | 2.28998 | 2.10968 | 1.55204 |
| 0.22004 | 4.44166 | 2.62768 | 2.29041 | 2.10968 | 1.55204 |
| 0.23001 | 4.44207 | 2.62768 | 2.29041 | 2.11008 | 1.55204 |
| 0.24003 | 4.44207 | 2.62768 | 2.29041 | 2.11008 | 1.55204 |
| 0.25004 | 4.44477 | 2.62772 | 2.29041 | 2.11008 | 1.55204 |
| 0.26001 | 4.44605 | 2.62772 | 2.29041 | 2.11008 | 1.55204 |
| 0.27002 | 4.44645 | 2.62772 | 2.29041 | 2.11008 | 1.55204 |
| 0.28004 | 4.44645 | 2.62772 | 2.29041 | 2.11008 | 1.55204 |
| 0.29001 | 4.44645 | 2.62772 | 2.29041 | 2.11008 | 1.55204 |
| 0.30002 | 4.44645 | 2.62772 | 2.29041 | 2.11008 | 1.55204 |
| 0.31004 | 4.44705 | 2.62819 | 2.29041 | 2.11008 | 1.55204 |
| 0.32 | 4.44802 | 2.6285 | 2.29041 | 2.11008 | 1.55204 |
| 0.33002 | 4.45727 | 2.62877 | 2.29041 | 2.11008 | 1.55204 |
| 0.34003 | 4.50465 | 2.66318 | 2.30029 | 2.11008 | 1.55438 |
| 0.35 | 4.63804 | 2.72921 | 2.37433 | 2.15641 | 1.58636 |
| 0.36002 | 4.87585 | 2.89934 | 2.49782 | 2.26471 | 1.64036 |
| 0.37003 | 5.23352 | 3.11191 | 2.68174 | 2.48684 | 1.97115 |
| 0.38 | 5.64254 | 3.44337 | 2.9328 | 2.69598 | 2.11482 |
| 0.39002 | 6.05604 | 3.69925 | 3.17926 | 2.89617 | 2.27509 |
| 0.40003 | 6.6197 | 3.97299 | 3.42505 | 3.08898 | 2.43117 |
| 0.41004 | 7.12502 | 4.2239 | 3.65117 | 3.30774 | 2.58279 |
| 0.42001 | 7.56241 | 4.48303 | 3.87227 | 3.49717 | 2.69622 |
| 0.43003 | 7.94428 | 4.7058 | 4.02879 | 3.64444 | 2.81087 |
| 0.44004 | 8.38938 | 4.91215 | 4.14844 | 3.76936 | 2.90364 |
| 0.45001 | 8.57373 | 5.14225 | 4.27496 | 3.8491 | 2.96245 |
| 0.46002 | 8.71163 | 5.20512 | 4.35452 | 3.88195 | 2.98886 |
| 0.47004 | 8.76612 | 5.24161 | 4.38818 | 3.89151 | 2.9982 |
| 0.48001 | 8.78878 | 5.24766 | 4.39162 | 3.89526 | 2.99993 |
| 0.49002 | 8.79201 | 5.24802 | 4.39477 | 3.8971 | 3.00203 |
| 0.50004 | 8.79201 | 5.25005 | 4.39678 | 3.89728 | 3.00263 |
| 0.51001 | 8.79212 | 5.25217 | 4.39752 | 3.89763 | 3.00268 |
| 0.52002 | 8.79212 | 5.25217 | 4.39753 | 3.89764 | 3.00268 |
| 0.53003 | 8.79212 | 5.25229 | 4.39771 | 3.89764 | 3.00268 |
| 0.54 | 8.79333 | 5.25229 | 4.39771 | 3.89764 | 3.00268 |
| 0.55002 | 8.79333 | 5.25229 | 4.39771 | 3.89764 | 3.00268 |
| 0.56003 | 8.79488 | 5.25229 | 4.39771 | 3.89764 | 3.00268 |
| 0.57 | 8.79913 | 5.25229 | 4.39771 | 3.89764 | 3.00268 |
| 0.58001 | 8.79913 | 5.25229 | 4.39771 | 3.89764 | 3.00268 |
| 0.59003 | 8.79913 | 5.25229 | 4.39771 | 3.89764 | 3.00268 |
| 0.60004 | 8.79913 | 5.25229 | 4.39771 | 3.89764 | 3.00268 |

Different forward speed tangential cumulative contact energy data table

| Time | Tangential cumulative contact energy |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 3.01m/s | 1.89m/s | 1.54m/s | 1.29m/s | 0.8m/S |
| 0 | 0 | 0 | 0 | 0 | 0 |
| 0.01001 | 0 | 0 | 0 | 0 | 0 |
| 0.02003 | 0 | 0 | 0 | 0 | 0 |
| 0.03004 | 0.00496 | 0.04084 | 0.02956 | 0.02414 | 0.01403 |
| 0.04001 | 0.20288 | 0.23899 | 0.10196 | 0.12562 | 0.09181 |
| 0.05003 | 0.84482 | 0.76594 | 0.52573 | 0.94541 | 0.41597 |
| 0.06004 | 1.98433 | 1.43976 | 1.28548 | 1.59505 | 1.04589 |
| 0.07001 | 3.56476 | 2.35542 | 2.34948 | 2.36994 | 1.62033 |
| 0.08002 | 4.96319 | 3.5916 | 3.2332 | 3.41096 | 2.54069 |
| 0.09004 | 6.23575 | 4.86168 | 5.57467 | 4.39741 | 3.12732 |
| 0.10001 | 7.83628 | 5.66124 | 6.82807 | 5.14916 | 3.83743 |
| 0.11002 | 9.29805 | 6.46116 | 7.37126 | 5.9021 | 4.54746 |
| 0.12004 | 10.66411 | 7.45689 | 7.99335 | 6.39087 | 5.053 |
| 0.13001 | 12.17279 | 8.27759 | 8.55205 | 6.91813 | 5.56515 |
| 0.14002 | 13.38625 | 9.11088 | 9.06777 | 7.40276 | 5.98121 |
| 0.15003 | 14.51452 | 9.83053 | 9.45783 | 7.8743 | 6.26287 |
| 0.16 | 15.17997 | 10.10267 | 9.69453 | 8.10016 | 6.43117 |
| 0.17002 | 15.42682 | 10.36595 | 9.82653 | 8.19909 | 6.49963 |
| 0.18003 | 15.47286 | 10.39433 | 9.85148 | 8.21214 | 6.51575 |
| 0.19 | 15.47388 | 10.39602 | 9.85504 | 8.21568 | 6.5174 |
| 0.20001 | 15.47388 | 10.39651 | 9.85803 | 8.21901 | 6.52102 |
| 0.21003 | 15.47487 | 10.40108 | 9.85958 | 8.22016 | 6.52252 |
| 0.22004 | 15.47538 | 10.40131 | 9.86095 | 8.22016 | 6.52253 |
| 0.23001 | 15.4759 | 10.40131 | 9.86095 | 8.22147 | 6.52254 |
| 0.24003 | 15.4759 | 10.40131 | 9.86095 | 8.22147 | 6.52254 |
| 0.25004 | 15.47677 | 10.40148 | 9.86095 | 8.22147 | 6.52254 |
| 0.26001 | 15.47701 | 10.40148 | 9.86095 | 8.22147 | 6.52254 |
| 0.27002 | 15.47713 | 10.40148 | 9.86095 | 8.22147 | 6.52254 |
| 0.28004 | 15.47713 | 10.40148 | 9.86095 | 8.22147 | 6.52254 |
| 0.29001 | 15.47713 | 10.40148 | 9.86095 | 8.22147 | 6.52254 |
| 0.30002 | 15.47713 | 10.40148 | 9.86095 | 8.22147 | 6.52254 |
| 0.31004 | 15.4778 | 10.40284 | 9.86095 | 8.22147 | 6.52254 |
| 0.32 | 15.48013 | 10.40366 | 9.86095 | 8.22147 | 6.52254 |
| 0.33002 | 15.4976 | 10.4039 | 9.86095 | 8.22147 | 6.52254 |
| 0.34003 | 15.74426 | 10.52944 | 9.87759 | 8.22147 | 6.52801 |
| 0.35 | 16.26247 | 10.86458 | 10.0931 | 8.3006 | 6.60087 |
| 0.36002 | 17.30595 | 11.4905 | 10.59751 | 8.61151 | 6.82365 |
| 0.37003 | 18.62665 | 12.75074 | 11.27563 | 9.29128 | 7.49301 |
| 0.38 | 20.24298 | 13.92475 | 12.40146 | 10.06549 | 7.99995 |
| 0.39002 | 21.88407 | 14.87444 | 13.41446 | 10.93177 | 8.9222 |
| 0.40003 | 23.45323 | 16.24591 | 14.42006 | 11.74803 | 9.65763 |
| 0.41004 | 25.18643 | 17.18136 | 15.25779 | 12.80052 | 10.25643 |
| 0.42001 | 26.62163 | 18.11456 | 16.10217 | 13.44655 | 10.80177 |
| 0.43003 | 27.97903 | 18.73385 | 16.78626 | 13.97944 | 11.4021 |
| 0.44004 | 29.21772 | 19.39975 | 17.42126 | 14.53766 | 11.74746 |
| 0.45001 | 29.78278 | 20.04023 | 17.9135 | 15.03282 | 12.06047 |
| 0.46002 | 30.30645 | 20.36516 | 18.71548 | 15.30125 | 12.14454 |
| 0.47004 | 30.53782 | 20.62875 | 19.23247 | 15.34284 | 12.22012 |
| 0.48001 | 30.63143 | 20.6501 | 19.26289 | 15.36087 | 12.23511 |
| 0.49002 | 30.63628 | 20.65114 | 19.26769 | 15.36377 | 12.23721 |
| 0.50004 | 30.63628 | 20.65397 | 19.26917 | 15.36445 | 12.23951 |
| 0.51001 | 30.63637 | 20.65566 | 19.27007 | 15.36531 | 12.23992 |
| 0.52002 | 30.63644 | 20.65566 | 19.27023 | 15.36545 | 12.23992 |
| 0.53003 | 30.63645 | 20.65583 | 19.27117 | 15.36546 | 12.23992 |
| 0.54 | 30.63715 | 20.65583 | 19.27117 | 15.36546 | 12.23992 |
| 0.55002 | 30.63717 | 20.65583 | 19.27117 | 15.36546 | 12.23992 |
| 0.56003 | 30.6377 | 20.65583 | 19.27117 | 15.36546 | 12.23992 |
| 0.57 | 30.63851 | 20.65583 | 19.27117 | 15.36546 | 12.23992 |
| 0.58001 | 30.63851 | 20.65583 | 19.27117 | 15.36546 | 12.23992 |
| 0.59003 | 30.63851 | 20.65583 | 19.27117 | 15.36546 | 12.23992 |
| 0.60004 | 30.63851 | 20.65583 | 19.27117 | 15.36546 | 12.23992 |

Table 13 The disturbance area of rotary tillage blade to soil

| Parameter | Actual value /cm2 | Simulative value /cm2 | Error /% |
| --- | --- | --- | --- |
| Longitudinal soil disturbance area | 157.31 | 163.43 | 3.89 |
| Overlooking soil disturbance area | 423.38 | 435.15 | 2.78 |