Supplementary Information

Emergence of Two High-pressure Superconducting Phases in Pressurized Optical Semiconductor GaP

Nixian Qian1,2, Yonghui Zhou1,2, Chunhua Chen1, Ranran Zhang1, Yifang Yuan3, Xuliang Chen1,2, Chao An4, Ying Zhou4, Min Zhang4, and Zhaorong Yang1,2,4,5

1Anhui Province Key Laboratory of Condensed Matter Physics at Extreme Conditions, High Magnetic Field Laboratory, HFIPS, Chinese Academy of Sciences, Hefei 230031, China.

2Science Island Branch of Graduate School, University of Science and Technology of China, Hefei 230026, China.

3Key Laboratory of Material Physics, Ministry of Education, School of Physics and Microelectronics, Zhengzhou University, Zhengzhou 450001, China.

4Institutes of Physical Science and Information Technology, Anhui University, Hefei 230601, China.

5Collaborative Innovation Center of Advanced Microstructures, Nanjing University, Nanjing 210093, China

Correspondence: Yonghui Zhou (yhzhou@hmfl.ac.cn) or Zhaorong Yang (zryang@issp.ac.cn)

Figure S1. Structural characterization of GaP single crystal at ambient pressure. (a) Schematic crystal structure of pristine cubic phase. (b) Room-temperature XRD pattern of GaP single crystal. (c) EDXS of GaP single crystal by area scanning mode. (d) Room-temperature Raman spectrum of GaP single crystal (λ = 532 nm).