Supporting Information

Synergistic Effect of N, O, S Heteroatoms in Bifunctional Covalent Organic Polymers Promotes Sensitive Detection and Efficient Capture of Mercury(II)

Ye Zhu,a Cailing Ni,*a Chao Zhang,a Zhimin Liu,b Guanghui Wu,a Yanqing Chen,a and Yuancheng Qina

a Key Laboratory of Jiangxi Province forPersistent Pollutants Control and Resources Recycle, Nanchang Hangkong University, Nanchang 330063, P. R. China

bSinocat Environmental Technology Co., Ltd.

Section 1 General Information and Synthesis Procedures

1.Synthesis of terephthalic hydrazide (HT)

A mixture of p-phthalic acid (2.3 g, 12.5 mmol), methanol (50 ml) and H2SO4 (1 ml) was heated to reflux for 4 h. The solution was evaporated under vacuum. The residue was dissolved in 150 ml CHCl3 and extracted with saturated sodium bicarbonate solution. The solvent was removed by rotary evaporation and given the product as a white solid (2.4 g, 93%). The product was used directly for the next step without further purification.

Dimethyl terephthalate (DMT) (1 g, 15 mmol), methanol (10 ml), toluene (10 ml) and Hydrazine hydrate (85%) (6.7 ml) were heated to reflux for 24 h under N2 atmosphere. The product precipitated during the reaction process and collected by filtration, washed with methanol and toluene, given the white solid (0.85 g, 85%).1H NMR (d6-DMSO, 300 MHz) δ 9.86 (s, 2H), 7.86 (s, 4H), 4.56 (s, 4H).

Synthesis of terephthalic hydrazide (HT)

2. The pseudo-first-order and pseudo-second-order rate models.

In order to describe the kinetics of mercury ion adsorption, we use a pseudo-first-order and pseudo-second-order model to fit the data, which can be known from the following equations:

1qt=k1qet+1qe                                       (1)

tqt=1k2qe2+tqe                                      (2)

In the formula, k1 (min–1) and k2 (mg g–1 min–1) are the rate constants for the pseudo-first-order and the pseudo-second-order models, respectively. qt (mg g−1) and qe (mg g−1) are the amount of mercury adsorbed at time t (min) and at equilibrium, respectively. The initial adsorption rate h (k2qe2) has been widely used for assessment of the adsorption rates. Typically, the distribution coefficient (Kd) is used to estimate the affinity of a sorbent for metal ions.

Section 2 Summary of Figures and Tables

Fig S1. The FT-IR spectrum of polymers HTDP-1 (a), HTDP-2 (b) and HTDP-3 (c).

Fig S2. Pore size distribution profile of HTDP-1, HTDP-2, and HTDP-3 (77K).

Fig S3. Hg2+ adsorption isotherm of HTDP-1, HTDP-2 and HTDP-3.

Fig S4. Fluorescence spectra of 1, 2, HTDP-2, and HTDP-2-Hg2+ in the dispersion solution of acetonitrile.

Fig S5. Fluorescence spectra of HTDP-2 in acetonitrile (black), DMF (red), THF (light blue), Acetone (purple), Ethanol (green) and Diethyl ether (dark blue).

Fig S6. FT-IR of HTDP-2 and HTDP-2-Hg2+.

Fig S7. XPS spectra of HTDP-2 and HTDP-2-Hg2+.

Table S1. Mercury (II) adsorption on the porous materials reported in the literature.

| Materials |  | Adsorption capacity/mg g−1 | Polymer dosage |  | Reference |
| --- | --- | --- | --- | --- | --- |
| POP-SH |  | 180 | 0.01g/10mL |  | [1] |
| TP-TC-MA |  | 351.6 | 0.02g/25mL |  | [2] |
| COF-S-SH |  | 1350 | 0.005g/10mL |  | [3] |
| COP-108-S |  | 241 | 0.03g/30mL |  | [4] |
| TpTSC |  | 1035 | 0.01g/50mL |  | [5] |
| SA@MnNP |  | 299 | 0.5g/30 mL |  | [6] |
| M-DAPS50-COF-SH |  | 383 | 0.005g/10mL |  | [7] |
| Sulfonated COF |  | 98.42 | 0.01g/50mL |  | [8] |
| PHTCZ-1-MA |  | 416 | 0.02g/50mL |  | [9] |
| HTDP-2 |  | 463.3 | 0.01g/50mL |  | This work |

Table S2. Comparison of various fluorescent probes for Hg2+ ion detection.

| Materials |  | LOD (ppm) | Linear range(ppm) | Reusability of fluorescence (Times of cycles) |  | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| N, S/C-dots |  | 0.4 | 0-8 | — |  | [10] |
| TNPP |  | 2.28×10-2 | 0-0.9 | 3 |  | [11] |
| BATH2-Bt |  | 5.2×10-3 | 0-5.5 | 5 |  | [12] |
| TFPPy-CHYD |  | 3.4×10-3 | 0-2 | 6 |  | [13] |
| COP-108-S |  | 2.89×10-3 | 0-2006 | 5 |  | [4] |
| TpTSC |  | 2 | 0-10 | — |  | [5] |
| COF-LUZ8 |  | 2.5×10-2 | 0-6680 | 3 |  | [14] |
| AH-COF |  | 2×10-2 | 0-8 | 4 |  | [15] |
| HPP-SH |  | 4.48×10-3 | 0-100 | — |  | [16] |
| UiO-66-PSM |  | 1.18 | 0-15.7 | — |  | [17] |
| FS-G |  | 3.34×10-2 | 0-12 | 7 |  | [18] |
| HTDP-2 |  | 0.7 | 0-150 | 5 |  | This work |

Reference

1. 	Cheng J, Li Y, Li L, et al (2019) New J Chem 43:7683–7693.

2. 	Zhang C, Peng Z, Guo Y, et al (2021) Sep Purif Technol 274:119097.

3. 	Sun Q, Aguila B, Perman J, et al (2017) J Am Chem Soc 139:2786–2793.

4. 	Li J, Wang S, Cao X, et al (2021) Mater Chem Front 5:3428–3435.

5. 	Tang CM, Qin YC, Ni CL, Zou JP (2022) ACS Appl Polym Mater 4:849–858.

6. 	Arshadi M (2015) Chem Eng J 259:170–182.

7. 	Huang L, Shen R, Liu R, Shuai Q (2020) J Hazard Mater 392:122320.

8. 	Panda A, Yang Y, Venkateswarlu S, et al (2020) Microporous Mesoporous Mater 306:110399.

9. 	Sang Y, Cao Y, Wang L, et al (2021) J Colloid Interface Sci 587:121–130.

10. 	Li L, Yu B, You T (2015) Biosens Bioelectron 74:263–269.

11. 	He Y, Wang X, Wang K, Wang L (2020) Dyes Pigments 173:107880.

12. 	Yin Y, Liu G (2021) Mater Today Commun 27:102440.

13. 	Cui WR, Jiang W, Zhang CR, et al (2020) ACS Sustain Chem Eng 8:445–451.

14. 	Yu YX, Li GL, Liu JH, Yuan DQ (2020) Chem Eng J 401:126139.

15. 	Ding SY, Dong M, Wang YW, et al (2016) J Am Chem Soc 138:3031–3037.

16. 	Lv Z, Chen Z, Feng S, et al (2022) Polym Chem 13:2320–2330.

17. 	Zhang X, Xia T, Jiang K, et al (2017) J Solid State Chem 253:277–281.

18. 	Tang Y, Liu Y, Qin Y, et al (2016) J Colloid Interface Sci 479:7–14.