Supplementary Information

Figure S1. The physical images of the composite sponges with different plant types and photo-catalysts.

Figure S2. FTIR spectra of the raw materials: chitosan (CS), cellulose from rise strew (RS), coconut coir (CC), and corn husk (CH).

Table S1. Porosity of composite sponges.

| CE type | TiO2 |  |  | SHP |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | 5 min | 10 min | 15 min | 5 min | 10 min | 15 min |
| RS | 85.35% | 85.53% | 86.33% | 88.08% | 89.73% | 88.67% |
| CC | 86.77% | 87.76% | 88.55% | 89.73% | 89.49% | 90.99% |
| CH | 86.24% | 87.48% | 87.32% | 79.50% | 88.32% | 87.51% |