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Figure S1. The physical images of the composite sponges with different plant types and photo-catalysts. 
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Figure S2. FTIR spectra of the raw materials: chitosan (CS), cellulose from rise strew (RS), coconut coir (CC), and corn husk (CH). 















Table S1. Porosity of composite sponges.
	CE type
	TiO2
	SHP

	
	5 min
	10 min
	15 min
	5 min
	10 min
	15 min

	RS
	85.35%
	85.53%
	86.33%
	88.08%
	89.73%
	88.67%

	CC
	86.77%
	87.76%
	88.55%
	89.73%
	89.49%
	90.99%

	CH
	86.24%
	87.48%
	87.32%
	79.50%
	88.32%
	87.51%
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