Extended Data Fig. 1 | Morphology characterizations of the coupled architecture. (A) The 45° tilted-view SEM and (B) STEM images of pure GaN NWs. (C) TEM image of the core-shell structure of Cr2O3@GaN NWs. TEM images of (D) Cr2O3-0.1@GaN and (E) Cr2O3-80@GaN, respectively. (F) The top view SEM image of pure GaN NWs. From this top view of the SEM image, the fill factor of GaN NWs on Si wafer is estimated to be about 53% by a photoshop software. Moreover, taking the length (L) of GaN NWs (~750 nm) and the mass density () of gallium nitride (6.1 g‧cm-2) into consideration, the weight of GaN NWs deposited on Si substrate (W) is evaluated to be ~0.24 mg‧cm-2 by the following equation: W = L *  * Fill factor.

Extended Data Fig. 2 | Spectroscopy characterizations of the coupled architecture. (A) XPS survey spectrum of Cr2O3@GaN and bare GaN. (B) The XPS of Ga 3d, N 1s, and O 1s for Cr2O3@GaN and bare GaN, respectively. (C) Photoluminescence spectra of GaN NWs and Cr2O3@GaN.

Extended Data Fig. 3 | Ethanol dehydrogenation experiment. (A) Schematic illumination of light-driven hydrogen production from bioethanol over Cr2O3@GaN nanoarchitecture supported by silicon wafer in a custom-built chamber. (B) Optimizing the decoration of Cr oxide onto GaN NWs for hydrogen evolution from ethanol. (C) The performance of various semiconducting platforms decorated with Cr2O3. Experiments conditions: 300 W Xenon lamp; light intensity, 5 W‧cm-2; bioethanol dosage, 1 mL; atmosphere, 1 atm air. SEM and elemental mapping images of (D) Cr2O3/Si, (E) Cr2O3@CdS, and (F) Cr2O3@TiO2.

Extended Data Fig. 4 | Surface coke characterization. (A) The atomic ratio of various elements based on XPS analysis for GaN, Cr2O3@GaN, Cr2O3@GaN after 3 hours of reaction under Ar and Air atmosphere, respectively. Raman optical images for (B) fresh GaN/Si and (C) fresh Cr2O3@GaN, respectively. Raman spectrum, Raman optical image, and the corresponding Raman signal intensity of defective carbon peak and graphite carbon peak for Cr2O3@GaN after reaction under (D, F, H, J) Ar and (E, G, I, K) Air, respectively.

Extended Data Fig. 5 | GC-MS signals of liquid products. (A) The gas chromatography-mass spectrograph (GC-MS) characterization of the liquid phase products of light-driven bioethanol reforming over Cr2O3@GaN nanoarchitecture under Air and Ar atmosphere, respectively. Typically, the largest peak around 3.29 mins was attributed to the signal of ethanol reactant. The insert was the signal of MS corresponding to the peak at 3.29 mins. (B-D) Fine chromatographic signal and mass spectrum signal (insert) at various time. Each signal corresponds to a production.

Extended Data Fig. 6 | Mechanism study. (A-E) Infrared spectroscopy of different regions. Typically, (A) no signal of the region corresponding to H2O; (B) almost negligible signal of the region corresponding to CO2; (C) the peak at 2117 cm-1 and 1933 cm-1 were ascribed to the CO formation; (D) the peaks at 1631 cm-1 was ascribed to the C=O bond corresponding to the aldehyde; and (E) the peaks at 1452 cm-1 were attributed to the CH2 bond corresponding to the surface ethoxy species. (F) Activity of various gaseous products from light-driven hydrogen production from bioethanol over Cr2O3@GaN nanoarchitecture under 16O2/Ar and 18O2/Ar atmosphere with a molar ratio of 2/8, respectively.

Extended Data Fig. 7 | Theoretical simulation. (A) Top, side, and prospective views of optimized geometries of GaN (1010) and Cr2O3@GaN surfaces. (B) Adsorption configurations for each reaction intermediates of ethanol decomposition on GaN (1010). (C) Adsorption configurations for each reaction intermediates of ethanol decomposition on Cr2O3@GaN. (D) Adsorption configurations for each reaction intermediates of C-C bond cleavage on Cr2O3@GaN in the presence of O2. Ga, green; N, purple; Cr, blue; C, brown; O, red; and H, pink.

Extended Data Table 1 | A brief overview of photocatalysts for hydrogen production published in the last five years (2018-2022).

| Photocatalysts | Substrate (Solvent) | H2 evolution (mmol gcat-1 h-1) | Durability (hours) | Light source | Reference |
| --- | --- | --- | --- | --- | --- |
| Cr2O3@GaN | Ethanol | 76,903.05 | 180 | 300W Xe-lamp | This work |
| Pt/FAPbBr3-xIx | HBr/HI (H2O) | 6.83 | 30 | 300W Xe-lamp | Energy Environ. Sci. 2022, 15, 1271 |
| PtSS-ZIS | TEOA (H2O) | 17.50 | 50 | 300W Xe-lamp | Nat. Commun. 2022, 13, 1287 |
| Pt/PY-DHBD-COF | Ascorbic acid (H2O) | 42.43 | 60 | Xe-lamp (>420 nm) | Nat. Commun. 2022, 13, 1355 |
| Cu/TiO2 | Methanol (H2O) | 101.70 | 30 | Xe-lamp | Nat. Commun. 2022, 13, 58 |
| Pt-CN/CuS | Methanol (H2O) | 7.25 | 15 | Xe-lamp | Angew. Chem. Int. Ed. 2021, 60, 2541 |
| Pt/CN | NaOH (Methanol) | 3.30 | 38 | 450W Xe-lamp | Angew. Chem. Int. Ed. 2021, 60, 26694 |
| Zn-Cu alloy | Methanol (H2O) | 328.00 | 4 | LA-251 Xe-lamp | J. Am. Chem. Soc. 2021, 143, 12145 |
| Sv-ZnIn2S4/MoSe2 | Ascorbic acid (H2O) | 63.21 | 20 | 300W Xe-lamp (>420 nm) | Nat. Commun. 2021, 12, 4112 |
| Pt/CsSnI | HI/H3PO2 (H2O) | 0.43 | 24 | 300W Xe-lamp (>420 nm) | Nat. Commun. 2021, 12, 4412 |
| ZnPor-DETH-COF | TEOA (PBS) | 0.41 | 120 | 300W Xe-lamp | Nat. Commun. 2021, 12, 1354 |
| Vs-ZnIn2S4 | CO2 (H2O) | 13.48 | 16 | 300W Xe-lamp | Nat. Commun. 2021, 12, 5923 |
| Cu/TCN | Methanol (H2O) | 10.60 | 20 | 300W Xe-lamp (>420 nm) | Adv. Mater. 2020, 32, 2003082 |
| Ni-a/TiO2 | Methanol (H2O) | 1.89 | 20 | 300W Xe-lamp | Angew. Chem. Int. Ed. 2020, 59, 7230 |
| Pt/ZnIn2S4/Ti3C2Tx | TEOA (H2O) | 3.48 | 24 | 300W Xe-lamp (>420 nm) | Angew. Chem. Int. Ed. 2020, 59, 11287 |
| Ag/g-C3N4 | TEOA (H2O) | 7.25 | 60 | 300W Xe-lamp (>420 nm) | Angew. Chem. Int. Ed. 2020, 59, 23112 |
| Ni/PCN | TEOA (H2O) | 0.08 | 36 | 300W Xe-lamp | Angew. Chem. Int. Ed. 2020, 59, 6827 |
| ML-MoS2 /MAPbI3-MCs | HI/H3PO2 (H2O) | 13.60 | 200 | 300W Xe-lamp (>420 nm) | Matter 2020, 3, 935 |
| PTB7-Th:EH-IDTBR | Ascorbic acid (H2O) | 64.45 | 16 | 300W Xe-lamp (350-800 nm) | Nat. Mater. 2020, 19, 559 |
| Rh/Cr2O3/CoOOH /SrTiO3: Al | H2O | 35.40 | 12.5 | 300W Xe-lamp | Nature 2020, 581, 411 |
| Ni/ZCS QDs | TEOA (H2O) | 18.90 | 28 | 300W Xe-lamp (>420 nm) | Sci. Adv. 2020, 6, eaaz8447 |
| Co/NGC/ZIS | TEOA (H2O) | 11.27 | 30 | 300W Xe-lamp (>400 nm) | Adv. Mater. 2019, 31, 1903404 |
| Pt/MNSs | Ascorbic acid (H2O) | 11.32 | 20 | 300W Xe-lamp (>420 nm) | Angew. Chem. Int. Ed. 2019, 58, 10198 |
| CTF-BT/Th | TEOA (H2O) | 6.60 | 25 | 300W Xe-lamp (>420 nm) | Angew. Chem. Int. Ed. 2019, 58, 8676 |
| TpDTz COF | TEOA (H2O) | 0.94 | 70 | 300W Xe-lamp | J. Am. Chem. Soc. 2019, 141, 11082 |
| Ru/ZnIn2S4 | DMF/MF (CH3CN) | 6.00 | 100 | 9W blue LEDs | Nat. Energy. 2019, 4, 575 |
| Pt/Al-TCPP | TEOA (CH3CN, H2O) | 0.13 | 16 | 300W Xe-lamp (>380 nm) | Adv. Mater. 2018, 30, 1705112 |
| Phosphorene/g-C3N4 | Lactic acid (H2O) | 0.57 | 14 | 300W Xe-lamp (>400 nm) | Adv. Mater. 2018, 30, 1800128 |
| Pt-Ir/MOF HNTM | TEOA (CH3CN, H2O) | 0.20 | 15 | 300W Xe-lamp (>400 nm) | Angew. Chem. Int. Ed. 2018, 57, 3493 |
| Pt/PCN-777 | Dibenzylamine (DMF, H2O) | 0.33 | 6 | Xe-lamp | Angew. Chem. Int. Ed. 2018, 57, 5379 |
| Pt/CTF-1-100W | TEOA/methanol (H2O) | 5.50 | 18 | 300W Xe-lamp | Energy Environ. Sci. 2018, 11, 1617 |
| Ni/CNPS-NH2 | TEOA (H2O) | 8.13 | 12 | 300W Xe-lamp (>420 nm) | Energy Environ. Sci. 2018, 11, 566 |
| Co9S8/ZnIn2S4 | TEOA (H2O) | 6.25 | 30 | 300W Xe-lamp (>400 nm) | J. Am. Chem. Soc. 2018, 140, 15145 |
| MoS2/CdS | Methanol (H2O) | 12.00 | 100 | 300W Xe-lamp (420-780 nm) | Nat. Commun. 2018, 9, 1181 |
| MG/hm-C(CN)3 | TEOA (H2O) | 1.01 | 44 | 300W Xe-lamp | Nat. Commun. 2018, 9, 3366 |
| P10 | TEA/Methanol (H2O) | 3.26 | 40 | 300W Xe-lamp | Nat. Commun. 2018, 9, 4968 |

Extended Data Table 2 | ICP-OES analysis of chromium element for Cr2O3@GaN. After digestion, the constant volume was 50 mL.

| Co-catalysts | Amount of precursor (μL) | Area (cm2) | Detected mass concentration (μg L-1) | Loading molar density (μmol cm-2) |
| --- | --- | --- | --- | --- |
| Cr0.1 | 0.1 | 0.5 | 1.09 | 0.002 |
| Cr20 | 20 | 0.5 | 29.44 | 0.057 |

Extended Data Table 3 | The abundance of 18O in the specific oxygen-containing gas products.

| Gas production | Abundance of 18O (At. %) |
| --- | --- |
| C18O | 38.18 |
| C18O2 | 20.22 |