Tab 1. Rcf values, Kinetic studies parameters, CrI and CrS of BC produced from SH medium, SW medium and standard HS medium.
	Medium
	Rcf a
	Substrate conversion

ration (%)b
	BC production

rate (g/Ld)b
	BC production

yield (%)b
	CrI

(%)c
	CrS

(nm)c

	HS
	0.0098
	34.77
	0.30
	12.24
	66.3
	4.19

	SW
	0.0108
	32.96
	0.08
	5.72
	46.2
	3.72

	SH
	0.0120
	18.44
	0.17
	5.55
	61.8
	3.48


