Supporting Information

Functionalized Cellulose with EDTA-like Chelating Groups for Removal of Heavy Metals

Lu Yang, Nan You*, Baohong Ding

(College of Petrochemical Engineering, Liaoning Petrochemical University, Fushun 113001, China)

* Corresponding author

E-mail: younan_77@163.com (N You)

Materials

All other reagents used which were of analytical grade, were obtained from Sinopharm Chemical Reagent Co., Shanghai, China, and used as received (Table S1). The individual stock solutions were prepared by dissolving 1 g of Cd2+ or Pb2+ in 1 L of distilled water and the desirable concentrations of Cd2+ or Pb2+ in experimental process were prepared by the dilution of stock solution.

Table S1 CAS registry number and purity of the chemicals

| Component | CAS Reg. No. | Purity |
| --- | --- | --- |
| Microcrystalline cellulose (<25 µm) | 9004-34-6 | AR |
| Sodium periodate | 7790-28-5 | AR |
| Diethylenetriamine | 111-40-0 | AR |
| Cadmium chloride | 10108-64-2 | AR |
| Lead chloride | 7758-95-4 | AR |
| Hydrochloric acid | 7647-01-0 | 31% |
| Hydroxylamine hydrochloride | 5470-11-1 | AR |
| Sodium hydroxide | 1310-73-2 | AR |

Characterization

The product obtained was characterized by FT-IR spectroscopy (model 5700, Nicolet, USA) was recorded using KBr pellets between 4000 and 400 cm−1 with the resolution of 1 cm−1, by scanning electron microscope (SEM, Shimadzu SS 550) operated at 12 kV equipped with an energy-dispersive X-ray (EDS) analyzer, by X-ray diffraction using Cu Kα radiation (XRD, Almelo PW-3060, Netherland) and by C13 nuclear magnetic resonance (CNMR, Bruker Avance III 400WB). All the pH values were measured by a ST20 pH meter (Ohaus Corporation, USA). The specific surface area was measured by N2 adsorption-desorption at 77 K (Micromeritics ASAP 2020). The specific surface area of the sample is calculated by using the multiple-point Brunauer–Emmett–Teller (BET) method. The concentrations of metals in aqueous solutions were determined by an AA-6300c flame atomic absorption spectrometer (FAAS, Shimadzu Corporation, Japan) with Pb and Cd hollow cathode lamps and air–acetylene flame.

Preparation of dialdehyde cellulose

The dialdehyde cellulose was obtained by an oxidation reaction of microcrystalline cellulose by sodium metaperiodate which is a gentle oxidant and can oxidized hydroxide, methyl to aldehyde group. 4 g sodium metaperiodate was dissolved into 50 mL H2O, and then 2 g of the microcrystalline cellulose was added. The resulting suspension mixture with the solution pH adjusted to 3 was stirred at 45 ◦C for 180 min. The main water-insoluble oxidized products were obtained by filtration, washed 5 times with deionized water, and freeze-dried for further grafting.

Determination of aldehyde content

The dialdehyde content of aldehyde cellulose was determined by the hydroxylamine hydrochloride method. Excessive hydroxylamine hydrochloride solution (5 %) was added into a suspension with a known amount of dialdehyde cellulose. The H+ concentration was released through a Schiff base reaction between the aldehyde groups of the dialdehyde cellulose and the amino groups of hydroxylamine hydrochloride. The stoichiometry between H+ ion and aldehyde group is 1. The H+ concentration was determined by the consumption of the 0.0100 mol L−1 of NaOH standard solution using methyl orange as indicator.

Calculation of adsorption capacity

q = (C0 − Ct) V/m                          (S1)

where q (mg g−1) is the adsorption capacity, C0 (mg L−1) is the initial concentration of metals, Ct (mg L−1) is the remnant concentration of metals, V (mL) is the volume of solution and m (g) is the mass of the Schiff base functionalized cellulose.

Regeneration

The regeneration efficiency (RE%) of the EDTA-CL is calculated as Eq.S2

RE%= q regeneration/q virgin×100%         (S2)

where q regeneration (mg g−1) is the adsorptive amounts of the regenerated EDTA-CL, qvirgin (mg g−1) is the adsorptive amounts of the virgin.

Adsorption isotherms

The linearized equations of Langmuir, Freundlich and Dubinin–Radushkevich (D–R) isotherm can be expressed as Eqs. (S3), (S4) and (S5), respectively.

Ce/qe= 1/(qmax b) + Ce/qmax                     (S3)

log qe = log kF + (1/n) log Ce                   (S4)

ln qe = ln qs – kadε2                                   (S5)

where qe (mg g−1) is the amount of metals adsorbed per unit mass of the Schiff base functionalized cellulose at equilibrium; Ce (mg L−1) is the concentration at equilibrium; qmax (mg g−1) is the maximum adsorption at monolayer coverage; b (L mg−1) is the adsorption equilibrium constant; KF (L g−1) is a Freundlich constant; n is a constant; kad (mol2 kJ−2) is the D–R isotherm constant; qs (mg g−1) is the saturation capacity from D–R isotherm; ε is the Polanyi potential and calculated as follows:

ε= RT ln (1+1/Ceq)                          (S6)

where R (8.314 J mol−1 K−1) is universal gas constant; T (K) is the absolute temperature. Ceq (mol L−1) is the equilibrium concentration of metal ions.

E (kJ mol−1) is the change of free energy transforming 1 mol of metal ions from solution to the surfaces and is conducive to the estimation of adsorption reaction type, and is obtained from kad as follows:

E= –(2kad) −1/2                                            (S7)

Kinetic analysis

The pseudo-first-order and pseudo-second-order rate expressions are linearly expressed as:

log(qe−qt) = log qe − k1t/2.303                  (S8)

t/qt= 1/k2qe 2 + t/qe                                         (S9)

where k1 (min−1) is the rate constant of the pseudo-first-order adsorption. qe and qt (mg g−1) are the adsorption capacity at equilibrium and the adsorption amount at time t (min), respectively. k2 (g mg−1 min−1) is the rate constant of the pseudo-second-order equation.

The Elovich equation is another kinetic model that is proposed for the description of the kinetics of the chemisorption of adsorbate by a solid in an aqueous medium. The linear form of Elovich equation is formulated as

qt = (1/β) ln (αβ) + (1/β) ln t                     (S10)

Where α is the initial adsorption rate of Elovich equation (mg g−1 min−1) and β is related to the extent of surface coverage and activation energy for chemisorption.

Thermodynamic analysis

Thermodynamic parameters such as standard Gibbs free energy change (ΔGº), enthalpy change (ΔHº) and entropy change (ΔSº) at equilibrium at different temperatures can be calculated from the constant (b, L mol−1) of L isotherm equation as the following equations:

ΔGo = −RT lnb                              (S11)

In order to use b in the thermodynamic calculations, the value of b expressed in L mg−1 in L isotherm equation can be multiplied by 1000 to convert the units in L g−1, and then multiplied by the atom weight of the metals, to transform b in L mol−1. ΔHº and ΔSº were obtained from Eq.S12.

lnb=ΔS0R-ΔH0RT                              (S12)

Figure S1 EDS mapping of the N elements in the regenerated EDTA-CL.

Table S2 The results of N contents and BET surface areas of the cellulose derivatives

| Cellulose-based sorbents | N density (mmol g-1) | Carboxyl density (mmol g-1) | BET surface area (m2 g-1) |
| --- | --- | --- | --- |
| Microcrystalline cellulose | ND. | ND. | 29 |
| Dialdehyde cellulose | ND. | ND. | 26 |
| Aminated cellulose | 8.2 | ND. | 68 |
| Amino-carboxyl cellulose | 8.1 | 11.5 | 116 |

Table S3 N Contents of the regenerated EDTA-CL

| Cellulose-based sorbents | N Contents (mmol g–1) |
| --- | --- |
| Regenerated N4-CL (cycle 1) | 7.5 |
| Regenerated N4-CL (cycle 2) | 7.4 |
| Regenerated N4-CL (cycle 3) | 7.2 |
| Regenerated N4-CL (cycle 4) | 7.2 |
| Regenerated N4-CL (cycle 5) | 7.1 |