Supplementary Materials

Visualization of Latent Fingerprints Based on Composites of Dye-Doped Cellulose with Red Emissive Fluorescence

Zhan-Chao Li 1,#,*, Da-Wu Li,2,3,#, Zhao-Hui Liu 1, Li-Ping Wu 1, Xiao-Sen lv 2,3, *

(1. Shenyang polytechnic college, Shenyang, 1100451. 2. College of Forensic Science, Criminal Investigation Police University of China, Shenyang, 110035, China; 3. Key Laboratory of Impression Evidence Examination and Identification Technology, Ministry of Public Security, Shenyang, 110035, China)

# The first three authors contributed equally to this paper

* Corresponding author

Email: lvxiaosen@126.com (X-S lv), and sylzc2023@163.com (Z Li)

Materials

All other reagents used which were of analytical grade, were obtained from Sinopharm Chemical Reagent Co., Shanghai, China, and used as received.

Characterization

The product obtained was characterized by FT-IR spectroscopy (model 5700, Nicolet, USA) was recorded using KBr pellets between 4000 and 400 cm−1 with the resolution of 1 cm−1, by scanning electron microscope (SEM, Shimadzu SS 550) operated at 12 kV equipped with an energy-dispersive X-ray (EDS) analyzer, and by X-ray diffraction using Cu Kα radiation (XRD, Almelo PW-3060, Netherland). The absorption and fluorescence spectral measurements were carried out using a Shimadzu UV-2550 UV Visible spectrophotometer and a Hitachi F-4500 fluorescence spectrometer, respectively.

Calculation of adsorptive amount

q = (C0 − Ct) V/m                          (S1)

where q (mg g−1) is the adsorptive amount, C0 (mg L−1) is the initial concentration of dyes, Ct (mg L−1) is the remnant concentration of dyes, V (mL) is the volume of solution and m (g) is the mass of cellulose.

Scheme S1 General process for the preparation of the RhB-cellulose.

Figure S1 Appearance of (a) the RhB5-cellulose, (b) RhB10-cellulose, and (c) RhB20-cellulose in daylight; Fluorescent appearance of (d) the RhB5-cellulose, (e) RhB10-cellulose, and (f) RhB20-cellulose under 365 nm UV-light irradiation.

Figure S2 The fluorescent images of the LFPs based on (a) the RhB5-cellulose, (b) RhB10-cellulose, and (c) RhB20-cellulose under 365 nm UV-light irradiation.

Table S1 Statistical table of ridge, Furrow and sweat hole size

| Number | Ridge/mm | Furrow/mm | Sweat pore length/mm | Distance of sweat pore/mm |
| --- | --- | --- | --- | --- |
| 1 | 0.227 | 0.291 | 0.085 | 0.283 |
| 2 | 0.271 | 0.199 | 0.095 | 0.248 |
| 3 | 0.301 | 0.183 | 0.122 | 0.309 |
| 4 | 0.358 | 0.223 | 0.064 | 0.337 |
| 5 | 0.388 | 0.257 | 0.126 | 0.375 |
| 6 | 0.259 | 0.215 | 0.124 | 0.256 |
| 7 | 0.252 | 0.268 | 0.08 | 0.395 |
| 8 | 0.299 | 0.195 | 0.093 | 0.335 |
| 9 | 0.267 | 0.270 | 0.080 | 0.398 |
| 10 | 0.232 | 0.220 | 0.071 | 0.227 |
| 11 | 0.217 | 0.245 | 0.134 | 0.311 |
| 12 | 0.257 | 0.274 | 0.088 | 0.433 |
| 13 | 0.232 | 0.347 | 0.118 | 0.268 |
| 14 | 0.217 | 0.199 | 0.144 | 0.225 |
| 15 | 0.257 | 0.306 | 0.125 | 0.311 |
| 16 | 0.232 | 0.126 | 0.089 | 0.433 |
| 17 | 0.271 | 0.151 | 0.134 | 0.267 |
| 18 | 0.233 | 0.189 | 0.126 | 0.301 |
| 19 | 0.262 | 0.180 | 0.063 | 0.249 |
| 20 | 0.257 | 0.119 | 0.085 | 0.332 |
| 21 | 0.232 | 0.145 | 0.068 | 0.298 |
| 22 | 0.27 | 0.205 | 0.072 | 0.289 |
| 23 | 0.233 | 0.121 | 0.068 | 0.234 |
| 24 | 0.262 | 0.146 | 0.068 | 0.255 |
| 25 | 0.299 | 0.183 | 0.144 | 0.284 |
| 26 | 0.202 | 0.203 | 0.063 | 0.309 |
| 27 | 0.158 | 0.163 | 0.108 | 0.297 |
| 28 | 0.183 | 0.192 | 0.072 | 0.69 |
| 29 | 0.193 | 0.188 | 0.085 | 0.248 |
| 30 | 0.196 | 0.171 | 0.109 | 0.278 |
| 31 | 0.197 | 0.176 | 0.084 | 0.314 |
| 32 | 0.158 | 0.145 | 0.109 | 0.280 |
| 33 | 0.233 | 0.214 | 0.107 | 0.354 |
| 34 | 0.197 | 0.163 | 0.072 | 0.401 |
| 35 | 0.223 | 0.203 | 0.112 | 0.442 |
| Max | 0.388 | 0.306 | 0.134 | 0.433 |
| Min | 0.158 | 0.119 | 0.063 | 0.225 |
| Average | 0.24 | 0.20 | 0.09 | 0.32 |