Supporting  data

Fig.11sublimentry data shows V2O5 sensor was also exposed to 100sccm flow of H2 operating temperature of 100°C response time and recovery time 67s-152s respectively, the sensor response is poor with the baseline shift. The resistance level did not reach its original baseline. This is because of poor adsorption and desorption.

Fig.12 a&b transmittance and band gap energy of V2O5 thin film sample s4