Supporting Information

Atomic Insights into the Unidirectional Alignment and Orientation-Pinning Behavior of h-BN Nucleation on Ir(111)

Jinliang Pan1,3,4, Tongwei Wu2,4, Chao Ma2,4, Yangfan Wu1,3, Yi Zheng1,3, Kui Hu1,3, Luye Sun1,3, Sumei Ma1, Mengxi Liu1,3*, Yanning Zhang2* and Xiaohui Qiu1,3*

1CAS Key Laboratory of Standardization and Measurement for Nanotechnology, National Center for Nanoscience and Technology, Beijing, 100190, P. R. China

2Institute of Fundamental and Frontier Sciences, University of Electronic Science and Technology of China, Chengdu, Sichuan, 610054, P. R.China

3University of Chinese Academy of Sciences, Beijing 100049, P. R. China

4These authors contributed equally: Jinliang Pan, Tongwei Wu, Chao Ma.

*e-mail: liumx@nanoctr.cn; yanningz@uestc.edu.cn; xhqiu@nanoctr.cn

Figure S1 A representative large-scale STM image of h-BN nuclei formed on Ir(111) via TPG method at 700 K. The h-BN nanoclusters with inverse adsorption orientation are marked by white and red circles, respectively. The yellow arrows represent the three equivalent crystallographic directions of Ir(111). The image is processed by Laplace-filter, and the image size is 230 nm × 230 nm.

The analysis of 2097 nanoclusters in multiple samples exhibits that the dominant orientation of h-BN nuclei is approximately 91%. The NtopBhcp atomic registration is the preferred oritation for all the samples, while the minority adopts NtopBfcc. The energy differences (∆E) between h-BN nuclei for opposite orientations are calculated to be 0.14 eV, according to the Boltzmann factors. Among them, one sample exhibits an unexpected ultrahigh proportion of dominant orientaiton, up to 97 %. The reason for this anomaly is currently unclear and requires further investigation.

Figure S2 nc-AFM images showing that h-BN crystallization is strictly in registry with the substrate lattices. The white arrows represent the three equivalent crystallographic directions of Ir(111). Scale bars: 5 Å.

Figure S3. DFT calculation of h-BN nuclei with different adsorption configuration on Ir(111) (a) Formation energy (Ef) of N-terminated (blue) and B-terminated (red) h-BN nuclei (n = 2–5) with Ntop-Bfcc (spuare) and Ntop-Bhcp (circle) adsorption sites. The formation energies indicate that the h-BN nanoplate with N termination is more energetically favorable than that with B termination. (b) Atomic structures of h-BN nuclei with n = 3 and n = 4 (c), combined with their formation energies listed below the structures.

Figure S4. The determination of adsorption sites of h-BN on Ir(111) using adjusted constant-height AFM images method with CO-functionalized tip. (a) The schematic diagram and the nc-AFM imaging for the determination of fcc (yellow triangles) and hcp sites (magenta triangles) of Ir(111) surface. (b) The adsorption sites of an h-BN nanosheet on Ir(111). The tip height (z) change on the step edge of Ir(111) is marked by red lines. Crossings of orange lines mark the positon of the top-layer Ir atoms. Tip heights are given with respect to an STM conductance set point of G = 100 pS (a) and 20 pS (b). The image is rotated - 46° (a) and 30° (b) in clockwise direction. Scale bars: 5 Å.