Supporting information

Tables

Table S1 Three factors with three levels of the preparation parameters in the orthogonal design

| Factors | Labels | Levels |  |  |
| --- | --- | --- | --- | --- |
|  |  | 1 | 2 | 3 |
| Molar ratio of Fe(II) to Mn(II) | A | 1 | 3 | 5 |
| Mass ratio of PS to Fe-Mn hydroxide | B | 1 | 3 | 5 |
| Molar ratio of OH- to Fe(II) | C | 2 | 4 | 6 |

Table S2 Three factors with three levels of the preparation parameters in the orthogonal design

| Factors | Labels | Levels |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | 1 | 2 | 3 | 4 | 5 |
| Initial pH | D | 3 | 5 | 7 | 9 | 11 |
| P-CP concentration (mM) | E | 2 | 4 | 6 | 8 | 10 |
| Dosage (g/L) | F | 0.5 | 1.0 | 1.5 | 2.0 | 2.5 |
| Temperature (°C) | G | 30 | 40 | 50 | 60 | 70 |

Table S3 Main effect of the preparation parameters on p-CP removal (default α = 0.05)

| Source | SS (III) | df | MS | F | Sig. |
| --- | --- | --- | --- | --- | --- |
| Corrected model | 11.207a | 6 | 1.868 | 17.104 | 0.056 |
| Intercept | 128.142 | 1 | 128.142 | 1173.465 | 0.001 |
| Molar ratio of Fe(II) to Mn(II) | 5.249 | 2 | 2.625 | 24.034 | 0.040 |
| Mass ratio of PS to Fe-Mn hydroxide | 5.488 | 2 | 2.744 | 25.130 | 0.038 |
| Molar ratio of OH- to Fe(II) | 0.469 | 2 | 0.235 | 2.149 | 0.318 |
| Error | 0.218 | 2 | 0.109 |  |  |
| Total | 139.568 | 9 |  |  |  |
| Corrected Total | 11.425 | 8 |  |  |  |

a: R2 = 0.981

Table S4 Main effect of the aqueous conditions on p-CP removal (default α = 0.05)

| Source | SS (III) | df | MS | F | Sig. |
| --- | --- | --- | --- | --- | --- |
| Corrected model | 89.877a | 16 | 5.617 | 2.302 | 0.117 |
| Intercept | 151.241 | 1 | 151.241 | 61.975 | 0.000 |
| Initial pH | 9.857 | 4 | 2.464 | 1.010 | 0.457 |
| P-CP concentration (mM) | 12.200 | 4 | 3.050 | 1.250 | 0.364 |
| Dosage (g/L) | 3.972 | 4 | 0.993 | 0.407 | 0.799 |
| Temperature (°C) | 63.848 | 4 | 15.962 | 6.541 | 0.012 |
| Error | 19.523 | 8 | 2.440 |  |  |
| Total | 260.641 | 25 |  |  |  |
| Corrected Total | 109.400 | 24 |  |  |  |

a: R2 = 0.822

Table S5 Parametrical statistics for the kinetics fitting

| Parametrical types | Factors | Levels | Adj. R2 | k |
| --- | --- | --- | --- | --- |
| Preparation parameters | Molar ratio of Fe(II) to Mn(II) | 1 | 0.98233 | 0.00362 |
|  |  | 3 | 0.99249 | 0.00416 |
|  |  | 5 | 0.9615 | 0.00156 |
|  | Mass ratio of PS to Fe-Mn hydroxide | 1 | 0.99607 | 0.00427 |
|  |  | 3 | 0.98563 | 0.00331 |
|  |  | 5 | 0.95593 | 0.0016 |
|  | Molar ratio of OH- to Fe(II) | 2 | 0.91481 | 0.00222 |
|  |  | 4 | 0.98805 | 0.00225 |
|  |  | 6 | 0.96711 | 0.00235 |
| Aqueous conditions | Initial pH | 3 | 0.98392 | 0.00131 |
|  |  | 5 | 0.96461 | 0.00125 |
|  |  | 7 | 0.95974 | 0.00125 |
|  |  | 9 | 0.98518 | 0.00182 |
|  |  | 11 | 0.98342 | 0.00242 |
|  | p-CP concentration (mM) | 2 | 0.93691 | -0.00286 |
|  |  | 4 | 0.94707 | -0.00191 |
|  |  | 6 | 0.963 | -0.0014 |
|  |  | 8 | 0.98136 | -0.00148 |
|  |  | 10 | 0.99561 | -9.6454E-4 |
|  | PS-hydroxide dosage (g/L) | 0.5 | 0.98563 | -0.00129 |
|  |  | 1.0 | 0.98145 | -0.0012 |
|  |  | 1.5 | 0.96642 | -0.00192 |
|  |  | 2.0 | 0.98533 | -0.00143 |
|  |  | 2.5 | 0.98818 | -0.00169 |
|  | Temperature (°C) | 30 | 0.95173 | -2.67683E-4 |
|  |  | 40 | 0.98018 | -4.47411E-4 |
|  |  | 50 | 0.9747 | -0.00193 |
|  |  | 60 | 0.96146 | -0.00383 |
|  |  | 70 | 0.95447 | -0.00457 |

Fig. S1 EDS of Fe-Mn hydroxide affected by the molar ratios of Fe(II) to Mn(II) and the PS-hydroxide influenced by the mass ratios of PS to Fe-Mn hydroxide

Fig. S2 FTIR spectrum of benzene