Supplementary Information

23% Efficient and Highly stable Quantum Dot-Based Blue Electroluminescent Devices

Wenjing Zhang1,†, Bo Li2,†, Chun Chang3,†, Fei Chen1*, Qin Zhang3, Qingli Lin1, Lei Wang1, Jinhang Yan1, Fangfang Wang1, Yihua Chong1, Zuliang Du1, Fengjia Fan2*, and Huaibin Shen1*

1 Key Laboratory for Special Functional Materials of Ministry of Education, National & Local Joint Engineering Research Center for High-efficiency Display and Lighting Technology, Henan University, Kaifeng 475004, China

2 Hefei National Laboratory for Physical Sciences at the Microscale and Department of Modern Physics, CAS Key Laboratory of Microscale Magnetic Resonance, Synergetic Innovation Center of Quantum Information and Quantum Physics, University of Science and Technology of China, Hefei 230026, China

3 Key Laboratory of Nondestructive Testing Ministry of Education, Nanchang Hangkong University, Nanchang 330063, China

†Authors contributed equally.

Correspondence and requests for materials should be addressed to H.B.S. (email: shenhuaibin@henu.edu.cn), to F.J.F. (email: ffj@ustc.edu.cn) or to F.C. (email: chenfei.henu@henu.edu.cn)

Table of contents

1. Supplementary Note

Supplementary Note 1

2. Supplementary Figure

Supplementary Figures 1-8

3. Supplementary Table

Supplementary Table 1

4. Supplementary References

Supplementary References 1-41

Supplementary Note 1

Fabrication of EOD and HOD.

The structure of EODs is: ITO/ZnMgO/TFB/QDs/ZnMgO/Al and ITO/ZnMgO/TFB/PBO/QDs/ZnMgO/Al. HODs were fabricated with a structure of ITO/PEDOT:PSS/TFB/QDs/MoO3/Al and ITO/PEDOT:PSS/TFB/PBO/QDs/MoO3/Al. The EODs and HODs were fabricated using ITO glass substrates. Before use, these substrates were ultrasonically cleaned with detergent, deionized water, acetone, and isopropanol for 15 min, respectively, and then treated with UV ozone for 15 min.

For fabricating the EODs, ZnMgO (20 mg mL-1) was spin-coated at 2000 rpm for 30 s, followed by baking at 80 °C for 30 min. Then, TFB was spin-coated at a concentration of 6 mg mL-1 in chlorobenzene (3000 rpm for 50 s), and then baked at 150 °C for 30 min. Next, the PBO solution in DMF was spin-coated at 3000 rpm for 30 s and baked at 120 °C for 30 min. Subsequently, the blue CdZnS/ZnS QDs solution in n-octane was then spin-coated at 2000 rpm for 40 s. In turn, ZnMgO (20 mg mL-1) was spin-coated at 2000 rpm for 30 s, followed by baking at 80 °C for 30 min. Finally, an Al anode was deposited via thermal evaporation at a rate of ≈ 0.1 nm s-1 under a high vacuum of 4×10-6 Torr.

For fabricating the HODs, the mixed solution (1:1) of PEDOT:PSS (poly(3,4-ethylenedioxythiophene)/poly(styrenesulfonate), AI 4083) and isopropanol used as HILs, was spin-coated onto the ITO substrates at the spin speed of 5500 rpm and baked at 150 °C for 15 min in air. Then, these substrates were immediately transferred to the N2-filled glove box for spin-coating of TFB, PBO and QDs. TFB was spin-coated at a concentration of 6 mg mL-1 in chlorobenzene (3000 rpm for 50 s), and then baked at 150 °C for 30 min. Next, the PBO solution in DMF was spin-coated at 3000 rpm for 30 s and baked at 120 °C for 30 min. Subsequently, the blue CdZnS/ZnS QDs solution in n-octane was then spin-coated at 2000 rpm for 40 s. In turn, MoO3 and Al anode were deposited via thermal evaporation at a rate of ≈ 0.1 nm s-1 under a high vacuum of 4×10-6 Torr, forming a 10 nm MoO3 layer and 100 nm anode.

Supplementary Figure 1. Hall effect measurements. The hole mobility of PBO, TFB, PVK, TCTA, CBP and TPD.

Supplementary Figure 2. AFM measurements of TFB, TFB/PBO, TFB/QD, TFB/PBO/QD films. (a) AFM topographies, (b) line scan and (c) 3D images.

Supplementary Figure 3. Schematic device structure, cross-sectional SEM image of QD-LED device and element distribution of each layer.

Supplementary Figure 4. CIE coordinate of QD-LEDs with PBO.

Supplementary Figure 5. QDs characterizations. (a) TEM image and histogram of diameters of 50 CdZnS/ZnS QDs. (b) XRD pattern of as-prepared QDs. Black line indicates the peak positions of standard references of bulk zinc-blende ZnS. (c)-(e) Energy dispersive spectroscopy (EDS) elemental mapping of Zn, Cd and S element in CdZnS/ZnS core/shell QDs. (f) Absorption and PL spectra of CdZnS/ZnS core/shell QDs. The inset is the photograph of QD-octane dispersion under UV irradiation.

Supplementary Figure 6. Device performances of QLEDs with PBO layers of different thicknesses. (a) J-V-L and (b) EQE-V characteristic curves.

Supplementary Figure 7. Transient EL measurements. Transient EL spectra for the devices under (a) 4.0 V and (b) 5.0 V without and with PBO.

Supplementary Figure 8. EA measurements for the devices with and without PBO. The EA spectra with different biases of fresh devices without (a) and with (c) PBO. The EA spectra with different biases of degraded devices (turn on for 30 min under 5 V bias) without (b) and with (d) PBO.

Supplementary Table 1. Comparison of state-of-the-art blue QD-LEDs in previous literature with the current work.

| Blue QD-LEDs | Year | Structure | PL (nm) | PL QY (%) | EQE (%) | Lmax (cd m-2) | τ50 (h) | EL (nm) | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Deep blue | 2012 | ITO/PEDOT:PSS/PVK/ZnSe/ZnS/ZnO/Al | 420 |  | 0.65 | -- | -- | 430 | 1 |
|  | 2012 | ITO/ZnO/CdZnS@ZnS/CBP/MoO3/Al | 433 | 70-80 | 1.7 | 2250 | -- | 437 | 2 |
|  | 2013 | ITO/PEDOT:PSS/PVK/ZnCdS/ZnS/ ZnO/Al | 452 | 98 | 7.1 | 2624 | -- | 452 | 3 |
|  | 2014 | ITO/PEDOT:PSS/TFB/ZnxCd1-xS/ZnS/ ZnO/Al | 441 | 100 | 3.8 | 4100 | -- | 445 | 4 |
|  | 2015 | ITO/PEDOT:PSS/TFB/ZnCdS/ZnS-OT/ ZnO/Al | 441 | 90 | 12.2 | 7600 | -- | 443 | 5 |
|  | 2015 | ITO/PEDOT:PSS/PVK/Cd1-xZnxS@ZnS/ ZnO/Al | 455 | 70-75 | 10.7 | 4000 | 1000 | 455 | 6 |
|  | 2015 | ITO/PEDOT:PSS/PVK/ZnSe/ZnS/ZnO NPs/Al | 425 | 83 | 7.83 | 2623 | -- | 429 | 7 |
|  | 2015 | ITO/PEDOT:PSS/TFB:PVK/ZnSe/ZnS/ZnO NPs/Al | 425 | 80 | 7.39 | 2856 | -- | 430 | 8 |
|  | 2017 | ITO/PEDOT:PSS/TFB/ZnxCd1-xS/ZnS/ZnO NPs/Al | 442 | 93 | 11.9 | 10400 | 4300 | 455 | 9 |
|  |  | ITO/PEDOT:PSS/PVK/ZnxCd1-xS/ZnS/ZnO NPs/Al |  |  | 15.6 | 4500 | 47 |  |  |
|  | 2018 | ITO/PEDOT:PSS/PVK/ZnCdS/10CdxZn1-xS/2ZnS/ZnO NPs/Al | 441 | 100 | 18 | 6768 | 47.4 | 445 | 10 |
|  | 2019 | ITO/PEDOT:PSS/TFB/ZnCdS/ZnS/TBS-PBO/ZnO:Mg/Al | 449 | 81 | 17.4 | 7992 | -- | 452 | 11 |
|  | 2019 | ITO/PEDOT:PSS/PVK/ZnSeTe/ZnSe/ZnS/ZnMgO/Al | 441 | 70 | 4.2 | 1195 | 14 | 445 | 12 |
|  | 2020 | ITO/PEDOT:PSS/PVK/ZnSeTe/ZnSe/ZnSeS/ZnS/ZnMgO-Mg(OH)2/Al | 445 | 84 | 9.5 | 2904 | -- | 447 | 13 |
|  | 2020 | ITO/PEDOT:PSS/PVK/ZnSe/ZnS/ZnMgO/Al | 428 | 85 | 14.7 | 390 | -- | 428 | 14 |
|  |  |  | 445 | 64 | 10.7 | -- | -- | 445 |  |
|  | 2021 | ITO/PEDOT:PSS/PVK/ZnSe/ZnS/ZnMgO/Al | 440 | 95 | 12.2 | 1055 | 237 | 445 | 15 |
|  | 2022 | ITO/PEDOT:PSS/PVK/ZnSe/ZnS/ZnMgO/Al | 442 | 95 | 13.6 | 1031 | 305 | 443 | 16 |
| Pure blue | 2007 | ITO/PEDOT:PSS/Poly-TPD/CdS/ZnS/Al | 460 | -- | -- | 1600 | -- | 460 | 17 |
|  | 2020 | ITO/PEDOT:PSS/TFB/ZnTeSe/ZnSe/ZnS-Cl(f)/QD(l)/ZnMgO/Al | 457 | 100 | 20.2 | 88900 | 15850 | 460 | 18 |
|  | 2021 | ITO/PEDOT:PSS/CNPr-TFB/QD/ZnMgO/Al | 462 | 70.5 | 11.3 | ≈8000 | 15.8 | 463 | 19 |
|  | 2022 | ITO/PEDOT:PSS/AuAg NPs-PVK/ZnSeTe/ZnSe/ZnSeS/ZnS/ZnMgO/Al | 460 | 85 | 7.1 | 6510 | -- | 460 | 20 |
| Sky blue | 2011 | ITO/PEDOT:PSS/Poly-TPD/CdSe/ZnS/ZnO/Al | 467 | -- | 0.22 | 4200 | -- | 470 | 21 |
|  | 2017 | ITO/PEDOT:PSS/PVK/CdSe/ZnS/ZnO NPs/Al | 466 | 87 | 19.8 | 4890 | 47.5 | 468 | 22 |
|  | 2017 | ITO/ZMO/InP/ZnS//ZnS/CBP/MoO3/Al | 477 | 76 | -- | 90 | -- | 488 | 23 |
|  | 2018 | ITO/PEDOT:PSS/TFB/ZnCdSe/ZnS//ZnS/PMMA/ZnO/Al | 472 | 92 | 16.2 | 14100 | 355 | 479 | 24 |
|  | 2019 | ITO/PEDOT:PSS/TFB/CdSe/ZnSe/ZnO/Al | 476 | 73 | 8.05 | 62600 | 7000 | 480 | 25 |
|  | 2019 | ITO/NiO/TFB/PVK/CsFAPbBr3/TPBi/LiF/Al | 483 | >60 | 9.5 | 700 | 250 s | 483 | 26 |
|  | 2020 | ITO/PEDOT:PSS/TFB/ZnCdSeS/ZnO/Al | 473 | 85 | 9.9 | 52360 | 2630 | 480 | 27 |
|  | 2020 | ITO/PEDOT:PSS/Poly-TPD/PVK/CdSeS/ZnSeS/ZnS/ZnMgO/Al | 480 | 60 | 10 | -- | 10000 | 480 | 28 |
|  | 2020 | ITO/PEDOT:PSS/TFB/InP/GaP/ZnS//ZnS/ZnO/Al | 488 | 81 | 1.01 | 3120 | 2 | 488 | 29 |
|  | 2020 | ITO/PEDOT:PSS/PVK/InGaP/ZnSeS/ZnS/ZnMgO/Al | 465 | 80 | 2.5 | 1038 | -- | 469 | 30 |
|  | 2021 | ITO/PEDOT:PSS/TFB /InP/ZnS/ZnS/ZnO/Al | 480 | 43 | 1.47 | 125 | -- | 484 | 31 |
|  | 2021 | ITO/PEDOT:PSS/CsPbBr3-xClx/TPBi/LiF/Al | 484 | -- | 16.8 | 1694 | -- | 486 | 32 |
|  | 2021 | ITO/PEDOT:PSS/PVK/(Cs/Rb/K/PEA)Pb(Br/Cl)3/DPEPO/TPBi/LiF/Al | 487 | 59.78 | 10.17 | 6728 | -- | 488 | 33 |
|  | 2022 | ITO/PEDOT:PSS/PF8Cz/CdZnSe/ZnS/ZnMgO/Al | -- | 90 | 21.9 | -- | 24000 | 479 | 34 |
|  | 2022 | ITO/PEDOT:PSS/PVK/ZnSe/ZnS/ZnCdSe/ZnS/ZnMgO/Al | 474 | 90 | 20.6 | 24020 | 2297 | 475 | 35 |
|  | 2022 | ITO/PEDOT:PSS/TFB / InPESC@ZnS/ZnMgO/Al | 483 | 52 | 1.4 | 1162 | -- | 487 | 36 |
|  | 2022 | ITO/PEDOT:PSS/TFB /InP/ZnS/ZnS/ZnMgO/Al | 474 | 93 | 2.6 | 422 | -- | 488 | 37 |
|  | 2022 | ITO/PEDOT:PSS/PVK/CsPbBr3/D-ZnO/Ag | 460 | 98 | 8.7 | 11100 | 15 | 470 | 38 |
|  | 2022 | ITO/PEDOT:PSS/Poly-TPD/CsPb(BrxCl1-x)3 /TPBi/LiF/Al | 488 | 95 | 14.6 | 403 | 12min | 490 | 39 |
|  | 2023 | ITO/PEDOT:PSS/PTAA/ FA1-xCsxPbBr1-xClx/ETM-B2/LiF /Al | -- | -- | 13.17 | 8656 | 20min | 490 | 40 |
|  | 2023 | ITO/PEDOT:PSS/TFB/ZnCdSe/ZnCdSeS/ZnS/ZnO/Al | 481 | 92 | 20.4 | -- | 80377 | 482 | 41 |
|  | 2023 | ITO/PEDOT:PSS/TFB/PBO/CdZnS/ZnS/PBO/ZnMgO/Al | 455 | ≈100 | 23 | 17641 | 41022 | 458 | This work |

REFERENCES

- Xiang, C. et al. Solution processed multilayer cadmium-free blue/violet emitting quantum dots light emitting diodes. Appl. Phys. Lett. 101, 053303 (2012).

- Kwak, J. et al. Bright and efficient full-color colloidal quantum dot light-emitting diodes using an inverted device structure. Nano Lett. 12, 2362-2366 (2012).

- Lee, K.H. et al. Highly efficient, color-pure, color-stable blue quantum dot light-emitting devices. ACS Nano 7, 7295-7302 (2013).

- Shen, H. et al. High-efficient deep-blue light-emitting diodes by using high quality ZnxCd1-xS/ZnS core/shell quantum dots. Adv. Funct. Mater. 24, 2367-2373 (2014).

- Shen, H. et al. High-efficiency, low turn-on voltage blue-violet quantum-dot-based light-emitting diodes. Nano Lett. 15, 1211-1216 (2015).

- Yang, Y. et al. High-efficiency light-emitting devices based on quantum dots with tailored nanostructures. Nat. Photonics 9, 259-266 (2015).

- Wang, A. et al. Bright, efficient, and color-stable violet ZnSe-based quantum dot light-emitting diodes. Nanoscale 7, 2951-2959 (2015).

- Lin, Q. et al. Cadmium-free quantum dots based violet light-emitting diodes: High-efficiency and brightness via optimization of organic hole transport layers. Org. Electron. 25, 178-183 (2015).

- Shen, H. et al. Efficient and long-lifetime full-color light-emitting diodes using high luminescence quantum yield thick-shell quantum dots. Nanoscale 9, 13583-13591 (2017).

- Wang, O. et al. High-efficiency, deep blue ZnCdS/CdxZn1-xS/ZnS quantum-dot-light-emitting devices with an EQE exceeding 18%. Nanoscale 10, 5650-5657 (2018).

- Li, D. et al. Blue quantum dot light-emitting diodes with high luminance by improving the charge transfer balance. Chem. Commun. 55, 3501-3504 (2019).

- Jang, E.P. et al. Synthesis of alloyed ZnSeTe quantum dots as bright, color-pure blue emitters. ACS Appl. Mater. Interfaces 11, 46062-46069 (2019).

- Han, C.-Y. et al. More than 9% efficient ZnSeTe quantum dot-based blue electroluminescent devices. ACS Energy Lett. 5, 1568-1576 (2020).

- Ryowa, T. et al. High‐efficiency quantum dot light‐emitting diodes with blue cadmium‐free quantum dots. J. Soc. Inf. Display 28, 401-409 (2020).

- Gao, M. et al. Bulk-like ZnSe quantum dots enabling efficient ultranarrow blue light-emitting diodes. Nano Lett. 21, 7252-7260 (2021).

- Gao, M. et al. Alleviating electron over-injection for efficient cadmium-free quantum dot light-emitting diodes toward deep-blue emission. ACS Photonics 9, 1400-1408 (2022).

- Tan, Z. et al. Bright and color-saturated emission from blue light-emitting diodes based on solution-processed colloidal nanocrystal quantum dots. Nano Lett. 7, 3803-3807 (2007).

- Kim, T. et al. Efficient and stable blue quantum dot light-emitting diode. Nature 586, 385-389 (2020).

- Wu, W. et al. An efficient hole transporting polymer for quantum dot light‐emitting diodes. Adv. Mater. Interfaces 8, 2100731 (2021).

- Kim, S.-K. et al. Localized surface plasmon-enhanced blue electroluminescent device based on ZnSeTe quantum dots and AuAg nanoparticles. Inorg. Chem. Front. 9, 3138-3147 (2022).

- Qian, L. et al. Stable and efficient quantum-dot light-emitting diodes based on solution-processed multilayer structures. Nat. Photonics 5, 543-548 (2011).

- Wang, L. et al. Blue quantum dot light-emitting diodes with high electroluminescent efficiency. ACS Appl. Mater. Interfaces 9, 38755-38760 (2017).

- Shen, W. et al. Synthesis of highly fluorescent InP/ZnS small-core/thick-shell tetrahedral-shaped quantum dots for blue light-emitting diodes. J. Mater. Chem. C 5, 8243-8249 (2017).

- Lin, Q. et al. Nonblinking quantum-dot-based blue light-emitting diodes with high efficiency and a balanced charge-injection process. ACS Photonics 5, 939-946 (2018).

- Shen, H. et al. Visible quantum dot light-emitting diodes with simultaneous high brightness and efficiency. Nat. Photonics 13, 192-197 (2019).

- Liu, Y. et al. Efficient blue light-emitting diodes based on quantum-confined bromide perovskite nanostructures. Nat. Photonics 13, 760-764 (2019).

- Wang, F. et al. Suppressed efficiency roll-off in blue light-emitting diodes by balancing the spatial charge distribution. J. Mater. Chem. C 8, 12927-12934 (2020).

- Pu, C. et al. Electrochemically-stable ligands bridge the photoluminescence-electroluminescence gap of quantum dots. Nat. Commun. 11, 937 (2020).

- Zhang, H. et al. High-brightness blue InP quantum dot-based electroluminescent devices: the role of shell thickness. J. Phys. Chem. Lett. 11, 960-967 (2020).

- Kim, K.-H. et al. Cation-exchange-derived InGaP alloy quantum dots toward blue emissivity. Chem. Mater. 32, 3537-3544 (2020).

- Yu, P. et al. Inorganic solid phosphorus precursor of sodium phosphaethynolate for synthesis of highly luminescent InP-based quantum dots. ACS Energy Lett. 6, 2697-2703 (2021).

- Shen, Y. et al. Interfacial nucleation seeding for electroluminescent manipulation in blue perovskite light‐emitting diodes. Adv. Funct. Mater. 31, 2103870 (2021).

- Zhu, C. et al. High triplet energy level molecule enables highly efficient sky-blue perovskite light-emitting diodes. J. Phys. Chem. Lett. 12, 11723-11729 (2021).

- Deng, Y.Z. et al. Solution-processed green and blue quantum-dot light-emitting diodes with eliminated charge leakage. Nat. Photonics 16, 505-511 (2022).

- Wang, F. et al. High‐performance blue quantum‐dot light‐emitting diodes by alleviating electron trapping. Adv. Opt. Mater. 10, 2200319 (2022).

- Suh, Y.H. et al. Engineering core size of InP quantum dot with incipient ZnS for blue emission. Adv. Opt. Mater. 10, 2102372 (2022).

- Zhang, W. et al. High quantum yield blue InP/ZnS/ZnS quantum dots based on bromine passivation for efficient blue light‐emitting diodes. Adv. Opt. Mater. 10, 2200685 (2022).

- Liu, A., Bi, C. & Tian, J. All solution‐processed high performance pure‐blue perovskite quantum‐dot light‐emitting diodes. Adv. Funct. Mater. 32, 2207069 (2022).

- Zhu, H. et al. Enriched-bromine surface state for stable sky-blue spectrum perovskite QLEDs with an EQE of 14.6. Adv. Mater. 34, 2205092 (2022).

- Yuan, S. et al. Balancing charge injection via a tailor-made electron-transporting material for high performance blue perovskite QLEDs. ACS Energy Lett. 8, 818-826 (2023).

- Chen, X. et al. Blue light-emitting diodes based on colloidal quantum dots with reduced surface-bulk coupling. Nat. Commun. 14, 284 (2023).