Supplementary Materials for

A Broad-spectrum Gas Sensor based on Correlated Two-Dimensional Electron Gas

Yuhao Hong1, Long Wei1, Qinghua Zhang3, Zhixiong Deng1, Xiaxia Liao4, Yangbo Zhou4, Lei Wang1, Tongrui Li1, Junhua Liu1, Wen Xiao1, Shilin Hu1, Lingfei Wang5, Lin Li1, Mark Huijben2, Kai Chen1, Gertjan Koster2, Guus Rijnders2*, Zhaoliang Liao1,2*

1National Synchrotron Radiation Laboratory, University of Science and Technology of China; Hefei, 230029, China.

2MESA+ Institute for Nanotechnology, University of Twente; Enschede, 7500 AE, the Netherlands.

3Beijing National Laboratory for Condensed Matter Physics, Institute of Physics, Chinese Academy of Sciences; Beijing, 100190, China.

4School of Physics and Materials Science, Nanchang University; Nanchang, 330031, China.

5National Research Center for Physical Sciences at Microscale, University of Science and Technology of China; Hefei, 230026, China.

*To whom correspondence should be addressed: a.j.h.m.rijnders@utwente.nl, zliao@ustc.edu.cn

- Growth of LaFeO3 and LaAlO3 films

Fig. S1 | Growth and surface characterization. a, RHEED intensity oscillations during the growth of LFO (5 u.c.) and LAO (10 u.c.). The growth started at t = 0 and stopped at the time indicated by arrows. RHEED patterns before (b) and post (c) growth. AFM surface topography before (d) and post (f) growth. Measured step heights before (e) and post (g) growth.

The LaFeO3 (LFO) and LaAlO3 (LAO) films were grown by pulsed laser deposition (PLD) in a layer by layer fashion as shown in Fig. S1a. The thickness of the LFO and LAO was controlled by counting the RHEED oscillations, enabling a precise unit cell (u.c.) control of the growth. RHEED patterns (See Fig. S1, b-c) indicate a 2D smooth surface. The AFM surface topography (Fig. S1d) and measured step heights (Fig. S1e) before growth indicate that a high-quality single TiO2-terminated SrTiO3 (001) substrates were obtained. Highly smooth film AFM surface image (Fig. S1f) shows that the grown film still has a two-dimensional structure, and measured step heights (Fig. S1g) of thin films shows that the LAO is subjected to tensile strain.

- X-ray diffraction and reflectivity of heterojunction film

Fig. S2 | Structure characterization. a, X-ray diffraction of (001) and (002) peaks for the heterojunction film. b, X-ray diffraction ω-rocking curve (XRC) of the as-grown heterojunction film (002) plane. Experimental (black dots) and model (red line) X-ray reflectivity curves (c) of the heterojunction film. d, X-ray scattering length density (SLD) profiles obtained from the X-ray reflectivity fits.

X-ray diffraction (Fig. S2a) shows that the heterojunction film has a good epitaxial relationship with the STO substrate. The full-width at half-maximum (FWHM, Fig. S2b) was measured to be 0.021°, indicating the good crystallinity of the heterojunction film. The simulation of XRR (Fig. S2c, red line) well confirm the layer by layer fashion monitored by RHEED. The simulation parameters are shown in Table S1.

- Detections of low boiling point and inert substances

Fig. S3 | Optimized activation resistance for broader gas detection. Measurements of H2 (a) and Ar (b).

By adjusting the carrier concentration at the interface of C-2DEG gas sensor, the resistance after activation does not exceed the measurement limit of the source meter, so as to realize the detection of those substances that sublime or boil at low temperature, such as H2 (Fig. S3a) and Ar (Fig. S3b).

- Evidence for Charged Gas Ice layer

Fig. S4 | Evidences for Charged gas ice layer. A, R-T curves of cooling (red line) and warmup (blue line) with gate applied at 300K. b, Response of sample with higher carrier concentration (2.54×1013 /cm2) in mixed gas environment. The inset is the first order differential of resistance around the CO2 sublimation temperature (135 K - 150 K).

Two smooth curves (Fig. S4a) show that applying back-gating at high temperature (300K) does not activate the device, but only the gas ice layer can be charged. The sudden change of the slope of the first differential (Fig. S4b) indicates the sublimation of CO2. Based on the parallel plate series model (1/C=1/C1+1/C2), the total capacitance is mainly contributed by the substrate since the film thickness is much thinner than the substrate. Under the temperature of 2 K and the electric field of 4200 V/cm, the STO (001) substrate has a relative permittivity of ~104.1 Therefore, after applying a back-gate voltage of 210 V, the gas charge concentration is ~2.32×1013/cm2, which is consistent with the depleted interface carrier concentration calculated in the main text.

- Characterization of carrier mobility before and after activation

Fig. S5 | Carrier mobility before and after activation as a function of temperature.

The carrier mobility after activation is almost the same as that of as grown, except that there is a maximum 20% change in the SOB temperature range, indicating that the activation does not change the carrier mobility, but only reduces the carrier concentration.

| Layer | Chem. Formula | Density (g/cm3) | Thickness (Å) | Roughness (Å) |
| --- | --- | --- | --- | --- |
| Layer 2 | LaAlO3 | 6.822347 | 37.22338 | 2.835766 |
| Layer 1 | LaFeO3 | 7.998116 | 19.9194 | 12.57356 |
| Substrate | SrTiO3 | 5.236075 |  | 7.181943 |

Table S1. The simulation parameters obtained from the X-ray reflectivity fits by GenX 3.6.16. Thickness fitting results of LFO and LAO are consistent with STEM images (Fig. 1c).

| Name | CO2 measure limit | Author |
| --- | --- | --- |
| C-2DEG Gas Senor | 0.025 torr (33 ppm at 1.0 atm) | Present work 2022 |
| Calcium doped ZnO | 50 ppm | Ghosh et al. 20192 |
| p-Si/MoO3 | 100 ppm | T. Thomas et al. 20213 |
| Li4Ti5O12 | 100 ppm | S. Joshi et al. 20164 |
| CoAl2O4 | 100 ppm | C. Michel et al. 20105 |
| ZnO | 400 ppm | Y. Hunge et al. 20186 |
| CeO2 | 800 ppm | A. Aboud et al. 20177 |
| SnO2 | 2000 ppm | D. Wang et al. 20168 |
| CNx/p-Si | 6 torr | N. Zouadi et al. 20159 |

Table S2. A literature review on the CO2 measure limit of gas senor. The test limit of our C-2DEG gas sensor for CO2 can be compared with the best MOS gas sensor that has been reported so far

| Compounds | Electron Affinity (eV) |
| --- | --- |
| H2 (g) | 0.7510 |
| N2 (g) | 0.0711 |
| CH4 (g) | -1.6312 |
| O2 (g) | 1.4613 |
| C2H4 (g) | -0.3812 |
| CO2 (g) | 0.6±0.214 |
| ice | 0.8±0.115 |
| Ar (g) | -1 |

Table S3. A literature review on the electron affinity of all gases appearing in the article. The higher the electron affinity, the stronger the ability to bind electrons, the more sensitive our gas sensors are to this gas and thus have a higher measurement limit.

Reference

1	Neville, R. C., Hoeneisen, B. & Mead, C. A. Permittivity of Strontium Titanate. Journal of Applied Physics 43, 2124-2131, doi:10.1063/1.1661463 (1972).

2	Ghosh, A., Zhang, C., Shi, S. & Zhang, H. High temperature CO2 sensing and its cross-sensitivity towards H2 and CO gas using calcium doped ZnO thin film coated langasite SAW sensor. Sensors and Actuators B: Chemical 301, doi:10.1016/j.snb.2019.126958 (2019).

3	Thomas, T. et al. Porous silicon/α-MoO3 nanohybrid based fast and highly sensitive CO2 gas sensors. Vacuum 184, doi:10.1016/j.vacuum.2020.109983 (2021).

4	Joshi, S., Lanka, S., Ippolito, S. J., Bhargava, S. K. & Sunkara, M. V. {111} faceted Li4Ti5O12 octahedra as the reference electrode material in a nanostructured potentiometric CO2 sensor. Journal of Materials Chemistry A 4, 16418-16431 (2016).

5	Michel, C. R. CO and CO2 gas sensing properties of mesoporous CoAl2O4. Sensors and Actuators B: Chemical 147, 635-641, doi:10.1016/j.snb.2010.04.013 (2010).

6	Hunge, Y. M., Yadav, A. A., Kulkarni, S. B. & Mathe, V. L. A multifunctional ZnO thin film based devices for photoelectrocatalytic degradation of terephthalic acid and CO2 gas sensing applications. Sensors and Actuators B: Chemical 274, 1-9, doi:10.1016/j.snb.2018.07.117 (2018).

7	Aboud, A. A. et al. CO2 responses based on pure and doped CeO2 nano-pellets. Journal of Materials Research and Technology 7, 14-20, doi:https://doi.org/10.1016/j.jmrt.2017.03.003 (2018).

8	Wang, D. et al. CO2-sensing properties and mechanism of nano-SnO2 thick-film sensor. Sensors and Actuators B: Chemical 227, 73-84, doi:https://doi.org/10.1016/j.snb.2015.12.025 (2016).

9	Zouadi, N., Messaci, S., Sam, S., Bradai, D. & Gabouze, N. CO2 detection with CNx thin films deposited on porous silicon. Materials Science in Semiconductor Processing 29, 367-371, doi:10.1016/j.mssp.2014.07.023 (2015).

10	McWeeny, R. The electron affinity of H2: a valence bond study. Journal of Molecular Structure: THEOCHEM 261, 403-413 (1992).

11	Haynes, W. M. CRC handbook of chemistry and physics.  (CRC press, 2016).

12	Hedges, R. M. & Matsen, F. A. Antisymmetrized Hückel Orbital Calculations of Ionization Potentials and Electron Affinities of Some Aromatic Hydrocarbons. The Journal of Chemical Physics 28, 950-953, doi:10.1063/1.1744302 (1958).

13	Kristiansson, M. K. et al. High-precision electron affinity of oxygen. Nat Commun 13, 5906, doi:10.1038/s41467-022-33438-y (2022).

14	Yin, W. J. et al. The Effect of Excess Electron and hole on CO2 Adsorption and Activation on Rutile (110) surface. Sci Rep 6, 23298, doi:10.1038/srep23298 (2016).

15	Gaiduk, A. P., Pham, T. A., Govoni, M., Paesani, F. & Galli, G. Electron affinity of liquid water. Nat Commun 9, 247, doi:10.1038/s41467-017-02673-z (2018).