Efficient degradation of sulfamethoxazole by diatomite-supported hydroxyl-modified UIO-66 photocatalyst

Hui-Lai LIU a, b, Yu ZHANG a, b, Xin-Xin LV a ,b, Min-Shu CUI a, Kang-Ping CUI a, Zheng-Liang DAI c， Bei WANG c, Rohan WEERASOORIYA b, d, Xing CHEN a, b, d*,

a   Key Laboratory of Nanominerals and Pollution Control of Higher Education Institutes, School of Resources and Environmental Engineering, Hefei University of Technology, Hefei 230009, P. R. China

b   Key Lab of Aerospace Structural Parts Forming Technology and Equipment of Anhui Province, Institute of Industry and Equipment Technology, Hefei University of Technology, Hefei, 230009, P. R. China

c   Anqing Changhong Chemical Co., Ltd., Anqing, 246002, P. R. China

d   National Centre for Water Quality Research, National Institute of Fundamental Studies, Hantana, Kandy, Sri Lanka

* Corresponding author:

Xing Chen (xingchen@hfut.edu.cn)

Text S1

Photoelectrochemical measurements

The photocurrent measurements were carried out on a CHI-760E electrochemical workstation (Chenhua Instrument, Shanghai, China) in a conventional three-electrode configuration with the sample modified ATO (20 mm * 50 mm) as the working electrode, Pt as the counter electrode, and Ag/AgCl as the reference electrode. The current measurement i-t curve was performed using an LED lamp (35 W) at 0.4 V bias voltage potential. A 0.5 M Na2SO4 aqueous solution was used as the electrolyte.

Fig. S1. The XRD patterns of synthesized photocatalysts

Fig. S2. (a) Kubelka–Munk curves of as-prepared catalysts and (b)Tafel polarization curves

Fig. S3. The effect of different catalysts on SMX adsorption performance. (Reaction conditions: initial SMX, 20.0 mg/L; catalyst, 400 mg/L)

Fig. S4. Removal efficiency of TOC. (Reaction conditions: pH 3.0; initial SMX, 20.0 mg/L; catalyst, 400 mg/L; H2O2, 4.0 mM)

Fig S5. Liquid-mass diagram of SMX and its intermediates in photo-Fenton system

Table S1. The structural information of the possible intermediates products.

| Compounds | Formula | m/z | Proposed structure |
| --- | --- | --- | --- |
| SMX | C10H11N3O3S | 254 |  |
| SMX 1 | C10H13N3O4S | 272 |  |
| SMX 2 | C10H11N3O6S | 299 |  |
| SMX 3 | C10H9N3O5S | 284 |  |
| SMX 4 | C6H6N2O5S | 235 |  |
| SMX 5 | C6H4N2O4S | 217 |  |
| SMX 6 | C4H6N2O4S | 181 |  |
| SMX 7 | C4H6N2O5S | 196 |  |
| SMX 8 | C4H4NO2 | 113 |  |
| SMX 9 | C6H8N2O2S | 172 |  |
| SMX 10 | C6H7NO2S | 156 |  |