- Characterizations

Fourier transform infrared (FTIR) spectrophotometer (Thermo electronic Nicolet iZ10) was used to characterize the chemical composition in 500-4000 cm-1 region. Transmission electron microscope (TEM 1400) and high-resolution transmission microscope (TEM-2100 UHR) were used to characterize low-resolution transmission and high-resolution transmission morphologies of the samples. Cold-field emission scanning electron microscopy (SEM, Regulus 8100, Japan) was characterized the morphology microscopic images of samples. X-ray photoelectron spectroscopy (XPS) (AXIS UltraDLD, Shimazu, UK) was used to determine the composition of sample element. The composite multifunctional horizontal X-ray diffractometer (XRD Ultima IV, Rigaku) was used to characterize crystalmorphology of the samples. Fluorescence emission spectra of samples were tested using a fluorescence   spectrometer (FS5) (Edinburgh, Scotland, UK); The optical absorption full-wavelength enzyme label (Read Max 1900) (Shanghai Flash Biotechnology Co., LTD., Flash Flash) was used to determine the absorption spectrum of the sample. The fluorescence lifetime of the samples was recorded by FLS 980 transient fluorescence spectrometer (EI, UK). pH meter (FiveEsay Plus) (Shanghai Mettler Tolitol Instrument Co., LTD.) was used to determine the pH value of the sample. Vacuum impregnation and drying of samples were carried out in vacuum drying oven (DZG-6020 model) (Shanghai Senxin Experimental Instrument Co., LTD.). The thermogravimeter (TGA) (Mettler Toledo) was used to measure the mass of the sample as a function of temperature (or time) in a programmed temperature-controlled nitrogen atmosphere. Atomic force microscope (AFM) (Bruker Multimode 8, USA) was used to characterize the surface morphology of the sample. Tobacco plants were cultured in RDN artificial climate box (RDN-260B-4) (Ningbo Southeast Instrument Co., LTD.).

- CPU-CDs for real-time monitoring of Cu2+ in zebrafish

All zebrafish experiments were conducted in accordance with the National Research Council's Guide for the Care and Use of Laboratory Animals and approved by the Institutional Animal Ethics Committee of the Nanjing Forestry University (NJFU-22275094) in Nanjing, China. According to the literature method, zebrafish embryos (male, 6 days, the sex of animals have no influence on study) were grown in E3 embryo media in a glass dish. Then CPU-CDs solution (10 μM) and CPU-CDs+Cu2+ solution were added into the embryos and co-cultured for 5 min before fluorescence imaging, respectively.

- Detection limit

Detection limit was determined using the formula.

DL=3σ/S

where σ is the standard deviation of blank control. S is the slope of the linear calibration versus Cu2+ concentration.

- Quantum yield (QY) measurements

The QYs of the sample was measured using a relatively classical method. Using quinine sulfate (QY = 55% in 0.1 mol L-1 H2SO4) as the reference. The fluorescence quantum yield is 54% at 360 nm excitation wavelength. The optical absorbance of sample aqueous solution and reference substance was measured. In order to reduce the reabsorption effect of fluorescent substances as much as possible, the concentrations of reference solution and sample solution were adjusted to make their absorbance values less than 0.05. Then, the fluorescence spectra of quinine sulfate and sample aqueous solution with known absorbance were tested. The QY of the sample was then calculated according to the following equation:

φ=φ0×A0I0×IA×n2n02

where φ, A, I, and n represent the QY, optical density, integral emission intensity, and refractive index (water = 1.33, ethanol = 1.36) of the sample, respectively, and φ0, A0, I0, and n0 represent the QY, optical density, integral emission intensity, and refractive index of quinine sulfate.