| Sodium & Potassium | 2205 |
| --- | --- |
| Calcium | 262 |
| Magnesium | 46 |
| Barium | 3.74 |
| Strontium | 6.5 |
| Chlorides | 4537 |
| Sulphates | 1750 |
| Bicarbonates | 378 |
| Carbonates | 0 |
| Hydroxides | 0 |
| T.D.S. | 11000 |

Table 1: The Characteristic Constituents of Formation Water Solution (in ppm)

Table 2: The Physical Properties of the Utilized Formation Water

| pH | 6.88 |
| --- | --- |
| Salinity as NaCl, ppm | 7449 |
| Total hardness, ppm | 842 |

Table 3: Corrosion Rates (mpy) and Inhibition Efficiencies (IE %) of Extracts in FW at 25 oC

| Extract | Conc. %(v/v) | CR (mpy) | Surface Coverage () | IE% |
| --- | --- | --- | --- | --- |
| Blank | 0 | 6.29 x10-8 | -- | -- |
| OPE | 0.5 | 1.34 x10-8 | 0.7878 | 78.78 |
|  | 1 | 1.25 x10-8 | 0.8011 | 80.11 |
|  | 1.5 | 1.05 x10-8 | 0.8329 | 83.29 |
|  | 2 | 7.85 x10-9 | 0.8753 | 87.53 |
|  | 2.5 | 4.51 x10-9 | 0.9284 | 92.84 |

Table 4: Chemical Kinetic Parameters for the corrosion of CS in Formation Water in Absence and Presence of Different Concentrations of Peel Extract

| Extract | Conc. % (v/v) | K (h-1) | t0.5 (h) |
| --- | --- | --- | --- |
| Blank | 0 | 1.15x10-6 | 6.02 x105 |
| OPE | 0.5 | 4.61 x10-8 | 1.50 x107 |
|  | 1 | 1.84 x10-7 | 3.76 x106 |
|  | 1.5 | 1.38 x10-7 | 5.02 x106 |
|  | 2 | 1.38 x10-7 | 5.02 x106 |
|  | 2.5 | 4.61 x10-8 | 1.50 x107 |

Table 5: Langmuir Adsorption Parameters of C- Steel in Formation Water in Presence of Different Concentrations from OPE using Weight Loss Method at 25 °C

| Kads (mol-1) | Slope | ∆Gadso (kJ/mol) | R² |
| --- | --- | --- | --- |
| 5.36 | 1.0306 | -13.874 | 0.9938 |

Table 6: Potentiodynamic Parameters for CS in FW in Absence and Presence of Various Concentrations of OPE at 25 °C

| Conc., %(v/v) | Ecorr (mV/SCE) | Icorr (mA/cm2) | βa (mV/dec) | -βc (mV/dec) | θ | IE% | CR (mpy) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 0 | -687 | 41.4 | 123 | 289 | - | - | 251 |
| 0.5 | -693 | 16.3 | 130 | 189 | 0.6063 | 60.63 | 191 |
| 1 | -679 | 15.1 | 100 | 188 | 0.6339 | 63.39 | 177 |
| 1.5 | -687 | 10.7 | 123 | 150 | 0.7410 | 74.10 | 126 |
| 2 | -676 | 8.5 | 135 | 160 | 0.7954 | 79.54 | 99 |
| 2.5 | -693 | 4.0 | 123 | 155 | 0.9013 | 90.13 | 53 |

Table 7: Potentiodynamic Parameters for C-Steel in FW in Absence and Presence of 2.5% Peel Extract at Temperature Range (25- 55 °C)

|  | Temp. (°C) | Ecorr (mV/SCE) | Icorr (mA/cm2) | βa (mV/dec) | -βc (mV/dec) | CR (mpy) | θ | IE% |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Blank | 25 | -687 | 41.4 | 123 | 289 | 251 | -- | -- |
|  | 35 | -675 | 44.5 | 100 | 161 | 270 | -- | -- |
|  | 45 | -673 | 79.4 | 124 | 129 | 360 | -- | -- |
|  | 55 | -660 | 97.7 | 124 | 250 | 390 | -- | -- |
| OPE | 25 | -693 | 4.5 | 123 | 155 | 53 | 0.9013 | 90.13 |
|  | 35 | -695 | 5.6 | 144 | 86 | 64 | 0.8804 | 88.04 |
|  | 45 | -690 | 7.5 | 156 | 72 | 81 | 0.8799 | 87.99 |
|  | 55 | -682 | 12.6 | 195 | 42 | 140 | 0.8686 | 86.86 |

Table 8: Activation Thermodynamic Parameters of CS in Absence and Presence of OPE using Potentiodynamic Polarization Method

|  | Ea* kJ/mol | ∆H* (kJ/mol | ∆S* J/(mol K) | ΔG* (kJ/ mol) |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | 25 oC | 35 oC | 45 oC | 55 oC |
| Blank | 13.12 | 10.52 | -163.93 | 59.37 | 61.01 | 62.65 | 64.29 |
| OPE | 25.63 | 23.03 | -135.40 | 63.4 | 64.73 | 66.09 | 67.44 |

Table 9: Langmuir Adsorption Isotherm Parameters for the Extract Adsorbed on CS Surface in FW Solution using Potentiodynamic Method at 25 °C

| Extract | Kads (mol-1) | Slope | ∆Gadso (kJ/mol) | R² | ∆Hadso (kJ/mol) | ∆Sadso (J/(mol K)) |
| --- | --- | --- | --- | --- | --- | --- |
| OPE | 2.03 | 0.967 | -11.71 | 0.971 | -12.31 | -2.013 |

Table 10: Percentage of Atomic Contents of Elements (Mass %) Obtained from EDX Spectra

| Element | Polished CS | CS in FW for 1 month | CS in FW and OPE for 1 month |
| --- | --- | --- | --- |
| N | - | - | 1.12 |
| C | - | 1.95 | - |
| O | - | 24.19 | 24.93 |
| Na | - | 1.95 | - |
| Mg | - | 1.08 | - |
| Si | - | 4.82 | - |
| S | - | 0.65 | 3.14 |
| Cl | - | 0.38 | - |
| Ca | - | 10.16 | - |
| Fe | 100 | 54.81 | 70.8 |
| Total | 100 | 100 | 100 |