Preparation and characterization of titanium oxide nanocapsules containing retinoic acid for sustained release

Xuecheng Yu 1, &, Yunhe Zhao 2, &, Gang Chen 3, Jing Yu 3, Ruolan Wang 1, Yuhao Deng 2, Xiaoying Wang 2, Xinru Yuan 1, Xue-Feng Yu 1, 4, Rui He 1, *

1 Shenzhen Institute of Advanced Technology, Chinese Academy of Sciences, Shenzhen 518055, China

2 Wuhan Science and Technology Institute of Advanced Technology, Wuhan 430000, China

3 Blank me R&D Center, Yongxi Tech Co., LTD, Shanghai 200011, China

4 Hubei Three Gorges Laboratory, Yichang 443007, China

& These authors contributed equally to this work.

* Corresponding author.

E-mail address: rui.he1@siat.ac.cn (R. H.)

- Table S1 RA-TiO2 nanocapsules under different synthesis conditions

- Fig. S1 The schematic diagram of sustained-release tests by elution process

- Fig. S2 The schematic diagram of photostability experiments

Table S1 Preparation of RA-TiO2 nanocapsules under different synthesis conditions

| Experimental number | Solubilizing agent | Core material contents | Shell-forming agents | Aqueous phase additives |
| --- | --- | --- | --- | --- |
| 1 (Fig. 2a) | None | 1 wt% | Ethyl titanate | Octadecyl trimethylammonium chloride(OTAC) |
| 2 (Fig. 2b) | Ethanol | 30 wt% | Ethyl titanate | OTAC |
| 3 (Fig. 2c) | Ethanol | 20 wt% | Ethyl titanate | OTAC |
| 4 (Fig. 2d) | Ethanol | 15 wt% | Ethyl titanate | OTAC |
| 5 (Fig. 2e) | Ethanol | 10 wt% | Butyl titanate | OTAC |
| 6 (Fig. 2f) | Ethanol | 10 wt% | Ethyl titanate | None |
| 7 (Fig. 2g) | Ethanol | 10 wt% | Ethyl titanate | Sodium dodecyl sulfate |
| 8 (Fig. 2h) | Ethanol | 10 wt% | Ethyl titanate | Ammonium chloride |
| 9 (Fig. 2i) | Ethanol | 10 wt% | Ethyl titanate | OTAC |

Fig. S1 The schematic diagram of sustained-release tests by elution process

Fig. S2 The schematic diagram of photostability experiments under sunlight irradiation