Supplementary Information

Effect of Li substitution on the structure and dielectric constant of Bi0.5(Na⁠1-xLix)0.5TiO⁠3 (0 ≤ x ≤ 0.20) solid solution series

K. Anjalia,b,  T. G. Ajithkumara,  P. A. Joya,*

a Physical and Materials Chemistry Division, CSIR-National Chemical Laboratory,

Pune 411008, India

b Department of Chemistry, School of Engineering, Presidency University,

Bengaluru 560064, India

* Corresponding author. E-mail: tg.ajithkumar@ncl.res.in; pa.joy@ncl.res.in

Table S1: Lattice parameters of the monoclinic unit cell (space group: Cc), reduced χ2 and Rp values of (1-x)BNT–xBLT obtained from Rietveld analysis.

| Sample | a (Å) | b (Å) | c (Å) | β (degree) | χ2 | Rp (%) |
| --- | --- | --- | --- | --- | --- | --- |
| BNT | 9.5263 | 5.4829 | 5.5091 | 125.43 | 2.065 | 5.18 |
| 0.02BLT | 9.5261 | 5.4832 | 5.5089 | 125.42 | 3.225 | 5.46 |
| 0.04BLT | 9.5238 | 5.483 | 5.5077 | 125.40 | 3.121 | 5.49 |
| 0.06BLT | 9.5249 | 5.4826 | 5.5064 | 125.39 | 3.260 | 5.65 |
| 0.08BLT | 9.523 | 5.4838 | 5.5056 | 125.39 | 3.562 | 5.79 |
| 0.10BLT | 9.5197 | 5.4834 | 5.503 | 125.36 | 3.664 | 5.91 |
| 0.12BLT | 9.5159 | 5.4864 | 5.4982 | 125.33 | 3.679 | 5.97 |
| 0.14BLT | 9.5154 | 5.4887 | 5.4955 | 125.32 | 3.322 | 5.65 |
| 0.16BLT | 9.5101 | 5.4904 | 5.4911 | 125.29 | 3.424 | 5.69 |
| 0.18BLT | 9.5081 | 5.4896 | 5.4897 | 125.28 | 3.789 | 5.92 |
| 0.20BLT | 9.508 | 5.4897 | 5.4897 | 125.27 | 3.858 | 5.96 |

Figure S1: Variation of unit cell volume of (1-x)BNT–xBLT solid solution series as a function of x.

Figure S2: Changes in the (a) peak position and (b) area under the peak of the band below 200 cm-1 in the Raman spectra as a function of x in (1-x)BNT–xBLT.

Figure S3: Changes in the individual peak positions of the Raman band in the 400800 cm-1region as a function of x in (1-x)BNT–xBLT. (a) 1st peak, (b) 2nd peak, and (c) 3rd peak, as defined in figure 4.

Figure S4: Total area and area under the individual peaks of the Raman band in the 400800 cm-1 region as a function of x in (1-x)BNT-xBLT, (a) total area, (b) area under the 1st peak, (c) area under the 2nd peak, and (d) area under the 3rd peak.