Thermal ratcheting in granular materials with irregular particle shapes

Yize Pan1, Xiaohui Gong1, Alessandro F. Rotta Loria1*

1 Mechanics and Energy Laboratory, Department of Civil and Environmental Engineering, Northwestern University, 2145 Sheridan Road, Evanston, Illinois 60208, USA

*Corresponding author: af-rottaloria@northwestern.edu

Supplementary Material

Table S1 Maximum and minimum void ratios of the three types of tested materials

| Tested materials | Maximum void ratio emax [-] | minimum void ratio emin [-] |
| --- | --- | --- |
| F-35 sand | 0.764 | 0.510 |
| NJ #00 sand | 0.995 | 0.642 |
| 1 Q-ROK sand | 1.049 | 0.708 |

Fig. S1. Particle size distributions and SEM images of the three types of granular materials. (a) Particle size distribution. (b) SEM images of rounded, subangular, angular sands (from top to bottom).

Fig. S2. Particle shape characterizations of the three types of granular materials. (a) Histogram of roundness R. (b) Histogram of sphericity S.

Fig. S3. Test protocol for the isothermal tests. (a) Loading paths (the variation of sample relative density DR is not represented for simplicity and clarity). (b) Prototype readings of vertical stress σz and sample temperature T over time t.

Fig. S4. Test protocols for the non-isothermal tests considering different temperature amplitudes ∆T and stress levels σz. Mechanical loading and unloading follow the same stress steps and time interval shown in Fig. S3. The variation of sample relative density DR is neglected for simplicity and clarity.  Red dots mark the stress levels at which thermal cycling is applied. (a) Theoretical paths and (b) actual readings of vertical stress σz and temperature T over time t considering ∆T=60 °C and σz=60 kPa. (c) Theoretical paths and (d) actual readings of vertical stress σz and temperature T over time t considering ∆T=60 °C and σz=500 kPa. (e) Theoretical paths and (f) actual readings of vertical stress σz and temperature T over time t considering ∆T=30 °C and σz=60 kPa.

Fig. S5. Detailed view of vertical stress σz and temperature T readings during one thermal cycle with a temperature amplitude of ∆T=60 °C. The example represents the readings between t = 150 and 415 min in Figure S4(b). (a) Readings of vertical stress σz during one thermal cycle. (b) Readings of temperature T during one thermal cycle.