Supplementary information:

Crystal Crafting: Controlling Crystallites Orientation and Facet Exposure for Enhanced Electrochemical Properties of Polycrystalline MoO3 Films

Konrad Trzcińskia,b*, Zuzanna Zaracha, Mariusz Szkodaa,b, Andrzej P. Nowaka, Mirosław Sawczakc

aFaculty of Chemistry, Gdańsk University of Technology, Narutowicza 11/12, 80-233 Gdańsk, Poland

bAdvanced Materials Center, Gdańsk University of Technology, Narutowicza 11/12, 80-233 Gdańsk, Poland

cCentre for Plasma and Laser Engineering, The Szewalski Institute of Fluid Flow Machinery, Fiszera 14, 80-231 Gdańsk, Poland

*corresponding author: kontrzci@pg.edu.pl

Fig. S1 SEM micrographs of MoO3 deposited on the FTO substrate at a) 400°C and b) 500°C under 0.5 mbar O2 for 120 minutes; c) SEM micrograph of MoO3 deposited on FTO/Mo substrate (Mo deposited on FTO using magnetron sputtering system), performed at 450°C under 0.5 mbar O2 for 120 minutes.

Fig.S2 SEM micrographs of a) MoO3 deposited at room temperature (120 minutes) with subsequent annealing for 4 hours at 450°C and b) MoO3 deposited at room temperature (120 minutes) with subsequent “rapid” annealing for 20 minutes at 575°C.

Fig. S3 Digital photos of samples deposited at room temperature (120 minutes) with subsequent annealing for a) 60 minutes and b) 5 minutes at 575°C.

Fig. S4 SEM micrographs of MoO3 films deposited at room temperature (120 minutes) with subsequent “rapid” annealing for 1 hour at a) 400°C and b) 450°C; c) XRD patterns of both samples.

Fig. S5 EDX results for the PLD_450°C(Ar,O2) electrode material after cathodic polarization at -0.1 V vs. Ag/AgCl (3 M KCl).