·Supplementary Information (SI) for

Remediation of As(Ⅴ) and Cd(II) contamination by a ZVI-biochar: experimental and DFT calculation

Bangwei Liu1, Yan Zhou1,Yiwei Zhang1, Dandan Chen1*, Wenhui Liu1, Ping Lu1, Xiaoyu Su1, and Tian Xia1

1.School of Energy and Mechanical Engineering, Nanjing Normal University, Nanjing 210023, China;

*Corresponding Author: Tel/Fax: +86–25–85481085; E-mail: dandanchen@njnu.edu.cn

The Supporting Information includes:

2 Texts

1 Table

3 Figures

Text S1 Kinetic model and Intra-particle diffusion model

(1) To investigate the adsorption equilibrium time and the possible mechanism, the kinetic equations of Pseudo-first-order model (Equation 1) and pseudo-second-order model  (Equation 2) were used to describe the adsorption kinetics of biochar on As(Ⅴ) and Cd(Ⅱ), respectively.

lnQe-Qt=lnQe-k1t  (1)

tQt=1K2Qe2+tQe  (2)

Qe ………… Adsorption capacity at equilibrium，

Qt…………Adsorption capacity at time t，

k1、k2……… Rate constants for two adsorption models.

(2) Intra-particle diffusion model

Qt=At0.5+B (3)

Qt………… Adsorption capacity at time t，

A…………Internal diffusion rate constant (g/kg)

B…………dimensionless constants

Text S2 Calculation formula for soil leaching experiments

（1）Single release of heavy metals in soil

The single release of heavy metals in the experimental soil column reflects the influence of leaching processes on the leaching characteristics of heavy metals in soil. The higher the single release of heavy metals, the more easily they migrate and the worse their bioavailability.

Ri=Ci×vm(4)

Ri…………Single release of heavy metals in soil samples for leaching experiments，mg/kg

Ci…………Concentration of heavy metals in the filtrate collected in the i-th leaching，mg/kg

ν…………Volume of filtrate during each leaching process，ml

m…………Experimental soil quality，kg

In the experiment, six leaching processes were carried out. The filtration volume of each leaching was 350 ml. the mass of the experimental soil was 120 g.

(2) Cumulative release of heavy metals in soils

R=R1+R2+…+R6(5)

R…………Cumulative release of heavy metals from soil samples under leaching experiments，mg/kg；

(3) Single release rate and cumulative release rate of heavy metals in soils

ki=RiMhm(6)

k=RMhm(7)

Ki…………Single release rate of heavy metals from soil in the i-th leaching%；

K…………Cumulative release rate of heavy metals in soils， %；

Mhm…………Total heavy metals in soils，mg/kg；

As and Cd concentrations in soil was 47 and 3 mg/kg, respectively.

Table S1 Fitting parameters of the kinetic models for CSC and ZVI-CSC

(a) As(Ⅴ) adsorption kinetics

| Types | Pseudo-first-order |  |  | Pseudo-second-order |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | K1 (min-1) | Qe (g.kg-1) | R2 | K1 (min-1) | Qe (g.kg-1) | R2 |
| CSC (pH=6) | 0.00443 | 6.29935 | 0.8997 | 0.00068 | 7.44654 | 0.9345 |
| ZVI-CSC (pH=6) | 0.0521 | 3.86243 | 0.8530 | 0.01897 | 4.10306 | 0.9689 |
| CSC (pH=3) | 0.12396 | 6.63473 | 0.8537 | 0.02741 | 6.91569 | 0.9824 |
| ZVI-CSC (pH=3) | 0.09689 | 13.74731 | 0.8179 | 0.00995 | 14.42402 | 0.9585 |

(b) Cd(II) adsorption kinetics

| Types | Pseudo-first-order |  |  | Pseudo-second-order |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | K1 (min-1) | Qe (g.kg-1) | R2 | K1 (min-1) | Qe (g.kg-1) | R2 |
| CSC (pH=3) | 0.08282 | 2.44023 | 0.9451 | 0.04678 | 2.56761 | 0.99037 |
| ZVI-CSC (pH=3) | 0.0548 | 3.12059 | 0.8211 | 0.02146 | 3.34594 | 0.85231 |
| CSC (pH=6) | 0.09797 | 4.39713 | 0.8167 | 0.02847 | 4.64723 | 0.95227 |
| ZVI-CSC (pH=6) | 0.08974 | 2.09247 | 0.9398 | 0.05951 | 2.19771 | 0.99158 |

Fig.S1 Soil leaching experimental setup

Fig.S2 Pore size distribution curves of CS, CSC, and ZVI-CSC

Fig.S3 XPS spectra of C 1s, O 1s and As 3d of CSC and ZVI-CSC