Chemical reagents:

MoS2 nanosheets and bulk MoS2 were purchased from Xianfeng NANO Materials Technology Co., Ltd. Hydrogen peroxide (H2O2) was bought from Sinopharm Chemical Reagent Co., Ltd. (Wuhan, China,). 3, 3’, 5, 5’-tetramethylbenzidine (TMB) was bought from Sigma (Shanghai, China,). The water used in the experiments was de-ionized (DI) and all analytical reagents were used as received.

Calculation details:

The calculations are carried out by means of spin-polarized density functional theory (DFT) methods using Vienna Ab-initio Simulation Package (VASP). The exchange and correlation energies are described by the generalized gradient approximation (GGA) with the Perdew-Burke-Ernzerhof (PBE) functional which is used to describe the electron-ion interactions. Based on careful convergence tests, the plane wave energy cutoff is set to 400 eV. To accurately describe the dispersion interaction, DFT-D3 method with Becke-Jonson damping for dispersion correction is employed. The transition states and detailed minimum-energy pathway are obtained using the climbing image nudged elastic band (CI-NEB) method combined with dimer method. The convergence criterion of electronic structure is set to 10-5 eV, and the atomic relaxation is continued until the forces acting on atoms being smaller than 0.05 eV/Å. The Brillouin zone is sampled with 3×3×1 Monkhorst-Pack k-point mesh, and a Gaussian smearing of 0.05 eV is applied to speed up electronic convergence. A vacuum height of 20 Å along the vertical direction is selected to avoid the unwanted interaction between the slab and its period images.

Characterization

Transmission electron microscope (TEM) was conducted on FEI JEM-2100F field emission transmission electron microscope (field emissetem, 200kv). K-alpha 250Xi X-ray photo-electron spectroscopy (XPS) was employed to analyze the surface valence states. Room-temperature electron spin resonance (ESR) signals were measured by using Bruker A300max ESR spectrometer. Atomic force microscopy (AFM, MPF-3D) was used to detect the height and size of different MoS2. The ammonia temperature programmed desorption (NH3-TPD, AutoChem II 2920) was used in the range of 50-800 oC with a linear heating rate of 10 oC/min in a flow of helium. Raman spectra was recorded on Renishaw MZ20-FC spectrometer with laser excitation of 532 nm.

Mimic enzyme tests

The enzymatic like activity of MoS2 was measured as follows: (a) 0.4 mM TMB+10 mM H2O2, (b) 0.4 mM TMB+ 0.5 mg/mL MoS2, (c) 10 mM H2O2+0.5 mg/mL MoS2, (d) 0.4 mM TMB+10 mM H2O2+0.5 mg/mL MoS2. The absorbance was recorded at 652 nm.

Credits

Jin Wang: Writing - original draft, data curation, investigation, and formal analysis.

Yi Wang: Conceptualization, Supervision, Writing - review & editing, and Funding acquisition.

Wenyu Ren: Resources and Formal analysis.

Dun Zhang: Supervision and funding acquisition.

Peng Ju and Kunpeng Dou: Software.

Table S1. Results of NH3-TPD of different MoS2 samples.

| Samples | NH3 desorption/cm3·gSTP-1 |  |  |
| --- | --- | --- | --- |
|  | T1 | T2 | T3 |
| 2D MoS2 | 0.32 | 14.05 | 2.97 |
| Bulk MoS2 | 0.45 | 0.95 |  |