Supplementary Information for

Non-Exchange Bias in Binary Nanoparticle Systems

Pierfrancesco Maltoni1*, Raúl López-Martín2, Elena H. Sánchez2, Peter S. Normile2, Marianna Vasilakaki3, Su Seong Lee4, Benito Santos Burgos2, Eloy A. López del Castillo2, Davide Peddis5, Chris Binns2, Kalliopi N. Trohidou3, Roland Mathieu1, Josep Nogués6,7*, José A. De Toro2*

1 Department of Materials Science and Engineering, Uppsala University, Box 35, SE-751 03 Uppsala, Sweden

2 Instituto Regional de Investigacio´n Cient´ıfica Aplicada (IRICA) and Departamento de F´ısica Aplicada, Universidad de Castilla-La Mancha 13071 Ciudad Real, Spain

3 Institute of Nanoscience and Nanotechnology, NCSR “Demokritos”, 153 10 Agia Paraskevi, Attiki, Greece

4 Institute of Bioengineering and Nanotechnology, 31 Biopolis Way, The Nanos, Singapore 138669, Singapore

5 Dipartimento di Chimica e Chimica Industriale, Università degli Studi di Genova, Via Dodecaneso 31, 1-16146, Genova, Italy

6 Catalan Institute of Nanoscience and Nanotechnology (ICN2), CSIC and BIST, Campus UAB, Bellaterra, Barcelona, 08193 Spain

7 ICREA, Pg. Lluís Companys 23, Barcelona, 08010 Spain

1. Magnetic properties of soft and hard nanoparticles

Fig. 1. a, Zero field cooled-field cooled (ZFC-FC) magnetization curves for the reference compacts of magnetically isolated (silica-coated) nanoparticles (reference) and b, the corresponding hysteresis loops at 5 K after field cooling. The insets in (a) shows the transmission electron microscopy images of the silica-coated particles. (c) and (d) show the ZFC-FC magnetization curves and the hysteresis loops for the compacts of bare soft (M100) and hard (M0) particles.

Table 1. Coercive field (HC), exchange-bias field (HEB) and blocking temperature (TB) values for the reference (silica coated) compacts and the corresponding M100 and M0 compacts made of bare nanoparticles.

|  | γ-Fe2O3 (reference) | γ- Fe2O3 (M100) | Co-doped γ-Fe2O3 (reference) | Co-doped γ-Fe2O3 (M0) |
| --- | --- | --- | --- | --- |
| HC (kOe) | 0.3 | 0.4 | 12.6 | 11.9 |
| HEB (kOe) | - | - | 1.20 | 1.28 |
| TB (K) | 11.5 | 170 | 93.5 | 255 |

2. Surface spin disorder

X-ray powder diffraction (XRPD; Fig. 2) and transmission electron microscopy (TEM, Fig. 1a,b in the main text) experiments were performed on the 2 sets of nanoparticles to evaluate their size and the results indicate that while both types of particles have an equally-sized diameter using TEM (dTEM; Table 2). The size obtained from the Scherrer equation,

dXRPD=k·λFWHM·cos⁡(θ)                        (Eq.1)

With λCuKα=1.5406 Å and k=0.9    for spherical particles is smaller in the Co-doped particles than in the γ-Fe2O3 ones (Table 2). In fact, the ratio dXRPD /dTEM evidences the plausible presence of disordered layer in the Co-doped particles.

Fig. 2. X-ray powder diffraction patterns for the γ-Fe2O3 and Co-doped γ-Fe2O3 nanoparticles.

Table 2. Average particle diameters obtained from XRPD, dXRPD, and TEM, dTEM.

| Sample | dXRPD (nm) | dTEM (nm) | dXRPD/dTEM |
| --- | --- | --- | --- |
| γ-Fe2O3 | 6.8(3) | 6.8(6) | 1.00 |
| Co-doped γ-Fe2O3 | 5.7(3) | 6.8(6) | 0.83 |

3 Hysteresis loops for the M0 – M100 series

Fig. 3. Low-field region of the hysteresis loops at 5 K after field cooling for the different Mx systems. The dashed lines near the origin mark the centre of the loops (bias field, HB).

4. Asymmetric reversal-induced bias

The role of the asymmetric reversal-induced bias of the hard loop in the enhanced global bias of the binary mixtures was investigated by superposing the experimental (unshifted and symmetric) loop for the soft particles and the simulated loops (with different degree of asymmetric reversal and coercivity) for the hard particles. This procedure was repeated for various soft particle fractions, and the resulting maximum attainable bias was plotted as a contour plot (see Fig. 5c in the main text) for each set of coercivity and squareness parameter of the hard particles, HBmax Shard, rightShard,  left;HC,hard, irrespective of the soft particle fraction at which this maximum is reached.  Fig. 4 shows the (a) horizontal and (b) vertical cuts from the contour plot: the maximum attainable bias is shown as a function of (a) the asymmetry for fixed HC,hard values and (b) as a function of HC,hard for determined Shard,left/rigt  values.

Fig. S4 a, Horizontal and b, vertical cuts from the contour plot (Fig. 5(c) in the main text). Note that in panel (b) the vertical axis is represented as HBmax/HC,hard  for a better view of the pseudo-linearity above 5 kOe.

5. Exchange vs dipolar energies in exchange biased nanoparticle

To evaluate the energies associated to the intraparticle exchange-coupling and interparticle dipolar interactions, the parameter Tex/Tdd was calculated by quantifying the exchange-coupling energy at the interface as EEX=kB Tex= HEBVFiMMS (where HB is the exchange-bias field, VFM is the volume of the ferromagnetic core and MS the saturation magnetization) and the dipolar interaction as Tdd= µ04πkbMS2Vφ (where φ is the packing fraction). Fig. 5 shows Tex/Tdd calculated for a number of systems with similar particle size, as a function of Tdd. We can deduce that, being Tex (exchange coupling energy) proportional to HEB, a higher HEB will generate a higher Tex/Tdd, independently from Tdd, as also shown in Table 3. Thus, y-scale informs of the dominance of exchange over dipolar energy for all systems but those with a very low exchange-bias field.

Fig. 5. Estimated Tex/Tdd ratio (with Tex defining the exchange-coupling energy at the interface and Tdd the dipolar interaction energy) for several exchange biased nanoparticle systems from the literature, as a function of dipolar interaction strength, Tdd; coloured crosses represent the mixtures Mx investigated in this study, for which Tex is constant, and equal to that of M0 (i.e., Tdd is the only varying parameter). The dashed line marks the Tex=Tdd.

Table 3. Estimated Tex/Tdd ratio and corresponding dipolar interaction strength, Tdd, ferromagnetic core diameter, dFM, and exchange-bias field, HEB.

| Ref. | Tex/Tdd |  | Tdd (K) | dFM (nm) | HEB (kOe) |
| --- | --- | --- | --- | --- | --- |
| Co-doped γ-Fe2O3 (fCo:0.2) [This study] | 13.5 | 29 |  | 6.7 | 1.28 |
| Co-doped γ-Fe2O3 (fCo:0.1)1 | 4.0 | 40 |  | 6.7 | 0.30 |
| CoO@Co0.5Ni0.5Fe2O42 | 5.1 | 10 |  | 4.7 | 0.80 |
| CoO@Co0.5Ni0.5Fe2O42 | 11.4 | 8 |  | 4.5 | 2.3 |
| Fe3−δO4@CoO3 | 17.6 | 60 |  | 9.6 | 1.68 |
| Fe3−δO4@CoO3 | 38 | 90 |  | 8.2 | 4.04 |
| Fe3−δO4@CoO3 | 11.8 | 110 |  | 9.6 | 1.36 |
| Fe3O4@CoFe2O44 | 1.0 | 40 |  | 7.2 | 0.09 |
| Fe3O4@CoFe2O44 | 0.7 | 85 |  | 10.3 | 0.05 |
| Fe3O4@CoO4 | 15.0 | 80 |  | 8.8 | 2.00 |

6. Estimation of Bias field (HB) for the individual components in the mixtures from the fits

Several attempts were carried out to fit the data, considering various fixed parameters to evaluate the possible correlations between parameters that could affect the fitting results. Interestingly, the results for soft particle concentrations higher than 50% are rather consistent independent of the fitting conditions, while below  this threshold the effect of loop asymmetry introduces fluctuations between Shard,left/right, HC,hard,  HB,hard and HB,soft, as can be seen in Fig. 9 for HB,hard and HB,soft. Different approaches were attempted to minimize the correlation effects. First, if we assume to have HB,soft=0 (i.e. none induced-bias on the soft particles), the corresponding HB,hard (black circles) turn out to largely vary, indicating that a HB,soft≠0 is necessary for the consistency of the variables. Then, by fixing HC,hard and  HB,hard in different combinations to the values of M0 (hard loop), we have quantified the fluctuations on the corresponding hard and soft field values, revealing a strong correlation between these parameters and the asymmetry of the hard component (for soft fractions <50%). To overcome this issue, the squareness parameters were constrained in this region by assuming Shard,left/rigt to not largely depart from those of M0, giving the ‘optimized fit’ results. Despite this constraint, it is important to highlight that although depending on the fitting condition the results somewhat fluctuate the observed trends are the same for all the fitting conditions.

In Fig. 10, the results for the coercivity of both the hard and soft components from the optimized fit are shown.

Fig. 6. Estimated bias fields for hard (circles) and soft (squares) particle fractions (HB,hard and HB,soft, respectively) from fitting analysis.

Fig. 7. Coercive field values for hard (HC,hard; circles) and soft (HC,soft; squares) from the optimized fit. Note that y-axis scales are different.

7. Monte Carlo results

Fig. 8. Loop shift of the hard (HB,hard)(blue) and soft (HB,soft)(red) counterparts obtained from the Monte Carlo simulations for different conditions: a, Soft particle core anisotropy, KS_core = 0.09(), 0.17(), 0.35(); b, Soft particle surface anisotropy, KS_surface = 10(),15(), 30(); c, Hard particle core anisotropy, KH_core = 25(), 50(), 80(); d, Hard particle surface anisotropy, KH_surface = 100(), 150(), 160(); e, Soft particle dipolar interactions, g1 = 12.33(), 13.70(), 15.07(); f, Hard particle dipolar interactions, g2 = 7.56() ,8.40(), 9.24(). The dotted lines are guides to the eye. Note that filled symbols are the data shown in Fig. 8 in the main text for the optimized parameters.

8. Discarding minor loop effects

Fig. 9. Dependence on the concentration of soft particles of the bias HB measured using a maximum field either HMax = 90 kOe (blue dots) or 50 kOe (black dots), respectively, for x  50%.; For comparison, the bias field extracted from the superposition loops for the case of M0 loops collected in a 90kOe or 50kOe field (black and blue circles, respectively) is also included.

Fig. 10. Criterium to determine the proper saturation of the hysteresis loops for M0 (which has the highest saturation field).

References

1.	Sánchez, E. H. et al. Crossover From Individual to Collective Magnetism in Dense Nanoparticle Systems: Local Anisotropy Versus Dipolar Interactions. Small 18, 2106762 (2022).

2.	Lavorato, G. et al. Exchange bias and surface effects in bimagnetic CoO−core/Co0.5Ni0.5Fe2O4-shell nanoparticles.  Phys. Rev. B 94, 054432 (2016).

3.	Liu, Y. et al. Investigation of the Collective Properties in Monolayers of Exchange-Biased Fe3− δO4@CoO Core–Shell Nanoparticles. J. Phys. Chem. C 122, 17456–17464 (2018).

4.	Sartori, K. et al. Strong interfacial coupling through exchange interactions in soft/hard core–shell nanoparticles as a function of cationic distribution. Nanoscale 11, 12946–12958 (2019).