Low-temperature giant coercivity in metallic Co6.2Ga3.8-xGex (x=2.4 to 3.2) with chemically tunable spin frustration

Supplemental Information

Jiro Kitagawa1,*, Himawari Nomura1& Terukazu Nishizaki2

1Department of Electrical Engineering, Faculty of Engineering, Fukuoka Institute of Technology, 3-30-1 Wajiro-higashi, Higashi-ku, Fukuoka 811-0295, Japan

2Department of Electrical Engineering, Faculty of Science and Engineering, Kyushu Sangyo University, 2-3-1 Matsukadai, Higashi-ku, Fukuoka 813-8503, Japan

Figure S1: SEM images of (a) x=2.0, (b) x=2.3, (c) x=2.4, (d) x=2.6, (e) x=2.8, (f) x=3.0, (g) x=3.2, and (h) x=3.5 for Co6.2Ga3.8-xGex, respectively. The chemical compositions determined by EDX are (a) main phase: Co60.0(5)Ga19.2(3)Ge20.8(4) impurity phase: Co62.8(3)Ga27.2(4)Ge10.0(1), (b) Co60.4(6)Ga16(1)Ge23.7(8), (c) Co60.7(3)Ga14.6(5)Ge24.8(5), (d) Co60.6(3)Ga12.3(7)Ge27.1(5), (e) Co60.9(6)Ga10.4(7)Ge28.7(1), (f) Co60.7(6)Ga8(1)Ge30.9(6), (g) Co60.3(5)Ga6.8(5)Ge32.9(2), and (h) Co60.4(4)Ga3.5(3)Ge36.0(3), respectively.

Figure S2: XRD patterns of x=2.0, x=2.3, and x=3.5 for Co6.2Ga3.8-xGex. The simulation pattern for x=2.3 sample is also shown. Each origin is shifted by 1 for clarity.

Figure S3: (a) Temperature dependences of χdc and 1/χdc of Co6.2Ga1.5Ge2.3. The external field is 500 Oe. The inset is the temperature derivative of χdc. (b) Isothermal magnetization curves of Co6.2Ga1.5Ge2.3 measured at 2K, 10 K, 25 K, 50 K, 150 K, and 300 K. (c) Expanded view of isothermal magnetization curves of Co6.2Ga1.5Ge2.3 measured at 150 K and 300 K.