Colorimetric pH Sensitive Smart Film Based on Carrageenan Containing Quercetin or Eucalyptus Extract for Freshness Monitoring of Chicken Meat

Akbar Mirzaeia, Yashar Bina Jorsharia, Shahrzad Javanshira*, Milad Nooria, Mohammad Mahdavib

a Pharmaceutical and Heterocyclic Compounds Research Laboratory, Chemistry Department, Iran University of Science and Technology, Tehran, Iran

b Endocrinology and Metabolism Research Center, Endocrinology and Metabolism Clinical Sciences Institute, Tehran University of Medical Science, Tehran, Iran

| Content | Page |
| --- | --- |
| FigureS1. QUE calibration curve. | S2 |
| Figure S2. a) QUE solution at pH=1-12, b) Uv-vis spectra of QUE solution, c) ELE solution at pH=1-12, and d) UV-Vis spectra of ELE solution. | S3 |
| Figure S3. Structure of quercetin. | S4 |
| Figure S4. Optical transmittance curves of a) CG-QUE film, b) CG-ELE film. | S5 |
| Figure S5. FESEM images of films. a,b) CG-QUE0.3, and c,d) CG-ELE0.3. | S6 |
| Figure S6: FTIR spectrum. | S7 |
| Figure S7. Color response of a) CG-QUE0.3, b) CG-ELE0.3 film at different pH values, sensing film applications for monitoring chicken freshness, c) 0 day, and d) after 3 days. | S8 |
| Table S1. TVBN levels for chicken. | S9 |
| Table S2. MIC values of developed QUE and ELE film against the tested bacteria strains. | S10 |
| Table S3. Mechanical test results of films. | S11 |

FigureS1. QUE calibration curve.

Figure S2. a) QUE solution at pH=1-12, b) Uv-vis spectra of QUE solution, c) ELE solution at pH=1-12, and d) UV-Vis spectra of ELE solution.

Figure S3. Structure of quercetin.

Figure S4.   Optical transmittance curves of a) CG-QUE film, b) CG-ELE film.

Figure S5.  FESEM images of films. a,b) CG-QUE0.3, and c,d) CG-ELE0.3.

Figure S6:  FTIR spectrum.

Figure S7.  Color response of a) CG-QUE0.3, b) CG-ELE0.3 film at different pH values, sensing film applications for monitoring chicken freshness, c) 0 day, and d) after 3 days.

| TVBN Test Samples | TVBN (100/mg) |  |
| --- | --- | --- |
|  | 0 day | 3 days |
| Control | 21.7 | 41.22 |
| CG-QUE0.3 | - | 29.75 |
| CG-ELE0.3 | - | 26.5 |

Table S1. TVBN levels for chicken.

| Microorganisms | Staphylococcus aureus ATCC 6538 | Staphylococcus epidermidis ATCC 12228 | Bacillus subtilis ATCC 6633 | Escherichia coli ATCC 8739 | Pseudomonas aeruginosa ATCC 9027 | Klebsiella pneumonia ATCC 10031 |
| --- | --- | --- | --- | --- | --- | --- |
| Compounds |  |  |  |  |  |  |
| Ciprofloxacin (µg/mL) | 0.195 | 0.195 | 0.195 | 0.012 | 0.195 | 0.006 |
| CG-ELE0.3 | 22 | 16 | 82 | 17 | 14 | 4 |
| CG-QUE0.3 | 45 | 27 | 90 | 37 | 26 | 8 |

Table S2. MIC values of developed QUE and ELE film against the tested bacteria strains.

| Thin film | TS (MPa) | EB | Young’s modulus |
| --- | --- | --- | --- |
| CG-QUE0.3 | 6 ± 0.1% | 14 ± 0.6 | 0.43 |
| CG-ELE0.3 | 5 ± 0.1% | 13.2 ± 0.6 | 0.38 |

Table S3. Mechanical test results of films.