Supplementary material:

Supplementary information (SD)  1 One-way ANOVA test results. Asterisk indicate statistically significant difference (p ≤ 0.05).

|  | Compare between samples | N | mean | SD | ANOVA | P-Value |
| --- | --- | --- | --- | --- | --- | --- |
| 24 h | Si-Zn doped HA | 4 | 90.31% | 2.221 | 15.059 | 0.001* |
|  | Non-doped HA | 4 | 86.84% | 5.668 |  |  |
|  | Control | 4 | 100% | 0 |  |  |
| 48 h | Si-Zn doped HA | 4 | 77.30% | 1.432 | 340.345 | 0.000* |
|  | Non-doped HA | 4 | 80.09% | 1.831 |  |  |
|  | Control | 4 | 100% | 0 |  |  |
| 72 h | Si-Zn doped HA | 4 | 76.04% | 12.747 | 5.969 | 0.022* |
|  | Non-doped HA | 4 | 75.54% | 15.180 |  |  |
|  | Control | 4 | 100% | 0 |  |  |
| 5 days | Si-Zn doped HA | 4 | 79.17% | 2.184 | 261.023 | 0.000* |
|  | Non-doped HA | 4 | 76.26% | 1.714 |  |  |
|  | Control | 4 | 100% | 0 |  |  |

Supplementary information (SD)  2 Bonferroni test results. Asterisk indicate statistically significant difference (p ≤ 0.05).

|  | Compare between samples |  | Mean Difference | P value |
| --- | --- | --- | --- | --- |
| 24 h | Si-Zn doped HA | Non-doped HA | 3.47% | 0.587 |
|  |  | Control | 9.69%*- | 0.011 |
|  | Non-doped HA | Control | 13.16%*- | 0.011 |
| 48 h | Si-Zn doped HA | Non-doped HA | 2.79%*- | 0.049 |
|  |  | Control | 22.70%*- | 0.000 |
|  | Non-doped HA | Control | 19.91%*- | 0.000 |
| 72 h | Si-Zn doped HA | Non-doped HA | 0.49% | 1.0 |
|  |  | Control | 23.97%*- | 0.048 |
|  | Non-doped HA | Control | 24.46%*- | 0.043 |
| 5 days | Si-Zn doped HA | Non-doped HA | 2.91% | 0.091 |
|  |  | Control | 20.83%*- | 0.000 |
|  | Non-doped HA | Control | 23.74%*- | 0.000 |

Supplementary information (SD)  3 NFB data of both grafted and control groups during different observation periods. Data were presented as Mean value ± SD

|  | 2 weeks | 4 weeks | 8 weeks | 12 weeks |
| --- | --- | --- | --- | --- |
| grafted | 44%±2.8% | 48%±1.4% | 64.5%±0.7% | 69%±1.5% |
| Control | 0 | 0 | 0 | 0 |